## Slide 1: WAMHTS-2 Summary: Modeling heater delays and quench propagation in a YBCO coil
Tiina Salmi, Tampere University of Technology
EuCARD-2 Task 10.3 meeting Dec.16th
For the entire presentation see https://indico.cern.ch/event/319762/timetable/#20141114.detailed
Thanks to : A. Stenvall (TUT) ,
G. Kirby (CERN), E. Härö (TUT), J. Van Nugteren (CERN)

## Slide 2
Heat diffusion from heater to cable:
Quench when Ic == Iop
Account for current redistribution
Heat generation in cable:
Heat generation in heater:
  T. Salmi et al., IEEE TAS. 24(4), 2014
  T. Salmi et al., IEEE TAS25(3), 2015
One coil turn

## Slide 3: Analyzed cable based on FM0
Wt = 12 mm
Wx = 5.5 mm
15 Tapes
5.7 mm
Cable 1
7.5 Tapes
11.4 mm
Cable 2
15-tape Roebel cable modeled as stacked tape cable
2 geometries conserving Acable and material fractions
Heater
Heater
  G. Kirby and M. Durante, EuCARD2 Milestone report, MS64, 2014
  Jc(B,T,α): J. Fleiter (see talk by G. Kirby)

## Slide 4: Heater with 4 times more energy than typical LTS heater
ASC-2014: In HTS heater typical LTS heater (25 µm thick with 50 W/cm2, τRC 50 ms) does not quench for Tcs > ~20 K
Here was analyzed a 50 µm thick stainless steel heater with 200 W/cm2 (40 W/mm3) and τRC 50 ms (50 µm Kapton)
  H. Felice et al., IEEE TAS 19(3), 2009
  T. Salmi et al., IEEE TAS 24(3), 2014
  T. Salmi and A. Stenvall, IEEE TAS 25(3), 2015

## Slide 5: Delay to hotspot under heater
1-D with ” --- ”
Cable 2
C
B
A
A: 4.5 K, 6 kA, 15 T (5°): Tcs = 22.3 K
B: 4.5 K, 10 kA, 10 T (5°): Tcs = 22.7 K
C: 4.5 K, 6 kA, 10 T (5°): Tcs = 28.8 K
D: 35 K, 6 kA, 1.5 T (5°) : Tcs = 52.5 K
Delays ~55 ms if Tcs ~22-23 K
Delays >100 ms if Tcs >28 K
Need 40 – 80 mm long heating stations (roebel?)
Simulation using geom. ”Cable 1” had ~50% shorter delays
  Jc(B,T,α): J. Fleiter (see talk by G. Kirby)

## Slide 6: NZPV
Cable 1 ” --- ”
Cable 2 ” __”
C
B
A
I = 6 kA (4.5 K)
B = 10  15 T
NZPV = 0.3  0.5 m/s
B = 10 T (4.5 K)
I = 6  10 kA
NZPV = 0.3  0.8 m/s
Geometry does not matter
Consistent with other studies
A: 4.5 K, 6 kA, 15 T (5°): Tcs = 22.3 K
B: 4.5 K, 10 kA, 10 T (5°): Tcs = 22.7 K
C: 4.5 K, 6 kA, 10 T (5°): Tcs = 28.8 K

## Slide 7: Delay to quench entire cable
C
B
A
Cable 2
Period (mm)
Delay (ms)
Max period 120 - 150 mm
  Or 300 K under heater before all quenched
  Coverage min 30-50% (compare to 10-30% in LTS)
If protected with heaters, better to find a way to cover all with the heater!
A: 4.5 K, 6 kA, 15 T (5°): Tcs = 22.3 K
B: 4.5 K, 10 kA, 10 T (5°): Tcs = 22.7 K
C: 4.5 K, 6 kA, 10 T (5°): Tcs = 28.8 K

## Slide 8: Conclusion
The CoHDA heater simulation tool now includes also quench propagation
Analysed heater delays in FM0 cable (modeled as stacked tape cable)
Simulated delays were ~55 ms for Tcs ~22 K, and > 100 ms for Tcs > 28 K
Slow quench propagation (< 1 m/s) suggested that better to try to cover the entire cable with heater and not rely on heating stations
  Problems: Large energy input to magnet, inputs for heater power leads
Must investigate also other protection options than heaters
Next step: Combine heater delays and quench propagation to a current decay model