## Slide 1: Quench Protection & Radiation Damage Protection
G. Ambrosio
on behalf on the MQXF team
MQXF International Design Review
December 10-12, 2014
CERN

## Slide 2: Outline
Quench Protection
Protection against Radiation Damage and Energy Deposition

## Slide 3: Quench Protection

## Slide 4: First Attempt (presented at MT23)
Simulations performed with QLASA and ROXIE using MATPRO property database
  Using preliminary MQXF requirements
  Assuming heaters only on the outer layer
  With conservative assumptions
    Slow layer-layer propagation
    Only copper (no bronze) in strands
    No dynamic effects
 Hot spot temp. ~ 350 K (max acceptable temp.)
  Without margin and redundancy
G. Manfreda, et al., “Quench Protection Study of the Nb3Sn low-beta quadrupole for the LHC luminosity upgrade,” IEEE Trans. Appl. Supercond., vol. 24, no. 3, Jun. 2014, Art. ID. 4700405.
G. Ambrosio, “Maximum allowable temperature during quench in Nb3Sn accelerator magnets”, Yellow Report CERN-2013-006, pp. 43–46, WAMSDO 2013, CERN, Geneva, CH.

## Slide 5: Feedback from HQ02 test
Measurement of quench propagation OL to IL
Measurement of Quench Integral vs. dump res.
Degradation vs. Hot Spot temperature (incomplete)
H. Bajas, et al., “Cold Test Results of the LARP HQ02b magnet at 1.9 K”, to be published in TAS
120 mm aperture, 1 m long quadrupole
Reached 98% SSL at 4.5K & 95% SSL at 1.9K

## Slide 6: HQ02 – Max Hot Spot Temperature
380+ K hot spot temperature without significant degradation
H. Bajas, G. L. Sabbi, G. Chlachidze, M. Martchevsky, F. Borgnolutti, D. Cheng, H. Felice, et al.

## Slide 7: Quench Protection Improvements
Understanding “dynamic effects” = energy extraction and quench propagation caused by inter-filament losses
Development of heaters with copper-cladding
Development of heaters for inner layer (to be demo.)
M. Marchevsky, "Design optimization and testing of the protection heaters for the LARP high-field Nb3Sn quadrupoles", presented at ASC2014.
Courtesy J. C. Perez
Courtesy M.Marchevsky, E.Todesco, D.Cheng, T.Salmi
If the 11T project successfully demonstrates inter-layer heaters,
we will be happy to use them

## Slide 8: Post-HQ02b Test: Bore, viewed from RE
Coil 16
Coil 17
Coil 20
Coil 15
Heater bubble

## Slide 9: Post-HQ02b Test: Bore, viewed from RE
Coil 16
Coil 17
Coil 20
Coil 15
Crazing/cracking of epoxy

## Slide 10: LHQ Coil
LHQ coil #3 has all the features of MQXF coils not tested in previous long coils (90 mm, 3 m)
  Ti ternary RRP strands
  Stainless steel core (25 um thick)
  Braided insulation
  Stainless steel end parts
  Use of tool and binder during winding
  Flexible features in saddles
Different protection heaters for MQXF optimization
  5 kV electrical strength
  with 50 um polyimide

## Slide 11: Protection Heater Studies
Both heaters are very efficient (delay < 10 ms) at operating current
Similar performance under similar conditions
B01
B02
G. Chlachidze, 11/14/14 LARP Mtg
Analysis in progress

## Slide 12: Updated Simulations
Demonstrated real beneficial effect of bronze
   Hot spot temp lower by ~ 30K
Compared property databases
   MATPRO is most conservative
Fine tuned by comparing HQ tests data with simulations
  See examples in next slides
V. Marinozzi, et al., “Study of quench protection for the Nb3Sn low-beta quadrupole for the LHC luminosity upgrade (HiLumi-LHC)”, to be published in IEEE Trans. Appl. Supercond., 2015.

## Slide 13
Inductance reduction for high dI/dt
MQXF Quench Protection Analysis – Vittorio Marinozzi
HQ simulation using the nominal inductance, experimentally measured at low dI/dt (<50 A/s)[1]
There is an evident disagreement, starting from the very beginning
Similar behavior has been experimentally observed in various HQ and LQ decays
It is not due to quench back, because of its suddenness
It has benefic effects on the protection, therefore its simulation in MQXF could be very useful
The explanation has been investigated as an electromagnetic coupling with Inter-Filament-Coupling-Currents (IFCC) in the strand, due to high dI/dt, which causes a considerable inductance reduction
[1] H. Bajas et al., “Cold Test Results of the LARP HQ Nb3Sn quadrupole magnet at 1.9 K”. Presented at the Applied Superconductivity Conference, Portland, Oregon, USA, 2012.
Rd=60mΩ
No PH
~100 kA/s

## Slide 14
IFCC as magnetization currents
MQXF Quench Protection Analysis – Vittorio Marinozzi
The differential inductance can be computed as:
Static inductance
Magnetic susceptibility related to IFCC
Under exponential assumptions, the magnetic susceptibility related to the IFCC can be computed as:
is the IFCC decay time constant[1]
is the current decay time constant
takes into account the insulation and the packing in the strand
[1] M. N. Wilson, “Superconducting Magnets”, Clarendon Press Oxford, 1983.
[2] L. Rossi and M. Sorbi, “QLASA: A computer code for quench simulation in adiabatic multicoil superconducting windings”, Nat. Inst. of Nucl. Phys. (INFN), Rome, Italy, Tech. Rep. TC-04-13,2004.
This model has been implemented in QLASA[2]
Notes: Dire che tau è la solita costante di tempo, taue la costante di scarica

## Slide 15
HQ simulation
MQXF Quench Protection Analysis – Vittorio Marinozzi
~30%
Considering dynamic effects allows to simulate well the experimental decay from the very beginning to t=~15 ms
In this decay, the MIITs produced considering dynamic effects are ~20% less then using nominal inductance
The disagreement after 15 ms could be due to quench back

## Slide 16
IFCC and quench back
MQXF Quench Protection Analysis – Vittorio Marinozzi
Quench back after 10 ms together with dynamic effects allow to reproduce the decay until its end
Conclusions:
Both quench back and dynamic effects are needed in order to reproduce the decay until the end
Quench back alone is not enough
QLASA cannot predict the time of quench back occurring, but it can now predict the inductance reduction due to dynamic effects. Improvement of QLASA is under way.

## Slide 17
MQXF protection scheme
MQXF Quench Protection Analysis – Vittorio Marinozzi
Dumping resistance | 48 mΩ
Maximum voltage to ground | 800 V
Voltage threshold | 100 mV
Validation time | 10 ms
Heaters delay time from firing (inner layer) (CoDHA)[1] | 12 ms
Heaters delay time from firing (outer layer) (CoDHA)[1] | 16 ms
[1] T. Salmi et al., “A Novel Computer Code for Modeling Quench Protection Heaters in High-Field Nb3Sn Accelerator Magnets”, IEEE Trans. Appl. Supercond. vol 24, no 4, 2014.

## Slide 18
MQXF protection with IL-PH
MQXF Quench Protection Analysis – Vittorio Marinozzi
No inner layer PH | Inner Layer PH
330 K | 290 K
The MQXF hot spot temperature decreases of ~40 K inserting inner layer protection heaters
Dynamic effects are not yet considered in these simulations

## Slide 19
Updated MQXF protection w and w/o IFCC
MQXF Quench Protection Analysis – Vittorio Marinozzi
No inner layer PH | No inner layer PH+ IFCC | Inner Layer PH | Inner Layer PH + IFCC
330 K (365 K) | 306 K (342 K) | 290 K (311 K) | 266 K (288 K)
IFCC dynamic effects decrease the MQXF hot spot temperature of 20-30 K. The effect is therefore appreciable, but we do NOT take it into account because it is not yet demonstrated in MQXF magnets, and the powering system is still under design.
Further improvements could come from quench back, which has not been considered (work in progress)
The numbers between parentheses show impact of failure of half of the heaters

## Slide 20
Protection assumptions | 
Voltage threshold | 100 mV
Dump resistor | 46 mΩ
Validation time | 10 ms
IL heaters | Yes
Dynamic effects | yes
Quench back | no
MQXF Quench Protection Analysis – Vittorio Marinozzi & Tiina Salmi
Peak Temperature vs. Location and Current

## Slide 21: CLIQ - I
Coupling-Loss Induced Quench System
Very effective on HQ02 test
E. Ravaioli, et al., “Protecting a Full-Scale Nb3Sn Magnet with CLIQ, the New Coupling-Loss Induced Quench System”, to be published in IEEE Trans. Appl. Supercond. 2015.
Courtesy of E. Ravaioli

## Slide 22: CLIQ - II
Very effective at mid-high current
Courtesy of E. Ravaioli
E. Ravaioli, et al., “Protecting a Full-Scale Nb3Sn Magnet with CLIQ, the New Coupling-Loss Induced Quench System”, to be published in IEEE Trans. Appl. Supercond. 2015.

## Slide 23: CLIQ Plans
Could provide perfect redundancy with heaters on outer layer
  In case of “bubble” issue with heaters on inner layer
To be demonstrated for long magnets:
  MQXFS1 with reduced CLIQ voltage and dump res.
  MQXFL1 with reduced dump res.
Study of “tunnel readiness” in progress:
  Capacitor banks based on present system for heaters
  Protection of magnets powered in series

## Slide 24: Voltages
Requirements (preliminary):
Heater-Coil Hi-pot: 2 kV
Coil Impulse test: 2 kV
Heater-Coil Hi-pot tests:
5 kV (LHQ coil 3 and MQXFS coil 1)
Impulse test:
> 3 kV (LHQ coil 3); 4.6 kV (MQXFS coil 1)

## Slide 25: Conclusion
Quench Protection is no more a big concern
We can optimize the protection system based on upcoming test results and optimization of the whole system.

## Slide 26: Protection against Radiation damage & energy deposition

## Slide 27: The Strategy
Simulations and code cross-check
  Fluka and MARS
Extensive literature survey, consultation with experts, workshops
  Fluckiger, Weber
  WAMSDO 2011
Irradiations and material tests
  EuCARD program
Optimization of solution in progress

## Slide 28: The Solution
Tungsten shielding inside coil aperture
  Mostly on midplanes
16 mm in Q1 and
6 mm elsewhere
tungsten inserts
on the beam screen
N. V. Mokhov and I. L. Rakhno, “Mitigating radiation loads in Nb3Sn quadrupoles for the CERN Large Hadron Collider upgrades” Phys. Rev. ST Accel. Beams 9, 101001, 2006.

## Slide 29
more details in the N. Mokhov’s talk
WP3 session tomorrow early afternoon
16 mm in Q1 and 6 mm elsewhere
tungsten inserts
on the beam screen
SHIELDING THE NEW TRIPLET – CP – D1 [II]
HL-LHC vs LHC
(BEFORE vs AFTER LS3)
beam screen gap in the interconnects is critical
tungsten in the BPM’s
more than 600 W in the cold masses
as well as in the beam screen
(i.e. 1.2-1.3 kW in total)
larger values for increasing crossing angle
First iteration with conceptual beam screen insert for 3000 fb-1

## Slide 30: Relative mechanical properties for CTD-101K
30
Elvis Fornasiere | CERN, 26th February 2013
TE-MSC-MDT
Outline
Structural req + energy deposition
Measurement techniques
CTD-101K + CE-epoxy results
Chart: CTD-101K, with 50% Vf virgin S-2 Glass
| 0.1 | 4.7 | 47 | 230
Torsional Shear Modulus | 1 | 0.84615 | 0.92308 | 0.95604
Compressive Strength | 1 | 0.90441 | 0.88235 | 0.79412
Compressive Modulus | 1 | 0.98985 | 0.6599 | 0.68528
Flexural Modulus | 1 | 0.80645 | 0.60411 | 0.45748
Torsional Shear Strength | 1 | 0.801 | 0.46269 | 0.45771
Fracture Resistance GIC | 1 | 0.77778 | 0.41667 | 0.44444
Torsional Shear Strain | 1 | 0.58974 | 0.38462 | 0.33333
Shear Strength | 1 | 0.70833 | 0.34417 | 0.055833
ILSS0 ≈ 120 MPa
30% degradation at 50 MGy
Shear strength degradation with irradiation is the most sensitive property
[29]+[30]+[31]
UTS: 35% reduction at 180 MGy from UTS0 ~ 1050 MPa
Compressive strength = 1080 MPa at 160 MGy (Loss 20%)
Fracture Resistance GIC: 66% reduction at 230 MGy
G10 SBS Test
70% degradation at 90 MGy
Plan
End
SBS test gives «apparent ILSS»
95% degradation at 160 MGy
Note: 41 references!

## Slide 31
31
Elvis Fornasiere | CERN, 26th February 2013
TE-MSC-MDT
t
t
t
t
t
t
t
t
30-40 MPa shear
t
t
t
t
Cool-down
Max-gradient (155 T/m)
150 mm Nb3Sn Shear stress
50-60 MPa shear
singularity?
Observation of Shear stress between turns and shear between inner and outer layers
~0 MPa shear
With courtesy of M. Juchno and P. Ferracin [4]
Outline
Structural req + energy deposition
Measurement techniques
CTD-101K + CE-epoxy results
G10 SBS Test
Plan
End

## Slide 32: Task 2: Support studies (1)
Macej Chorowski & Jarek Polinski (PWR) PWR, CEA, CERN
7.2.1 Radiation studies for insulation and impregnation (PWR with CEA and CERN)
Aim: Certify radiation resistance of coil insulation and impregnation
Situation in 2009:
Most work (outside ITER) on insulator rad resistance >15 years ago
Scattered literature
High dose expectations for HL-LHC low beta zones ( ≥50 MGy)
Work done in the 4 years:
Literature study
Identification of HL-LHC radiation dose situation
Inventory of insulator candidates for HL-LHC Nb3Sn coils
Selection of irradiation test beam and conditions
Design and construction of irradiation cryostat
Design and construction of material property measurement equipment (mechanical cold test, electrical insulation cold test, thermal conductivity cold test)
Irradiations at Swierk (Pl) and material test (PWR & CEA)
32

## Slide 33: Irradiation set-up
designed and commissioned at PWR and transferred to NCBJ, Swierk
Accelerator 0.2 mm thick Ti window
Irradiation set-up

## Slide 34: Radiation certification electrical tests summary
4 material types irradiated with 6 MeV e- beam 50 MGy dose
LARP technology has large margin

## Slide 35: Radiation certification mechanical tests
2 materials (Mix71 and LARP) irradiated (50 MGy)
2 materials (Mix237 and CE-epoxy mix) following by autumn 2013
@50MGy LARP mix reduces 50 %
but Mix 71 is unusable
35
Requirement: 20 MPa (at pole)
LARP technology has large margin

## Slide 36: Effect on Critical Current
Jc of high-Jc strands increases with irradiation
Peak fluence in Q1

## Slide 37
DPA ESTIMATE
[N. Mokhov and his team]
[A. Lechner]
3000 fb-1 [A. Lechner]
After these peak DPA
Copper RRR starts degrading
but ~80% is recovered after warm up
“These numbers should be acceptable for the superconductors and copper stabilizer provided periodic annealing during the collider shutdowns” PDR

## Slide 38
BEAM SCREEN AND ABSORBER DESIGN
16 mm absorbers
6 mm absorbers
conceptual version
(BS #1)
executive version
(BS #2)
revisited version
(BS #3)
≡

## Slide 39
Peak Dose @ Ultimate Lifetime w Latest Absorber
2-3 mm radial resolution
50cm BS gap in the ICs

## Slide 40
INERMET IMPACT

## Slide 41
Blue rectangles indicate the azimuthal regions shielded by the tungsten absorbers
Black rectangles indicate the azimuthal regions covered by coils
2D VIEW [IV]
Needs design optimization

## Slide 42
DESIGN IMPACT
More design-simulation iterations are needed

## Slide 43
Energy Deposition
radially averaged over the cable thickness
50cm BS gap in the ICs
Cooling and thermal analysis in next talk

## Slide 44: Conclusions – Where we are now
The optimization of the radiation absorber is in progress.
The target is to keep the peak dose < 25/33 MGy at nominal/ultimate luminosity, far from the pole turns.
Under these conditions the LARP/MQXF technology meets requirements with sufficient margin.
Your feedback is very welcome!

## Slide 45: Back up splides

## Slide 46
RADIATION SOURCE
14 kW delivered in collisions (L=7.5L0)
on each side of ATLAS and CMS,
a 54mm aperture TAS absorber takes 750W
and let 5kW impact the machine
54 mm
5 mm
21 m
700 MJ per beam (7 TeV protons, 2.2 1011 p per bunch, ~2800 bunches)
295 urad half vertical crossing angle

## Slide 47: MQXF Main Parameters
140 T/m in 150 mm coil aperture
Q1/Q3 length: 8 m
Q2 length: 6.8 m
Max outer diameter: 630 mm
1.9 K operating temperature
Radiation strength: > 33 MGy
Field quality: see WP3 page at https://espace.cern.ch/HiLumi/WP3/SitePages/Home.aspx
ATLAS
CMS

## Slide 48: MQXF Main Design Features
Same design for Q1/Q3 and Q2s:
Two-layer coils
  Without internal splice
  With one wedge per layer
Al shell structure preloaded by bladders and keys
  Segmented Al shell
Axial preload by tie-rods
Quench protection by active heaters
  and possibly CLIQ
P. Ferracin, et al., “Magnet design of the 150 mm aperture low-β quadrupoles for the high luminosity LHC,” IEEE Trans. Appl. Supercond., vol. 24, no. 3, p. 4002306, Jun. 2014

## Slide 49: Latest success: LARP HQ02
90 mm aperture, 1 m long quadrupole
Tested at FNAL & CERN
Reached 98% SSL at 4.5K & 95% SSL at 1.9K
R. Hafalia
H. Bajas, G. Chlachidze, M. Martchevsky,
F.Borgnolutti, D. Cheng, H. Felice, et al.
4LOr2C-06 “Cold Test Results of the LARP HQ02-b magnet at 1.9 K”; H. Bajas, et al.,

## Slide 50: Conclusions
The MQXF design has successfully addressed previous concerns:
  Quench protection, 3D stress analysis, …
The short model program is at full speed
  Coils fabrication, structure procurement and QC, …
  At next Hi-Lumi Collab Mtg we will discuss test results
The long prototype program is starting soon
  The 120mm magnets/coils have provided risk reduction
Test of QXF coils is starting in a few months
The demonstration of MQXF magnets for HL-LHC upgrade is getting closer and closer!

## Slide 51
High Field Quadrupole (HQ)
Goal: demonstrate all performance requirements for Nb3Sn IR Quads in the range of interest for HL-LHC (magnetic, mechanical, quench protection etc.)
Main design parameters and features in the latest models tested (HQ02a/b):
Conductor and cable | 
Strand diam. (mm) | 0.778
Cu/Sc | 1.2
No. strands | 35
Cable width (mm) | 14.8
Cable thickness (mm) | 1.375
Keystone angle (deg.) | 0.75
Short Sample Performance |  | 
Param. | 4.5K | 1.9K
Iss [kA] | 16.4 | 18.2
Bpk [T] | 12.9 | 14.2
Gss [T/m] | 186 | 205
Al shell
Coil
Bladder
locations
Alignment key
Iron yoke
Al
collar

## Slide 52
HQ02 Results
Accelerator Quality
Order of magnitude reduction of dynamic effects (ramp rate, field quality) with cable core
Quench performance
HQ02: 98% at 4.5K
HQ02b: 95% at 1.9K with 200 MPa pre-load
Quench protection
380K quench temperature without degradation
Successful first test of the CLIQ system in Nb3Sn
250K
320K
380K
H. Bajas, et al., “Cold Test Results of the LARP HQ02-b magnet at 1.9 K”,
to be published in IEEE Trans. Appl. Supercond., 2015.

## Slide 53: Simulations vs. Measurements
Under the assumptions used for MQXF, the heaters-induced quench simulations are conservative.
At the current of interest (0.8 of SSL), the MIITs are overestimated by about 13 % (~ 65 K)
Margin is due to:
  dI/dt effects
  conservative assumptions in modeling of heaters and propagation OL to IL
Current/SSL | 0.8 | 0.7 | 0.6 | 0.5 | 0.4
MIITs difference % (no dump case) | 14.5 | 13.2 | 9.6 | 10.7 | 8.1
MIITs difference % (3 mΩ dump case) | 13.4 | 11.1 | 6.4 | 5.3 | 0.9
Most significant case for MQXF

## Slide 54: LHQM01 Quench Training
2.2 K
2.2 K
4.5 K
QP study
89% of SSL
90% of SSL
Quench training at 20 A/s
G. Chlachidze, 11/14/14 LARP Mtg

## Slide 55
3.1 MQXF inner-layer quench heaters
MQXF Quench Protection Analysis – Vittorio Marinozzi
In order to improve the protection, various quench heaters for the inner layer have been designed[1]
The protection heaters are designed in order to avoid as best as possible the damages coming from helium bubbles
[1] M. Marchevsky, "Design optimization and testing of the protection heaters for the LARP high-field Nb3Sn quadrupoles", presented at ASC2014.