## Slide 1: Performance of nitrogen doped cavities
Anna Grassellino
SRF cavity test group leader, High Q program manager, TD
LHeC Workshop June 24-26, 2015 Geneva

## Slide 2: Nitrogen Doping: a breakthrough in Q
Standard state-of-the art preparation
Typical Q obtained in VTS with 120C bake ~ 1.7e10 at 2K, 16 MV/m
Record after nitrogen doping – up to 4 times higher Q! Average values obtained on nine cell Q(2K, 16MV/m)~ 3.5e10
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)
1.3 GHz

## Slide 3: Doping Treatment: small variation from standard protocol, large difference in performance
3
Example from a doping process developed for LCLS-2:
Bulk EP
800 C anneal for 3 hours in vacuum
2 minutes @ 800C nitrogen diffusion
800 C for 6 minutes in vacuum
Vacuum cooling
5 microns EP
Cavity after Equator Welding
EP 140 um
Ethanol Rinse
External 20 um BCP
Short HPR
800C HT Bake
RF Tuning
EP 40 um
Ethanol Rinse
Long HPR
Final Assembly
Long HPR
Helium Tank Welding Procedure
VT Assembly
HPR
HOM Tuning
Ship to DESY
Leak Check
120C bake
XFEL
X

## Slide 4: A bit of history about N doping
Discovered at FNAL in 2012 on single cells treated with nitrogen in high temperature furnace
During the first two years FNAL focused on understanding root of improvement and making process controllable and reproducible on single cells
Different doping recipes were designed based on simple diffusion models and implemented/tested; went from one step diffusion to two step diffusion to create flatter, deeper nitrogen concentration – this improved robustness and quench fields
In 2014 LCLS-2 decided to invest on this technology to go from wide demonstration on single cell to production ready nine cell; three partner labs working together FNAL-Cornell-Jlab
More than 100 N doped cavity tests with 16 nine cell qualified for the two LCLS-2 prototype cryomodules
Vendors RI and Zanon currently being qualified for N doping production process for LCLS-2
R&D continues for further understanding and improvements (quench, B sensitivity)

## Slide 5: Origin of the Q improvement
Reverse field dependence of the BCS surface resistance component  lowest RBCS
Lower than typical residual resistances (seems to zero all contributions but trapped flux)
A.Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001
A. Romanenko, A Grassellino, Appl. Phys. Lett. 102, 252603 (2013)
Cause of MFQS
Origin of Q antislope

## Slide 6: Physics – perceived BCS limit has been overcome
A. Grassellino et al, 2013 Supercond. Sci. Technol. 26 102001 (Rapid Communication)
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)
Anti-Q-slope emerges from the BCS surface resistance decreasing with field
This is what BCS theory predicted to be the lowest possible surface resistance
The increasing Q with field allows to run at higher gradient with lower cryo-cost

## Slide 7: The importance of a high Q technology – the case of the CW machine LCLS-2
Example of N doped
Dressed cavity for LCLS-2
Below the one cryoplant threshold
LCLS-II one vs two 2K cryoplants threshold
Two vs three 2K cryoplants threshold
One vs two 2K cryoplants threshold
N doping technology allows significantly lower refrigeration costs (capital, operating)
Larger margin and possibility for an energy upgrade for same refrigeration cost
Example of 120C baked (standard ILC/XFEL technology)
Would possibly require > 2 full cryoplants

## Slide 8
Higher Q ~ 3e10 compared to 1.7e10 will translate into ~1.5 millions saving per year in operating costs
Capital cost savings go in thresholds of several tens of millions (LCLS-2)
The importance of a high Q technology – the case of the CW machine LCLS-2

## Slide 9: From single cell R&D to cryomodule ready technology: the two LCLS-II prototype cryomodules (FNAL and Jlab)
<Q>=3.6e10
<Emax>=22.2 MV/m
Emaxmedian=22.8MV/m
It is the highest average Q ever demonstrated in vertical test for 1.3 GHz nine cells at 2K, 16 MV/m in the history of SRF (larger than a factor of two the state of the art)

## Slide 10: N doping applied to 650 MHz cavities at FNAL Q~ 7e10 at 2K, 17 MV/m – record at this frequency!
Applying N doping to 650 MHz (beta=0.9) leads to double Q compared to 120C bake (standard surface treatment ILC/XFEL)
But from frequency scaling from 1.3GHz, with ideal recipe the projected Q value is ~1e11 at 17 MV/m, 2K! Need to optimize doping recipe at lower freq

## Slide 11: What does the N treatment do? N doping profiles via SIMS
11
Nitrides
Interstitial nitrogen in Nb
Non-doped
Doped
Depth (um)
A. Romanenko, talk at LINAC 2014, Geneva
And D. Gonnella et al, LINAC 2014, Geneva
C. Reece et al, WEPWI026

## Slide 12: Surface Nitrides (post bake, pre-EP) – imaged by SEM
Flat Nb sample baked at 800C˚
for 2 min with N2 + 6 min annealing
Flat Nb sample baked at 800C˚ for
20 min with N2 + 30 min annealing
Bad (poorly SC) nitride phases that need to be removed via EP

## Slide 13: Room T TEM on post gas bake, pre-EP surface (2/6 recipe)
a) μm-sized areas of “uniform” contrast in near-surface show only Nb reflections
Nb [113]
Nb [113]+Nb2N [210]+?
b) few Nb nitrides-features (Nb2N reflections) in Nb near-surface. Nitride “teeth” go ~0.2 μm deep
Pt layer
Pt layer
~0.2 μm
Courtesy of Y. Trenhikina, FNAL

## Slide 14: Room T TEM on N doped surface AFTER EP
Preliminary: no visible Nb nitrides-teeth in near-surface show only Nb reflections
Confirms that root of improvement is from nitrogen as interstitial in the lattice
Nb [100]

## Slide 15: Cryogenic TEM on N doped surface AFTER EP
Nb [100]
ROOM T
90K
Preliminary: large near-surface area is affected by Nb nanohydride precipitation! But different than typical: closely spaced, very small/thin Nb hydrides.
Nanohydrides in standardly treated samples: Trenikhina et. al. J. of Appl. Phys., 117, 154507 (2015).

## Slide 16: Open questions: nature of premature quench in N doped
16 MV/m
2.7e10
Recipe 2/6
“light doping”
Recipe 20/30
“heavy doping”
Heavier doping levels result in premature quench
Single cell N doped demonstrated up to 39 MV/m
Nine cells lower than single cell for same treatment
<Q>=3.6e10
<Emax>=22.2 MV/m
Emaxmedian=22.8MV/m
<Q>=3.24e10
<Emax>=16.3 MV/m
Emaxmedian=16.5MV/m
16

## Slide 17: New insights on quench in N doped cavities – magnetic peak field driven
M. Martinello et al, WEPTY034, IPAC15
A. Vostrikov et al, WEPTY022, IPAC15
Nitride teeth…residual nanonitrides post EP?

## Slide 18: High Q discovery 2 – efficient flux expulsion
Full expulsion of the magnetic field should increase the field at equator ~2 times when going superconducting
Fluxgate
magnetometers
H
Efficient flux expulsion
Poor flux expulsion
It turns out the expulsion efficiency can be controlled by the cooldown procedure through Tc=9.2K (fast/slow, uniform or not)
Same Meissner behavior for EP, EP+120C, N doping, fine/single grain, cooling is what matters

## Slide 19: Record Q up to the highest fields combining N doping and efficient flux expulsion
High thermal gradient provides depinning force allowing efficient magnetic field expulsion
Ultra-high Q0 even in 190mG
A. Romanenko, A. Grassellino et al. J. Appl. Phys. 115, 184903 (2014)
A. Romanenko, A. Grassellino et al. Appl. Phys. Lett. 105, 234103 (2014)

## Slide 20: It’s a matter of thermogradient along the cell (at the phase front) – and geometry of the problem has an effect, too…
Romanenko, A. Grassellino, A.Crawford, D. A. Sergatskov, Appl. Phys. Lett. 105, 234103 (2014)
M. Martinello et al, arXiv:1502.07291

## Slide 21: Details of superconductivity nucleation matter
  Fast cooldown – well-defined superconducting/normal boundary is moving from bottom to the top => no energy barrier for flux to be expelled
Superconducting
(T<Tc)
Normal conducting
(T>Tc)

## Slide 22: Details of superconductivity nucleation matter
  Slow uniform cooldown – superconductivity is nucleated at multiple spots which reach T<Tc
  Flux surrounded by superconducting areas has an energy barrier for escape=> more flux trapping is possible

## Slide 23: Results on 650MHz – cooling studies – fast vs slow cooling
Cooling details have been shown to play an important role in Q retention
Slow cooling through Tc shown to severely deteriorate Q for 1.3 GHz cavities
At 650 MHz we find a much weaker effect, likely due to smaller impact of trapped flux at lower frequency
Very promising for Q retention in cryomodule
T=2K
A. Romanenko, A. Grassellino, O. Melnychuk, D. A. Sergatskov, J. Appl. Phys. 115, 184903 (2014)
A. Romanenko, A. Grassellino, A.Crawford, D. A. Sergatskov, Appl. Phys. Lett. 105, 234103 (2014)

## Slide 24: R&D on trapped flux dependence as a function of mfp
Model by Mattia Checchin
Experiments ongoing! (M. Martinello and S. Posen)

## Slide 25: SRF cavity in its liquid helium filled tank: operating at 2 degrees above absolute zero (-456 deg F)
Higher Order Mode extraction
Power Coupler Port
Tuner
Cryogen fill pipe
Field Probe
Ports:
  Beam in /out
  Bring in power
  Monitor field
  Extract un-wanted frequencies

## Slide 26: LCLS-2 cavities dressed with instrumentation inside vessel
D. Gonnella et al,
J. Appl. Phys. 117, 023908 (2015)

## Slide 27: Sweeping the flux into the beampipes via fast cooling
Thermoelectric induced field, as first discussed in J. Vogt et al Phys.Rev.ST Accel.Beams 16 (2013) 10, 102002
Flux wave, travelling from cavity to beampipe
Flux wave
Flux all confined to beampipes, after efficient expulsion from cavity cells

## Slide 29: Horizontal dressed cavity tests at FNAL, Cornell, Jlab Meeting final LCLS-2 specs in cryomodule environment!
Courtesy of D. Gonnella
State of the art ‘undoped’

## Slide 30: Conclusions
Tremendous progress in the past two years in understanding of contributors to RF surface resistance
Record Q achieved from bare cavity tests all the way down to cryomodule environment, by implementing N doping and understanding of flux expulsion via efficient cooling through Tc
High Q at high gradient via doping is the frontier to be explored, exciting R&D ongoing
Flux trapping/detrapping and losses due to trapped flux for different surface processing is also a very interesting R&D path currently being pursued
Lower frequency N doping (~700 MHz) already doubled Q of standard treatment, and promises Q ~ 1e11 at 2K mid field – R&D ongoing