## Slide 1
R&D on u-strpip sensors @ SDR
E. Currás, M. Fernández, J. González, R. Jaramillo, D. Moya, I. Vila.
Instituto de Física de Cantabria(CSIC-UC)
P. Fernández, S. Hidalgo, V. Greco, G. Pellegrini, D. Quirion.
Centro Nacional de Microelectrónica at Barcelona (CSIC)

## Slide 2: Outline
Motivations for the R&D.
A 2D position sensitive microstrip sensor.
  Laser, radioactive source and particle beam characterization
Improving the design
  Integrated signal routing lines (Crosstalk suppression).
  Incrementing the signal: Low Gain Avalanche Detectors.
Summary

## Slide 3: R&D Motivation
Charge division in microstrips:
  Long microstrips ladders (several tens of centimeters) proposed for the ILC tracking detectors.
  Getting the particle hit coordinate along the strip using the charge division method.
  Avoid the complexity of double sided sensors and the additional material of a second layer of sensors.
Low gain segmented p-type pixels (strips)
  Implementing a small gain in the segmented diode so we can reduce the thickness of the sensors without reducing the signal amplitude
  Smaller contribution to the material budget.

## Slide 4: Charge Division in uStrips
Simple single-side AC-coupled microstrip detectors
X-coordinate: cluster-finding algorithms for strip detectors.
Aluminium
x
L
S1
S1=f(y)
S2=f(L-y)
with resistive coupling electrodes.
Aluminium
Resistive material
x
y
L
S1
S2
Y-coordinate: Resistive charge division method.
Resistive material: high doped polysilicon
** V. Radeka, IEEE Transaction on Nuclear Science NS-21 (1974) 51
** Electrode resistance >> preamplifier impedance.
y A2
L A1+A2
=

## Slide 5: Proof-of-Concept Prototype
256 channels
peaking time = 25ns
S/N≈20 for standard no irradiated detectors
ALIBAVA DAQ system for microstrip detectors, based on the Beetle analogue
readout ASIC
2 Beetle chips
Pulsed DFB laser λ=1060nm
Gaussian beam spot width ≈ 15 μm
pulse duration 2ns
3D axis stage with displacement accuracy ≈ 10 μm
Clean room laboratory at IFCA, Santander

## Slide 6
Systematic error
=>
Ballistic deficit
R/l=2.8 Ω/μm
R/l=12.2 Ω/μm
20000 events ∀ measurement

## Slide 7: Longitudinal spatial resolution for 6 MIPs signal
σA1=1.83 ADU
σA2=1.80 ADU
R/l=2.8 Ω/μm
R/l=12.2 Ω/μm
1.1% L => 220 μm
1.2% L => 240 μm
A2
A1+A2

## Slide 8
Test beam at CERN SPS Pion Beam, Nov 2012
First successful integration and synchronization with AIDA MIMOSA pixel telescope
Test Beam Characterization

## Slide 9: Test Beam: Spatial Resolution
Trans. Coordinate X  25 mm (pitch/= 23 mm)
Long. Coordinate Y  1.7 mm ( 8.5% strip length)

## Slide 10: Radioactive Source: SNR estimation
Defined as (drives the spatial resolution)
x
x
x
2 mm
Trigger PMT
Support
Sr90
Sensor
Collimator
SNR for non-resistive sensor
20% drop

## Slide 11: Charge-division sensor: Intermediate summary
The charge-division concept on microstrips has been confirmed experimentally, two limitations:
  Both ends readout difficult to integrate in long ladder (need to combine the information from both ends)
  Signal attenuation due to the strip resistance (current prototypes 20% signal loss for 2cm length sensor).
Proposed solutions:
  Integrated signal lines in the sensor to route the signals to the same end.
  Reduce the strip resistivity (limited by the amp. charge resolution) and/or integrate charge amplification mechanism in the sensor.

## Slide 12: Resistive strips with internal signal routing

## Slide 13: Resistive strips with internal signal routing (2)
Induced signal on metallic vias superposed to “direct signal” propagated through polysilicon electrode.
Measured Fractional position shows a clear bias

## Slide 14: Isolation structures for cross-talk suppression
p-
p++
n+
n+
n+
Al
p
Poly-Si
Poly-Si
Poly-Si
p
p+
p+
p+
Poly-Si
Poly-Si
Poly-Si
Al
Al
n-
n++
Al
Al
Poly-Si
OLD DESIGN
NEW DESIGN
Common P-stop and field plates
Al
Spin-off of FOSTER sensors proposed by KIT at CMS

## Slide 15: Crosstalk suppression (common stop)
Time Resolved Readout IR-laser induced (e-TCT like measurement)
No grid Al. Implant – Al routing – Implant
S8

## Slide 16: Crosstalk Suppression: Current pulses
Infrared pico second laser
(fast, 1GHz readout channel)
A
B
C
D
CH1
CH2
CH3
p-
p++
n+
n+
n+
Al
p
Poly-Si
Poly-Si
Poly-Si
p
Al
A
B
C
D

## Slide 17: Cross-talk suppression: Integrated charge
17
Poly-Si
Strip
Poly-Si
Strip
Aluminum
Strip
Flat charge pedestal for Al routing track, suppressed by calibration

## Slide 18: Signal Attenuation studies
Time-resolved study of the pulse shape and charge
Laser longitudinal scan
(42 points, 500um steps
0 mm from r/o pad
10 mm from r/o pad
5 mm from r/o pad

## Slide 19: Signal Attenuation studies (2)
Charge and amplitude vs. distance
Constant charge
Reduced
Amplitude

## Slide 20: Increasing the signal: LGAD
Implanting an n++/p+/p- junction along the centre of the electrodes. Under reverse bias conditions, a high electric field region is created at this localised region, which can lead to a multiplication mechanism (impact Ionization).
285 um
N+
P
High Electric Field region leading to multiplication
P. Fernandez et al, “Simulation of new p-type strip detectors with trench to enhance the charge multiplication effect in the n-type electrodes” , Nuclear InstrumentsandMethodsinPhysicsResearchA658(2011) 98–102.
Advantages = Thinning while keeping same S/N as standard detectors.

## Slide 21: PAD LGAD: Red laser TCT characterization
285 um
e-
h+
Red laser (1060 nm)
Bottom injection
Standard diode n on p
P-type diffusion diode
5ns

## Slide 22: Strip LGAD: Electric Field
Standard Strip
Strip with P-type diffusion
Strip with P-type diffusion: 2D and 1D doping profiles
- To obtain the manufacture parameters (doping profiles)

## Slide 23: Current status: preliminary results on strips
Very preliminary test do not show signal amplification.
New run in progress and new concept to implement: p-on-p sensor (holes readout with electron amplification in a non-structured anode (pad-like) to ensure uniform amplification
RD50 LGAD GROUP
(CERN, CNM, Barcelona, Torino, Ljbljiana, Santander, SCIPP, Freiburg, Glasgow, Liverpool)

## Slide 24: Summary
A novel 2D position-sensitive semiconductor detector concept based on the resistive charge-division readout method and manufactured using standard semiconductor planar techniques has been introduced.
A full testing cycle of this technology has been successfully completed: laser, RS and test beam source.
To be used as a tracking sensor suitable:
  Single end readout  the integration in the sensor of signal routing tracks
  Increase SNR  Reduction of the strip resistivity and Linear gain of the signal
The first issue has been tackled integrating isolation structures (preliminary results are positive).
New detector designs aim to fabricate detectors with moderate gain (RD50) and p-on-p strip LGAD.

## Slide 25: THANK YOU !

## Slide 26: Equivalent Electrical Circuit
Peaking time 25ns (Beetle chip ALIBAVA DAQ system).
rise time 2ns
Q~4fC
Detector (p+-on-n) model ***
80 cells 250 μm long
p
Vbias
e-
h+

## Slide 28: Signal Propagation – Linearity (Simulation)
t
t
t1
t2
V
Particle
S1
S2
2 mm
S1
S2
y
18 mm

## Slide 29: Red laser TCT characterization
Charge collection efficiency
Standard diode
P-type diffusion diode