## Slide 1: From Ferrite Characterization to Preliminary Design of Ferrite Loaded Accelerating Cavity
PhD project:
Development of a Ferrite-Loaded Accelerating Cavity
CERN Supervisor: Dr.-Ing. Christine Völlinger
TEMF Supervisor: Prof. Dr.-Ing. Harald Klingbeil
Johannes Eberhardt
CERN, Beams Department / TU Darmstadt, TEMF Institute

## Slide 2: Motivation: Ferrite Loaded Accelerating Cavity
Idea: Same RF system to accelerate different types of particles
→ Accelerating Cavity with frequency swing 18 – 40 MHz
Cavity design with electromagnetic simulation program
→ Relative permeability and losses of ferrite
as input for simulations
Ferrite
Cavity

## Slide 3: Introduction – How does an accelerating cavity work?
accelerating gap
beam pipe
cylindrical structure
ERF
HRF
λ/4

## Slide 4: Introduction – Why Ferrite Loaded?
∆
Tuning 18 – 40 MHz →
ferrite ring

## Slide 5: Introduction – Relative Permeability
Depends on:
RF frequency

## Slide 6: Introduction – Lessons learned
Sample 1
Sample 2
Sample 3
Depends on:
RF frequency
Magnetic bias history
Temperature
Location in ferrite
Bias field orientation
Dispersive characteristics
Random – degaussed
Room temperature
Average over volume
Perpendicular to RF magnetic field
,

## Slide 7: From Ferrite Characterisation to FLC
B
/
mT
Reflection Measurement
µ’
(
f
res
)
Resonant Measurement
f
res
/MHz
Q
total
Eigenmode
Simulation
f
res
/MHz
d
fres
/%
Calculate
Q
Q
1-Port Reflection
Measurement
Resonant
Measurement
Simulation of
Resonant
Measurement
Calculate

## Slide 8: Reflection Measurement
Ibias
Bbias
B
/
mT
35
40
300
Reflection Measurement
µ’
(
f
res
)
Resonant Measurement
f
res
/MHz
Q
total
Eigenmode
Simulation
f
res
/MHz
d
fres
/%
Calculate
Q
Q

## Slide 9: Reflection Measurement
Coaxial short-circuit technique to determine
Measuring S11(f) of empty and filled SH
Analytical calculation of (S11(f))
B
/
mT
35
40
300
Reflection Measurement
µ’
(
f
res
)
13
8.0
1.17
Resonant Measurement
f
res
/MHz
Q
total
Eigenmode
Simulation
f
res
/MHz
d
fres
/%
Calculate
Q
Q

## Slide 10: Resonant Measurement
B
/
mT
35
40
300
Reflection Measurement
µ’
(
f
res
)
13
8.0
1.17
Resonant Measurement
f
res
/MHz
18.8
23.4
43.7
Q
total
Eigenmode
Simulation
f
res
/MHz
d
fres
/%
Calculate
Q
Q
9
40
1046

## Slide 11: Numerical Simulation Results
Ferrite ring
Teflon foil
Inner conductor
Outer conductor
B
/
mT
35
40
300
Reflection Measurement
µ’
(
f
res
)
13
8.0
1.17
Resonant Measurement
f
res
/MHz
18.8
23.4
43.7
Q
total
9
40
1046
Eigenmode
Simulation
f
res
/MHz
18.6
23.1
43.3
d
fres
/%
1.1
1.3
0.9
Calculate
Q
Q
8
35
5000

## Slide 12: Numerical Simulation Results
low is dominated by
once exeeds has maximum
high is dominated by

## Slide 13: Numerical Simulation Results
Resonance frequency depends on with ∆
Required can be achieved, but for relative low

## Slide 14: Preliminary Design of FLC 18 – 40MHz
Simulation Input |  | Simulation Results for Vacc=1kV |  |  | 
µ’(fres) |  | fres/MHz |  | R/Q/Ω | P/W
8 | 35 | 17.6 | 37 | 213 | 63.3
1.17 | 5000 | 40.9 | 4683 | 108 | 1
Simulation Input |  | Simulation Results for Vacc=1kV |  |  | 
µ’(fres) |  | fres/MHz |  | R/Q/Ω | P/W
8 | 35 | 17.6 | 37 | 213 | 63.3
1.17 | 5000 | 40.9 | 4683 | 108 | 1
Ferrite stack
Beam pipe
Accelerating gap
Example | 
Vacc/kV | P/kW
8.3 | 4.4
62.5 | 3.9
1125mm

## Slide 15: Conclusion and Outlook
Measurement of relative permeability and losses of ferrite material
Simulation model of resonant measurements setup
Preliminary design of ferrite loaded accelerating cavity
Influence of non-uniform µ’ has to be analysed
RF power measurements have to be done
FLC model will be further elaborated

## Slide 16
Thank you for your attention!

## Slide 17: Preliminary Design
For 4kW RF power with
8.3kV accelerating voltage at 18MHz
62.5kV accelerating voltage at 40MHz

## Slide 18: Resonant Measurement
measurement for 300mT bias field
B
/
mT
35
40
300
Reflection Measurement
µ’
(
f
res
)
13
8.0
1.17
Resonant Measurement
f
res
/MHz
18.8
23.4
43.7
Q
total
9
40
1046
Eigenmode
Simulation
f
res
/MHz
d
fres
/%
Examined
Q
ferr
Q
ferr