## Slide 1: Photoionization of diamond interacting with 30fs intense laser field
Boyan Obreshkov
and
Tzveta Apostolova
INRNE-BAS

## Slide 2: Motivation
Laser engineering of diamond for writing conductive paths is an important subject of research for its application in radiation detection (3D detectors)[1,2].
[1] S. Lagomarsino et al Appl. Phys. Lett. 103, 233507 (2013)
[2] S. Lagomarsino , et al Diamond & Related Materials 43 (2014) 23–28
A deep insight of the process of laser graphitization of diamond is critical to tune at best the laser parameters and obtain low resistivity channels with minimum damage of the surrounding diamond lattice.
Laser ablation and nano-structuring of diamond.
Simulate ultra-short laser-induced electronic excitation, absorption and relaxation processes in CVD monocrystalline diamond and compare to the experiment.

## Slide 3
515 nm, 0.2 ps (FWHM), 35 TW/cm2, natural diamond
N=1
N=2
N=3
N>1000
Spallative ablation + graphitization (?) Single-shot threshold – 20 TW/cm2
Micro-Raman

## Slide 4
515 nm, 0.2 ps (FWHM), 35 TW/cm2
Nanostructuring, multi-shot threshold – 20 TW/cm2
N=1000
N=1000
N=300
crater
N=100
N=30

## Slide 5
Laser radiation
electron
hole
Conduction band
Valence band
Forbidden band
CVD diamond
Laser -PI, MPI
IB, II, E-E
AR, XF, XD,E-PHN
PI

## Slide 6: Photoionization yield (expt. vs. theory) CVD diamond
measurements
model
Log Qmeas. (a.u.)
Log ncalc.(a.u.)
L.V. Keldysh, JETP 20, 1965, Apostolova et al in press NIMA, 2014, Otobe et al, PHYSICAL REVIEW B 77, 165104, 2008 (interpretation in terms of MPI, good agreement with the experiment)
n=4.4
Energy (μJ)

## Slide 7: PI yield (expt), lower intensities
n (cm-3)
E (J)
MPI, n=4
Change of slope
(suggesting electron-hole recombination after pulse irradiation)

## Slide 8
Density of states
Boltzman equation including direct and phonon-assisted photoionization

## Slide 9: Theoretical model
(gauge freedom)
(electron density)
(adiabatic representation)
(Schrӧdinger picture)
(empirical pseudopotential model)

## Slide 10: Static band structure
Indirect gap 5.42 eV. Gap at k=(0,0,0) is 7 eV, requires minimal number of photons n=5 to undergo a transition (multiphoton ionization)
Band gap

## Slide 11
|n=1,k=0> (ground state)
|n=2,k=0> (three fold degenerate)
|n=5,k=0> - lowest conduction band
(Bloch orbitals)

## Slide 12
Electron dynamics
red – parallel to C-C bond
black - perp. to C-C bond

## Slide 13
Green-2
Black-3
Red-2.5
Nonadiabatic fraction
red-nonadiabatic

## Slide 14: Photoionization yield (2 band model)
Predicts strong dependence on the polarization of the laser field. Adiabatic approximation predicts 6-photon process and gives lower densities)

## Slide 15: Polarization dependence
Emission of longwavelength electrons (small k). Charge density - polarization independent, current density - polarization dependent.

## Slide 16: Photoionization yield
I=

## Slide 17: Conclusion
Multiphoton ionization by electron-hole pair creation occurs after absorption of 9 photons. Non-monotonic dependence of ionization yield on the laser intensity.
Good qualitative agreement with experiment
(slope changes near I= in agreement with expt.)
(n(exp)=4 vs. n(th)=9  5 photons in excess. But the expt. assumes that the collected charge is equal to the generated one)