## Slide 1: Upgrade of the CMS Tracker for the High Luminosity LHC
VERTEX2015: Santa Fe

## Slide 2: Outline
Challenges for the CMS Tracker
Rad-Hard Sensors
Track Trigger Modules
Tracker Layout
Prototyping of Sensors and Modules
Introduction

## Slide 3: Out of Scope
CO2 Cooling
Powering
Mechanics
Track Trigger
  Thursday, 4 June at 09:00 ”CMS developments for track-triggers” Marco De Mattia
CMS Pixel Upgrade
  Earlier today, 1 June at 14:00 ”CMS pixel upgrade for the HL-LHC” Robert Stringer
Introduction

## Slide 4: The High Luminosity LHC and CMS
Upgrade of the LHC by 2020 to achieve 5x the current design luminosity: 5 x 1034 cm-2s-1
  Original LHC integrated luminosity: ~500 fb-1
  Integrated luminosity with upgrade: ~ 3000 fb-1
Significant gain in collected events!
Current CMS Tracker was designed to operate for 10 years in LHC environment
  End of lifetime reached by 2022
 Replacement necessary to keep CMS running
Introduction

## Slide 5: Challenges
Higher density of tracks
  Increase granularity of sensor elements
Increase in radiation
  Radiation hard components, in particular sensors
L1 Trigger needs input from tracker
  Transmitting full tracker information at 40 MHz not possible
  Data selection inside the tracker
Introduction

## Slide 6: Radiation tolerant silicon sensors

## Slide 7: Radiation tolerant sensor materials
Wafer layout with 34 different structures
  Small strip and pixel sensors
  Dedicated test structures
Produced by Hamamatsu on
  FZ: 200 and 320 µm thickness
  ddFZ*: 120 and 200 µm active thickness
  MCz: 200 µm thickness
  Epi: 50 and 100 µm thickness
Each material processed with
  p-on-n
  n-on-p (pspray)
  n-on-p (pstop)
FZ200 in all three processes with 2nd metal layer
Total of 164 wafers
Extensive irradiation and measurement campaign
* ddFZ = deep diffused FZ
Sensors

## Slide 8: Irradiation Targets
Fluences target 20 and 40 cm radius in the outer tracker after 3000 fb-1
Highest fluence for innermost layers of the outer tracker at 1.5 x 1015 neqcm-2
radius | proton Φeq [cm-2] | neutron Φeq [cm-2] | total Φeq [cm-2] | Active thickn.
40 cm | 3 ∙ 1014 | 4 ∙ 1014 | 7 ∙ 1014 | ≥ 200 μm
20 cm | 1 ∙ 1015 | 5 ∙ 1014 | 1.5 ∙ 1015 | ≥ 200 μm
Sensors

## Slide 9: Collected Charge
N-type sensors (hole collection) show higher signal degradation than p-type
Beyond ~1015 neqcm-2 200 µm of active silicon show a similar signal to 300 µm
Sensors

## Slide 10: Random Ghost Hits (RGH)
Very high charge collected in highly irradiated n-type silicon
Not originating from charge created by a particle
Not observed in p-type silicon!
RGH rate = 0%
RGH rate = 3%
Adds non-Gaussian noise
Noise above threshold will show as “hits”
Similar to micro-discharges
  but assumed not to be the same effect
Sensors

## Slide 11: Annealing
Charge collected in 200 µm sensors stays relatively constant up to 20w@RT
  Thick sensors show more pronounced loss
mCZ shows no loss (even gain) after 20w@RT
  Full depletion voltage stays constant
Annealing in mCZ would decrease leakage current (and therefore noise) with no loss in signal
20w@RT
Sensors

## Slide 12: Baseline for the Phase II Outer Tracker
P-type materials (n-on-p) are the baseline
  Slower signal degradiation
  No Random Ghost Hits (RGH)
200 µm active thickness is preferred
  Collected charge similar to 300 µm after high fluences
  Lower dark current
200 µm physical thickness is preferred
  Less material
mCZ is preferred
  No change in the Vdepl with annealing
Not shown: P-spray and p-stop show sufficient strip isolation after high fluences
Sensors

## Slide 13: Detector Modules

## Slide 14: Detector modules with data filtering
On-module data reduction by only sending hits from particles with a transverse momentum pt of > a few GeV/c
At given magnetic field the track curvature depends on the particle’s pt
Different curvature results in different incident angles at a given radius
Estimate incident angle from hit displacement over a short distance  two parallel sensor planes
Modules

## Slide 15: The pt Module Concepts
The 2S Module
2 x Strip sensors: 2S sensor
  Size: 10 x 10 cm2
  Pitch: 90 µm
  Length: 5 cm
  No. of strips per sensor: 2x1016
2 x 8 CMS Binary Chips: CBC
  2x127 channels per chip
  Bump bonded to flexible hybrid
  Connects to top and bottom sensors
  Interchip communication via hybrid
Concentrator ASIC: CIC
  collects data from 8 CBCs (half module)
Low Power GigaBit Transceiver LP-GBT
  Bandwidth: 3.2 Gb/s (4.8 Gb/s raw)
2-stage DCDC powering
  12 V to
    2.5 V (opto)
    1.2 V (ASICS)
Modules

## Slide 16: The pt Module Concepts
The PS Module
MacroPixel sensor: PS-p sensor
  Size: 5 x 10 cm2
  Pitch: 100 µm
  Length: 1.5 mm
  No. of pixels: 32x960
Strip sensors: PS-s sensor
  Size: 5 x 10 cm2
  Pitch: 100 µm
  Length: 2.5 cm
  No. of strips: 2x960
2 x 8 Short Strip ASIC: SSA
  120 channels per chip
  Sends hits to MPA
  Bump bonded to flexible hybrid
16 MacroPixel ASIC: MPA
  120 x 16 pixels per chip
  Bump bonded to MacroPixel sensor
  Includes correlation logic
Concentrator ASIC: CIC
  collects data from 8 MPAs
Low Power GigaBit Transceiver LP-GBT
  Bandwidth: 3.2 Gb/s (4.8 Gb/s raw)
2 stage DCDC powering
  12 V to
    2.5 V (opto)
    1.2 V (ASICS)
    0.8 V (ASICS)
Modules

## Slide 17: Electronic system
Readout chain for 2S and PS identical from CIC onwards
Front to back end transmission using optical fibres at 4.8 Gb/s (raw)
Clock, data and control use the same system
Main dataflow now to Trigger (80-90%) and not to DAQ
Exact specifications not yet fixed, eg.:
  Dynamic or fixed allocation of bandwidth for TRG and DAQ
  Asymmetric bandwidth for up- and downstream in LP-GBT
Modules

## Slide 18: Tracker Layout

## Slide 19: Tracker Layout Concept: Baseline
Barrel and endcap geometry
2S modules for r > 60 cm
PS modules for r < 60 cm
Sensor spacings optimised with 2 (2S) or 3 (PS) groups
2 module types in 2 (3) flavours (sensor spacing) sufficient to built barrel and endcaps!
Similar number of hits vs. η at larger coverage than existing tracker
At lower material budget than existing tracker
  CO2 cooling
  DCDC powering
  No dedicated control electronics
PS Modules
2S Modules
Pixel
Layout

## Slide 20: Layout Concept: Tilted Barrel
PS modules in inner barrel tilted “towards” IP
Reduction of number of modules/sensors
  From ~7000 to ~5700 PS modules
Significant reduction in material budget
Safes costs
Significant increase of mechanical engineering required!
Layout

## Slide 21: Layout Concept: 8” Sensors
Costs per area on 8” is significantly cheaper than on 6”
Keep electronics identical for 6” and 8”
3 PS sensors per wafer
Elongate 2S sensor from 10 x 10 cm2 to 10 x 15 cm2: 2S long
High occupancy in innermost 2S layer
  Shorten sensor to 10 x 7.5 cm2 and cut two from one wafer: 2S short
Break even if cost per wafer
  8” < 1.5 x 6”
Layout

## Slide 22: Prototyping

## Slide 23: From Proposals to Prototypes
Technical Proposal (TP) for the Phase II Tracker is ready
  Full CMS Phase II TP will be published soon
First prototypes are being procured and built
  Starting with sensors and modules
Prototypes

## Slide 24: Small size PS Prototype: MAPSA light
MacroPixel SubAssembly: MaPSA
Scaled down version of the pixel part of the PS module
MPA light chip
  # of pixels: 3 x 16
  Pixel size: 100 x 1446 µm
  Chip size 1.7 x 6.5 mm2
  Process: 65 nm TSMC
PS-p light sensor
  Material: FZ p-type
  Thickness: 200 µm
  # of pixels: 48 x 6 ≅ 6 x MPA-light chips
  Sensor size 7.8 x 12 mm2
  Produced at: CiS, Erfurt DE
PS Module
Pixelated part: MaPSA
Small prototype: MAPSA light
Prototypes

## Slide 25: Early 2S prototypes
First mini 2S prototype modules were built in 2013
  Two 5 x 2.3 cm2 sensors with 256 strips from Infineon or CNM
  2 x CBC2 readout chips bumped to hybrid
Beam test at DESY in 2013
Demonstrate stub finding efficiency
  Angle between sensor surface and beam was changed
  Translated into an equivalent pT at a radius of 75 cm
pT Threshold
Nominal: 2.14 GeV
Measured: 2.2 GeV ± 0.1 GeV
Prototypes

## Slide 26: Full size 2S Prototypes
Dummy modules built for assembly studies
  Prototype readout hybrids without chip
  Inactive dummy sensors
Functional module to be built next
  Prototype readout hybrids with 8xCBC2
  Fully functional sensors
  Realistic mechanical components
  No CIC, DCDC or GBT
Prototypes

## Slide 27: Baseline Design 2S Sensor
Wafer
  Wafer diameter (6” wafer): 150 mm
  Forbidden margin 5 mm -> 140 mm usable
Sensor
  N-on-p
  Strips: 2032 (2 x 8 x 127)
  Strip Pitch: 90 µm
  Width/Pitch: ~ 0.25
  P-stop: Atoll
2S Sensor size
  Sensor width: 94.183 mm
  Sensor length: 102.7 mm
  Active size: 100.6 x 91.5 mm2
And more …
  Test sensors to evaluate design options
  Test structures (Diodes, MOS, Sheet, Van-der-Pauw, Cross-Bridge-Kelvin-Resistors, etc …)
150 mm
5 mm
140 mm
94.183 mm
102.7 mm
2S Sensor
Baby
CenterBias
PStopGeo
NoPStop
PCommon
KITtest
Irrad
PSlight
SegArea
Prototypes

## Slide 28: 2S Sensor Production
Production at HPK
Material
  20 x mCZ with 320 µm physical thickness
  20 x ddFZ with 240 µm active thickness
Strip isolation
  Both materials split 15 x p-stop and 5 x p-spray
Status
  Layout adapted by HPK
  Production started recently
  ETA: End of August 2015
Production at Infineon
Material
  30 x FZ with 200 µm physical thickness
Strip isolation
  P-stop and p-spray, details to be decided
Status
  Layout to be adapted by CMS in the coming weeks
  Production start envisaged for July
  ETA: Autumn 2015
Prototypes

## Slide 29: 8” Sensors from Infineon

## Slide 30: Baseline Design 2S Sensor (8” version)
94 mm
102.7 mm
94 mm
153.4 mm
Wafer:
  Wafer diameter (8” wafer): 200 mm
  Forbidden margin 10 mm -> 180 mm usable
  FZ with 200 µm physical thickness
  Resistivity ~ 7 kΩcm
Sensor
  Same as the 6” version but elongated
  N-on-p
  Strips: 2032 (2 x 8 x 127)
  Strip Pitch: 90 µm
  Strip length: 75.6 mm
  Width/Pitch: ~ 0.25
  P-stop: Atoll
2S Sensor size
  Sensor width: 94.183 mm
  Sensor length: 153.4 mm
Status
  In production at Infineon
  ETA: September 2015
8” Sensors

## Slide 31: Summary
A consistent concept of Phase II Outer Tracker has been presented
Feasibility of the main ingredients have been demonstrated
  Radiation hardness of the sensors
  Track trigger capabilities of the modules
Decisions between open design options and detailed engineering on-going
  Prototype sensors and modules to be built in 2015 will facilitate these decisions

## Slide 32
Thank you for your attention!

## Slide 33: Random Ghost Hits
Occurrence of RGH Depends on bias voltage, irradiation, annealing, temperature and strip geometry
Simulations suggest an increase of electric field maxima with Qox at strip edges for n-type sensors
For p-type sensors the maxima goes down with an increase in Qox

## Slide 34: Tracker Layout: tilted IB
Modules supported by Rings
Rings joined by longitudinal bars.
Cooling supply pipes, wires and fibres routed along the bars.