## Slide 1: RF Dipole Cavity HOM Coupler Fabrication
JLAB, February 25, 2015

## Slide 2: Fabrication Step 1 – Brazing
Nb coupler body + SS flange (316 LN)
QC after brazing
  Leak check
  Concentricity
Machined Nb top
Brazing
Rolled/formed Nb can
Courtesy of Teddy Capelli

## Slide 3: Fabrication Step 2 – EBW
QC after welding
  Measure gap, perpendicularity
Use fixture to control the gap
Courtesy of Teddy Capelli

## Slide 4: Fabrication Step 3 – EBW
Courtesy of Teddy Capelli

## Slide 5: Fabrication Step 4 – BCP
BCP with active thickness monitoring
150 μm removal
After BCP/Rinse the spool piece will be mounted to protect hook
Spool piece to enclose the hook during BCP
Courtesy of Teddy Capelli

## Slide 6: Fabrication Step 5 – He Jacket Weld
EBW or TIG
Standard SS tubing
Courtesy of Teddy Capelli

## Slide 7: Summary
Courtesy of Teddy Capelli

## Slide 8: High Pressure Rinse
Stationary nozzle
Nozzle inserted below the hook
Coupler assembly attached to the rotating turn table
Water pressure adjusted not to bend the hook

## Slide 9: Fabrication Traveler
Nb Sheet
316 LN Bulk
Nb Bulk
Nb Bulk
316 LN Tube
316 LN Bulk
Roll / Form
Machine bottom flange
Machine Hook & T
Machine can top
Cut to the length
Machine top flange
Dimensions Roundness
Dimensions
Dimensions
Dimensions
Dimensions
Dimensions
Machine Braze OD
Braze
Braze
Leak check
Cold shock / cycle
Leak check
Leak check
Cold shock / cycle
Leak check
EBW
Perpendicularity
Gap dimension
Tune
EBW
BCP / Rinse
Dimensions
Parallelism top & bottom flanges
Install Spool
EBW or TIG
Leak check / Survey / Cleaning

## Slide 10: Manufacturing Tolerance
  Deviations introduced during manufacturing and also the most crucial GD&T for performance
  gap_bar
  rot_about_z
Introduced during manufacturing, easily controlled or large allowable tolerance
  tank_radius
  bar_radius
  gap_top
  rot_about_x
Introduced during assembly but with large tolerance
  y_tip
  gap_probe
gap_bar
gap_top
gap_probe
bar_radius
tank_radius
rot_about_z
(+)
rot_about_x
(+)
ytip

## Slide 11: Tolerance Control
Precision machined fixture will be used during welding to control the hook and T alignment.
Weld joint will be optimized to reduce the deformation.

## Slide 12
Chart: varying transverse gap between probe bar/hook and T, move T along x-dir
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
-0.1 mm | 503081.9281 | 1869.4678 | 178.783 | 295.9046 | 1369.2366 | 137.1698 | 266.1976 | 262.8087 | 60.9364 | 226.511 | 2411.4046 | 309.5645 | 19.6356 | 46.5879 | 8512.6649 | 48.4039 | 16884.475 | 1731.7632 | 885.9279 | 147.4151 | 2048.449 | 98.3433 | 80.6042 | 30307.5842 | 39.1585 | 1176.757 | 78191.2991 | 63.4754 | 50651.642 | 109.2792 | 37076.6032 | 73.2249 | 23801.784 | 129.2312 | 8970.4641 | 340199.8682 | 2834.8914 | 4356.6316 | 3878.8003 | 48364.1999 | 115637.914 | 40242.0518 | 349.4898 | 230.4002 | 7699.4353
0.1 mm | 503097.8833 | 863.3712 | 206.262 | 281.8017 | 1369.1749 | 136.6714 | 266.1986 | 731.1543 | 262.1418 | 60.227 | 220.1087 | 2394.2578 | 301.5041 | 19.6395 | 46.5713 | 8494.0554 | 48.3976 | 17129.7852 | 1731.403 | 899.5478 | 146.9404 | 2037.6986 | 98.3607 | 79.6254 | 30865.9157 | 39.1678 | 1175.6998 | 78365.8004 | 63.5194 | 50445.5707 | 108.9736 | 73.2032 | 34288.0137 | 23697.6068 | 129.1823 | 8461.1484 | 339174.0906 | 2835.0211 | 4676.6679 | 3893.2604 | 48334.4652 | 115582.1331 | 40258.7272 | 349.9552 | 230.3414 | 7676.5773 | 11603.8956
0.5 mm | 503072.0416 | 2985.5245 | 290.3023 | 245.4226 | 1368.1041 | 135.7402 | 266.1424 | 686.8891 | 260.7502 | 58.8603 | 207.9389 | 2359.5605 | 286.196 | 19.6294 | 46.599 | 8455.6836 | 48.4014 | 17628.8696 | 1731.8152 | 927.317 | 146.0447 | 2015.2536 | 98.3289 | 77.5538 | 32120.2452 | 39.1764 | 1173.4912 | 78957.3362 | 63.633 | 49894.1514 | 108.4393 | 73.1062 | 28780.8322 | 23424.3712 | 128.8614 | 7506.4954 | 337520.3735 | 2836.5872 | 5656.9129 | 3920.6933 | 48365.6562 | 115157.2816 | 40230.2424 | 350.227 | 230.3924 | 7668.6589 | 11633.7537
H-HOM Error analysis and tolerances

## Slide 13
Chart: varying transverse gap between hook and T, move hook along x-dir
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
-0.1 mm | 503100.6068 | 1248.7235 | 503100.6068 | 194.096 | 295.4816 | 1369.3849 | 136.8489 | 266.1639 | 736.3283 | 262.2609 | 60.4119 | 221.6099 | 2397.6905 | 303.8142 | 19.6373 | 46.583 | 8543.2799 | 48.4029 | 17194.3702 | 1731.6826 | 902.5261 | 145.1939 | 2013.5002 | 98.3365 | 78.2261 | 31099.9982 | 39.1613 | 1175.7738 | 78524.0427 | 63.5853 | 50441.1908 | 109.0313 | 73.215 | 34961.8378 | 23719.7826 | 129.1562 | 8533.4439 | 339554.4793 | 2835.007 | 4526.1594 | 3889.6095 | 48360.2256 | 115929.8925 | 40241.1638 | 349.8155 | 230.3883 | 7675.6237
0.1 mm | 503105.1099 | 1333.8438 | 503105.1099 | 189.3301 | 283.3913 | 1369.0174 | 136.9768 | 266.2327 | 749.8906 | 262.7846 | 60.7987 | 224.9202 | 2407.7537 | 307.4355 | 19.6344 | 46.5873 | 8473.2878 | 48.4005 | 16817.8508 | 1731.5336 | 882.5538 | 149.2469 | 2074.1649 | 98.3573 | 82.1482 | 30056.6913 | 39.166 | 1176.5964 | 78035.6057 | 63.4103 | 50609.0782 | 109.2958 | 73.219 | 36354.2349 | 23760.083 | 129.2094 | 8885.1724 | 339425.3677 | 2835.2869 | 4489.23 | 3883.8827 | 48342.8439 | 115449.3989 | 40264.1035 | 349.7202 | 230.3934 | 7683.4946 | 11587.8678
0.5 mm | 503064.8614 | 1523.0372 | 503064.8614 | 188.468 | 259.4837 | 1367.7387 | 137.2729 | 266.2861 | 780.2004 | 263.9584 | 61.6394 | 231.8526 | 2429.9433 | 315.3696 | 19.6353 | 46.5955 | 8332.5774 | 48.4075 | 16062.0054 | 1731.7105 | 843.1968 | 158.5358 | 2210.6655 | 98.3806 | 90.6645 | 28048.8991 | 39.1626 | 1178.0916 | 77470.4911 | 63.0343 | 51053.3082 | 109.8491 | 73.1983 | 39304.0729 | 23800.6068 | 129.2455 | 9590.3952 | 342184.1396 | 2835.6895 | 4518.9625 | 3873.5418 | 48342.9387 | 115483.4311 | 40225.837 | 349.1329 | 230.4389 | 7712.9116
H-HOM Error analysis and tolerances

## Slide 14
Chart: introducing hook rotation about x-axis
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
0.5 deg | 503129.4674 | 1412.2964 | 208.2082 | 302.1615 | 1369.5245 | 137.4152 | 265.9353 | 262.4213 | 59.3324 | 253.0778 | 2616.4077 | 355.0857 | 19.6945 | 46.4884 | 9008.2764 | 48.4427 | 17273.8175 | 1733.093 | 898.9327 | 146.5801 | 3.3504 | 1957.2528 | 98.4039 | 66.2586 | 26958.1204 | 38.9983 | 1220.5728 | 54443.4052 | 63.6742 | 65930.0749 | 108.202 | 72.7805 | 35929.1574 | 22699.1518 | 129.6999 | 8732.1049 | 312406.6925 | 17.5496 | 2838.1837 | 4566.4693 | 3835.3953 | 47869.5286 | 121195.2184 | 36735.3926 | 7444.6307 | 11523.8144 | 3334.0833 | 207.952 | 23272.6313 | 23737.4862 | 51.3197
-0.5 deg | 503215.3203 | 1204.3483 | 172.2195 | 279.9072 | 1368.1604 | 136.3387 | 266.3255 | 721.7463 | 262.1409 | 62.292 | 201.2363 | 2160.8091 | 265.0941 | 19.6161 | 46.6513 | 8057.6082 | 48.4075 | 16777.8698 | 1732.9798 | 890.0583 | 149.9847 | 2155.075 | 98.2503 | 34356.3212 | 39.2418 | 1129.4243 | 117136.3638 | 63.2132 | 30240.3674 | 110.1362 | 73.4352 | 34677.1802 | 25101.3122 | 128.4474 | 8528.7232 | 362522.5968 | 17.4572 | 2832.7017 | 4274.1679 | 3938.9799 | 49637.792 | 106200.1087 | 44508.4207 | 346.0847 | 230.6534 | 8133.6799 | 11568.0182 | 3343.114 | 207.5817
1 deg | 503124.4939 | 1496.1001 | 223.9448 | 317.1595 | 1373.6434 | 138.0482 | 265.9826 | 784.2175 | 261.7436 | 58.4239 | 289.8299 | 2792.798 | 411.6481 | 19.8102 | 46.1952 | 9521.522 | 48.433 | 17615.8859 | 1731.5129 | 908.7824 | 148.3201 | 1910.1258 | 98.6161 | 55.4589 | 24136.7142 | 38.8301 | 1260.6302 | 38705.7506 | 63.7257 | 50922.0231 | 107.0378 | 72.2801 | 35467.6894 | 21424.0207 | 130.6337 | 8542.6069 | 286519.6365 | 2836.8401 | 4469.7194 | 3789.1049 | 46742.5573 | 129111.4614 | 33929.3293 | 345.3238 | 229.9679 | 7002.0549 | 11526.6303 | 15.0348 | 3345.3905 | 208.2899
H-HOM Error analysis and tolerances

## Slide 15
Chart: introducing hook rotation about z-axis, first pivot point
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
-0.5 deg | 503077.2375 | 2634.4567 | 218.5089 | 263.0522 | 1369.9051 | 256.5802 | 61.9253 | 279.1914 | 2550.7959 | 378.3963 | 19.6391 | 46.5735 | 9361.0213 | 48.4014 | 18150.3486 | 1732.5532 | 954.409 | 155.8288 | 2163.7396 | 98.3805 | 86.033 | 33632.8569 | 39.1859 | 1170.7198 | 79780.6437 | 64.0441 | 48784.7174 | 108.3094 | 73.3509 | 40517.1147 | 23898.904 | 129.5163 | 9640.0496 | 343699.6323 | 2836.2019 | 5027.9142 | 3833.7067 | 47953.2752 | 128991.9721 | 35185.2104 | 364.8878 | 230.7695 | 8279.3588 | 11617.4582
0.5 deg | 503090.1858 | 714.3036 | 185.4168 | 315.9128 | 1368.671 | 136.7977 | 266.078 | 266.4006 | 60.1445 | 181.4929 | 2257.6477 | 249.9379 | 19.6413 | 46.5757 | 7783.6367 | 48.4031 | 16046.8344 | 1731.323 | 841.3783 | 140.2962 | 1946.8381 | 98.3209 | 76.0329 | 27421.1445 | 39.1363 | 1182.3222 | 76301.2054 | 62.7802 | 52413.7125 | 110.0161 | 73.0171 | 30404.0766 | 23546.381 | 128.8375 | 7673.4685 | 330834.4902 | 2832.4745 | 3781.6102 | 3950.6107 | 48704.3008 | 100738.4398 | 46987.6725 | 330.1115 | 229.7907 | 723.4067 | 11535.9373
1 deg | 503109.5351 | 570.7013 | 196.1919 | 346.8324 | 1367.8931 | 136.7322 | 268.6629 | 61.1909 | 151.5486 | 2138.1779 | 207.0025 | 19.6411 | 46.6031 | 7174.832 | 48.4267 | 15218.2811 | 1730.8688 | 798.173 | 134.6236 | 1865.5762 | 98.2389 | 73.5311 | 24208.2499 | 39.0942 | 1188.2889 | 74645.1721 | 61.8661 | 54353.8954 | 111.244 | 72.7093 | 25038.048 | 23169.4871 | 128.1665 | 6567.2135 | 322913.1827 | 2828.6309 | 3048.5667 | 4030.3638 | 48977.7919 | 87089.8731 | 55365.3186 | 305.2465 | 229.0136 | 13800.0264 | 11427.1446
H-HOM Error analysis and tolerances

## Slide 16
Chart: varying gap between T and top of tank, move T along y-dir
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818
-0.5 mm | 503084.6597 | 1458.4929 | 192.1361 | 291.8705 | 1369.8943 | 137.0155 | 266.2154 | 745.4636 | 262.6045 | 60.697 | 222.5995 | 2397.7517 | 304.715 | 19.6534 | 46.5443 | 8533.1844 | 48.4029 | 17212.5958 | 1731.5579 | 904.6716 | 147.103 | 2030.5809 | 98.3579 | 79.4027 | 30474.089 | 39.1432 | 1176.5497 | 78275.1296 | 3884.2735 | 50582.7741 | 109.1298 | 36933.6609 | 73.1922 | 23790.4492 | 129.2815 | 8864.3633 | 339329.3428 | 2833.7584 | 4328.0694 | 3880.3534 | 48329.2814 | 115571.5672 | 40226.3543 | 349.4352 | 230.3563 | 7686.3393
0.5 mm | 503093.7857 | 1147.4664 | 191.1728 | 286.5905 | 1369.2303 | 136.8283 | 266.1996 | 740.5507 | 262.3118 | 60.4889 | 223.9007 | 2407.2391 | 306.2521 | 19.647 | 46.5587 | 8474.5444 | 48.4019 | 16804.0229 | 1731.579 | 880.7567 | 147.378 | 2056.8134 | 98.3688 | 81.0265 | 30711.2931 | 39.1637 | 1175.2949 | 78254.7104 | 63.4005 | 50510.743 | 109.0743 | 34449.2819 | 73.161 | 23687.5592 | 129.1859 | 8572.4878 | 337059.8997 | 2834.9287 | 4685.7439 | 3890.7869 | 48320.5675 | 114804.072 | 40223.8519 | 349.6201 | 230.3668 | 7672.3518
1 mm | 503084.8211 | 1040.1838 | 190.8502 | 284.4886 | 1368.8012 | 136.7169 | 266.1985 | 737.6262 | 262.2269 | 60.443 | 224.6165 | 2411.3043 | 307.3371 | 19.6349 | 46.5874 | 8456.4664 | 48.4007 | 16595.7201 | 1731.5415 | 868.2091 | 147.7076 | 2073.5327 | 98.369 | 82.1833 | 30850.1318 | 39.1842 | 1174.5211 | 78323.5564 | 63.3285 | 50385.8961 | 109.0875 | 73.1646 | 33250.7663 | 23616.9569 | 129.1175 | 8447.8673 | 339730.3855 | 2835.7887 | 3896.7288 | 48354.3871 | 115400.237 | 40247.0925 | 349.6931 | 230.3866 | 7690.6766 | 11593.3538
H-HOM Error analysis and tolerances

## Slide 17
H-HOM Error analysis and tolerances
Chart: varying gap between probe bar and hook, move probe along y-dir
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818
0.1 mm | 503085.8364 | 1287.4973 | 190.0529 | 290.7162 | 1369.3509 | 136.8487 | 266.2062 | 740.2119 | 262.518 | 60.6932 | 223.2182 | 2401.2283 | 305.938 | 19.6407 | 46.5704 | 8528.6396 | 48.3989 | 17010.5812 | 1731.6021 | 892.5291 | 146.7976 | 2033.8828 | 98.4331 | 80.0783 | 30463.4834 | 39.0356 | 1175.3108 | 77475.0437 | 63.3234 | 52147.6994 | 108.6847 | 72.7219 | 35521.1002 | 23775.3372 | 129.3988 | 8737.4601 | 339531.0809 | 2828.7833 | 4507.0065 | 3868.2338 | 48535.4428 | 115843.9018 | 39448.3067 | 349.8823 | 230.4211 | 7760.3859
-0.1 mm | 503081.204 | 1291.4982 | 193.0195 | 287.6959 | 1368.7906 | 136.9768 | 266.1876 | 746.0045 | 262.4942 | 60.4901 | 223.4551 | 2404.3571 | 305.2626 | 19.6232 | 46.6116 | 8481.9397 | 48.4312 | 16990.852 | 1731.6984 | 892.9933 | 147.4403 | 2038.8071 | 98.3781 | 80.2606 | 30370.5367 | 39.0703 | 1173.4738 | 78327.4474 | 63.4127 | 4.7406 | 50081.8697 | 109.0092 | 35642.4052 | 72.8773 | 23677.2954 | 8690.7145 | 129.2547 | 336115.0244 | 2832.7958 | 4507.353 | 3882.6975 | 48618.5059 | 113362.7892 | 40054.3368 | 347.6411 | 230.4879 | 7766.9781 | 11582.3743 | 15.0315
0.5 mm | 503078.2021 | 1282.2518 | 184.5918 | 296.8849 | 1368.6585 | 136.5295 | 266.1602 | 262.7334 | 61.0696 | 222.8442 | 2395.094 | 307.3695 | 19.6237 | 46.6124 | 8621.9509 | 48.3998 | 17035.3608 | 1731.6345 | 890.9725 | 145.8026 | 30621.058 | 39.1793 | 1176.1429 | 78394.9374 | 63.4392 | 50611.5268 | 109.2351 | 73.2377 | 35710.7845 | 23740.5772 | 129.1854 | 8794.1719 | 342069.6888 | 2835.4778 | 4528.8244 | 3885.7416 | 48345.187 | 116843.933 | 39179.8106 | 347.7915 | 230.5002 | 7707.0921 | 11564.0893 | 3333.5485 | 207.5748 | 15.0387 | 23554.9945

## Slide 18
Chart: varying transverse gap between T and probe move probe along x-dir
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
-0.1 mm | 503100.6094 | 1248.7235 | 194.096 | 295.4816 | 1369.3849 | 136.8489 | 266.1639 | 736.3283 | 262.2609 | 60.4119 | 221.6099 | 2397.6905 | 303.8142 | 19.6373 | 46.583 | 8543.2799 | 48.4029 | 17194.3702 | 1731.6826 | 902.5261 | 145.1939 | 2013.5002 | 98.3365 | 78.2261 | 31099.9982 | 39.1613 | 1175.7738 | 78524.0428 | 63.5853 | 50441.1867 | 109.0313 | 73.215 | 34961.8378 | 23719.7826 | 129.1562 | 8533.4439 | 339554.4772 | 2835.007 | 4526.1594 | 3889.6095 | 48360.2256 | 115929.897 | 40241.1636 | 349.8155 | 230.3883 | 7675.6237 | 11601.9985 | 3349.3036 | 207.2795
0.1 mm | 503105.1116 | 1333.8438 | 189.3301 | 283.3913 | 1369.0174 | 136.9768 | 266.2327 | 749.8906 | 262.7846 | 60.7987 | 224.9202 | 2407.7537 | 307.4355 | 19.6344 | 46.5873 | 8473.2876 | 48.4005 | 16817.8507 | 1731.5336 | 882.5538 | 149.2469 | 2074.1649 | 98.3573 | 82.1482 | 30056.6913 | 39.166 | 1176.5964 | 78035.6061 | 63.4103 | 50609.0763 | 109.2958 | 73.219 | 36354.2349 | 23760.083 | 129.2094 | 8885.1724 | 339425.3693 | 2835.2869 | 4489.23 | 3883.8827 | 48342.8439 | 115449.3946 | 40264.1027 | 349.7202 | 230.3934 | 7683.4946 | 11587.8678 | 3340.8353 | 207.3324
0.5 mm | 503064.8609 | 1523.0372 | 188.468 | 259.4837 | 1367.7387 | 137.2729 | 266.2861 | 780.2004 | 263.9584 | 61.6394 | 231.8526 | 2429.9433 | 315.3696 | 19.6353 | 46.5955 | 8332.5774 | 48.4075 | 16062.0054 | 1731.7105 | 843.1968 | 158.5358 | 2210.6655 | 98.3806 | 90.6645 | 28048.8991 | 39.1626 | 1178.0916 | 77470.4919 | 63.0343 | 51053.3082 | 109.8491 | 73.1983 | 39304.0729 | 23800.6068 | 129.2455 | 9590.3952 | 342184.1384 | 2835.6895 | 4518.9625 | 3873.5418 | 48342.9386 | 115483.4398 | 40225.8371 | 349.1329 | 230.4389 | 7712.9116 | 11565.7347 | 3323.9114 | 207.1958
H-HOM Error analysis and tolerances

## Slide 19
Chart: varying y- location of tip of filter, move all components simultaneously along y-dir
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818
-1 mm | 503076.4901 | 1223.3291 | 188.6093 | 281.0433 | 1369.3687 | 137.0026 | 266.2762 | 740.2201 | 260.6724 | 59.6476 | 210.6889 | 2356.8557 | 272.04 | 19.6392 | 46.5743 | 7884.079 | 48.3985 | 16830.7451 | 1731.7842 | 886.7196 | 149.8783 | 2011.0466 | 98.3462 | 3658.3825 | 29032.8504 | 39.1265 | 1180.4908 | 76668.6285 | 63.676 | 50049.9935 | 108.934 | 73.2866 | 37569.3974 | 24009.3374 | 129.284 | 8936.4501 | 340884.1722 | 2834.6907 | 4284.8616 | 3864.9734 | 48440.9281 | 117229.2736 | 39347.1855 | 353.1043 | 230.4922 | 7944.5288
1 mm | 503178.6658 | 1388.6637 | 193.0499 | 298.4882 | 1369.6383 | 136.8265 | 266.0637 | 745.5895 | 264.269 | 61.6777 | 237.6272 | 2454.8409 | 345.1288 | 19.6796 | 46.5142 | 9216.7211 | 48.4277 | 17257.2824 | 1732.9854 | 902.4433 | 143.9921 | 2066.4858 | 98.3733 | 84.7873 | 32233.1322 | 39.1405 | 1173.235 | 79291.7247 | 63.3109 | 52413.84 | 109.0311 | 33529.8468 | 72.9623 | 23583.3438 | 129.1611 | 8502.64 | 336247.7097 | 2835.7247 | 4755.6136 | 3893.9668 | 48348.0188 | 114282.5902 | 40195.1997 | 345.263 | 230.3546 | 7521.8125 | 11562.7539
3 mm | 503066.7489 | 1555.7735 | 199.4068 | 318.9209 | 1368.9097 | 136.6185 | 265.9934 | 753.8254 | 268.0326 | 63.9487 | 268.8997 | 2551.3648 | 436.0472 | 19.6297 | 46.5945 | 10800.1931 | 48.4019 | 18182.9677 | 1731.2076 | 941.7938 | 137.0139 | 2129.2996 | 98.4796 | 97.9012 | 37334.3733 | 39.1387 | 1159.6021 | 83150.8981 | 62.9956 | 51506.1566 | 108.875 | 72.5337 | 29523.6355 | 22930.04 | 129.2487 | 8103.5167 | 331623.8534 | 2833.7268 | 5394.3622 | 3936.1942 | 48128.221 | 109665.7923 | 41966.8466 | 336.9353 | 229.9378 | 7141.2144
H-HOM Error analysis and tolerances

## Slide 20
Chart: introducing filter rotation about Y axis
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
-0.5 deg | 503194.1909 | 1316.3736 | 190.987 | 289.8834 | 1371.4698 | 136.9469 | 266.0976 | 262.303 | 60.6441 | 223.5858 | 2405.0919 | 306.4916 | 19.7504 | 46.381 | 8516.1346 | 48.4522 | 17001.1079 | 1731.9156 | 893.2157 | 147.5839 | 2042.1641 | 98.3741 | 80.595 | 30622.3397 | 39.0569 | 1173.8897 | 79576.5222 | 63.3612 | 49915.1469 | 108.9937 | 72.8082 | 35520.4733 | 24003.5452 | 129.1513 | 8783.124 | 343442.4491 | 2831.3366 | 4467.9406 | 3882.0784 | 48545.5725 | 112840.9826 | 40538.9301 | 347.5839 | 230.5277 | 8075.8342 | 11568.6504 | 3346.9595
0.5 deg | 503197.4457 | 1310.7172 | 191.1458 | 289.4699 | 1367.614 | 136.8759 | 266.0845 | 743.9263 | 262.5086 | 60.4627 | 223.5044 | 2407.3516 | 305.9829 | 19.6124 | 46.6638 | 8509.165 | 48.4194 | 17013.5251 | 1733.3297 | 893.4013 | 146.8452 | 2029.0429 | 98.2877 | 79.6492 | 30106.659 | 39.1456 | 1177.0708 | 77630.4124 | 63.566 | 50564.1321 | 109.3008 | 73.1533 | 35815.985 | 23593.5364 | 129.0475 | 8694.4694 | 335443.153 | 2838.4745 | 4523.9326 | 3878.0392 | 48584.5886 | 116490.332 | 39367.6775 | 347.975 | 230.4706 | 7710.6181 | 11583.9858 | 3342.529 | 207.2482
1 deg | 503186.1091 | 1316.9642 | 190.6325 | 289.6855 | 1371.2275 | 136.9805 | 266.2121 | 743.9354 | 262.2937 | 60.6671 | 223.8692 | 2405.8653 | 307.0031 | 19.7282 | 46.4084 | 8531.6373 | 48.4379 | 17001.6712 | 1731.9397 | 891.7261 | 146.1904 | 2021.5118 | 98.3976 | 79.213 | 29770.2994 | 39.0644 | 1175.0129 | 75840.592 | 63.424 | 50258.3654 | 109.0061 | 72.8062 | 35746.0224 | 23455.7728 | 129.3103 | 8638.9202 | 329703.9392 | 2833.2993 | 4577.8215 | 3872.4357 | 48306.3607 | 118210.117 | 38689.0929 | 348.3741 | 230.4392 | 7382.5431 | 11560.8152 | 3338.9448
3 deg | 503140.1962 | 1311.5197 | 191.0873 | 289.1985 | 1368.011 | 136.8547 | 266.0554 | 744.5544 | 262.6053 | 60.4907 | 224.1587 | 2414.9899 | 307.8804 | 19.6249 | 46.6501 | 8553.8471 | 48.4302 | 17036.5502 | 1733.4512 | 892.1142 | 144.4894 | 1993.2981 | 98.2711 | 77.5652 | 28641.4953 | 39.1332 | 1177.4812 | 71154.8186 | 63.6562 | 48912.875 | 108.9596 | 73.2644 | 36188.9421 | 22922.5347 | 129.2252 | 8519.8708 | 309286.8071 | 2839.5627 | 4738.3974 | 3859.171 | 47754.7146 | 124278.3144 | 36295.1647 | 350.0162 | 230.3323 | 6887.5409 | 11596.7016 | 3338.8151
H-HOM Error analysis and tolerances

## Slide 21
Chart: varying hook and T dimensions due to BCP
| 400.76462912701902 | 627.35654885855297 | 633.88880252763602 | 450.80985948170201 | 716.03441462282501 | 735.56103230495683 | 761.05822337673101 | 783.43933647403901 | 800.22903276995396 | 875.72826305337605 | 909.78767854042997 | 946.6573978562011 | 1033.54652946191 | 1073.90835924206 | 1053.4022003549601 | 1100.4600424801699 | 1104.28415612956 | 1152.36544624006 | 1212.8918304163999 | 1232.68487344297 | 1234.9532051562301 | 1263.2896895384299 | 1268.1091165549601 | 1283.66606024365 | 1073.9083592479001 | 1362.4739000586701 | 1371.99596293582 | 1373.95274812257 | 1375.3241111960101 | 1416.48822676492 | 1450.21322755811 | 1452.81090205956 | 1475.0625120480099 | 1481.0072243475299 | 1495.21514079547 | 1569.5714143672501 | 1588.4956302457001 | 1600.6587939057099 | 1619.2681473735599 | 1622.6484559374601 | 1641.0880814024999 | 1641.31844039307 | 1666.16607420784 | 1681.3358815966801 | 1696.3888357127801 | 1521.1625508797199 | 1707.1918188914101 | 1717.9970472699199 | 1724.46605602205 | 1724.1233704357101 | 1729.37974246515 | 1729.8318063072099 | 1762.3229391525699 | 1769.71583532404 | 1782.2850505438601 | 1783.28035062454 | 1742.7011947645501 | 1815.82768438482 | 1819.68005917502 | 1828.1581505757899 | 1837.9150790659801 | 1842.6753256459799 | 1845.6806127218399 | 1854.3687609368001 | 1857.56415310395 | 1877.4883346357999 | 1898.54349848225 | 1902.38060134786 | 1877.57579273225 | 1908.1445819891901 | 1924.5620626714001 | 1929.21533993085 | 1950.6304460413301 | 1959.22100794179 | 1960.0844893219501 | 1972.52180997951 | 1980.9652872105301 | 1988.7317732608501 | 1989.0143011725199 | 2002.9180722947699
ideal | 503083.7917 | 1289.1906 | 191.4776 | 289.2256 | 1369.7394 | 136.9323 | 266.2225 | 743.0434 | 262.4569 | 60.6215 | 223.339 | 2402.3047 | 305.6589 | 19.6533 | 46.5394 | 8507.4941 | 48.3981 | 17003.8049 | 1731.4563 | 892.3399 | 147.1729 | 2043.2067 | 98.3769 | 80.1338 | 30581.5831 | 39.1579 | 1175.8096 | 78146.3088 | 63.4771 | 50490.331 | 109.0464 | 73.191 | 35676.2467 | 23753.9647 | 129.2845 | 8717.0864 | 336825.907 | 2834.2851 | 4502.312 | 3884.6064 | 48317.9863 | 114870.307 | 40217.4837 | 349.5554 | 230.3114 | 7679.5818 | 11584.7628
0.1 mm | 503217.5718 | 2328.5799 | 176.5886 | 302.7797 | 1368.4078 | 137.4854 | 266.1562 | 262.8153 | 62.4865 | 235.2935 | 2411.5875 | 320.5326 | 19.6118 | 46.6591 | 8743.7333 | 48.4156 | 17093.2358 | 1732.5084 | 892.4786 | 145.0024 | 2013.5022 | 98.3091 | 78.0756 | 30895.0263 | 39.157 | 1177.1644 | 77860.7595 | 63.6374 | 50604.44 | 109.0838 | 73.2316 | 36840.1497 | 23884.2289 | 129.1229 | 8996.598 | 341893.815 | 2837.4234 | 4655.4491 | 3856.8378 | 48516.8473 | 120211.9483 | 37701.1265 | 356.7138 | 230.7224 | 8236.4669 | 11574.6533 | 3334.4473 | 207.1976
-0.1 mm | 503178.1612 | 828.4067 | 206.6669 | 281.1235 | 1369.4294 | 136.3172 | 266.1257 | 716.7753 | 261.8686 | 58.7231 | 212.2258 | 2400.1776 | 293.0315 | 19.6751 | 46.5021 | 8304.977 | 48.4113 | 16905.9149 | 1731.8579 | 893.3191 | 149.2019 | 2058.2941 | 98.3767 | 82.2901 | 29865.2895 | 39.1201 | 1175.1217 | 77594.419 | 63.3866 | 51309.5393 | 108.892 | 73.0238 | 34280.8232 | 23572.7981 | 129.2309 | 8448.7684 | 334434.9418 | 2834.2379 | 4366.8116 | 3899.573 | 48655.4815 | 110079.3049 | 41693.5469 | 339.9121 | 230.2122 | 7511.3266 | 11528.691
-0.5 mm | 503209.1363 | 5734.5044 | 286.6963 | 288.9148 | 1367.1559 | 133.3147 | 265.5083 | 612.3321 | 257.8629 | 51.673 | 168.2519 | 2395.0225 | 245.5094 | 19.721 | 46.4463 | 7545.4237 | 48.4537 | 16584.4715 | 1732.4754 | 895.5205 | 157.8356 | 2162.031 | 98.3551 | 92.1809 | 27609.2849 | 39.0746 | 1179.4835 | 74536.1016 | 63.0571 | 57370.1319 | 108.9594 | 72.6686 | 29642.0675 | 22844.1606 | 128.9191 | 7559.253 | 322854.0231 | 2834.0026 | 3979.8898 | 3956.1411 | 48482.3402 | 98952.4985 | 47464.7805 | 315.8339 | 229.3525 | 8710.3017 | 11440.3193 | 3327.5382
H-HOM Error analysis and tolerances

## Slide 22: Fabrication Readiness
All conventional proven fabrication technique
  Braze : same as cavity beam pipe
  EBW : hook welding to cylindrical surface used for other HOM couplers
Coupler design provides necessary access for controls
Inspection and correction possible between each step

## Slide 23: Acknowledgement
Design and engineering – CERN EN, STFC/UK, Fermilab
Fabrication guidance – JLAB Machine shop, JLAB SRF Engineering