## Slide 1: Target and ion source development report
Tânia Melo Mendonça
EN-STI-RBS

## Slide 2: Beam and target developments 2014
NaF:LiF
MWCNT
Nano-TiC
Nano-LaC
Nano-UC
PbBi loop (2016)

## Slide 3: TiC-Carbon Black nanocomposite
João Pedro Ramos
Mixing TiC and Carbon (different vol. ratios)
TiC + MWC nanotubes
Test for nanostructure stability at 1500, 1650 and 1800oC
TiC + Carbon black
TiC +Graphite
TiC + Carbon Black - Milling and mixing
TiC + Carbon black (50 vol.%) nanostructure, which was stable up to 1800oC, was selected to produce a full target prototype.

## Slide 4
João Pedro Ramos
TiC-Carbon Black nanocomposite
Target #527 operated successfully online (November 2014) with a surface ion source
Successfully extracted isotopes of Li, Na, Al, K
Very stable yields
Release curves taken at different temperatures: 1650, 1800 and 2000oC
Isotope | Temp. | Yield (/μC) | Yield Ti foils (/μC)
9Li (178 ms) | 2000oC | 7.8E5 | 3.2E5 (SC)
26Na (1.07 s) | 2000oC | 8.1E6 | 1.5E6 (SC)
37K (1.2 s) | 2000oC | 1.2E6 | 7.1E6
39Ca (860 ms) | 2000oC (CF4) | 1.4E2 | 2.0E4
39Ca extracted with CF4
Target not suitable for 35Ca (25 ms) – probable reaction of Ca with carbon black?
nanoTiC-C - ½ Production rate
(lower density of Ti atoms)
Preliminary data!!

## Slide 5: LaC2–MWCNT Spallation Target Material Development
Julien Guillot, Wonjoo Hwang
Alexander Gottberg
La(OH)3 particle size reduction by suspension grinding
Theoretical Production Yields
after comparing all possible spallation target nuclei
2 µm
200 nm
LaC2-MWCNT Nano Composite (After Carbo-Thermal Reduction)
After 10 days at 1900°C
After 10 days at 1900°C

## Slide 6: #526 nano LaC2 – Re Online Tests
Isotope | #526 [µC-1] | Reference
115Cs (1.4 s) | 2 | delayed p
116Cs (3.5 s) | 110 | delayed p
118Cs (14 s) | 2×106 | Gamma
120Cs (57 s) | 5×107 | Gamma
124Cs (30.8 s) | 6×108 | Gamma
126Cs (1.6 min) | 2×109 | Gamma
128Cs (3.8 min) | 9×109 | Gamma
114Ba (0.42 s) | 0.2 | delayed p
117Ba (1.6 s) | 3 | delayed p
119Ba (5.4 s) | 6×102 | delayed p
120Ba (24 s) | >1×104 | Gamma
124Ba (11.9 min) | 1×107 | Gamma
126Ba (100 min) | 2×108 | Gamma
The target material could be tested with and without fluorination by CF4 injection at 2 different temperatures (1700°C and 1900°C)
Isotopes of Li, Na, In, Cs, Ba could be assessed.
The material was found to sublimate LaC2 significantly at 1900°C and above, and the total beam intensity starts limiting the ion source efficiency
The release of Cs is limited presumably because of effusion limits at <1900°C (nano-UC2 results)
Figure: Systematic control and optimization of Cs vs. In vs. total ionization efficiency
Julien Guillot
Alexander Gottberg, Wonjoo Hwang

## Slide 7
Alexander Gottberg
Within ENSAR FP7 – ActILab a new material was developed
New material (Target#525 tested in December 2014):
  consists of nanometric uranium carbide particles immerged in a MWCNT fiber matrix
  increases isotope yield of most investigated elements (Li, Na, K, Ca, Cu, Ga, Rb, In, Ra, Fr)
  reduced ageing effects (reduction of yield over time)
  reduces actinide waste by 60%
two orders of magnitude
Ageing of nano UCx (red) vs. ISOLDE reference (blue) for 30Na
ENSAR-ActILab: Nano Uranium Carbide at ISOLDE

## Slide 8
Alexander Gottberg
ENSAR-ActILab: Nano Uranium Carbide at ISOLDE
Chart: yield [µC-1]
| 8Li (#466 UC-Re) | 9Li (SC) | 25Na | 26Na (SC) | 30Na | 46K (SC) | 50K | 50Ca | 68Cu (highest DB entry) | 68mCu (highest DB entry) | 76Ga (highest DB entry) | 81Ga (highest DB entry) | 81Rb | 88Rb (#493 UC-Ta) | 93Rb (SC) | 96Rb (SC) | 132In | 142Cs (#477 UC-W) | 139Cs (#477 UC-W) | 207Fr (SC)
ISOLDE Conventional UCx | 4100000 | 3900000 | 290000000 | 600000000 | 51000 | 8900000 | 50000 | 24000 | 80000000 | 300000000 | 10000000 | 200000 | 170000 | 400000000 | 130000000 | 14000000 | 8000 | 400000000 | 1500000000 | 2300000
ActILab nano UCx | 28000000 | 19000000 | 2800000000 | 920000000 | 140000 | 390000000 | 86000 | 68000 | 960000000 | 340000000 | 29000000 | 1100000 | 22000000 | 8000000000 | 260000000 | 15000000 | 17000 | 1100000000 | 2100000000 | 85000000

## Slide 9: Boron beams - Multi walled carbon nano tubes target
Investigate extraction of boron and identify suited materials & target unit (Extraction of 8B desired)
  Diffusion studies of Boron in different target materials (Graphite, MWCNT, Y2O3) – implantation of 10BF2+
    10B(n,α)7Li: highest mobility in MWCNT
Formation of molecules
B+3F->BF3
Christoph Seiffert

## Slide 10: Boron beams - Multi walled carbon nano tubes target
Christoph Seiffert
Release of boron fluorides
3B+SF6 3BF2 +S
BF2+:
Target unit #499 (online September 2014)
Target material MWCNT, ρ=0.43 g/cm3
Cold transfer line, VADIS ion source with gas leak (SF6, leak rate: 0.37 x10-4 mbar∙l/s)
Activity on mass A=8 originating from 8Li and positron emitter
Positron activity corresponds to 300 /µC - extraction of 8B to be validated
Activity below detection limit of Boron in fluoride (8BFn ) and oxofluoride (BOF ) form

## Slide 11: Molten NaF:LiF salt
Validation of results obtained in 2012 (1st prototype #478):
Reproducibility of 8x108 11CO/µC
Diffusion coefficient of neon in molten salts
Tânia Melo Mendonça
21.6 cm
- Material: Haynes 242
(corrosion resistant alloy)
- VADIS ion source
εNe~1.8%
(via cold transfer line)
- Three thermocouples
(container, chimney, cold line)
- Salt fills up ¾ of the container volume
D(Ne) in NaF:LiF ~10-9 m2/s
D(Ne) in NaF:LiF is 8 orders of magnitude higher than oxide targets (CaO, Al2O3 with D~10-17 m2/s)

## Slide 12
Target #520 (online 27th October to 2nd November 2014)
Despite several problems at the start of the run (no thermocouples, HV trippings…) we could successfully validate the results obtained in 2012.
Systematic measurement of release curves for Ne diffusion coefficient in fluoride salts. Data analysis ongoing.
Tânia Melo Mendonça
Molten NaF:LiF salt
Isotope | Temp. | Yield (/μC)
6He (807 ms) | 760oC (6x1012 ppp) | 2E5
18Ne (1.67 s) | 720oC (6x1012 ppp) | 6.4E4
19Ne (17.22 s) | 760oC (6x1012 ppp) | 2.9E7
11CO (20.38 min) | 715oC (8x1012 ppp) | 6.6E8

## Slide 13: Liquid eutectic Pb/Bi loop for EURISOL LIEBE project
LIEBE target proposed design
(LIEBE Design Study Report –June 2014)
Target design review – June 2014
Complex unit and many challenges to overcome – online tests postponed to 2016
Melanie Delonca
Tânia Melo Mendonça
Irradiation chamber
Diffusion chamber
Heat exchanger
Fill and drain reservoir
Electromagnetic pump
Modifications

## Slide 14: Liquid eutectic Pb/Bi loop for EURISOL LIEBE project
Shower formation feasibility tests
Melanie Delonca
Tânia de Melo Mendonça
Vacuum pump
Camera
Vacuum pump
Shower at start.
Shower at the end.
  Shower feasibility proven: smallest spacing between holes of 0,5 mm for 0,1 mm holes
  Oxidation prevent a proper operation of the grid (analysis of the grid foreseen)
  Size of droplets vary between the start and the end of the shower – from 0.3 to 0.5 mm

## Slide 15: Liquid eutectic Pb/Bi loop for EURISOL LIEBE project
Radioisotope inventory ( collaboration with SINP-India)
- Irradiation of Pb/Bi samples using RaBBIT setup (2012)
- Measurements performed in different campaigns (2012/2013)
M. Maiti et al., J Radioanal Nucl Chem 302 (2014) 1003
- Comparison with simulations (FLUKA, MCNPX) to be published
Prof. Susanta Lahiri et al.

## Slide 16: ISOLDE Yield database
User yield database updated with new values in December 2014
Graphical restoration ongoing
Hayley Osman
Tânia Melo Mendonça

## Slide 17
Thank you for the attention!
The TISD team:
Thierry Stora
Tania M. Mendonça
Alexander Gottberg
João Pedro Ramos
Melanie Delonca
Jochen Ballof
Basil Gonsalves