## Slide 1: Radiation damage in Materials
C.A. English (2011)

## Slide 2: Transmutation

## Slide 3: Tungsten Transmutations in Fusion Reactor

## Slide 4: Tungsten Transmutations - activity

## Slide 5
Tungsten transmutation in fusion power reactor

## Slide 6
Tungsten transmutation in fusion power reactor
5yr
Re
Os
Ta
W
Os
Re
% Transmutant
Reactor Full Power Years

## Slide 7
Tungsten transmutation in fusion power reactor
Ion irradiation can’t mimic transmutation effects
But we can MODEL what transmutations we expect
And can ion-irradiate pre-made W alloys
To see what effect displacement damage -
(and if we like, He, H )
have on microstructures and properties.

## Slide 8: Radiation-induced clustering in alloys
W- 5%Re should be a stable solid solution
… but it’s not when it is irradiated
Under Fusion Power Reactor conditions, pure W transmutes to give 5%Re in ~ 7 years.
5%
8%
Ion irradiation to 2.64 x 1015 W+/cm2 (33dpa) Dose rate: 3.57 x 10-4 dpa / s
Temperature: 300°C
A. Xu (Oxford) unpublished 2013
Notes: NB – DEMo - 50-80 dpa per FPY at divertor, ITER, ~1dpa / FPY.

## Slide 9: Clustering and Hardening in “Transmuted” W
W 1%Re
W 1%Re 1%Os
2MeV W+
33dpa
FIB-lift-out
Re
Os
573 K
773 K
Nanoindentation hardness (GPa) (100nm depth)
35nm
Preliminary analysis indicates that the clusters are very weak obstacles:
Fc  85°
But there are lots of them, very closely spaced
especially in W-Re-Os
Same would apply to neutron irradiation ???
A. Xu, D.E.J. Armstrong (Oxford) K. Rajan (Iowa State) unpublished 2014
Notes: Thanks to Krishna Rajan,

## Slide 10: Transmutation gases

## Slide 11
Transmutations producing He in fusion power reactor

## Slide 12
P. Jung, J. Henry, J. Nucl. Mater. 318 (2003) 241–248 & 249–259.
J.-L. Boutard et al. C. R. Physique 9 (2008) 287–302
Fracture surface
He g.b. bubbles
He –V nanoclusters
Effects of Implanted He on T91 steel
“Uniform implantation of 23 MeV α-particles up to 5000 appm at 250°C carried out at the compact cyclotron of Forschungszentrum Jülich (FZJ)”

## Slide 13
2
4
6
8
10
12
Hardness (GPa)
300
3000
3000
300
3000
0.4
13
13
13
dpa
appm He
Tungsten – Hardening by Displacement Damage and Helium
Polycrystalline W 99.99% pure, sequentially ion-implanted with W+ and He+ at 300°C
W implantation depth 0 - 200nm; He implantation depth range 0 - 2500 nm
Hardness data at 100 nm indenter depth .
dpa
appm He
0.03
0.003
C. Beck & D. Armstrong (Oxford) unpublished 2013

## Slide 14
2
4
6
8
10
12
Hardness (GPa)
300
3000
3000
300
3000
0.4
13
13
13
dpa
Tungsten – Hardening by Displacement Damage and Helium
Polycrystalline W 99.99% pure, sequentially ion-implanted with W+ and He+ at 300°C
W implantation depth 0 - 200nm; He implantation depth range 0 - 2500 nm
Hardness data at 100 nm indenter depth .
dpa
appm He
0.03
0.003
C. Beck & D. Armstrong (Oxford) unpublished 2013

## Slide 15
Tungsten – Embrittlement by Displacement Damage and Helium
Polycrystalline W 99.99% pure, ion-implanted with W12+ (36MeV) and He+ at 800°C
W + He simultaneously implanted
W implantation depth ~2.5 mm; He depth range ~ 2.8 mm
Fracture data from microbeams 3 mm deep .
Irradiation | Fracture ?
none | 0 / 7
1.7 dpa W12+ | 1 / 16
600 appm He | 0 / 13
1.7 dpa W12+ + 600 appm He | 7 / 10
J. Gibson & D. Armstrong (Oxford) unpublished 2013

## Slide 16: “Damage”

## Slide 17
Elastic scattering of neutrons
…. What about the “target” atoms?
 | Ed |  | Ed |  | Ed
Al | ~32eV | Fe | ~24eV | Si | ~13eV
Cu | ~25eV | W | ~40eV | C (graphite) | ~25-60eV
Fusion neutrons are ~14MeV !

## Slide 18
Elastic scattering of neutrons
M1,u1
M1,v1
M2
f
v2
For 14 MeV neutrons into iron, M1 = 1, M2 = 56, so L = 0.069
So = 482 keV …. about 34 collisions per neutron

## Slide 19
Elastic scattering of neutrons
I0
I
x
N nuclei/m3
For s = 3.2 barns, N = 8x1028 m-3
Neutrons penetrate in Fe to 100 – 200 mm
If ~ 30 collisions over this depth, and “random walk”,
Spacing between neutron collisions is ~ 10 - 20mm
M2

## Slide 20
The collision cascade
Ion energy (keV)
0.1
1
10
100
1000
10000
Energy loss from C ions in graphite
100
10
1
1000
(eV/nm)
electronic
collisions
Eex
Eex (keV) ~ M2 (a.m.u.)
At high energies, ions lose energy mostly by electronic excitation
At low energies, ions lose energy mostly by collisions

## Slide 21
SRIM / TRIM
http://www.srim.org/

## Slide 22
The collision cascade
Tracks of ten 482keV Fe ions in Fe target.
“Consequent events” show in red and green.
Note long gaps between sub-cascades, and randomness of process.

## Slide 23
Ion irradiation: dpa
750 ion tracks: 482keV Fe ion in Fe target
Displaced target atoms vs depth
Unit: Number / (Å – ion) (!)
D: displacements / (m – ion) f: irradiating particles / m^2
r: atoms / m^3 in target
dpa = displacements per (target) atom
=
Here: Fe ions into Fe
D: ~ 4.5 at peak
r: 8x1028m-3
f: typically 1018 m-2 (1014cm-2)
= 0.56 dpa
Depth
0
400nm
0
2
4
Depth
0
400nm

## Slide 24
The collision cascade: evolution after initiation
n
E2 > Ek
pka
E2 
E2 < Ek
A few 100 nm
“Displacement spike”
Vacancy-rich core
Interstitial-rich shell
“Thermal”
i=1
i=2
i=3
i=….
After ith stage,
We have 2i displaced atoms:
Stops when:
So Ndisplacements 2i = Ek / 2Ed

## Slide 25
The collision cascade: evolution after initiation
“Molecular dynamics” simulation: up to 30 ps.
Only the out-of-place atoms are shown – vacancies in green; self interstitials in red.
Started by a low-energy collision (10keV ion): end of cascade branch.
10 keV < Eex,
so Ndisplacement ~ 10000/25 = 400
n
D. Bacon, Y. Osetsky, U. Liverpool

## Slide 26: Radiation  dislocation loops
Missing sheet of atoms
Dislocation loop

## Slide 27: Radiation  dislocation loops
Iron, ion-irradiated to 2.5 dpa at 300°C

## Slide 28: Dislocation loops in Fe irradiated at 500°C
Dose: 3x1018 ions m-2, Dose: 1x1019 ions m-2
UHP-Fe irradiated at 500oC with 150 keV Fe+ ions
loops are of <100> type.
loops are of interstitial type
200nm
g = 110

## Slide 29: Radiation Damage as it happens…
IVEM – Argonne NL
MIAMI – U. Huddersfield

## Slide 30: Damage accumulation; Fe, 300°C , high dose

## Slide 31: Loop density vs dose: W-5%Re
0
Unit: 1013W+/cm2
g=200
~1015 loops/m2

## Slide 32: Loop density vs dose: W-5%Re
0
0.38
Unit: 1013W+/cm2
g=200
~1015 loops/m2

## Slide 33: Loop density vs dose: W-5%Re
0
0.38
1.0
Unit: 1013W+/cm2
g=200
~1015 loops/m2

## Slide 34: Loop density vs dose: W-5%Re
0
0.38
1.0
Unit: 1013W+/cm2
1.75
g=200
~1015 loops/m2

## Slide 35: Loop density vs dose: W-5%Re
0
0.38
1.0
Unit: 1013W+/cm2
1.75
3.25
g=200
~1015 loops/m2

## Slide 36: Loop density vs dose: W-5%Re
0
0.38
1.0
Unit: 1013W+/cm2
1.75
3.25
6.25
g=200
~1015 loops/m2

## Slide 37: Loop density vs dose: W-5%Re
0
0.38
1.0
Unit: 1013W+/cm2
1.75
3.25
6.25
10.0
g=200
~1015 loops/m2

## Slide 38
Self-ion irradiations of pure materials and FeCr alloys
- 100keV room temperature irradiations
1E15
1E16
1E17
1E18
1E19
1E12
1E13
1E14
1E15
1E16
Defect density (m-2)
Dose of 100 keV self-ions (ions m-2)
Iron-based metals (Body centred cubic metals in general?) are more resistant to radiation damage.
Fewer defects
Threshold dose
Cu
Ni
Fe
Fe5Cr
Fe8Cr
Fe11Cr

## Slide 39: Effects of radiation damage on materials
Sputtering
Stored energy
  “Wigner energy” release
Point defect accumulation
  Swelling, dislocation loops, nano-voids
  Changes in thermal & electrical conductivity
Enhanced diffusion
  Radiation-enhanced creep
  Faster kinetics of phase transitions
  Radiation-enhanced grain-boundary segregation
Gas from transmutation
  Bubbles, swelling (with 2)
Soluble and insoluble transmutation products
  Hardening, precipitation
Knock-on randomisation of structure
Non-equilibrium microstructures? (related to 3. 6)
Hardening (from 2, 4, 5)
Embrittlement (from 7, 3c, 4)
Radiation-enhanced corrosion (related to 3a, maybe 5)

## Slide 40: Radiation-induced swelling
G. Was, Michigan
Type 316 stainless steel:
Fe 16-18%Cr, 10-14%Ni, 2%Mo, <0.08%C

## Slide 41: Radiation-induced swelling
G. Was, Michigan
(%)

## Slide 42: Radiation-induced grain boundary segregation
G. Was, Michigan
Type 304L stainless steel: Fe 18-20%Cr, 8-12%Ni, <0.03%C

## Slide 43: Radiation-induced dislocation loops: effects on mechanical properties
“Strain localisation”

## Slide 44: Stress-strain curves: Iron alloys
Strain (%)
Stress (MPa)
T91 steel
Eurofer 97
Fe Cr alloys
n-irrad up to 1.5 dpa
Tirr =300°C, TTEST=27°C
T91: Fe - 8.3%Cr – 0.4%Mn - 1%Mo - 0.2%V - 0.08% Nb - 0.1%C
Eurofer 97: Fe - 8.9%Cr – 1%W - 0.2%V - 0.14%Ta - 0.12%C

## Slide 45: Stress-strain curves: Iron alloys
Strain (%)
Stress (MPa)
Eurofer 97
n-irrad up to 1.5 dpa
Tirr =300°C, TTEST=27°C
Plastic instability after yield

## Slide 46: Dose Rates
Radiation Source | Dose Rate (dpa / s) in Iron-based Alloys
Fission Reactor Pressure Vessels (RPV) | ~ 10-12 – 10-11
Rotating Target Neutron Source (RNTS-II) | ~ 10-10
Fast Flux Test Facility (FFTF)/DEMO Fusion Reactor | ~ 10-8 – 10-6
Ion Implantation – Low Dose Rate | 3 x 10-5
Ion Implantation – High Dose Rate | 6 x 10-4
HVEM Irradiation | ~ 10-3
C. D..Hardie 2013

## Slide 47: Nanoindentation hardness: Fe 5%Cr 0.6dpa
High Dose Rate
Un-irradiated
Low Dose Rate
Indenter

## Slide 48: Nanoindentation hardness: Fe 5%Cr 0.6dpa
High Dose Rate
Un-irradiated
Low Dose Rate
Indenter

## Slide 49: TEM of ion irradiation damage Fe 5%Cr 300ºC
110
110
100nm
Low dose rate
High dose rate
S. Xu 2012

## Slide 50: APT of ion irradiation damage Fe 5%Cr 400ºC
Low dose rate
High dose rate
APT data for the Fe 5%Cr alloy irradiated at 400 Cwith the low dose rate (a)and high dose rate.(b)The figureincludes an atom map showing Fe atoms and a0.5 at.%CrN isoconcentration surface (i)and proximity histograms showing the variation in composition from the centre of enrichment outwards into the matrix (ii).Centre of enrichment is definedas the region of highest CrN concentration.
C.D. Hardie et al. J Nuclear Materials 439 (2013) 33–40

## Slide 51: Micro-mechanical Testing
Chris Hardie, D.Phil Thesis, Oxford, 2013
0 dpa
6.8 dpa
Fe-12%Cr
Ion – irradiated
Fe+
0.5MeV & 2MeV
320°C

## Slide 52: Micro-mechanical Testing
Chris Hardie, D.Phil Thesis, Oxford, 2013
0.1mm
1mm
0 dpa
6.8 dpa
Fe-12%Cr
Ion – irradiated
Fe+
0.5MeV & 2MeV
320°C
Fe-6%Cr
neutron – irradiated
288°C
1.7 dpa

## Slide 53
Neutron-irradiated
Unirradiated
Ion- irradiated
Micromechanical testing Fe-6%Cr – Size effects
6.0
4.0
2.0
0.0
0.0
2.0
4.0
6.0
8.0
Yield Stress (GPa)
Beam depth (mm)
0.1mm

## Slide 54
Neutron-irradiated
Unirradiated
Ion- irradiated
Micromechanical testing Fe-6%Cr – Size effects
6.0
4.0
2.0
0.0
0.0
2.0
4.0
6.0
8.0
Yield Stress (GPa)
Beam depth (mm)
0.1mm

## Slide 55
Neutron-irradiated
Unirradiated
Ion- irradiated
Micromechanical testing Fe-6%Cr – Size effects
6.0
4.0
2.0
0.0
0.0
2.0
4.0
6.0
8.0
Yield Stress (GPa)
Beam depth (mm)
0.1mm

## Slide 56
Neutron-irradiated
Unirradiated
Ion- irradiated
Micromechanical testing Fe-6%Cr – Size effects
6.0
4.0
2.0
0.0
0.0
2.0
4.0
6.0
8.0
Yield Stress (GPa)
Beam depth (mm)
0.1mm

## Slide 57: Protons ?

## Slide 58
SRIM : 2 MeV protons into Fe

## Slide 59: Proton irradiation for (micro) mechanics?
SRIM : 2 MeV protons into Fe
Could use specimens 10 – 12 mm thick – well beyond the size-dependent mechanics regime
25mm
0mm
25mm
0mm

## Slide 60: Proton irradiation for (micro) mechanics?
SRIM : 2 MeV protons into Fe
25mm
0mm
For 2MeV H+ into Fe:
  Total damage:
  ~1 x10-4 events / (Å - ion)
  ~1021 ions cm-2 for 1 dpa
  Depth ~ 15 mm

## Slide 61: Proton irradiation for (micro) mechanics?
SRIM : 2 MeV protons into Fe
25mm
0mm
For 2MeV H+ into Fe:
  Total damage:
  ~1 x10-4 events / (Å - ion)
  ~1021 ions cm-2 for 1 dpa
  Depth ~ 15 mm
5mm
0mm
For 2MeV Fe+ into Fe:
  Total damage:
  ~4 events / (Å - ion)
  ~2 x 1016 ions cm-2 for 1 dpa
  Depth ~ 1 mm

## Slide 62: Radiation damage in Materials
C.A. English (2011)