## Slide 1
ActiLab Closing Meeting
ActiLab Activities at INFN
Stefano Corradetti
and Alberto Andrighetto
SPES Target Group

## Slide 2: Outline
UCx synthesis (Task #1): 2013 activity
UCx thermal characterization (Task #2): 2014 activity

## Slide 3: UCx synthesis
New equipment (purchased in Jan ‘13)
- Reduce and homogenize the grain size of oxide and carbon source → selection and control of the precursors (as defined in ActiLab SC May 2012, strategy for UCX production at INFN)
- Vibratory micromill and sieves purchased at UNIPD lab (grain size down to few mm) to treat small quantities of precursors

## Slide 4: UCx synthesis
‘Original’ UO2 batch: ~ 20 g
Chart: First milling (60') of original UO2
| > 100 μm | 71-100 μm | 40-71 μm | 20-40 μm | 10-20 μm
First milling | 0.63 | 0.78 | 1.5 | 0.86 | 0.76
First milling → ~ 5 g of UO2
Milling and sieving → UO2 particle size control

## Slide 5: UCx synthesis
Final particle size population
Chart: Final UO2 particle size selection
| > 100 μm | 71-100 μm | 40-71 μm | 20-40 μm | 10-20 μm
Milling of fraction > 40 | 0 | 0 | 5.76 | 6.1 | 5.09
Sieves below 10 mm mesh also available (Nylon mesh) and tested
Small amount of powder ground to < 10 mm size in reasonable time
< 20 mm ("10-20 mm") was selected as a precursor size to produce 10 pellets, sent to IPNO for off-line characterization and irradiation tests
Subsequent millings to produce enough UO2 for 10 UCx pellets

## Slide 6: UCx synthesis
% wt. UO2 | % wt. C | % wt. binder | Weight (g) | Diameter (mm) | Thickness (mm) | Density (g/cm³)
77.60 | 20.30 | 2.10 | 0.57 | 13.01 | 0.95 | 4.50
“Green” UO2 + C pellets
Weight (g) | Diameter (mm) | Thickness (mm) | Density (g/cm³) | Total porosity (%) | Weight loss (%) | Theoretical weight loss (%)
0.47 | 12.66 | 0.86 | 4.33 Similar to SPES standard | 58.90 | 17.57 | 16.90
UC2 + 2C pellets after carburization (UO2+6C→UC2+2C+2CO)
Thermal treatment:
2°C/min up to 1250°C (binder decomposition occurs)
8 hours at 1250 °C, then 2 °C/min up to 1350 °C (carburization)
8 hours at 1350 °C, then 1.5 °C/min up to 1730°C (carburization)
6 hours at 1730 °C
Expected composition of the samples: UC2, graphite and a minor amount of UC
Pellets production → 10 UCx discs

## Slide 7: UCx synthesis
Pellets production → 10 UCx discs
H2O, binder decomposition
CO, carburization

## Slide 8: UCx synthesis
Pellets production → 10 UCx discs
Sample before treatment
Disc | Weight (mg) | r (g/cm3) | Thickness (mm)
1 | 466 | 4.31 | 0.86
2 | 476 | 4.36 | 0.87
3 | 467 | 4.37 | 0.86
4 | 466 | 4.31 | 0.86
5 | 475 | 4.31 | 0.87
6 | 473 | 4.38 | 0.86
7 | 476 | 4.29 | 0.88
8 | 473 | 4.42 | 0.85
9 | 457 | 4.37 | 0.83
10 | 474 | 4.22 | 0.89
Samples after treatment

## Slide 9: UCx synthesis
Shipping of the pellets to IPNO
Authorization from IPNO to send the samples took 3 – 4 months
2) Shipping to Orsay (September 2013) took less than
two weeks (Cost: ~ 1k€)
INFN (UNIPD) →→→→ IPNO OK

## Slide 10: UCx characterization
Original setup – INFN/LNL
Newly developed setup (Padova)
M. Manzolaro et al., Rev. Sci. Instr. 84 (2013) 054902.
Allowing measurements for samples of smaller sizes (down to  ̴30 mm)
Creation of a thermal gradient on the tested disc by means of irradiation from a heated graphite crucible
Thermal conductivity

## Slide 11: UCx characterization
Thermal conductivity
Creation of thermal gradients in the disc caused by irradiation from the crucible
A low temperature pyrometer (range 600 ÷ 1400 °C) is used to monitor temperature in the disc center and periphery (repeated cycles of heating)
Inverse analysis → k (T) (tipically in 600 ÷ 1200 °C range)
M. Manzolaro, S. Corradetti, A. Andrighetto, L. Ferrari, Rev. Sci. Instrum. 84, 054902 (2013)

## Slide 12: UCx characterization
Thermal conductivity
FEM model of the chamber – crucible – disc system
DT between center and peryphery: comparison between numerical and experimental
k (T) is obtained minimizing the differences between the DTs
k (T) = C0+C1*T (average T)

## Slide 13: UCx characterization
Thermal conductivity
UO2 + C + binder, UO2 < 20 mm → same material sent to IPNO (only this was tested)
UO2 + C + binder, 20 mm < UO2 < 40 mm
UO2 + C + binder, 40 mm < UO2 < 71 mm
Treatment
Mat. | Weight (g) | r (g/cm3) | Thickness (mm)
1 | 3.51 | 3.87 | 1.38
2 | 3.57 | 3.85 | 1.40
3 | 3.58 | 3.48 | 1.54
f 30 mm samples produced

## Slide 14: UCx characterization
Thermal conductivity
Temperature [°C] measurements
vs. numerical data
Inverse analysis gives
Thermal conductivity [W/m°C]
Calibration of the system with a graphite disc
LNL Manzolaro 2013
UNIPD Corradetti 2014

## Slide 15: UCx characterization
Thermal conductivity
Measurements on UCx discs
Temperature [°C] measurements
vs. numerical data
Inverse analysis gives
Thermal conductivity [W/m°C]

## Slide 16: UCx characterization
Emissivity
Measurement of the thermal emissivity of a sample placed on a heated
graphite crucible by means of a dual-frequency pyrometer
Pyrometer (Kodial viewport in the vacuum chamber)

## Slide 17: UCx characterization
Emissivity
Pellets shipment from IPNO
pellet | n° | mass (g) | main phase | mass of U (g) | diameter (mm) | thickness (mm)
GATCHINA | 299 | 1.80 | UC | 1.71 | 13.17 | 1.03
PARRNe894 | 3 | 0.82 | UC2 | 0.74 | 12.95 | 1.92
OXA | 1 of the 7 | 0.61 | UC | 0.70 | 7.40 | 1.87
PARRNeBP | 7 | 0.87 | UC2 | 0.79 | 12.63 | 1.53
COMP30 | 4 | 0.68 | UC2 | 0.62 | 8.28 | 2.51
TOTAL |  | 4.78 |  | 4.57 |  | 
    Selected samples from the batch tested in March 2013 at IPNO (unirradiated)
    Authorization to send requested in summer 2013
    Samples received at UNIPD in July 2014
    IPNO →→→→ INFN (UNIPD) ~OK

## Slide 18: UCx characterization
Emissivity
SPES UCX (f 30 mm) with <20 mm UO2
IPNO UCX by U3O8 + C
Designed to obtain UC, but result is UC2 + minor am. C
HD UC

## Slide 19: UCx characterization
Emissivity
Instability in emissivity can be related to reaction with the graphite crucible (both UC-based samples, Gatchina and OXA, were found sticked on the crucible)?

## Slide 20: UCx characterization
Emissivity
UC-based samples
De Coninck, 1975

## Slide 21: UCx characterization
Emissivity
pure UC2-based sample
De Coninck, 1976

## Slide 22: UCx characterization
Emissivity
UCx-based samples
Biasetto 2010 - UCx
Biasetto 2008 - graphite

## Slide 23: UCx characterization
Conclusions
Consistency of the thermal conductivity setup with the previous one verified (graphite test samples)
Among the first results of ISOL-like UCx materials thermal conductivity obtained
Numerical model still to be improved (non-linear behavior for high temperatures, reduction of differences between experimental and numerical leading to narrower confidence bands)
Temperature spectrum to be widened to explore more realistic operating conditions
Emissivity correlation to structure and phases → useful in defining parameters for thermo-electrical simulations

## Slide 24
Thank you for your attention