## Slide 1
Bye Bye ActILab
The CERN ActILab Highlights
Alexander Gottberg (CERN)

## Slide 2: Nominal Density Uranium Carbide (Task 4)
Release fractions from Rabbit samples, ALTO 2013
[1] V. N. Panteleev, et al., Eur. Phys. J. A 42,
495-501 (2009)
[2] V. N. Panteleev, EMIS-15, June 25, (2007)

## Slide 3: Nominal Density Uranium Carbide (Task 4)
Production yield ratio HD : LD in first pellet
Production yield ratio HD : LD in last pellet
fission rate 12.1 g·cm-3 [cm-3·µA-1]
106
1012
105
1011
fission rate 3.5 g·cm-3 [cm-3·µA-1]

## Slide 4: Nominal Density Uranium Carbide (Task 2 + 4)
Li
Na
K
Rb
Cs
Fr

## Slide 5: Nominal Density Uranium Carbide (Task 2 + 4)
Porosity from picnometry in IPNO (tbc): less than 1%
Geometrical porosity: 0%
But microscopic morphology more complex than anticipated

## Slide 6
Characterization of UCX
Task 2

## Slide 7: Oxidation on Microscopic Level
5 µm
U oxide
UC2
5 µm
1.7 µm
K. Hallam et al., University of Bristol, UK
As prepared (stored under argon)
Stored in air
Oxidation process without thermodynamic activation is slow (in conventional UCx) and follows a surface to bulk mode.

## Slide 8: Material Investigation at PSI/SLS (non irradiated)
as prepared (≤1850◦C)
as operated (2100◦C for 5 days)
10µm
2µm
200nm
2µm

## Slide 9: EXAFS for indirect identification of uranium valence at PSI/SLS
Valence-induced shift of adsorption edge is very small and hart to resolve
Change in lattice are causing major changes in EXAFS oscillatory features
UC (Fm-3m) as NaCl
UC2 (I4/mmm) as MoSi2

## Slide 10: Material Investigation at PSI/SLS (non irradiated)
µ-spot X-ray fluorescence mapping
Uranium
Gallium
SEM Uranium
20µm
0
1
5
2
4
3
8
6
7
UC2 reflex 1
µ-spot X-ray diffraction
UC2 reflex 3

## Slide 11: Why is UCx such successful target material?
α-UC2(002)
UC (200)
10 µm

## Slide 12: UCx Diffusion Study
For pure diffusion and short half life:
R. Kirchner, NIM B, B70, 186-199 (1992)
→ r2 / D,
diffusion constant D(T) from initial particle size measurements: D(2300 K) = 6· 10-11 cm2/s
2 µm

## Slide 13
Post-Irradiation Studies
Task 3

## Slide 14: Irradiated UCx Target Unit 466
      Irradiation in October + November 2011 on both front ends
      total of 8.8·1018 protons of 1.4 GeV
      Road transport in January 2013 from CERN to Paul Scherrer Institute (270 km)
      4 mSv/h on contact with parcel

## Slide 15: Dismantling UCx Target Unit 466
      Opening target vessel in hot cell chain in air (6 mSv/h on contact with Al beam window)
      Extraction of tantalum container (19 mSv/h on contact with Ta proton beam window)
      Sealing of ion source and mass marker outlet with epoxy glue to prevent oxidation of carbide material

## Slide 16: Opening Ta Container of UCx Target Unit 466
      Transfer of Ta container with UCX into inert-gas hot cell
      Cutting of sealed container
      Extraction of UCx for further investigations (500 µSv/h on contact with single pellet)

## Slide 17: UCx Post-Irradiation Studies at PSI
Post-irradiation analysis:
2µm
before irradiation
after irradiation
Pellets appear macroscopically unchanged
Microscopic evolution of pore distribution and grain size under irradiation observed
Synchrotron data only partially analyzed

## Slide 18: UCx Post-Irradiation Studies

## Slide 19: Electron Probe Micro Analysis at PSI
Preparation (polishing) of samples in nitrogen atmosphere
2µm
Extensive EPMA data set still under analysis
Fission product concentration below detection limit
Confirmation of zones with varying carbon concentration causing UC2-UC phase competition
Non-irradiated reference
Proton beam entrance
From container center
Proton beam exit
Uranium
Carbon
Chlorine

## Slide 20
Material Synthesis
Task 1

## Slide 21
two orders of magnitude
Composing a Recipe for Nano-Grained UO2
Lanthanum Hydroxide Nanopowder
Ultrasound-Dispersed Multi-Walled Carbon Nanotubes
Synthesis of de-novo designed uranium carbide matrixes:
Different microstructures, densities, grain sizes, crystal structures tested → tailor-made matrix:
Suspension grinding of UO2 powder to 160 nm average particle size
Wet-mixing with multi-walled carbon nanotubes
Ultrasound drying of mixture and pressing to 1.6 g/cm3 pellets
Fast reactive sintering to mixed uranium carbide in carbon nanotube matrix
2 µm
500 nm
2 µm
200 µm
LaC2-MWCNT Nano Composite (After Carbo-Thermal Reduction)
Microstructure investigations of UC2-MWCNT nano composite currently in preparation
After 10 days at 1900°C
After 10 days at 1900°C

## Slide 22: Some few Material Characteristics
 | ISOLDE conventional |  |  |  | 2014 Nano |  |  |  | UC HD
 | graphite | UO2 | UO2 + 6C pellet | UC2 + 2C pellet | graphite CNT | UO2 | UO2 + 5C pellet | UC + 2C pellet | UC pellet
particle size [µm] | 28 | 16 |  |  | 0.01 x 10 | 0.21 |  |  | 
SSA [m2/g] | 3.6 | 4.9 | 5.2 | 0.1 | 287 | 16 | 30 | 221 | 2.20
diameter [mm] |  |  | 14 | 12.3 |  |  | 15 | 14.1 | 13.2
thickness [mm] |  |  | 1.6 | 1.45 |  |  | 1.04 |  | 1.00
density [g/cm3] |  |  | 4.50 | 3.67 |  |  | 1.89 | 1.95* | 13.20
reduced U fraction |  |  |  | 0.999 |  |  |  | ≈0.95* | 1.000
UC2 phase fraction |  |  |  | 0.295 |  |  |  | 0.149* | 0.941
C phase fraction |  |  | 0.309 | 0.147 |  |  | 0.190 | 0.082* | 0.059
UO2 phase fraction |  |  | 0.222 | 0.000 |  |  | 0.136 | 0.009* | 0.000
porosity |  |  | 0.469 | 0.558 |  |  | 0.674 | 0.760* | 0.000
total target mass [g] |  |  | 110 | 94 |  |  | 51.49 | 39.63 | 361.8
 |  |  |  | 100.00% |  |  |  | 42% | 414.07%
UO2 + 6(5)C pellets
UC2 + 2C pellets
* Property needs to be confirmed

## Slide 23
Online Tests at ISOLDE
Task 4
unit #498 on HRS in 2012 – difficult, but 11Be and 30Na yield evolution studied
unit #525 on GPS in 2014 – tests successful

## Slide 24: ENSAR-ActILab: Nano Uranium Carbide at ISOLDE
Chart: yield [µC-1]
| 8Li (#466 UC-Re) | 9Li (SC) | 25Na | 26Na (SC) | 30Na | 46K (SC) | 50K | 50Ca | 68Cu (highest DB entry) | 68mCu (highest DB entry) | 76Ga (highest DB entry) | 81Ga (highest DB entry) | 81Rb | 88Rb (#493 UC-Ta) | 93Rb (SC) | 96Rb (SC) | 132In | 142Cs (#477 UC-W) | 139Cs (#477 UC-W) | 207Fr (SC)
ISOLDE Conventional UCx | 4100000 | 3900000 | 290000000 | 600000000 | 51000 | 8900000 | 50000 | 24000 | 80000000 | 300000000 | 10000000 | 200000 | 170000 | 400000000 | 130000000 | 14000000 | 8000 | 400000000 | 1500000000 | 2300000
ActILab nano UCx | 28000000 | 19000000 | 2800000000 | 920000000 | 140000 | 390000000 | 86000 | 68000 | 960000000 | 340000000 | 29000000 | 1100000 | 22000000 | 8000000000 | 260000000 | 15000000 | 17000 | 1100000000 | 2100000000 | 85000000

## Slide 25: Nano Uranium Carbide Online at ISOLDE
isotope | half life | yield [μC-1]
8Li1 | 840 ms | 2.8·107
9Li1 | 178 ms | 1.9·107
25Na1,5 | 59.6 s | 2.8·109
26Na1,5 | 1.07 s | 9.2·108
30Na2 | 48 ms | 1.4·105
46K1,4 | 115 s | 3.9·108
50K1,2,4 | 472 ms | 8.6·104
50Ca2 | 13.9 s | 6.8·104
41Sc1,5 | 596 ms | 1.1·105
68Cu2,7 | 30 s | 9.6·108
68mCu1,7 | 3.8 min | 3.4·108
76Ga2 | 32.6 s | 2.9·107
81Ga2 | 1.22 s | 1.1·106
81mRb2 | 30.3 min | 2.2·107
88Rb1,4 | 17.8 min | 8.0·109
93Rb1,4 | 5.84 s | 2.6·108
96Rb1,5 | 199 ms | 1.5·107
114Ag2,8 | 4.5 s | 1.4·102
116mAg2,8 | 8.2 s | 9.0·102
117Ag2,8 | 72.8 s | 1.6·103
118Ag2,8 | 3.7 s | 6.2·104
120Ag2,8 | 1.17 s | 2.3·104
122Ag2,8 | 0.52 s | ≤1.3·103
132In1,2 | 0.20 s | 1.7·104
139Cs1,4 | 9.3 min | 2.6·109
142Cs1 | 1.68 s | 1.1·109
148Cs1,4 | 158 ms | 1.7·104
207Fr3 | 0.148 s | 8.5·107
230Fr1,4 | 0.596 s | 7.1·105
A = 2256 |  | 1.1·109
1assessed through β detection with release curve integration
2assessed through γ detection
3assessed with scintillator, assuming 50% α detection efficiency
4beam composition assessed through γ spectroscopy
5beam composition assessed through half-life measurement
6faraday cup measurement
7resonant laser ionized
8extracted in its 2+ state
9assuming 100% branching into investigated γ transition

## Slide 26: Nano Uranium Carbide Online at ISOLDE
New material:
  Seems increases isotope yield of most investigated elements (Li, Na, K, Ca, Cu, Ga, Rb, In, Ra, Fr)
  reduced ageing effects (reduction of yield over time)
  reduces actinide waste by 60%
  chemically unstable
  Resource-intense to synthesize (additional development needed)
  Rich in synthesis-induced contaminations

## Slide 27: What has ActILab brought us? (my perspective)
  A healthy collaboration between several European institutes leading to results that where out of reach before
  Paving the way for easier access to infrastructure between the labs
  Blowing breaches into Europe’s shipment channels for actinide materials
  Extension of collaborative effort into other materials (Julien Guillot)
  Deep insights to conventional UCX properties, dynamics, ageing mechanisms
  At least one new and promising target material
  LOTS OF FUN