## Slide 1
Thin films and surfaces treatments in accelerator technology
M.Taborelli
On behalf of TE-VSC
9/4/2015
Thin films for accelerating Nb cavities
Thin films for pumping
Thin films against electron cloud
Cleaning for UHV
Plating for accelerator applications
Electropolishing

## Slide 2
Superconducting niobium RF accelerating cavities
Nb (TC=8.5K) with the required purity is very expensive
1-2 µm Nb thin film are sufficient (skin depth) for 5-7 MV/m fields at 100MHz-GHz frequency range
successfully developed at CERN in the 80’s, recent development for HIE-ISOLDE project
CERN, LEP 352MHz
CERN, LEP
CERN SPL
E
beam

## Slide 3
Diode sputtering, Nb (1-5 µm).
Purity (vacuum!) and substrate preparation (chemical polishing) are crucial to avoid field emission and related energy dissipation
High T bake out of the cavity (600°C)
HIE Isolde quarter wave accelerating cavities:
Nb thin film coating
Cu substrate
Nb 14 layers
FIB cross section, courtesy of EPFL
2 μm
beam
Coating in 14 steps (5 days)

## Slide 4
Why?...
LEP dipole vacuum chamber
NEG
coating
Thin film of Non-Evaporable-Getter as vacuum pump
In accelerators at ultra-high-vacuum (<10-10 mbar) the trend is to bring the pump closer to the outgassing source and distribute the pumping speed evenly.
 transform the entire vacuum chamber in a pump by coating it with a getter thin film: ~2μm of TiZrV deposited by DC magnetron; activated with a standard vacuum bake-out at 180°C-230°C (24h), operates at RT
Pump space hindrance and conductance vs pressure profile!
Pumps (chemisorption) H2, CO, CO2, …..
Does not pump CHx and noble gases
Characterised by XRD, EDX, SEM, XPS…
pump
pump
pump
pump

## Slide 5
Activation process: Monitoring by surface analysis (XPS)
Heating stepwise for 1h at each T
Surface Oxygen decrease
Diffusion of O into the bulk
Reduction of the surface oxides of all the metals: the surface is metallic and reactive
Ti
Zr
V
ox
ox
ox
met
met
met

## Slide 6
CAPE09 Cambridge M.Taborelli CERN
Coating plant for vacuum chambers up to 7 m length
7 km of LHC

## Slide 7
Electron cloud and SEY
+
+
+
+
Proton bunch (charge +)
Electron (charge -)
 Perturbation of the beam (emittance growth), thermal load on cryogenics, noise on beam instrumentation; the problem is more important for high beam currents (beam potential) and short bunch spacing
To reduce the effect one must reduce the secondary electron yield (SEY) of the walls or attract the generated electrons by other means
Gas molecule

## Slide 8
The possible solution : carbon a-C coatings
-Carbon (graphitic) coating on copper deposited by magnetron sputtering
-SEY does not change for thicknesses above 50 nm
-development started in 2008 for an upgrade of SPS
a-C(Ne9)
Dose below
10-6 Clb/mm2
as received

## Slide 9
Cathode:
graphite targets
(cells)
Cathode in the SPS MBB dipole
LIU-SPS: Carbon coating of the SPS vacuum chambers
`
Project of coating of the Super Proton Synchrotron dipoles with carbon to mitigate electron cloud (744 dipoles x 6.5 m each, 18 t)
hollow cathode coating (cannot apply axial B-field for magnetron in the yokes)
successful on short section, tested with beam in SPS (section ~200 m)
development ongoing to do the coating in the tunnel in 2018
6.5 m
6.5 meter

## Slide 10
Carbon coating of triplet magnets of LHC in situ during LS2
ARC types, ≥Q7 (c.bore inner diam. 50 mm)
LSS types, Q1–Q6 (cold bore inner diameters 50, 53, 63, 69 and 74 mm)
In order to cope with the thermal load on cryogenics provoked by e-cloud
Close to interaction points
Coating 35 m of beamscreen without dismounting the cryogenic magnets
35 m

## Slide 11
Stainless steel 316LN
Cleaning UHV components and monitoring cleanliness :
XPS
Wavenumber [cm-1]
CH3 asymmetric deform. of Si-CH3
CH3 symmetric deform. of Si-CH3
Si-O-Si stretching
Si-C stretching and CH3 rocking
CH stretching of CH3
Transmittance [%]
S.Ilie, C.Petitjean, C.Dias-Soares
FTIR
Through elution with C6H14
Precision cleaning is important to reduce outgassing and achieve UHV (standard up to 7m length)

## Slide 12
Plug-in Modules with RF Fingers
RF bridge (fingers) to interconnect superconducting magnets (~ 1 700 PIM)
Au/CuBe and Rh/Cu plating: different metals to avoid cold welding under vacuum and soft-on-hard contact to have sufficiently low resistivity (< 0.1 mOhm contact resistance)
RF bellows
Copper transition tube
Upstream flange
Downstream flange
Plug-in module transition tube
RF-contact Gold coating 5 m
RF-contact strips
coating 5 m
Indium brazed
RF-contact strips
coating 5 m
Indium brazed
RF-contact transition flange
Rhodium coating 3 m
Screw & Spring washer
Screw & Spring washer
Room temperature position
Working position at cryogenic temperature
Courtesy R. Veness
cooling
Au
Rh

## Slide 13
Electrolytic deposition: on stainless steel, copper and aluminum
Copper electroplating
Cover of DTL LINAC 4
Rhodium electroplating
RF transition LHCVSR
Gold electroplating
LINAC3 test chamber
Silver electroplating
RF fingers TDI shield
Ag plating on Al stripline contact AD
Cu plating on DTL tank of Linac 4

## Slide 14
Chart: J profile - β-1-SPL - optimised
Bulk Nb superconducting cavities: Optimization of the Electropolishing
5-cell cavity
Simulation with smooth electrode (red) and optimized electrode (blue) to get more uniform current and polishing
Electrode and current density map
COMSOL
software

## Slide 15
Ongoing projects and R&D interests
Carbon coating «in situ» (hollow cathode, RF magnetron, PLD…) X
SC RF cavities: coating by HIPIMS, new materials as Nb3Sn… X, X
Simulations of plasma for coating systems X
flexible insulating coatings X
Treatments or coatings to lower the SEY of surfaces (metals and insulators) X,X
NEGs with lower activation temperature than TiZrV X
Coatings as permeation barriers for high transparency vacuum chambers X,X
Methods to produce thin films of refractory metals in small diameter tubes (< 10 mm), as electrochemical means… X,X
Novel cleaning techniques for UHV applications X
- ……..

## Slide 16
THANK YOU!

## Slide 17
17
Wet surface treatments: Cu plating of DTL tank of LINAC4
Final assembly with the electrodes for the accelerator
Difficult to obtain uniform plating
and plating in the ports

## Slide 18
Range of composition of TiZrV thin films :
low activation T
(EDX composition)
Strong correlation between composition, structure and activation T: fast diffusion at lower T is favoured in coatings with very small grains?
grain size below 5 nm
grain size
above 100nm
From X-ray diffraction
From surface analysis

## Slide 19
2kW, standard bakeout
4kW, standard bakeout
8kW, special bakeout, baseline recipe
8kW, special bakeout, baseline recipe
Final geometry
Preseries geometry
HIE Isolde quarter wave accelerating cavities:
Q factor performance

## Slide 20
Pumping action of TiZrV NEG:
The sticking probability is the ratio between sticking and impinging molecules. It shows the pumping efficiency
The sticking probability increases when the NEG is activated (all measurements made at the same T, after thermal activation)
Pumping speed [l s -1 cm-2]
Pumping speed [l s -1 cm-2]
Sticking probability
Sticking probability
150 200 250 300 350
2h heating temperature [C]
150 200 250 300 350
2h heating temperature [C]

## Slide 21
electron gun
Ip = Is + Ic
d = Ic / (Is + Ic)
Sample
Ip
Ic
A
Is
A
Ic
XPS
SEY
measurement
Measurement of SEY
Coatings

## Slide 22
XPS: comparison with graphite
The C1s peak is wider than that of freshly cleaved graphite: due to the oxygen on the surface (8-10% typical) and chemical shift of C-O bonds or due to the more disordered structure and different C-C bond species?
a-C(Ne)
HOPG
cleaved in air
C1s
Coatings

## Slide 23
Structure from Raman
Based on the ratios of D/G peaks
and G position:
the coatings are in the region
of high sp2 content
Graphite like/amorphous coating
..but, no clear correlation between SEY and the detailed position in the diagram (possibly because several effects are in competition)
A.Ferrari et al PRB65

## Slide 24
Effect of hydrogen
0 0.05 0.10 0.15 0.20 0.25 0.30 0.35
H2% in Ar gas
1.6
1.5
1.4
1.3
1.2
1.1
1.0
0.9
0.8
SEY
Effect of hydrogen content in the sputtering gas
Hydrogen is the most important residual gas in a baked vacuum system (outgassing), therefore a special care must be taken to have a «clean» coating system
Remark: it is very difficult to measure the H content in a carbon coating!