## Slide 1: goes to Industry
Magnet Components and Assemblies
2015-06-26
F. Savary

## Slide 2: Outline
Magnets for HiLumi LHC
New challenges
How can industry contribute to magnets for HL-LHC?
Examples of critical components
Summary

## Slide 3: Magnets in the framework of HiLumi-LHC
Present triplets
NC D1
SC D1
Corrector
Package
Q1
Q2a
Q2b
Q3
D2
Q4
CC

## Slide 4: The 11T Dipole Two-in-One for DS
Create space in the dispersion suppressor regions of LHC, i.e. a room temperature beam vacuum sector, to install additional collimators (TCLD), which are needed to cope with beam intensities that are larger than nominal, such as in the High Luminosity LHC (HL LHC)
Replace a standard MB by a pair of 11T dipoles (the 11T dipole is also called MBH)
Interconnect
Space for Collimator
11 T dipole cold mass
By-pass cryostat
15660 mm

## Slide 5: HiLumi LHC magnet zoo
Triplet QXF (LARP and CERN)
Separation dipole D1 (KEK)
Recombination dipole D2
(INFN design)
Q4 (CEA)
11 T dipole (CERN)
Sextupole (INFN)
Dodecapole (INFN)
Octupole (INFN)
Decapole (INFN)
Orbit corrector (CIEMAT)
Overall, about 150 magnets are needed
Skew quadrupole (INFN)

## Slide 6: Main HiLumi-LHC Magnet Features
 | Type | Material | Field/Gradient (T) / (T/m) | Aperture (mm) | Length (m) | Units (-)
Q1,Q3 Q2 | Single aperture | Nb3Sn | 11.4 / 132.6 | 150 | 2 x 4.2 2 x 7.2 | 40 (½ LARP, ½ CERN)
D1 | Single aperture | Nb-Ti | 6.5 | 150 | 6.3 | 6 (KEK)
D2 | Twin aperture | Nb-Ti | 4.5 | 105 | 7.8 | 6 (INFN)
Q4 | Two-in-one aperture | Nb-Ti | 6.0 / 115 | 90 | 4.2 | 6 (CEA)
DS 11T | Two-in-one aperture | Nb3Sn | 11 | 60 | 2x5.5 | 12 (32) (CERN)

## Slide 7: 11T Dipole – 3 phases
TODAY
Graph showing nominal upgrade parameters - 3000 fb-1 would be reached in 2036
1
2
3

## Slide 8: 11T Dipole – scope in numbers
 | Phase 1 – LS2, all RRP | Phase 2 – LS3 | Phase 3 – LS4
Models | MBHSM101 (done) MBHSP101 (done) MBHSP102 (done) In addition: 3 x 1-in-1 2 x 2-in-1 | PIT (new X-section): 4 x 1-in-1 2 x 2-in-1 RRP (new X-section): 2 x 1-in-1 1 x 2-in-1 | None Same design as for LS3
Prototypes | P1: MBH_P001 | P2: MBH_P002 [PIT] P3: MBH_P003 [RRP] | 
Series baseline | First of a kind 1 x (2 MBH + 1 BPC1) | 2 in IP2 + 2 in IP7 or 4 in IP7 tbc 4 x (2 MBH + 1 BPC) | To complete IP7 or in IP2 2 x (2 MBH + 1 BPC)
Series spares | - | - | 1 x (2 MBH + 1 BPC)
Option | - | - | IP1-IP5 Max. 8 x (2 MBH + 1 BPC)
BPC stands for By-Pass Cryostat

## Slide 9: Assembly Breakdown Structure (main elements)
Cryo-assembly
  Cryostat, main and by-pass
  Bus bars for by-pass cryostat
  Jacks (RT support, cryostat to ground)
  Cold mass assembly
    Coils
    Collared coils
    Active part, including bus bars
    Ancillaries (e.g. spool pieces 6-poles, N-line, protection diode…) and cold mass envelope (e.g. end covers)
  Cold feet
  Thermal shield
  Current leads for trim
Interconnects (with W-bellows)

## Slide 10: NEW challenges w.r.t. to Nb-Ti magnets - 1
Reaction treatment (48 h @ 210°C – 48 h @ 400°C – 50 h @ 640°C

## Slide 11: NEW challenges w.r.t. to Nb-Ti magnets - 2
Impregnation
Insulation system:
Mica C-shaped tape
Braided fiber glass
Impregnated with epoxy resin

## Slide 12: How can industry contribute to magnets for HL-LHC?
Item # | Description | Raw material | 2018 | Later | What is challenging
1 | Coil keys | AISI 316 L – DIN 1.4435 |  |  | Machining (accuracy & elasticity)
2 | End spacers | SLS – AISI 316 L – DIN 1.4435 |  |  | 3D-metrology, electrical insulation is needed
3 | Saddles | Impregnated glass fiber as per IEC/EN 61212-3-1 EP-GC22 |  |  | 5-axes machining, GC22, accuracy
4 | Removable pole | TA6V annealed (Ti6Al4V; 3.7165) |  |  | Accuracy & material
5 | Wedges – precision profiles | Aluminum oxide dispersion strengthened copper (ODS) |  |  | Accuracy, material ODS
6 | Quench heaters | Polyimide – St.Steel – Copper |  |  | Flexible Printed Circuits
7 | Collars | YUS-130S (High Mn Steel) |  |  | Fine blanking, accuracy
8 | Collaring keys | AISI 316 L – DIN 1.4435 |  |  | Accuracy
9 | Yoke laminations & inserts | Low carbon steel |  |  | Fine blanking, accuracy
10 | Heat exchanger tube | Oxygen Free Cu – UNS C10200 |  |  | Cu quality
11 | Bus bars – hollow bars | Oxygen Free Cu – UNS C10200 |  |  | Length, Cu quality
12 | Lyras | Oxygen Free Cu – UNS C10200 |  |  | Cu quality
13 | Shells | AISI 316 LN – DIN 1.4429 |  |  | Raw material, thickness, accuracy
14 | End covers | AISI 316 LN – DIN 1.4429 |  |  | Raw material, accuracy
Legend:
We are covered
We need more suppliers
We desperately need suppliers

## Slide 13: Coil keys – end spacers – saddles
Can be produced from STP files
Item 4: coil key, AISI 316 L
Item 5: Selective Laser Sintering (SLS) end spacer, AISI 316 L, with flex. legs
Item 6: Saddle, EP-GC22, base material woven glass cloth, matrix epoxy resin
After curing
After reaction
After impregnation

## Slide 14: Loading pole – ODS Wedge
Insulated cable
Filler Wedge
Loading plate
Inter-layer
Inner ground wrap
Outer ground wrap
Wedges, to be made of aluminum oxide dispersion strengthened copper, cold drawn in length of 2.6 m
a
b
c
d
e
f
Loading pole, to be made of titanium, 240 mm long

## Slide 15: Quench heaters
Basically a strip of stainless steel of 20 m running along the coil outer surface
A thin copper layer of 5 m (electrolytic deposition) lower the resistance of the strip in between 2 heating areas
The substrate is a 50 m polyimide film
The metallic circuit is encapsulated with a 37.5 μm to 50 μm thick polyimide film as cover layer with an adhesive coating
+
+
-
-
Heating areas
(stainless steel)
Non-heating areas
(copper plated stainless steel)
Polyimide film
(substrate)
Overall length: 5600 mm
Width: 160 to 300 mm

## Slide 16: Collars – collaring keys – yoke laminations
    3 mm thick high Mn steel
    0.2 > 400 MPa
Yoke laminations: 5.8 mm thick low carbon steel
Collars

## Slide 17: Shells – end covers, main parts of the He containment vessel
Material: AISI 316 LN, hot rolled plates formed in folding press
Thickness: 15 mm
Tight fit with yoke laminations, i.e. need to be precise
Leak tightness
Weldability
Material: AISI 316 LN
Powder metallurgy for the dished cover, or welded construction for the flat cover
Leak tightness
Weldability

## Slide 18: Summary
We are seeking for additional suppliers for magnet components
Components are not standard, specifications are demanding
  Materials (remember … will work between -271°C and +640°C for the coil components)
  (Very) tight tolerances in most cases
Limited quantities, but quality counts
Technology development may be needed, e.g. quench heaters
Finding the Higgs boson, and more, requires exploring the unexplored, going beyond its own limits
Challenging, however rewarding

## Slide 19
Thank you
for your attention