## Slide 1: RD50 Status Report – June 2015
Gianluigi Casse Michael Moll University of Liverpool, UK CERN, Geneva, Switzerland
LHCC – 3.June 2015, CERN
OUTLINE:
RD50 Collaboration
Scientific results
  Defect and Material Characterization
  Detector Characterization
  New Detector Structures
  Full Detector Systems
RD50 key results 2014/2015
RD50 Work Program 2015/2016
RD50 achievements
RD50

## Slide 2: Motivation and Challenge
LHC upgrade (and beyond…. FCC)
  upgrade of the LHC to the High Luminosity LHC (HL-LHC) after LS3 (~2024)
  expected integrated luminosity: 3000 fb-1 (x6 nominal)
[I. Dawson, P. S. Miyagawa, Sheffield University, Atlas Upgrade radiation background simulations]
Silicon detectors will be exposed to hadron fluences equivalent to more than 1016 n/cm2  detectors used now at LHC cannot operate after such irradiation
  RD50 mission: development and characterization of silicon sensors for HL-LHC and beyond, analyze and understand radiation damage in silicon detectors
Notes: HE: 16.5 TeV (CERN-ATS-2010-177)
Plot taken from Igor Mandic (Vienna 2013 presentation)

## Slide 3: The RD50 Collaboration
RD50: 49 institutes and 275 members
41 European and Asian institutes Belarus (Minsk), Belgium (Louvain), Czech Republic (Prague (3x)), Finland (Helsinki, Lappeenranta ), France (Paris, Orsay), Germany (Dortmund, Erfurt, Freiburg, Hamburg (2x), Karlsruhe, Munich(2x)), Italy (Bari, Florence, Perugia, Pisa, Torino), Lithuania (Vilnius), Netherlands (NIKHEF), Poland (Krakow, Warsaw(2x)), Romania (Bucharest (2x)), Russia (Moscow, St.Petersburg), Slovenia (Ljubljana), Spain (Barcelona(2x), Santander, Valencia), Switzerland (CERN, PSI), Ukraine (Kiev), United Kingdom (Glasgow, Liverpool)
6 North-American institutes Canada (Montreal), USA (BNL, Fermilab, New Mexico, Santa Cruz, Syracuse) 1 Middle East institute Israel (Tel Aviv) 1 Asian institute India (Delhi)
Detailed member list: http://cern.ch/rd50
No changes since last LHCC report in June 2014

## Slide 4: RD50 Organizational Structure
Co-Spokespersons Gianluigi Casse and Michael Moll (Liverpool University) (CERN PH-DT)
Defect / Material Characterization Mara Bruzzi (INFN & Uni Florence)
Detector Characterization Eckhart Fretwurst (Hamburg University)
Full Detector Systems Gregor Kramberger (Ljubljana University)
Characterization of microscopic properties of standard-, defect engineered and new materials pre- and post- irradiation
DLTS, TSC, ….
SIMS, SR, …
NIEL (calculations)
WODEAN: Workshop on Defect Analysis in Silicon Detectors (G.Lindstroem & M.Bruzzi)
Characterization of test structures (IV, CV, CCE, TCT,.)
Development and testing of defect engineered silicon devices
EPI, MCZ and other materials
NIEL (experimental)
Device modeling
Operational conditions
Common irradiations
Wafer procurement (M.Moll)
Device Simulations (V.Eremin)
3D detectors
Thin detectors
Cost effective solutions
Other new structures
Detectors with internal gain (avalanche detectors)
LGAD–Low Gain Avalance Det.
Slim Edges
HVCMOS
3D (R.Bates)
LGAD (V.Greco)
Slim Edges (V.Fadeyev)
LHC-like tests
Links to HEP
Links electronics R&D
Low rho strips
Sensor readout (Alibava)
Comparison: - pad-mini-full detectors - different producers
Radiation Damage in HEP detectors
Test beams (M.Bomben & G.Casse)
New Structures Giulio Pellegrini (CNM Barcelona)
Collaboration Board Chair & Deputy: G.Kramberger (Ljubljana) & J.Vaitkus (Vilnius), Conference committee: U.Parzefall (Freiburg) CERN contact: M.Moll (PH-DT), Secretary: V.Wedlake (PH-DT), Budget holder & GLIMOS: M.Glaser (PH-DT)

## Slide 5: Defect & Material Characterization

## Slide 6: Defect Characterization
Aim of defect studies:
  Identify defects responsible for Trapping, Leakage Current, Change of Neff , Change of E-Field
  Understand if this knowledge can be used to mitigate radiation damage (e.g. defect engineering)
  Deliver input for device simulations to predict detector performance under various conditions
Method: Defect Analysis performed with various tools inside RD50:
    C-DLTS (Capacitance Deep Level Transient Spectroscopy)
    TSC (Thermally Stimulated Currents)
    PITS (Photo Induced Transient Spectroscopy)
    FTIR (Fourier Transform Infrared Spectroscopy)
    EPR (Electron Paramagnetic Resonance)
    TCT (Transient Current Technique)
    CV/IV (Capacitance/Current-Voltage Measurement)
    PC, RL, I-DLTS, TEM,… and simulation
  RD50: several hundred samples irradiated with protons, neutrons, electrons and 60Co-g
  … significant progress on identifying defects responsible for sensor degradation over last 5 years!
Example: TSC measurement on defects produced by electron irradiation (1.5 to 27 MeV)
space charge trapping leakage current
[R.Radu et al, JAP 117, 164503, 2015]

## Slide 7: Summary on defects with strong impact on device performance after irradiation
Some identified defects
  Trapping: Indications that E205a and H152K are important (further work needed)
  Converging on consistent set of defects observed after p, p, n, g and e irradiation.
  Defect introduction rates are depending on particle type and particle energy and (for some) on material!
positive charge (higher introduction after proton irradiation than after neutron irradiation)
positive charge (higher introduction after proton than after neutron irradiation, oxygen dependent)
leakage current & neg. charge current after  irrad, V2O (?)
Reverse annealing (negative charge)
Boron: shallow dopant (negative charge)
Phosphorus: shallow dopant (positive charge)
Leakage current: V3
A table with levels and cross sections is given in the spare slides.

## Slide 8: Electron Damage: Defects & NIEL
Study on defects concentrations and damage after electron irradiation (1.5 to 27 MeV)
  Aim: Understand defect generation as function of electron energy (“silicon recoil energy scan”)
  What is the threshold for defect cluster formation in terms of PKA (Primary Knock-on Atom) energy?
    Electrons above ≈ 3 MeV produce “cluster damage”
    Reverse annealing (Neff) observed and matching the observed defect concentrations (H-defects)
[Effective NIEL: Inguimbert et al., IEEE TNS 57 (2010)1915]
[more details: R.Radu et al, JAP 117, 164503, 2015]
Example: 15 MeV e (2.2 x1014 e/cm2), STFZ
Observation on the NIEL (Non Ionizing Energy Loss) for electrons below 30 MeV
  The leakage current damage factor (alpha) does not scale with the “classical NIEL”
  We had to use the “effective NIEL” as calculated by Molecular Dynamics (MD) calculations to describe the leakage current and the introduction of cluster related defects correctly
..type inversion during annealing

## Slide 9: Device Characterization & Simulation

## Slide 10: TCAD simulations
Why do we need TCAD simulations ?
  Complexity of the problem
    Coupled differential equations (semiconductor equations)
    Impact of defects depending on local charge densities, field-strength, … (“feedback loop”)
    Complex device geometry and complex signal formation in segmented devices ….
    Interplay of surface and bulk damage
    Example: 3D sensors
Electric field distribution in 3D detector (Al & oxide layer transparent for clarity)
n+
p+
n+
LV
LV
LV
LV
V=0
Column depth =
bulk thickness
Np,n = 5e18 cm-3
Nbulk = 1.7e12 cm-3
Doping profiles
Example of 3D sensor: T.Peltola (HIP, Helsinki): CMS & RD50

## Slide 11: RD50 Simulation working group
Aim: Develop simulations (TCAD input parameters) allowing to simulate performance of irradiated silicon sensors and performance predictions under various conditions (sensor design and material, irradiation fluence and particle, annealing,…).
  Close collaboration with CMS Tracker sensor simulation working group (A.Messineo)
  Example of results (simulation vs. measurement):
    Comparison between simulation results (Synopsis TCAD) and CMS test beam data (strip sensors)
    Surface damage included via interface charge layer.
[ T.Peltola, Vertex 2015– June 2015]
Simulations of irradiated devices in TCAD are getting predictive power!

## Slide 12: Segmented Sensors with read-out at the n+ contact (n-in-p or n-in-n)

## Slide 13: Reminder: Segmented sensors: n+ vs. p+ readout
p-type strip sensors with n+ readout (brought forward by RD50)
  are now the sensor choice for ATLAS and CMS Tracker upgrades
  n+-electrode readout (“natural in p-type silicon”):
    favorable combination of weighting and electric field in heavily irradiated detector
    electron collection, multiplication at segmented electrode
  Situation after high level of irradiation:
holes
p+
readout
n+
electrons
n+
readout
p+
[G. Kramberger, Vertex 2012]
p+ readout
n+ readout
S. Wonsak, 25th RD50 Workshop Nov. 2014

## Slide 14: Thin p-type pixel sensors
Thin FZ p-type pixel sensors: 75 to 300 mm with 450 mm edge (MPI/CIS/VTT)
ATLAS FEI4, 25 MeV protons, 800 MeV protons, neutrons, data obtained with beta source
S. Terzo, 24th RD50 Workshop June 2014
B. Paschen, 25th RD50 Workshop Nov. 2014
Detectors irradiated up to 1.4 1016 neq/cm2
Sensor modules still functional (even if in homogeneously irradiated)
Detectors irradiated with 5 1015 neq/cm2
100mm thick sensors give more charge than 75mm thick sensors, both saturate with voltage
200 mm thick sensors give more charge than 300 mm thick sensors at moderate voltage
Beam tests show 97-99% hit efficiency (thickness tested 100 -200 μm, 500V)

## Slide 15: Slim Edges

## Slide 16: New structures
Charge Multiplication (Sensors with intrinsic gain)
HVCMOS (towards monolithic sensors)

## Slide 17: Reminder: Charge Multiplication
Ref: Diode: J.Lange et al, 16th RD50 Workshop, Barcelona
Strip: G. Casse et al., NIMA 624, 2010, Pages 401-404
3D: M.Koehler et al., 16thRD50 Workshop, Barcelona
Charge Multiplication observed and characterized after high levels of irradiation with different techniques and in several different types of devices
Diodes (Feq=1016 cm-2)
Leakage Current & Charge Collection
Strip sensors (Feq=5×1015 cm-2, 26 MeV p)
Charge Collection (Beta source, Alibava)
3D sensors (Feq=1-2×1015 cm-2)
Charge Collection (test beam)
140 mm thick device
300 mm thick device
Questions:
Can we simulate and predict charge multiplication ?
Can we better exploit charge multiplication?

## Slide 18: Low Gain Avalanche Detectors (LGAD)
Diodes with implemented multiplication layer (deep p+ implant)
  APD concept [ n++-p+-p-p+ structure] with JET (Junction Edge Termination)
  Gain of approx. 10-20 before irradiation : linear mode : spectra are Landau spectra (90Sr)
Gain reduces with irradiation
  Dropping to about 1.5 after 2e15 n/cm2
    Why? Boron removal in p-type layer?
    Soon: Test of Gallium implants
  Charge (Sr-90) Multiplication versus Current Multiplication (Sr-90)
Further work ongoing (strip, pixel, …)
Test of timing capabilities (thin sensors)
  “Ultrafast sensors project”
[G.Kramberger, 22nd RD50 Workshop, Albuquerque, June 2013]
N++
P+
N
P
Simulation of E-Field [V/cm]
[G.Pellegrini, 9th Hiroshima, 9/2013]
[G.Kramberger, RD50, June 2013]

## Slide 19: HVCMOS & monolithic devices
RD50 started to work on HVCMOS device characterization in 2014
  close collaboration with ATLAS HVCMOS group
  RD50 focus on characterizing radiation damage.
Typical HVCMOS device
  Depleted active pixel detectors implemented in CMOS process
  Sensor element is deep n-well in (usually) low resistivity (~10 Ωcm) p-type substrate
  Depletion with 60 V ~ 10 μm → charge collection via drift of ~1000 electrons
  Pixel and strip detectors possible
Edge-TCT measurements
HVCMOSv3
Edge-TCT
laser light
scan in y
fast readout amplifier
Drift and Diffusion component visible
M. Fernandez, 25th RD50 Workshop, Nov. 2014

## Slide 20: HVCMOS
Several HVCMOS devices tested after neutron irradiation up to 2x1016cm-2
  Example: HVCMOSv3; investigating 100 mm test structure
  Edge-TCT measurements
Signal: 3ns integration ; integration: 3-25ns
Total collected charge in 25ns
M. Fernandez and C.Weisser, 25th RD50 Workshop, Nov. 2014
Drift component t<3ns contributing before and after irradiation
Diffusion component 3ns < t <25ns contributing before and after irradiation
  For >80V the 1015 cm-2 irradiated sample gives more charge than non irradiated
  After 2x1016 neq/cm2 still ≈50% CCE !

## Slide 21: TPA – Two Photon Absorption
Investigation on a new technique for sensor characterization (TPA – TCT)
  Deposition of charge at specific position in detector
  Laser: l  1300 nm; P  50-100 pJ; DT  240 fs
  Proof of principle achieved:
Diode
Displacement
80 x nindex_Si  280 um
Two Photon absorption:
[I.Vila, 25th RD50 Workshop, CERN, November 2014]

## Slide 22: Workplan for 2015/2016 (1/2)
Defect and Material Characterization (Convener: M.Bruzzi, INFN and University of Florence, Italy)
  Consolidate list of defects and their impact on sensor properties (Input to simulation group) including introduction rates & annealing for different type of irradiations and materials
  Extend work on p-type silicon including low resistivity material
    Understand boron removal in lower resistivity p-type silicon: Performance of MAPS, CMOS sensors, LGAD
  Review NIEL approach; Modeling and understanding role of clusters;
    Study of electron damage: Implement results into simulations
  Characterization of Nitrogen enriched silicon
Detector Characterization (Convener: E.Fretwurst, University of Hamburg, Germany)
  TCAD sensor simulations
    Cross-calibration of different simulation tools (ongoing)
    Refine defect parameters used for modeling (from effective to measured defects)
    Extend modeling on charge multiplication processes
  Extend experimental capacities on edge-TCT (implement set-up at more RD50 institutions)
    Parameterization of electric field (fluence, annealing time, etc.)
    Studies on charge multiplication processes
  Understand potential of Two Photon Absorption for sensor characterization
  Continue study on “mixed” irradiations
  Explore fluence range to1017cm-2 (to prepare for future needs in forward physics)

## Slide 23: Workplan for 2015/2016 (2/2)
New structures (Convener: Giulio Pellegrini, CNM Barcelona, Spain)
  Continue work on thin and 3D sensors (especially in combination with high fluence)
  Continue characterization of dedicated avalanche test structures (LGAD)
    Understand impact of implant shape and other geometrical parameters on avalanche processes
  Evaluate ‘low resistance strip’ sensors
  HVCMOS
    Continue characterization of existing devices (close collaboration with ATLAS HVCMOS working group)
    End of year: submission of first RD50 devise in an engineering run on AMS 35 process
Full detector systems (Convener: G.Kramberger, Ljubljana University, Slovenia)
  Further studies of thin (low mass) segmented silicon devices
  Study performance of thin and avalanche sensors in the time domain (Fast sensors!)
  Long term annealing of segmented sensors (parameterize temperature scaling)
  Continue study on “mixed” irradiations (segmented detectors)
  Continue RD50 program on slim edges, edge passivation and active edges
Links with LHC experiments and their upgrade working groups
  Continue collaboration on evaluation of radiation damage in LHC detectors
  Continue common projects with LHC experiments on detector developments

## Slide 24: RD50 main achievements & links to LHC Experiments
Some important contributions of RD50 towards the LHC upgrade detectors:
p-type silicon (brought forward by RD50 community) is the base line option for the ATLAS and CMS Strip Tracker upgrades
n- MCZ (introduced by RD50 community) might improve performance in mixed fields due to compensation of neutron and proton damage: MCZ is under investigation in ATLAS, CMS and LHCb
Double column 3D detectors developed within RD50 with CNM and FBK. Development was picked up by ATLAS and further developed for ATLAS IBL needs.
RD50 results on very highly irradiated planar segmented sensors have shown that these devices are a feasible option for the LHC upgrade
RD50 data are essential input parameters for planning the running scenarios for LHC experiments and their upgrades (evolution of leakage current, CCE, power consumption, noise,….).
Charge multiplication effect observed for heavily irradiated sensors (diodes, 3D, pixels and strips). Dedicated R&D launched in RD50 to understand underlying multiplication mechanisms, simulate them and optimize the CCE performances. Evaluating possibility to produce fast segmented sensors?
Close links to the LHC Experiments:
  Many RD50 groups are involved in ATLAS, CMS and LHCb upgrade activities (natural close contact).
  Common projects with Experiments: Irradiation campaigns, test beams, wafer procurement and common sensor projects.
  Close collaboration with LHC Experiments on radiation damage issues of present detectors.

## Slide 25: Recent key results
Progress in understanding microscopic defects
  Defects responsible for positive space charge in DOFZ, MCZ and EPI and defects provoking reverse annealing are characterized!
  Consistent list of defects produced covering electron, gamma, neutron and proton/pion damage
TCAD simulations : Good progress on simulations [Note: RD50 profiting from strong CMS simulation group]
  Commercial TCAD packages well understood and proved to be well adopted to our needs (defect description)
  Simulations can reproduce pulse shapes, depletion voltage, charge collection and leakage current. Getting predictive capabilities!
Systematic analysis of the Charge multiplication mechanism
  Noise issue particularly important for exploitation of this feature in Experiments
  New dedicated sensors produced to test avalanche effects, sensors working after irradiation
Consolidation of data obtained on p-type and thin segmented sensors
  Further results on radiation tolerance and further results on long term annealing
  Thin sensors seem to extend fluence reach of silicon detectors; Optimization: Optimum thickness depends on many parameters !
Slim and active edges
  Further progresses towards reduction of insensitive area (edges) of detectors
New structures based on mixed technologies
  Exploitation of DRIE etching: 3D-trench electrode, semi-3D sensors; planar strip with trenched electrodes, active edge planar pixel, ….….; Use of deep implantation for controlling avalanches.
Use of tools developed in framework of RD50: ALIBAVA & Edge-TCT & Beam telescope
  Edge-TCT and TCT systems are now produced centrally and can be procured by interested groups
  Use of the ALIBAVA readout system in many RD50 institutions

## Slide 26: Spare Slides
Some spare slides
More details on http://www.cern.ch/rd50/
  Most results presented here have been shown on the last RD50 Workshop

## Slide 27: Summary on defects with strong impact on device performance after irradiation
Most important defects [for details and references see JAP 117, 164503, 2015]

## Slide 28: Reminder: NIEL – Non Ionizing Energy Loss Displacement damage functions
Hypothesis: Damage parameters scale with the NIEL
  Be careful, does not hold for all particles & damage parameters (see later)
1 MeV neutron equivalent damage
1
1 MeV
0.62 (24 GeV/c protons)
1.85 (26 MeV protons)
1.14 (300 MeV pions)
0.92 (reactor neutrons >100 keV)

## Slide 29: NIEL for electron damage
Non Ionizing Energy Loss (NIEL)
  Used to calculate effective damage for different particles with different energy.
  Normalization usually to 1 MeV neutron equivalent damage
  Study on the validity of NIEL for electrons in the range of 1.5 MeV to 27 MeV
  Two approaches:
    a) Classical NIEL (our standard; based on two body elastic collisions between PKAs, 0K)
    b) Effective NIEL (Molecular Dynamics calculations taking into account many body interactions)
[Effective NIEL: Inguimbert et al., IEEE TNS 57 (2010)1915]
[R.Radu et al, JAP 117, 164503, 2015]

## Slide 30: Ratio of cluster to point defects
[more details: R.Radu et al, JAP 117, 164503, 2015]

## Slide 31: Edge-TCT to Study Fields
Study of Electric field inside silicon sensor very challenging problem
New tool (2010): Edge-TCT (Transient Charge Technique)
  Illuminate segmented sensor from the side with sub-ns infrared laser pulses
  Scan across the detector thickness
  Record current pulses as function of depth
  Extract rise time and collected total charge
  Reconstruct the electric field
Expectations
  Significant electric field only in depleted volume
  Charge generated in ‘undepleted’ part of detector is lost
[Edge-TCT, G. Kramberger, IEEE TNS, VOL. 57, NO. 4, AUGUST 2010, 2294]
[N.Pacifico, 20th RD50 Workshop, Bari, 2012]

## Slide 32: Charge Multiplication

## Slide 33: New structures: slim and active edges
RD50 slim edges project (reduce dead space around the active sensor)
Active edges (VTT & MPI Munich)
  Thin wafers with active edges produced at VTT [ A.Macchiolo, 22nd RD50, Albuquerque, June 2013]
inactive area
slim edge
active area
guard rings
[V. Fadeyev, 22nd RD50 Workshop, Albuquerque, June 2013]
  Scribe XeF2 etch, diamond scribe, DRIE
  Cleave automated, manual
  Passivate nitride, oxide (n-type) alumina ALD (p-type)
1015 p/cm2 Testbeam:
no difference between edge and other pixel!
… development picked up by HPK (see Hiroshima Symposium 9/2013)

## Slide 34: 3D