## Slide 1: Phase 2 Production Discussion
We would like to review the conclusions reached at Caltech on US involvement in the phase 2 outer tracker
This will be presented to the Tracker Management board in 3 weeks
  Intentions – not commitments
Has the vision evolved since CalTech?
  How does the MREFC play into the balance between pixels and OT?
    Can OT centers also do pixels?
  Does the HGC decision affect production plans?
    Many HGC operations share infrastructure with the tracker
    Expect Fermilab to work on HGC modules
  What infrastructure costs can be paid by the project/local institutions?

## Slide 2: US interests
build and test a fraction of the PS modules (~4000).
Develop assembly techniques
Test sensors
Develop and model sensor designs
Design flat barrel section
Participating US Institutions
  Brown University
  Cornell University
  Davis
  Fermilab
  Rutgers University
  University of Rochester
  Santa Barbara
  Princeton University

## Slide 3: Our interests in OT modules
develop and build the support and cooling structure for the flat part of the barrel
and in the assembly of a number of the PS modules.
  The PS modules consist of a strip sensor and a pixel sensor.
  The strip sensor has two rows of AC coupled strip with a length of 2.5 cm and a pitch of 100 𝜇m. It is bonded on either side to a hybrid with a row of short-strip ASIC (SSA) readout chips.
  The pixel sensor has 32 rows of macro-pixels of length 1.5 mm and pitch 100 𝜇m. The macro-pixel ASIC (MPA) readout chips will be bump-bonded directly onto the sensor to form a macro-pixel-sub-assembly (MaPSA).
  The module assembly has to provide for precise alignment of the two sensors relative to each other and supply power and cooling to the sensors and readout chips.

## Slide 4: PS Module Participation plans
 | Task |  | Brown | Cornell | Davis | Fermilab | Santa Barbara | Rochester | Rutgers | Princeton
 | Module Constrtcution Tasks |  |  |  |  |  |  |  |  | 
1 | Sensors |  |  |  |  |  |  |  |  | 
1.1 | Sensor Quality Control |  | X |  |  |  |  | X |  | 
1.2 | Process Quality Control |  | X |  |  |  |  | X |  | 
1.3 | Irradiation Tests |  | X |  | X |  |  | X |  | 
2 | Hybrids |  |  |  |  |  |  |  |  | 
2.1 | FE or Service Hybrid QA |  | X? |  |  |  |  |  | X? | 
3 | Mechanics |  |  |  |  |  |  |  |  | 
3.1 | Al-CF production(vendor contact) and QA |  |  |  |  | X |  |  |  | 
3.2 | Al-CF coating |  |  |  |  | X? |  |  |  | 
3.3 | CF production (vendor contact) and QA |  |  |  |  | X? |  |  |  | 
4 | MaPSA |  |  |  |  |  |  |  |  | 
4.1 | Vendor Contact and QA |  | X | X |  |  |  |  | X? | 
5 | Assembly |  |  |  |  |  |  |  |  | 
5.1 | Gluing |  | X | X | X | X | X | X | X | x
5.2 | verification of geometrical precision |  | X | X |  | X | X | X | X | x
5.3 | Wirebonding |  | X | X |  | X | X? | X | X | x
5.4 | QA assembled modules (connectivity etc) |  | X | X |  | X | X? | X | X | x
5.6 | Full QA w/ extended operation & thermal cycles |  | X | X | X | X |  | X | X | x
5.7 | Transport Equipment |  |  |  | X |  |  |  | X? | 
6 | Mechanical Structures |  |  |  |  |  |  |  |  | 
7 | Tracker Integration |  | X | X |  | X | X? | X | X | 
8 | Backend Electronics/L1 Track Trigger |  |  | X |  |  | X |  | X | 
 |  |  |  |  |  |  | Not a production | assembly w/ |  | w/Rutgers
 |  |  |  |  |  |  | center | Cornell |  | 

## Slide 5: Centers and equipment
 | Test system | CMM | Auto. Probe station | Assembly fixtures | Auto Wirebonder | Cooling system | Burn-in system | Gantry
Hybrid Testing | X |  |  |  |  |  |  | 
Sensor pkg assembly |  | X |  | X |  |  |  | 
MPA testing | X |  | X |  |  |  |  | 
Hybrid assembly to base | X |  |  | X | X- | X |  | ?
Sensor assembly to base | X | X |  | X | X | X | X | X
Assembly to rods | X | X |  | X |  | X | X | 

## Slide 6: Infrastructure: module assembly
Wire bonder : ~$200K
Pull tester. e.g. Dage 4000: ~10K$
Microscope for optical inspection. Microscope with LED display for quick viewing. ~5K$
Glue dispensing robot. ~20K$
Gantry style robot. Aerotech AGS10000 for TOB construction. ~100K$
Automatic Probe station with cold chuck: ~150K$
Camera with LabVIEW Vision system for robot. ~$20k
Keithley 237 voltage sources. Standard lab power supplies. ~10-20K$
Vacuum oven: ~20K$
Dry storage units with grounding capability. ~10-20K$
Anti-static protection system. ~5-10K$
CMM ???
Cooling system
Burn-in system
Test systems
Clean Room?
Estimate: 400K$ + wire bonder (200K$) + clean room

## Slide 7: Sensor tests
HPK wants to reduce the level of probing
Measure IV/CV curves for ~20% of sensors
Carry out strip measurements (w/o interstrip) for 5% of sensors
Carry out full strip testing (including interstrip) for 1% of sensors
Perform radiation testing on diodes early in the production to control the material properties
  Irradiate mini-sensors and test-structures to 150% maximum fluence during production, Measure before and after irradiation
  Bias voltage up to 1000V. Perform measurements with sensors at -20°C
Establish strong feedback between module and sensor testing

## Slide 8: Infrastructure: sensors
Clean room (class 100,000 or better)
Basic equipment
  Source meter ≥ 1000V, Imax ≥ 1mA
  pAmmeter (2 or 3)
  LCR-Meter 100Hz ≤ f ≤ 1MHz
  Voltage source
  Temperature controlled vacuum chuck (~20°C) for sensors up to 16 cm long
  Light-tight and humidity controlled metallic enclosure
  Probes, vacuum tweezers, microscope
  Humidity controlled storage
Additional equipment for strip measurements
  automatic probe station (up to 2032 strips, 5 parameters each)
  XYZ-stage (accuracy ~5µm)
  Switching-matrix including HV switching
  Long-term setup to monitor leakage current at 500 V for 48h
Estimate: 250K$ + wire bonder (200K$) + clean room

## Slide 9: Institutional Interests R&D
 | Task |  | Brown | Cornell | Davis | Fermilab | Santa Barbara | Rochester | Rutgers | Princeton
 | R&D Tasks |  |  |  |  |  |  |  |  | 
 | Module Prototyping |  | X | X | X | X | X |  | X | 
 | Development of assembly procedures |  | X |  |  | X | X | X |  | X
 | Development of testing procedures |  | X | X |  |  |  |  | X | 
 | Development of production infrastructure |  | X | X |  | X | X |  |  | X
 | Support Development |  |  |  | X | X |  |  |  | 
 | Mechanical and thermal tests |  |  |  | X |  | X | X |  | X
 | Readout and test electronics |  | X | X |  |  |  |  | X | 
 | Beam tests |  | X | X | X | X | X | X | X | X

## Slide 10: Novati Wafer Tests
We performed initial tests on the Novati 8” sensor wafers
5 Wafers received
  2 x 725 micron p-spray + p-stop
  1 x 725 micron p-stop only
  2 x 500 micron p-spray + p-stop
We do not expect to be able to deplete the 725 micron thick devices

## Slide 11: Initial VI
Chart: 
| 0.0 | -10.0 | -20.0 | -30.0 | -40.0 | -50.0 | -60.0 | -70.0 | -80.0 | -90.0 | -100.0 | -110.0 | -120.0 | -130.0 | -140.0 | -150.0 | -160.0 | -170.0 | -180.0 | -190.0 | -200.0 | -210.0 | -220.0 | -230.0 | -240.0 | -250.0 | -260.0 | -270.0 | -280.0 | -290.0 | -300.0 | -310.0 | -320.0 | -330.0 | -340.0 | -350.0 | -360.0 | -370.0 | -380.0 | -390.0 | -400.0 | -410.0 | -420.0 | -430.0 | -440.0 | -450.0 | -460.0 | -470.0 | -480.0 | -490.0 | -500.0
W1_TS1_LD | -9.712e-11 | -6.6053e-08 | -9.292e-08 | -1.1396e-07 | -1.3232e-07 | -1.4877e-07 | -1.6379e-07 | -1.7796e-07 | -1.9125e-07 | -2.0387e-07 | -2.1594e-07 | -2.2765e-07 | -2.3838e-07 | -2.4955e-07 | -2.6032e-07 | -2.7072e-07 | -2.8091e-07 | -2.9096e-07 | -3.0071e-07 | -3.1014e-07 | -3.1933e-07 | -3.2814e-07 | -3.3679e-07 | -3.4512e-07 | -3.5312e-07 | -3.6105e-07 | -3.6885e-07 | -3.7657e-07 | -3.8412e-07 | -3.915e-07 | -3.9883e-07 | -4.0596e-07 | -4.1303e-07 | -4.1997e-07 | -4.2676e-07 | -4.3338e-07 | -4.3995e-07 | -4.4632e-07 | -4.528e-07 | -4.5917e-07 | -4.6574e-07 | -4.7253e-07 | -4.7972e-07 | -4.8822e-07 | -4.994e-07 | -5.1688e-07 | -5.4775e-07 | -6.061e-07 | -7.1761e-07 | -9.194e-07 | -1.2535e-06
Guard | 3e-13 | -5.5242e-09 | -8.2136e-09 | -1.0341e-08 | -1.2231e-08 | -1.3973e-08 | -1.5545e-08 | -1.7023e-08 | -1.8373e-08 | -1.9657e-08 | -2.0875e-08 | -2.2024e-08 | -2.3116e-08 | -2.4176e-08 | -2.5174e-08 | -2.6202e-08 | -2.7174e-08 | -2.8075e-08 | -2.8942e-08 | -2.98e-08 | -3.0644e-08 | -3.1435e-08 | -3.2224e-08 | -3.2992e-08 | -3.3721e-08 | -3.446e-08 | -3.5165e-08 | -3.588e-08 | -3.6592e-08 | -3.7309e-08 | -3.8033e-08 | -3.8761e-08 | -3.9508e-08 | -4.0263e-08 | -4.1017e-08 | -4.1788e-08 | -4.2571e-08 | -4.342e-08 | -4.4328e-08 | -4.5335e-08 | -4.6563e-08 | -4.8141e-08 | -5.0392e-08 | -5.4033e-08 | -6.0557e-08 | -7.3327e-08 | -9.9676e-08 | -1.536e-07 | -2.6089e-07 | -4.5924e-07 | -7.8929e-07
Wafer 4 – 725 micron – first VI

## Slide 12: Breakdown seems to decrease after first measurement
Chart: 
| 0.0 | -10.0 | -20.0 | -30.0 | -40.0 | -50.0 | -60.0 | -70.0 | -80.0 | -90.0 | -100.0 | -110.0 | -120.0 | -130.0 | -140.0 | -150.0 | -160.0 | -170.0 | -180.0 | -190.0 | -200.0 | -210.0 | -220.0 | -230.0 | -240.0 | -250.0 | -260.0 | -270.0 | -280.0 | -290.0 | -300.0 | -310.0 | -320.0 | -330.0 | -340.0 | -350.0 | -360.0 | -370.0 | -380.0 | -390.0 | -400.0 | -410.0 | -420.0 | -430.0 | -440.0 | -450.0 | -460.0 | -470.0 | -480.0 | -490.0
It | 3.601e-11 | -1.7018e-08 | -2.2999e-08 | -2.7496e-08 | -3.1233e-08 | -3.4486e-08 | -3.7381e-08 | -4.0015e-08 | -4.2423e-08 | -4.4641e-08 | -4.6691e-08 | -4.8595e-08 | -5.0294e-08 | -5.1946e-08 | -5.3453e-08 | -5.4887e-08 | -5.621e-08 | -5.7445e-08 | -5.858e-08 | -5.964e-08 | -6.0622e-08 | -6.1552e-08 | -6.2385e-08 | -6.3197e-08 | -6.3929e-08 | -6.462e-08 | -6.528e-08 | -6.5879e-08 | -6.6461e-08 | -6.6999e-08 | -6.7516e-08 | -6.7985e-08 | -6.847e-08 | -6.892e-08 | -6.9361e-08 | -6.9775e-08 | -7.0191e-08 | -7.055e-08 | -7.0921e-08 | -7.1272e-08 | -7.1629e-08 | -7.1982e-08 | -7.2343e-08 | -7.2735e-08 | -7.3099e-08 | -7.3504e-08 | -7.3891e-08 | -7.4332e-08 | -7.4861e-08 | -5.0009e-05
Test_3 | 4.189e-11 | -1.7017e-08 | -2.3004e-08 | -2.7505e-08 | -3.1245e-08 | -3.4498e-08 | -3.7398e-08 | -4.0031e-08 | -4.2441e-08 | -4.4662e-08 | -4.672e-08 | -4.8622e-08 | -5.0313e-08 | -5.1958e-08 | -5.3495e-08 | -5.4903e-08 | -5.6233e-08 | -5.7473e-08 | -5.8607e-08 | -5.9683e-08 | -6.0658e-08 | -6.1566e-08 | -6.2422e-08 | -6.322e-08 | -6.3974e-08 | -6.466e-08 | -6.5318e-08 | -6.5913e-08 | -6.6495e-08 | -6.703e-08 | -6.7557e-08 | -6.8038e-08 | -6.8516e-08 | -6.8957e-08 | -7.6812e-08 | -4.0907e-05 | -5.0008e-05
Test_2 | 3.023e-11 | -1.7011e-08 | -2.2999e-08 | -2.7499e-08 | -3.1234e-08 | -3.449e-08 | -3.739e-08 | -4.002e-08 | -4.243e-08 | -4.4653e-08 | -4.6702e-08 | -4.8604e-08 | -5.0302e-08 | -5.1954e-08 | -5.3483e-08 | -5.4899e-08 | -5.6214e-08 | -5.7456e-08 | -5.8595e-08 | -5.9657e-08 | -6.0639e-08 | -6.1559e-08 | -6.2413e-08 | -6.3211e-08 | -6.3958e-08 | -6.4642e-08 | -6.5299e-08 | -6.5903e-08 | -6.6465e-08 | -6.703e-08 | -6.7518e-08 | -6.8023e-08 | -6.8499e-08 | -6.8949e-08 | -6.9395e-08 | -3.4249e-05 | -5.0009e-05
First Vi
Next 2

## Slide 13: But it is all from the guard
Chart: 
| 0.0 | -10.0 | -20.0 | -30.0 | -40.0 | -50.0 | -60.0 | -70.0 | -80.0 | -90.0 | -100.0 | -110.0 | -120.0 | -130.0 | -140.0 | -150.0 | -160.0 | -170.0 | -180.0 | -190.0 | -200.0 | -210.0 | -220.0 | -230.0 | -240.0 | -250.0 | -260.0 | -270.0 | -280.0 | -290.0 | -300.0 | -310.0 | -320.0 | -330.0 | -340.0 | -350.0 | -360.0 | -370.0 | -380.0 | -390.0 | -400.0 | -410.0 | -420.0 | -430.0 | -440.0 | -450.0 | -460.0 | -470.0 | -480.0
Total | 3.1622e-10 | -1.7063e-08 | -2.3058e-08 | -2.7573e-08 | -3.1283e-08 | -3.4492e-08 | -3.7473e-08 | -4.0055e-08 | -4.2485e-08 | -4.4731e-08 | -4.6781e-08 | -4.8687e-08 | -5.0444e-08 | -5.208e-08 | -5.3619e-08 | -5.5042e-08 | -5.6202e-08 | -5.7605e-08 | -5.8742e-08 | -5.9796e-08 | -6.0803e-08 | -6.1716e-08 | -6.2577e-08 | -6.3372e-08 | -6.4123e-08 | -6.4837e-08 | -1.7564e-05 | -4.1691e-05 | -7.9606e-05 | -0.0001115 | -0.0001501 | -0.0001897 | -0.0002323 | -0.0002744 | -0.0003169 | -0.0003599 | -0.0004043 | -0.0004468 | -0.0004892 | -0.0005318 | -0.0005751 | -0.0006192 | -0.0006644 | -0.000712 | -0.0007637 | -0.0008195 | -0.0008806 | -0.0009474 | -0.001
Active | 2.9991e-10 | -1.5533e-08 | -2.1014e-08 | -2.4909e-08 | -2.8069e-08 | -3.0723e-08 | -3.3316e-08 | -3.5439e-08 | -3.7498e-08 | -3.9395e-08 | -4.1102e-08 | -4.2699e-08 | -4.4222e-08 | -4.5569e-08 | -4.6823e-08 | -4.7981e-08 | -4.9052e-08 | -5.0048e-08 | -5.0957e-08 | -5.1789e-08 | -5.2556e-08 | -5.326e-08 | -5.3908e-08 | -5.4504e-08 | -5.5047e-08 | -5.5547e-08 | -5.6023e-08 | -5.6535e-08 | -5.7021e-08 | -5.7483e-08 | -5.7926e-08 | -5.8374e-08 | -5.8815e-08 | -5.9259e-08 | -5.9676e-08 | -6.0103e-08 | -6.0525e-08 | -6.0933e-08 | -6.133e-08 | -6.1727e-08 | -6.2141e-08 | -6.2544e-08 | -6.2987e-08 | -6.3448e-08 | -6.3937e-08 | -6.4492e-08 | -6.5051e-08 | -6.5659e-08 | -6.6119e-08

## Slide 14: CV- Depletes around 400 V W9-TS1-SD
Chart: 
| 0.0 | -20.0 | -40.0 | -60.0 | -80.0 | -100.0 | -120.0 | -140.0 | -160.0 | -180.0 | -200.0 | -220.0 | -240.0 | -260.0 | -280.0 | -300.0 | -320.0 | -340.0 | -360.0 | -380.0 | -400.0 | -420.0 | -440.0 | -460.0
1/c^2 | 1.0007e+20 | 1.5051e+21 | 2.7599e+21 | 3.8863e+21 | 4.8958e+21 | 5.8413e+21 | 6.7233e+21 | 7.5399e+21 | 8.2821e+21 | 9.0089e+21 | 9.6965e+21 | 1.0354e+22 | 1.0975e+22 | 1.1567e+22 | 1.2137e+22 | 1.2684e+22 | 1.3204e+22 | 1.3709e+22 | 1.418e+22 | 1.4458e+22 | 1.507e+22 | 1.4858e+22 | 1.489e+22 | 1.4935e+22

## Slide 15: W9_TS4_LD
Chart: 
| 0.0 | -20.0 | -40.0 | -60.0 | -80.0 | -100.0 | -120.0 | -140.0 | -160.0 | -180.0 | -200.0 | -220.0 | -240.0 | -260.0 | -280.0 | -300.0 | -320.0 | -340.0 | -360.0 | -380.0 | -400.0 | -420.0 | -440.0 | -460.0 | -480.0 | -500.0 | -520.0 | -540.0 | -560.0
1/c^2 | 7.0507e+18 | 1.0041e+20 | 1.9327e+20 | 2.8092e+20 | 3.6536e+20 | 4.4593e+20 | 5.2353e+20 | 5.9812e+20 | 6.6792e+20 | 7.3762e+20 | 8.0483e+20 | 8.7035e+20 | 9.3398e+20 | 9.9564e+20 | 1.0564e+21 | 1.1153e+21 | 1.1727e+21 | 1.2286e+21 | 1.2824e+21 | 1.3172e+21 | 1.3277e+21 | 1.3343e+21 | 1.3378e+21 | 1.3424e+21 | 1.3448e+21 | 1.5465e+21 | 1.5591e+21 | 1.5664e+21 | 1.5708e+21

## Slide 16: Resistivity
Neff Calc |  |  | 
 | mup= | 502 | cm2/Vs
 | eps= | 11.9 | 
 | eps0= | 8.85419E-14 | F/cm
 | D | 0.05 | cm
 | q0 | 1.60218E-19 | 
 | Vdep | 400 | V
 | Neff | 2.10E+12 | 
 | Resistivity | 5.91E+03 | Ohm-cm