## Slide 1: DQW Cryogenic Magnetic Shield Internal Review
Niklas Templeton
06/05/15

## Slide 2: Contents
Specification
Opera Magnetic Analysis
Overview
  Design Approach
  Common Features
Design & Assembly Procedure
  DQW
  RFD
Shield Analysis
  Thermal Stress
  Self Weight XYZ
1

## Slide 3: Specification
Less than 1µT on cavity surface
Cold Magnetic Shield
  1mm APERM Cryophy (to be used with 3mm Mu Metal outer shield)
  Internal to Helium Vessel
  Suspended in 2K Helium
  Mounted off Helium vessel – no cavity connection
Designed for (worst case) earth magnetic field. Local sources to be isolated separately
  Earths South to North Field 48µT
  SPS ambient Magnetic field with moderately shielded Busbars <200µT
Magnetic shielding for SPL cavities: T Junginger 2010
Estimate of the Ambient Magnetic Field in the SPS Crab Cavity Location: J Bauche, A Macpherson 2014
2

## Slide 4: Summary of Opera Analysis - Kiril Maranov
The magnet group within ASTeC (STFC) have converted the mechanical design CAD files into a simplified geometry acceptable for Opera 3D (Tosca) and then assessed shielding performance based on simulations.
Two shielding solutions were considered: a single-layer solution (mu-metal only) and a double-layer solution (mu-metal + cryoperm)
The conclusion from this work is to go ahead with the double-layer solution. The single layer solution meets the spec by a narrow margin, but there is no room for contingency and the risk is higher.
3

## Slide 5: Magnetic shielding effect is anisotropic
The external field is radial
The external field is axial
A cylinder is twice as effective against radial field as against axial field.
4

## Slide 6: Single layer: the field is parallel to the long side
BEarth=60µT
BEarth=60µT
A single-layer shield is within spec (~0.5 µT) at the cavity locations, but this gives a limited factor of safety.
B>1 µT
5

## Slide 7: Performance: the field is parallel to the long side
BEarth=60µT
BEarth=60µT
B>1 µT
B<< 0.1 µT (very small!)
6

## Slide 8: Shield Design Approach
Satisfy space constraints
  Internal to Bolted Helium Vessel
  Close fitting to cavity
Feasible assembly
Minimise number & size of penetrations
Ease of manufacture & assembly
  Minimise number of panels
  Bent / Folded sheet
  *Pressed / Formed panels possible future batch shield orders
Maximise penetration attenuation
Maximise curvature
7

## Slide 9: Reason for Close fitting shield
To maximise space for panel connections & flexi-mounts.
Allows longer tubular shielding for attenuation of shield penetrations.
The shielding factor is inversely proportional to the shield diameter (if approximated to a cylinder):
A - attenuation factor of a perpendicular field
μ – magnetic permeability
t – wall thickness
d - diameter
High field regions requiring <1µT
Reference - F. Pobell, Matter and Methods at Low Temperatures. Springer-Verlag, third ed., 2007.
8

## Slide 10: Common Design Features
Helium Holes
Shield peppered with at least 142 x Ø3mm holes on 50-100mm pitch for helium transfer
142 holes give 10cm2 transfer area, so that at worst case heat load (10W) heat flow is at least 1W/cm2
1mm APERAM Cryophy - Cold Rolled Strip
Panels to be manufactured from Cryophy sheet metal which is cut, bent/folded, and fastened using self clinching nuts & spring washers
9

## Slide 11: Common Design Features
Tubular Shielding
Prevents field penetration through openings.
Ideally H = ØD
Fitted & Curved Shape
More effective at containing channelled magnetic flux
Additional Cover Strips
Overlapping joints prevent gaps & allows magnetic flux to follow a continuous low-reluctance path
Flexi-Mounts
Flexible Gr2 Titanium mounts connect the shield to the Helium Vessel. 8 mounting pairs are utilized in 3 orientations for maximum shield stability
10

## Slide 12: DQW Shield Design & Assembly
Y
Z
X
 | Concept A | Concept B | Concept C
No. of panels | 9 | 9 | 7
Curvature YZ | R40, R10, R50, R50 | - | R50, R50
Curvature XY | - | R100, R40, R30, R100 | R100, R40
A
B
C
Concept Analysis
11

## Slide 13: DQW Shield Design & Assembly
470
314
420
Assembled Shield Mass: ~10kg
12

## Slide 14: DQW Shield Design & Assembly
Y
Z
X
13

## Slide 15: DQW Shield Design & Assembly
Y
Z
X
2 Bottom Panels assembled 1st
Cavity orientation shown upside down for clarity
14

## Slide 16: DQW Shield Design & Assembly
Y
Z
X
Shield & cavity mounted to base plate of the Helium Vessel
Top End caps are attached as well as bottom side panel and Dummy beam pipe attenuation sleeve.
15

## Slide 17: DQW Shield Design & Assembly
Final 2 top panels are brought into place and remaining cover strips and brackets are fastened
16

## Slide 18: DQW Shield Design & Assembly
Side and top Vessel walls are assembled with remaining Flexi-Mounts before Helium Vessel is closed
17

## Slide 19: RFD Shield Design & Assembly
RFD Helium Vessel 20/04/15
Assembled Shield Mass: ~10kg
18

## Slide 20: RFD Shield Design & Assembly
19

## Slide 21: RFD Shield Design & Assembly
Pre-assembled shield body is assembled Top and Bottom
20

## Slide 22: RFD Shield Design & Assembly
Shield Body is mounted to Helium Vessel Base
21

## Slide 23: RFD Shield Design & Assembly
Split folded-end panels are assembled around 3 ports
End Cover is assembled to main body and fastened with cover panels and brackets
22

## Slide 24: RFD Shield Design & Assembly
2 Curved-End panels are assembled around Beam Pipe
23

## Slide 25: RFD Shield Design & Assembly
Split panels complete the Shield at the FPC & HOM Ports
Remaining cover strips are assembled
24

## Slide 26: RFD Shield Design & Assembly
Flexi Mounts are connected and Helium Vessel is assembled
25

## Slide 27: FEA: Cool Down & Self Weight
Material Data
Helium Vessel & Flexi-Mounts: Titanium Grade2 (ES371110)
  RT Yield Strength= 275MPa
  Thermal Expansion from RT to -269K = -5.2 E-6.K
Magnetic Shield: Aperam Cryophy (Magnetic Shielding LTD)
  RT Yield Strength = 280MPa
  Thermal Expansion from RT to -269K = -8 E-6.K
26

## Slide 28: DQW & RFD Thermal Stress
Loads & Constraints
Cool down from RT to 2K
Fixed at input coupler interface
Results
Solution contains erroneous result due to skew mesh geometry
Stress > 150Mpa shown in red
Some localised high stresses at shield connections
Conclusion
Cryophy Stresses affects shielding properties in immediate stress location, localised stresses are (at worst) comparable to a small hole – effect is negligible.
Localised stress can be avoided using sufficient clearance at connections.
27

## Slide 29: DQW Self Weight Horizontal
Fixed at Flexi Mount – Helium Vessel interface
Gravity applied in ANSYS Z direction
Max shield deformation 0.08mm
Max shield stress 13MPa
28

## Slide 30: DQW Self Weight Vertical
Fixed at Flexi Mount – Helium Vessel interface
Gravity applied in ANSYS Y direction
Max shield deformation 0.04mm
Max shield stress 14MPa
29

## Slide 31: DQW Self Weight Side
Fixed at Flexi Mount – Helium Vessel interface
Gravity applied in ANSYS X direction
Max shield deformation 0.07mm
Max shield stress 32MPa
30

## Slide 32: DQW Self Weight Horizontal
Fixed at Flexi Mount – Helium Vessel interface
Gravity applied in ANSYS Z direction
Max shield deformation 0.01mm
Max shield stress 9MPa
31

## Slide 33: RFD Self Weight Vertical
Fixed at Flexi Mount – Helium Vessel interface
Gravity applied in ANSYS Y direction
Max shield deformation 0.01mm
Max shield stress 9MPa
32

## Slide 34: RFD Self Weight Side
Fixed at Flexi Mount – Helium Vessel interface
Gravity applied in ANSYS X direction
Max shield deformation 0.02mm
Max shield stress 27MPa
33

## Slide 35: Discussions with Magnetic Shielding LTD
We have liaised with Magnetic Shields LTD from the UK throughout the design of the shield.
We obtained a budget cost for the previous shield concepts (welded helium vessel).
Cost estimate was £8-12K (excluding VAT) per shield
New designs could be more expensive, up to ~£15K (€20K)
Formed / pressed shield panels are feasible for larger quantity orders.
34

## Slide 36: Thank You!
Questions?