## Slide 1: Update on THGEMs and Micromegas production for RICH-1 COMPASS Upgrade on behalf of THGEM Trieste group
S . Levorato
INFN - Sezione di Trieste

## Slide 2
RICH-1 at COMPASS experiment at CERN Upgrade starting fall 2015: Reminder
radiator:
C4F10
5 m
6 m
3 m
UV mirror
wall
radiator gas: C4F10
Photon detectors system now:
              12 MWPC + CsI 600 x 600 mm2
              4 MAPMT 600 x 600 mm2 (2006)
… in 2016
MWPC + CsI
MAPMT
4 New 600 x 600 mm2 MPGD based photon detector
will be installed for a total sensitive surface of ̴ 1.1 m2
Remark  mechanical constrains to guarantee compatibility with the present structure
Photon Detectors
To improve the detector performance
in view of the COMPASS phase 2

## Slide 3
Detector concept: architecture chosen a reminder
Hybrid Detector (2 x THGEM + B-Micromegas)
Double THGEM: t = 0.4 mm; p = 0.8 mm; h = 0.4 mm
Multi-Pad Anode
(8mm pitch 500 mm interpad )
Simple; robust; cheap;
High photoelectron extraction efficiency in CH4 rich mixtures;
Fast signals time resolution ;
Closed Geometry;
Cascade   single photon detection;
IBF ;
Stability: time & high rates
Staggered THGEMs
Each 600mmx600mm detector is made of 2 modules
Each of them consisting of:
          2 300mmx600mm THGEMs
          1 300mmx600mm Bulk Micromegas

## Slide 4
Detector: integration of the new architecture

## Slide 5
Detector: THGEM production material
Thickness PCB variance as big as 15% for non selected PCB
Gain Variance > 40%*
example THGEM: t = 0.8 mm; p = 0.8 mm; h = 0.4 mm
Need of material preselection
50 foils of raw PCB material bought
*Standard daq chain Cremat+Ortec+MCA, Ar/CO2 70/30 atmosphere

## Slide 6
THGEM production: thickness measurement
Y
X
800 mm
800 mm
36 x 36 points in square pattern from (0,0) to (700,700)
(0,0)
#No.
Top View
From 1245 mm x 1092 mm
Raw PCB foil XY reduction
Expected more uniform in
thickness ( production procedure)
On average 3 measured pcs/day
Each foil has its unique n identifier
Thermalized room with Mitutoyo EURO CA776

## Slide 7
THGEM production, material seection
50 PCBs
700 x 700 mm2
N pieces needed (300mm x 600 mm): 16, we can easily select 8 foils with
<3% ( reminder 5% in thickness  15% in gain )

## Slide 8
THGEM production, material selection

## Slide 9
THGEM production
24 fixation points to guarantee
THGEMs flatness and positioning
Pillars in PEEK
2 reference holes to guarantee
the THGEMs staggering
PCB for alignment and spacing
Segmentation in 12 sectors
0.7 mm
sector
separation
t = 0.4 mm; p = 0.8 mm; h = 0.4 mm

## Slide 10
THGEM production
24 fixation points to guarantee
THGEMs flatness and positioning
Pillars in PEEK
2 reference holes to guarantee
the THGEMs staggering
PCB for alignment and spacing
Segmentation in 12 sectors
0.7 mm
sector
separation

## Slide 11
THGEM production
PCB material Sent to ELTOS for production, Agreed on procedure with ELTOS first batch delivery 08/06/2015:

## Slide 12
THGEM characterization
In Trieste Cleaning procedure will be applied : polish, high pressure water cleaning, ultrasonic Bath + microetching, distilled water rinsing and oven @ 160 ºC, final step Gain Characterization
THGEMs stored for transport in dedicated boxes for gold coating to CERN.

## Slide 13
THGEM characterization: proof of the principle
Ar/CO2 (70:30);
Pre-amplifier + Amplifier
+ MCA; 55Fe
55Fe main peak
Escape Peak
55Fe positioning
Corresponding connector
selection
Spectra collection
Uniformity gain, E res. spectra
Operation is time consuming, and affected by gain variation due to the P,T gas/environmental changes

## Slide 14
THGEM characterization
Gain Uniformity will be measured with X-Ray source (up to now 55Fe), Data collected with SRS system.
Each THGEM will be fully characterized. Amore software adapted, Different Mapping Option added to have Pads: Thanks to Eraldo for borrowing us the FEC!
Next weeks 55Fe X-rays gun

## Slide 15
Detector Micromegas production
Final anode design to be completed in the next weeks for production at TVR company,
first delivery foreseen for half of July, they will be delivered to CERN for BULK Micromegas production (Agreed with RUI)
Prototypes have already been produced @ CERN with good results in terms of gain uniformity and detector stability
Start of production
of BULK MM (final pieces)
at the end of July
Then 2 pieces for month

## Slide 16
Detector Micromegas production
Final anode design to be completed in the next weeks for production at TVR company,
first delivery foreseen for half of July, they will be delivered to CERN for BULK Micromegas production (Agreed with RUI)
Prototypes have already been produced @ CERN with good results in terms of gain uniformity and detector stability
Start of production
of BULK MM (final pieces)
at the end of July
Then 2 pieces for month
55Fe source Ar/CO2 Cremat+Ortec+Amptek
OK

## Slide 17
Full detector characterization: Gain Uniformity, HV monitoring, PT variation
Caen HV 1471 A
Correction of Voltage
according to linearized exponential law
System fully automated + logging
LabVIEW based
wireless PicoAmmeter + automated logging Linux SW QT-based
The correction under study but encouraging results!
Hybrid prototype 2 THGEMs + Micromegas
w/o PT correction ± 20% gain variation during the day
with PT correction ± 5%.
Thanks to P. Ciliberti

## Slide 18
Full detector characterization: Gain Uniformity, HV monitoring, PT variation
Thanks to B.G.
Thanks for your attention!