## Slide 1: Novati Wafer Studies
Initial studies with Novati wafers shows good VI and CV curves with a couple of peculiarities.
Guard rings break down below 500 V. It is common that the breakdown is higher in initial tests than subsequent measurements. This is particularly true of the p-spray + p-stop devices.
The active area does not break down until higher (as yet undetermined) voltage.
CV curves on the 500 micron devices show depletion at about 400V
Chart: 
| 0.0 | -10.0 | -20.0 | -30.0 | -40.0 | -50.0 | -60.0 | -70.0 | -80.0 | -90.0 | -100.0 | -110.0 | -120.0 | -130.0 | -140.0 | -150.0 | -160.0 | -170.0 | -180.0 | -190.0 | -200.0 | -210.0 | -220.0 | -230.0 | -240.0 | -250.0 | -260.0 | -270.0 | -280.0 | -290.0 | -300.0 | -310.0 | -320.0 | -330.0 | -340.0 | -350.0 | -360.0 | -370.0 | -380.0 | -390.0 | -400.0 | -410.0 | -420.0 | -430.0 | -440.0 | -450.0 | -460.0 | -470.0 | -480.0 | -490.0
It | 3.601e-11 | -1.7018e-08 | -2.2999e-08 | -2.7496e-08 | -3.1233e-08 | -3.4486e-08 | -3.7381e-08 | -4.0015e-08 | -4.2423e-08 | -4.4641e-08 | -4.6691e-08 | -4.8595e-08 | -5.0294e-08 | -5.1946e-08 | -5.3453e-08 | -5.4887e-08 | -5.621e-08 | -5.7445e-08 | -5.858e-08 | -5.964e-08 | -6.0622e-08 | -6.1552e-08 | -6.2385e-08 | -6.3197e-08 | -6.3929e-08 | -6.462e-08 | -6.528e-08 | -6.5879e-08 | -6.6461e-08 | -6.6999e-08 | -6.7516e-08 | -6.7985e-08 | -6.847e-08 | -6.892e-08 | -6.9361e-08 | -6.9775e-08 | -7.0191e-08 | -7.055e-08 | -7.0921e-08 | -7.1272e-08 | -7.1629e-08 | -7.1982e-08 | -7.2343e-08 | -7.2735e-08 | -7.3099e-08 | -7.3504e-08 | -7.3891e-08 | -7.4332e-08 | -7.4861e-08 | -5.0009e-05
Test_3 | 4.189e-11 | -1.7017e-08 | -2.3004e-08 | -2.7505e-08 | -3.1245e-08 | -3.4498e-08 | -3.7398e-08 | -4.0031e-08 | -4.2441e-08 | -4.4662e-08 | -4.672e-08 | -4.8622e-08 | -5.0313e-08 | -5.1958e-08 | -5.3495e-08 | -5.4903e-08 | -5.6233e-08 | -5.7473e-08 | -5.8607e-08 | -5.9683e-08 | -6.0658e-08 | -6.1566e-08 | -6.2422e-08 | -6.322e-08 | -6.3974e-08 | -6.466e-08 | -6.5318e-08 | -6.5913e-08 | -6.6495e-08 | -6.703e-08 | -6.7557e-08 | -6.8038e-08 | -6.8516e-08 | -6.8957e-08 | -7.6812e-08 | -4.0907e-05 | -5.0008e-05
Test_2 | 3.023e-11 | -1.7011e-08 | -2.2999e-08 | -2.7499e-08 | -3.1234e-08 | -3.449e-08 | -3.739e-08 | -4.002e-08 | -4.243e-08 | -4.4653e-08 | -4.6702e-08 | -4.8604e-08 | -5.0302e-08 | -5.1954e-08 | -5.3483e-08 | -5.4899e-08 | -5.6214e-08 | -5.7456e-08 | -5.8595e-08 | -5.9657e-08 | -6.0639e-08 | -6.1559e-08 | -6.2413e-08 | -6.3211e-08 | -6.3958e-08 | -6.4642e-08 | -6.5299e-08 | -6.5903e-08 | -6.6465e-08 | -6.703e-08 | -6.7518e-08 | -6.8023e-08 | -6.8499e-08 | -6.8949e-08 | -6.9395e-08 | -3.4249e-05 | -5.0009e-05
Chart: 
| 0.0 | -10.0 | -20.0 | -30.0 | -40.0 | -50.0 | -60.0 | -70.0 | -80.0 | -90.0 | -100.0 | -110.0 | -120.0 | -130.0 | -140.0 | -150.0 | -160.0 | -170.0 | -180.0 | -190.0 | -200.0 | -210.0 | -220.0 | -230.0 | -240.0 | -250.0 | -260.0 | -270.0 | -280.0 | -290.0 | -300.0 | -310.0 | -320.0 | -330.0 | -340.0 | -350.0 | -360.0 | -370.0 | -380.0 | -390.0 | -400.0 | -410.0 | -420.0 | -430.0 | -440.0 | -450.0 | -460.0 | -470.0 | -480.0
Total | 3.1622e-10 | -1.7063e-08 | -2.3058e-08 | -2.7573e-08 | -3.1283e-08 | -3.4492e-08 | -3.7473e-08 | -4.0055e-08 | -4.2485e-08 | -4.4731e-08 | -4.6781e-08 | -4.8687e-08 | -5.0444e-08 | -5.208e-08 | -5.3619e-08 | -5.5042e-08 | -5.6202e-08 | -5.7605e-08 | -5.8742e-08 | -5.9796e-08 | -6.0803e-08 | -6.1716e-08 | -6.2577e-08 | -6.3372e-08 | -6.4123e-08 | -6.4837e-08 | -1.7564e-05 | -4.1691e-05 | -7.9606e-05 | -0.0001115 | -0.0001501 | -0.0001897 | -0.0002323 | -0.0002744 | -0.0003169 | -0.0003599 | -0.0004043 | -0.0004468 | -0.0004892 | -0.0005318 | -0.0005751 | -0.0006192 | -0.0006644 | -0.000712 | -0.0007637 | -0.0008195 | -0.0008806 | -0.0009474 | -0.001
Active | 2.9991e-10 | -1.5533e-08 | -2.1014e-08 | -2.4909e-08 | -2.8069e-08 | -3.0723e-08 | -3.3316e-08 | -3.5439e-08 | -3.7498e-08 | -3.9395e-08 | -4.1102e-08 | -4.2699e-08 | -4.4222e-08 | -4.5569e-08 | -4.6823e-08 | -4.7981e-08 | -4.9052e-08 | -5.0048e-08 | -5.0957e-08 | -5.1789e-08 | -5.2556e-08 | -5.326e-08 | -5.3908e-08 | -5.4504e-08 | -5.5047e-08 | -5.5547e-08 | -5.6023e-08 | -5.6535e-08 | -5.7021e-08 | -5.7483e-08 | -5.7926e-08 | -5.8374e-08 | -5.8815e-08 | -5.9259e-08 | -5.9676e-08 | -6.0103e-08 | -6.0525e-08 | -6.0933e-08 | -6.133e-08 | -6.1727e-08 | -6.2141e-08 | -6.2544e-08 | -6.2987e-08 | -6.3448e-08 | -6.3937e-08 | -6.4492e-08 | -6.5051e-08 | -6.5659e-08 | -6.6119e-08

## Slide 2: CV from Novati_FNAL_tests.xlsx
CV curves indicate depletion at 400V, resistivity about 6 kOhm-cm
Does the second structure correspond to GR breakdown?
Chart: 
| 0.0 | -20.0 | -40.0 | -60.0 | -80.0 | -100.0 | -120.0 | -140.0 | -160.0 | -180.0 | -200.0 | -220.0 | -240.0 | -260.0 | -280.0 | -300.0 | -320.0 | -340.0 | -360.0 | -380.0 | -400.0 | -420.0 | -440.0 | -460.0 | -480.0 | -500.0 | -520.0 | -540.0 | -560.0
1/c^2 | 7.0507e+18 | 1.0041e+20 | 1.9327e+20 | 2.8092e+20 | 3.6536e+20 | 4.4593e+20 | 5.2353e+20 | 5.9812e+20 | 6.6792e+20 | 7.3762e+20 | 8.0483e+20 | 8.7035e+20 | 9.3398e+20 | 9.9564e+20 | 1.0564e+21 | 1.1153e+21 | 1.1727e+21 | 1.2286e+21 | 1.2824e+21 | 1.3172e+21 | 1.3277e+21 | 1.3343e+21 | 1.3378e+21 | 1.3424e+21 | 1.3448e+21 | 1.5465e+21 | 1.5591e+21 | 1.5664e+21 | 1.5708e+21
Neff Calc |  |  | 
 | mup= | 502 | cm2/Vs
 | eps= | 11.9 | 
 | eps0= | 8.85419E-14 | F/cm
 | D | 0.05 | cm
 | q0 | 1.60218E-19 | 
 | Vdep | 400 | V
 | Neff | 2.10E+12 | 
 | Resistivity | 5.91E+03 | Ohm-cm

## Slide 3: Silvaco Model of TS edge
Model of edge of test structure 805V
Breakdown beginning?
Rerun with extended
Vbias

## Slide 4: Silvaco Model of TS edge
Model of edge of test structure 605, 805V

## Slide 5: Oxide charge effect
Varied oxide charge from 0, 5e10, 5e11. Breakdown decreases with increasing oxide charge

## Slide 6: Pstop only
P stop + p spray 0 oxide charge
P stop only 0 oxide charge
P stop only 5E10 oxide charge
Guard Currents