## Slide 1
TE-MSC-MDT

## Slide 2: Splicing and Instrumentation Coil 11T #110
TE-MSC-MDT
G. Maury
19 Mai 2015

## Slide 3: Splicing Operation
Interlayer MICA 2x0.25mm
Quench heaters
Soldering with Tin-Lead filler Metal (Sn60P40) and Flux FrontArgen F600
Copper Leads 2x0.2mm

## Slide 4: Difference with other Splicing
Splicing operation on Coil #109
Coil #110 with Interlayer?

## Slide 5: Trace installation on outer layer
Trace 0.15 mm

## Slide 6: Closing impregnation mold
Fiber Glass Type E 0.08mm
No-stick coating 0.08mm

## Slide 7: Mold Opening after impregnation
Opening side down for before!

## Slide 8: Powering leads
Tin-Silver filler Metal (Sn96Ag4) for soft brazing

## Slide 9
TE-MSC-MDT