## Slide 1
Open issues
Schedule

## Slide 2: Open issues
cable geometry (cable width, strand distribution)
stamped tape edge quality  copper plating
impregnation with charged resin
Roebel cable twist
new dummy cable lengths availability ?
  Need for aligned block : 2 x 31 m for Feather-2+ 6 m for Feather-0
  Need for cosine theta : 2 x 20 m for two dummy coils
sc cable delivery ?

## Slide 3: Schedule
Feather zero: assembled after successful impregnation tests. Expected End of summer 2015.
Feather two: detailed design is ongoing, manufacture assembly autumn 2015
Cosine theta : dummy coil autumn 2015
Twist tests to be discussed/planned
Stacked tapes : winding tools design starting this summer

## Slide 4: Twist tests
Tests on Roebel cable twisting are needed
  Sample preparation by CEA
  Tests by KIT ?
Test program to be discussed:
  Pure twist, different configurations :
    angle : 30°, 61°, 77°, 90° (if needed for block design)
    Length : 80 (110 mm, 240 mm)
    Orientation : right or left, over-twisting or untwisting Roebel cable following its orientation
  Cosine theta configuration options
  How many sample per configuration ?
SC cable need
  3-4 m of SC Roebel cable are needed