## Slide 1: Quench protection of Bi-2212 magnets
Tengming Shen
Fermi National Accelerator Laboratory
WAMHTS-3, Lyon, France, Sept 11, 2015
1
Work supported by U.S. DOE-OHEP through a U.S. DOE Early Career Award, and performed in collaboration with my colleagues at Fermilab including Pei Li, Liyang Ye, Dan Assell, and Dan Turrioni, members of BSCCo especially the FSU 2212 group and Arup Ghosh with BNL, and other university and industry partners, especially Justin Schwartz with NCSU.

## Slide 2: Designing a quench protection system depends crucially on knowing:
At what hot spot temperature can a normal zone be detected?
    NZPV at cm/s gives small normal zones with a length of ~10s cm or less
Quench degradation limits of Bi-2212 wires
    What role does stress/strain have?
They determine the time constant of quench protection.
2

## Slide 3: Samples - two 6-layer, epoxy impregnated Bi-2212 solenoids (1 bar HT) made from 1.2 mm OST wire
Coil A: mullite insulation
(~100 mm thick)
Coil B: nGimat/NCSU TiO2 insulation (~22 mm thick)
OST, Φ1.2 mm, 85x18 wire,
3
Pei Li, Dan Assell

## Slide 4: Ic-B of these coils and uniformity of Ic
Coil B@14 T
No electric shorts.
Quite uniform Ic.
Coil A quenched during
Ic measurements.
4
Liyang Ye, Dan Turrioni

## Slide 5: Heater induced quench experiments and temperature measurement
Epoxy heater
Kapton (33 mm thick) separates
heater and coil windings except
the turn to be quenched.
Coils A + B have survived more than 100 quenches without degradation.
5
Liyang Ye

## Slide 6: Coil A: High hot spot temperature is needed to see 0.1 – 1 V for high Jo operation. Strong influence of Jo on quench detection
Coil A – 100 mm mullite insulation
Note: Temperature from voltage measurement, not from TCs. TCs tend to underestimate Tmax when dT/dt>10 K/s.
6
Shen, Ye, Li, Turrioni, Supercond. Sci. Technol. 28 (2015) 075014

## Slide 7
Coil B – 20 mm nGimat TiO2
Coil B: Moderate hot spot temperature is needed to see 0.1 – 1 V. Small influence of Jo on quench detection
Note: Temperature from voltage measurement, not from TCs. TCs tend to underestimate Tmax when dT/dt>10 K/s.

## Slide 8: Dependence of quench degradation limit of Bi-2212 wires on axial stress up to 160 MPa for high critical current density, overpressure processed Bi-2212 wires*
Liyang Ye1,2, Pei Li1, Jan Jaroszynski3, Justin Schwartz2, and
Tengming Shen1
Fermi National Accelerator Laboratory
North Carolina State University
National High Magnetic Field Laboratory
* Will be included in L Ye NCSU PhD thesis work
8
Work was supported by U.S. DOE-OHEP through a U.S. DOE early career award. LY thanks Joint University-Fermilab Doctoral Program in Accelerator Physics and Technology. TS thanks NHMFL for 31 T DC magnet time. Special thanks go to Dan Assell with Fermilab and NHMFL staffs especially Dima Abraimov, Ulf Trociewitz, David Labarlestier.

## Slide 9: Earlier Ye thesis works investigating quench degradation limits and degradation mechanisms provide strong motivation for examining the role of strain state on quench degradation limit
Quench degradation is driven by local straining of 2212 filaments with Tmax limit close to 500 K.
    Irrespective of dTmax/dx, conductor design, heat treatment, porosity levels et al.
    Quenched degraded filaments develop cracks.
    Reversible and irreversible behavior consistent with Jc dependence on Tmax.
How strongly would quench degradation limit depend on axial stress/strain states of conductor?
L. Ye et al., manuscript in final preparation.
Ic-axial strain of Bi-2212 wires (ten Haken and ten Kate,
Cheggour, Godeke)
Reversible

## Slide 10: Ic measurement using ITER barrels – results consistent with standard Ic measurement of short straight samples on G-10 sample holders OP produces high Jc
10
PMM101108-2, 37x18, 0.8 mm,
Nexans’ 521 composition powder
Force pointing inward, hoop stress ≈ 0
With collaborations with Arup Ghosh@BNL
Ye, Li, Ghosh, Shen, ICMC2015, poster

## Slide 11: Determining axial stress limit using ITER barrels
11
5% Ic degradation at 156 MPa @4.2K and 15 T for 25 bar OP PMM101108-2
Force pointing outward
Hoop stress ≈ BJR

## Slide 12: Dependence of quench degradation temperature limit on axial stress up to 145 MPa in a 25 bar OP Bi-2212 wire at 4.2 K in field of 15-30 T
12
4.2K, 15T
Decreasing from 500 K at zero hoop stress to ~150 K with increasing hoop stress to 146 MPa at 4.2 K and 15 T

## Slide 13: Summary
For 2212/HTS magnets, hot spot temperature at which a normal zone can be detected depends strongly on voltage detection criterion, operating current density, and fabrication methods such as insulation used
    So is quench detection and protection
    Many other implications such as thin insulation or non-insulation winding method that promote 3-D propagation are strongly encouraged.
Quench degradation temperature limit for Bi-2212 wires.
    Strongly depends on the axial stress/strain states.
    >500 K when not stressed, 320 K with 100 MPa axial stress, 160 K with 140 MPa axial stress. Axial stress limit~156 MPa for a high Jc OP wire.
    Good news for dipole magnets.
13