## Slide 1
Roebel cables for EuCARD²:
experience and options.
A. Kario, S. Otten, A. Kling, A. Jung, B. Runtsch, R. Nast, W. Goldacker
Institute for Technical Physics, Karlsruhe Institute of Technology, Karlsruhe

## Slide 2
Recipe for the ’’good’’ Roebel cable:
Ingredients: EuCARD2 coated conductor material. Punching vs. tape homogeneity.
2. Directions: Punch and coat.
3. Outcome: Roebel cable geometry.

## Slide 3
Recipe for the ’’good’’ Roebel cable:
Ingredients: EuCARD2 coated conductor material. Punching vs. tape homogeneity.
2. Directions: Punch and coat.
3. Outcome: Roebel cable geometry.

## Slide 4
Coated conductors performance at 4.2 K:
Target performance for RE123 tape at 4.2 K perpendicular magnetic field:
Jeng = 450 A/mm2 at 15 T
Jeng = 400 A/mm2 – 600 A/mm2 at 20 T
C. Senatore, C. Barth, M. Bonura, G. Mondonico, M. Kulich, 1st Workshop on Accelerator Magnets in HTS, DESY, 21 - 23 May 2014.

## Slide 5
Tape architectures – macroscopically (sketch):
Bruker
Cu 20 µm
REBCO 1-3 µm
Hastelloy 60 µm
Cu 20 µm
Cu 20 µm
REBCO 1-3 µm
Steinless Steel 100 µm
Cu 20 µm
SuperOx, SuNAM
Cu 20 µm
REBCO 1-3 µm
Hastelloy 50, 30 µm
Cu 20 µm
SuperPower
Cu 20 µm
REBCO 3-6 µm
Hastelloy 75 µm
Fujikura
Tape Width 12 – 12.3 mm.
Tape Thickness 0.1 - 0.2 mm.
Stabilizing copper layer technology.
electroplating
electroplating
electroplating
laminate
REBCO 3-6 µm
Cu 20 µm
electroplating
Cu 20 µm
Hastelloy 75 µm

## Slide 6
The critical current is measured before and after punching (T = 77 K, self-field)
Chart: Critical current per unit width
| 1-8 | 1-2 | 2-3 | 3-4 | 4-5 | 5-6 | 6-7 | 7-8
Before punching | 9.925 | 9.9333 | 10.25 | 10.0833 | 9.5083 | 10.2667 | 9.9917 | 10.2583
After punching | 8.8545 | 9.6364 | 9.3636 | 9.2727 | 9.4727 | 9 | 7.1 | 9.7091
Chart: n-value
| 1-8 | 1-2 | 2-3 | 3-4 | 4-5 | 5-6 | 6-7 | 7-8
Before punching | 27.7 | 26.8 | 27.6 | 27.5 | 29.1 | 28.5 | 27.7 | 28.3
After punching | 16.4 | 24.5 | 23.8 | 23.8 | 25.6 | 22.2 | 10.1 | 25.9
The critical current degraded by 9% percent on average over the different segments.
The cause of this defect was found to be the excessive tape width of 12.26 mm. The punching tool is suitable only for widths up to 12.1 mm.
A. Usoskin, A. Rutt: Bruker tape provided in frame of EuCARD2 project.
Punching defect due to tape being wider than
specified:

## Slide 7
The punching tool was modified to accommodate tape widths up to 12.4 mm, and the punching test was repeated on a new sample.
Chart: Critical current per unit width
| 1-8 | 1-2 | 2-3 | 3-4 | 4-5 | 5-6 | 6-7 | 7-8
Before punching | 9.35 | 9.6083 | 9.4833 | 9.5917 | 8.9 | 9.525 | 9.6417 | 9.3833
After punching | 9.1455 | 9.4727 | 9.4909 | 9.4727 | 8.5818 | 9.4364 | 9.4364 | 9.3091
The average degradation of the segments was low at 1.4%, and there were no visible punching defect as in the previous sample.
A. Usoskin, A. Rutt: Bruker tape provided in frame of EuCARD2 project.
Successful punching after tool modification:
56 μm
68 μm
88 μm
26 μm
16 μm
113μm

## Slide 8
Tape edge after punching process with smeared Cu:
Cu
Hastelloy
Punching direction
REBCO
REBCO
Hastelloy
Cu
Punching direction
Cu
Hastelloy
Punching direction
Cu
Stainess Steel
YBCO
20 µm
20 µm
20 µm

## Slide 9
Non-planarity and delamination and after punching:
5.5 mm
16 mm
5 mm
16 mm
Delamination examples:
Non planarity and punching defect:
Side view of the 12 mm Bruker tape
5.5 mm
12 mm
A. Usoskin, A. Rutt: Bruker tape provided in frame of EuCARD2 project.

## Slide 10
Microscopically - linear defects:
D.J. Miller et al.,
http://www.superpower-inc.com/files/
2006_ASC+4MI12+ANL+Poster.pdf
12 mm width
across tape
Ag cap
42.7 mT
50 K
12 mm width
across tape
Ag cap
10 filaments
42.7 mT
50 K
Laser grooves

## Slide 11
Recipe for the ’’good’’ Roebel cable:
Ingredients: EuCARD2 coated conductor material. Punching vs. tape homogeneity.
2. Directions: Punch and coat.
3. Outcome: Roebel cable geometry.

## Slide 12
20 µm
The average critical current per unit width degraded by 6% after punching and copper plating. Stinless steel
No local defects were found.
A. Usoskin, A. Rutt: Bruker tape provided in frame of EuCARD2 project.
Cu-plated tape after punching - Bruker:
181 µm
207 µm
185 µm
176 µm
185 µm
188 µm
176 µm
181 µm
176 µm
202 µm
Stainless Steel
Cu
Ag
punching burr
width of this Cu plated tape is 5.46-5.67 mm and thickness 175 µm
Chart: Critical current per unit width
| 1-10 | 1-2 | 2-3 | 3-4 | 4-5 | 5-6 | 6-7 | 7-8 | 8-9 | 9-10
Before punching | 10.7917 | 10.8 | 11.1167 | 10.9583 | 10.8083 | 10.2833 | 10.9083 | 10.8833 | 10.9417 | 10.8333
After punching | 10.2364 | 10.2182 | 10.6545 | 10.2727 | 10.3091 | 9.7455 | 10.4727 | 10.1455 | 10.4364 | 10.4
After copper plating | 9.8545 | 10.1818 | 10.5273 | 10.1273 | 10.0909 | 9.4 | 10.4 | 10.1273 | 10.4727 | 10.3091

## Slide 13
Cu-plated tape after punching - SuperOx:
Thickness of Cu plated tape between 115 µm - 131 µm
Hastelloy
Cu
Ag
punching burr
10 µm
28 µm
70 µm
131 µm
10 µm
121 µm
121 µm
121 µm
119 µm
117 µm
114 µm
118 µm
115 µm
No dog-bone effect.
Cu layer homogeneous across and along the tape.
A. Molodyk, SuperOx, tape provided in frame of collaboration.

## Slide 14
Recipe for the ’’good’’ Roebel cable:
Ingredients: EuCARD2 coated conductor material. Punching vs. tape homogeneity.
2. Directions: Punch and coat.
3. Outcome: Roebel cable geometry.

## Slide 15
Roebel geometry parameters:
Wl = 5.5
Wc = 5.5
Ri= 10
Tp = 126, 226, 426
α
Horizontal gap
Vertical gap
Search for optimal geometry with good alignment of the strands in the cable…

## Slide 16
Roebel enclosed between two 12 mm tapes:
Roebel dummy cable cross-section
126 mm transposition length
10 strands
0.4 mm x 1 mm central space
Roebel strands
12 mm Stainless steel tapes
Roebel dummy enclosed between two 12 mm stainless steel tapes.
Strands pressed together.
Homogeneously filled central Roebel gap with filled epoxy resin.
Vertical gap

## Slide 17
Roebel central space insert – rectangular smaller than central space:
1 mm
1 mm
1 mm
0.9 mm
0.6 mm
The 12 mm cable, 15 strands, 226 mm transposition length.
Insert is twisting when inserted, it was added after cabling procedure.

## Slide 18
1079 µm
924 µm
795 µm
800 µm
1059 µm
1084 µm
Roebel dummy with 15 strands
Transposition length: 226 mm
Core was rolled using 0.8 mm wire
It was done with Turk head rolling machine
Inserted into cable after cabling
Roebel central space insert – rectangular filling central space:

## Slide 19
318 µm
340 µm
514 µm
534 µm
Maximum 7 strands
Vertical space: 0.3 mm
Roebel with reduced central space – changed
strand geometry:
Wl = 5.9
Wc = 5.9
Ri= 10
Tp = 126
α

## Slide 20
Roebel with reduced central space – changed
strand geometry:
Wl = 5.9
Wc = 5.9
Ri= 10
Tp = 226
α
Maximum 14 strands
Vertical space: 0.12 -0.3 mm
686 µm
897 µm
200 µm
200 µm

## Slide 21
For racetrack type coil winding horizontal gap is important parameter:
CEA – Saclay: increasing of horizontal gap
Pictures by courtesy of M. Durante, C. Lorin.
Transposition length ~ 350 mm with 5.9 mm wide strands result in 7 mm distance between strands.

## Slide 22
Quality of punching depends on tape properties:
Coated conductor macroscopic homogeneity - tape planarity and constant
width of the tape.
Microscopic defects in the tape.
Quality of punching influences properties of cable:
Punching tool for specific tape – tape thickness, material (substrate and stabilization).
Punching tool length = transposition.
Tool control (wear off).
Cable geometry:
Should be adjusted to coil design.
Recipe for the ’’good’’ Roebel cable: