## Slide 1: EuCARD-2 baseline design: Aligned block design status (Feather M0/M2)
Glyn Kirby – CERN

## Slide 2: Over view
Feather2
Dummy and Real cable
Design 3d model
Philosophy
FEA 2d And 3D
Winding development
Jointing tests.
Impregnation
Instrumentation
  Spot heaters
  Quench detection using temperature
Cable geometry , internal support.
Drawing Complex shapes tolerances costs
Tooling
Field quality

## Slide 3: Roebel Real & Dummy stainless steel, Copper plated, cables
CERN 2m chemically cut dummy tapes hand assembled cables
KIT. longer lengths 20-30 m Punched tapes semiautomatic assembly.
SuperOx provided a demonstration length of Robel cable with ReBCO tapes.
General Cable Superconductors Limited (“GCS”) 2 x34m dummy Cu plated stst cable.
Thanks to Nick Long cable GCS NZ.
CERN
GCS NZ

## Slide 4: Feather2 the starting idea's

## Slide 5: Feather 2
Baseline design

## Slide 6: Complex , early designs ,

## Slide 7: Coil idea

## Slide 8: Fresca2
Don’t touch the
100 mm aperture

## Slide 9: High field support for Feather2

## Slide 10: Philosophy leaning against wall.
REBCO

## Slide 11
(REMEMBER: Transverse limit on cable 253 MPa)
Transversally compressive peak stress on coil (X)
≈ 170 MPa
Feather2 FEA 20Tesla coil stress under control 170 / 253 MPa
99.0 mm outer dia of Feather2
Coil stress 170 MPa @ 20 Tesla
Coil deflection 270 um
Outer support tube deflection 120 um
Uniform Je over coils

## Slide 12
O X:
0.12 mm
O X: 0.27 mm
O X: -0.19 mm
O X: -0.06 mm
mm
O X: 0.14 mm
O X: -0.10 mm
FEATHER M2 2D Total deformation vector plot, Cool down + powering 9kA + 16 T background field ≈ 20 T in the bore
Safe factor we can allow radial play of 0.5 mm

## Slide 13: Drawing complex shapes

## Slide 14: Flared ends

## Slide 15: 3D Printed former to test flared end

## Slide 16: Hard-way bend of Roebel cable, test wind on printed former

## Slide 18: Dummy cable tests , Fixing the hard way bend

## Slide 19: Test winding developing the tooling

## Slide 21: Layer Jump cover
3D printed Mould to for manufacture of GRP layer jump covers

## Slide 22: Jacky Mazet
Big thank you to Jacky our lead tech.

## Slide 23: One joint end design,

## Slide 24: Joint between poles
Copper Heat exchanger
tape joints

## Slide 25: Joint tests

## Slide 26: Aligned block Feather0, development foe Eucard2 5-20T
~1000 m REBCO tape
~70 m of cable
~100 m REBCO tape
~6 m of cable

## Slide 27: Feather 0 FEA,
Feather zero Finite element analysis of magnet assembly, cool down and powering in 10 Tesla background field. magnified coil pack deformation during powering, 3.6 micron deflection.

## Slide 28: First impregnation, bucket “open mould design”

## Slide 29: Closed mould design

## Slide 30: Short cable, so added one extra cable.
Feather zero needs 6 m of cable but the first real REBCO cable that we have is 5 m. So we tested adding a dummy cable to test assembly.
Extra dummy cable

## Slide 31: Spacer extra turn

## Slide 32: Cable geometry
Individual tapes can be transversely up to 200 um out of position!
And tape cross overs vary by the available gap.
Section through part of Feather0 dummy stst coil

## Slide 33: Cable impregnation
Thanks to Stephane Langeslag for the sample preparation for the cable images
Above filed resin CTD101G test

## Slide 34: Cable support

## Slide 35: Internal cable supports, to add with tape positioning
Two possible solutions have been foreseen to hold the tapes in the correct geometry:
Bracelets that wraparound each side individually.
Or
2) Two independent tapes woven into the cable .
The solutions also adds with supporting the cable during handballing.
Provisional European patent application is EP15179513.5.

## Slide 36: Feather0

## Slide 37: Feather 0

## Slide 38: Feather 0 removal from impregnation mould

## Slide 39: Measurement and Analysis of AC-loss in ReBCO Roebel Cables
Jeroen Van Nugteren

## Slide 40: Measured at the Universities of Twente & Southampton
Loads of beautiful data as function of temperature
Harder to compare since Jc dependence on temperature in model not so accurate (not measured
Transient heating seen as expected.

## Slide 41: Modelling of Current distribution in cable
Magnetisation in cable displayed only one tape
But all tapes are powered.
Feather2 in 16T background field
Current ins only flowing at the edges of the tapes

## Slide 42: Dynamic Field quality
  “b3, 60 unit’s variation at low field
  reducing to < 20 units at high field.
  b5 and b7 we see ~ 10 units variation,
  then converge to low values at high field.”*
First simulation give b3 , 3units at low field
Decreasing at high field 20 T
However modelling assumption assume perfect cable geometry and zero thickened REBCO layer (reality 0.001mm)
Aligned Block design
Cos theta design

## Slide 43: External field for EuCARD2 HTS magnets CERN/CEA Fresca2 and HL-LHC KEK D1
Test station Fresca 2 under construction
Test assembly fresca2
Fresca2 reacted Nb3Sn coil
Thanks to Tatsu @ KEK for the images
Fresca2 | 13 -16 Tesla | 100 mm aperture
D1 KEK | 5 - 6 Tesla | 150 mm aperture
Fresca2
D1
D1

## Slide 44: Spot heater, square wave pulse,

## Slide 45: Quench Detection
HTS is very different to LTS when it comes to quench behavior.
Minimal Quench Energy is high (stable)
  Normal Zone Propagation Velocity is low (hard to detect)
  Roebel cable 15 tapes!
Also due to the alignment of the blocks the operating current density can be very high (> 600 A/mm in block)
Feather zero will test
  Voltage taps
  Pickup-coils
  Temperature sensor array
  Acoustics
  Optics Fiber
Mr. voltage tap
Optics
Hall
Acoustic
NI-DAQ
Pickup Coils
[1] J. van Nugteren, “Normal Zone Propagation in a YBCO Superconducting Tape”, graduation thesis University of Twente, 2012
Temp sensor array

## Slide 46: Acoustics
Thanks to Maxim,
M. Marchevsky et al. “Acoustic emission during quench training of superconducting accelerator magnets” Cryogenics 69 (2015) 50–57

## Slide 47: Quench analysis
Thanks to : Erkki Härö, Tiina Salmi, Antti Stenvall
At 4.2 K and 7100 A, the minimum temperature margin is 8.6 K, the lowest margin is there where the field is the most perpendicular to the cable
The blue volumes.

## Slide 48
Chart: Polynomial fit for temperature sensor CCS A2 N 301
| 4.126790655899402 | 4.292156774383455 | 4.47430268465695 | 4.675890288483789 | 4.900174977375805 | 5.15117937942493 | 5.433929920377948 | 5.75478298100964 | 6.12188051314991 | 6.545795251370306 | 7.040457539222809 | 7.624506692390526 | 8.323292417877082 | 9.171888153265627 | 10.21970742346668 | 11.53770736096036 | 13.22985184441931 | 15.45173985287267 | 18.44156905648623 | 22.57287589832359 | 28.44678943151375 | 37.0581752832095
 | 3580 | 3480 | 3380 | 3280 | 3180 | 3080 | 2980 | 2880 | 2780 | 2680 | 2580 | 2480 | 2380 | 2280 | 2180 | 2080 | 1980 | 1880 | 1780 | 1680 | 1580 | 1480
Iin
Iout
V
Ueq
Spot heater
Sensor + Thermal grease
Temperature sensor array quench detection

## Slide 49: Tests to select spacing between temp sensors

## Slide 50: CCS temp sensors

## Slide 51: Fibers mounted in Feather zero

## Slide 52
FBG: longitudinal periodic variation of the refractive index in the optical fiber core
FBG temperature sensitivity
8 - 12 pm/K @ room T
< 0.1 pm/K below 40 K
Bare FBG no suitable for cryogenic temperature!
Zhang H. et al. Development of Strain Measurement in Superconducting Magnet Through Fiber Bragg Grating, IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 18, NO. 2, JUNE 2008;
Fiber optic sensors based on Fiber Bragg Grating technology
Bare FBG
Coated/Embedded FBG
DlB (T, e)
Cladding
Core
Broadband light
Host materials improve the sensitivity at cryogenic temperature
Variation of the reflected lB with changes in e and T

## Slide 54
CLIQ – Coupling-Loss Induced Quench (EU Patent EP13174323.9, June 2013)
EU Patent EP13174323.9, June 2013.
G. Kirby,V. Datskov, E. Ravaioli,
QXF IR HL LHC
CLIQ test on LHC dipole
E. Ravaioli, "CLIQ", PhD thesis University of Twente, 2015. http://doc.utwente.nl/96069/

## Slide 55: Protection: Coupling Loss Induced Quench applied to HTS
Quench heater are too slow for HTS cable in Feather2
We hope to detect and turn off before quench.
CLIQ simulation for long magnet 5 m long , 16T HTS coil gives rapid quench 2ms quench the cross over tapes full coil on 20 ms.
Promising result if we protect by quenching?
2 ms in to a CLIQ pulse tape cross overs are normal.
Hysteresis losses

## Slide 56: Planning

## Slide 57: Conclusion
Modelling of the current in the REBCO tapes and cable has given unexpected good outlook on achieving future good dynamic field quality.
  We will start on fin-tuning coil design, now that we have good working model with current distribution.
First Feather zero coils have been wound and impregnated. More tests to come!
Feather2 development coil test winding started.
  Need good impregnation system
  Need to test joint designs.
Feather2 design advanced! Ordering parts.

## Slide 58: The End
Thankyou for your attention
VERY close to the first
Accelerator type HTS magnet

## Slide 59: 3 spot heaters impregnated into Feather coil
On top of straight section
On wide face of straight section
Inner wide face at end