## Slide 1: HTS magnet quench criteria
3rd Workshop on Accelerator Magnets in HTS (WAMHTS-3)
thibault.lecrevisse@cea.fr
September, 11th 2015

## Slide 2: Overview
Physics of a Quench
  Principle
  “Danger”
  Issue with HTS
HTS Quench protection criteria
  Heat balance and adiabatic hot spot
  “quench capital” vs “quench tax”
  Increase the quench capital
  Lower the quench tax :
    Fast detection
    Accelerate the dump
    Winding adaptation
Conclusion

## Slide 3: Physics of quench: Principe
Definition of a quench: resistive transition in a superconducting magnet leading to appearance of voltage, temperature increase, thermal and electromagnetic forces (and cryogen expulsion).
current sharing
Tcs<T<Tc
Stabilizer
Superconductor
T<Tcs
quenched
T>Tc
HTS resistivity over Tc
Tcs,REBCO: 5-92 K
Tc,REBCO: 92 K

## Slide 4: Physics of quench: “Danger”
Not a problem up to ~ 40 T if it happen uniformly in all the winding.
(REBCO tape from 4 K to 300 K : Em= 7·108 J/m3 Bmax = 41 T)
BUT : it does not happen uniformly (low quench velocity) and less than 1 % of the total magnet mass might absorb the total energy  large damage potential
Why is it a problem ?
The magnetic energy is transformed in heating through the resistive volume
is converted in
L
Rq
V
+
-
BSCO impregnated pancake, by courtesy of P. Tixador and A. Badel
REBCO dry wound coil
S. Matsumoto et al., IEEE Trans. Appl. Supercond., vol. 22, no. 3, pp. 9501604, June 2012

## Slide 5: Physics of quench: “Danger”
A 0.5 T / 773-mm Cold Bore MgB2 Magnet
(FBML, 2007)
An unscheduled quench (top coil)
 Permanent damage
MgB2 coil, by courtesy of Yukikazu Iwasa (FBML, 2007)

## Slide 6: Physics of quench: Issue with HTS
Issue with HTS:
Very low quench propagation in a winding typical few tens of mm/s (2-3 order of magnitude lower than LTS)  Small volume dissipating Em
 Need an Active protection or another dumping method.
4.2 K; 17 T; 196 A (515 A/mm²) :
T. Lécrevisse et al., IEEE Trans. Appl. Supercond., vol. 23, no. 3, June 2013
Y. Miyoshi et al., IEEE Trans. Appl. Supercond., vol. 25, no. 3, June 2015
10 K; 8 T; 280 A (286 A/mm²) :

## Slide 7
Issues to be considered (LTS/HTS):
Temperature increase and temperature gradients (thermal stresses)
Voltages within the magnet, and from magnet to ground (whole circuit)
Forces caused by thermal and electromagnetic loads during the magnet discharge transient
Cryogen pressure increase and expulsion (liquid cooling)
A quench invariably requires detection and, in case of HTS, definitively needs actions to safely turn-off the power supply and discharge the magnet.
Physics of quench: Issue with HTS

## Slide 8: HTS Quench protection criteria: Heat balance and adiabatic hot spot
Thot-spot : < 200 K, Safe ; <300 K, risky ; >300 K, very risky (*, pp.470)
Heat equation (*, pp. 352):
Conductor’s thermal energy
Thermal conduction into the conductor
Joule heating
non-Joule heat generation
Cooling by cryogen
adiabatic heat balance (simplest and conservative approach) :
Average heat capacity
Average resistivity
*Yukikazu Iwasa, Case Studies in Superconducting Magnets, Second Edition, Springer, 2009

## Slide 9: HTS Quench protection criteria: “quench capital” vs “quench tax”
Can be integrated:
(or Z(Top, Tmax)):
“Quench Capital”*
(conductor/winding property)
“Quench Tax”*
(circuit linked)
* L. Bottura, Magnet Quench 101, WAMSDO CERN proceedings 2013

## Slide 10: HTS Quench protection criteria: “quench capital” vs “quench tax”
“Quench Capital”*
(conductor/winding property)
“Quench Tax”*
(circuit linked)
- Winding (shunt ratio)
- Materials
what tquench?
 Detection
 Protection
Enhance the protection by either increasing the quench capital and/or lowering the quench tax.

## Slide 11: HTS Quench protection criteria: Increase the quench capital
Issue:
Lower  lower voltage (increase tdetection)
Lower the resistivity
Add more shunt
Use purer materials
Quench Capital
L. Bottura, Magnet Quench 101, WAMSDO CERN presentation

## Slide 12
Increasing the quench capital by adding some low resistance shunt
Simulation (SCS4050-AP with 2x20 µm Cu)
If only adiabatic longitudinal propagation: 4.2 K, 14 T (// ab), 340 A/mm²
Voltage at Thot-spot= 250 K > 200 mV
Time at Thot-spot= 250 K > 400 ms
T. Lécrevisse et al., IEEE Trans. Appl. Supercond., vol. 23, no. 3, June 2013
Vdetection?
tdetection?
tdump?
HTS Quench protection criteria: Increase the quench capital
OK but are we able to detect and dump in 400-800 ms?
(Quench Tax)

## Slide 13: HTS Quench protection criteria: protection enhancement by lower the “quench tax”
Constant external dump:
PS
Rdump
Rquench
L
Protection can be enhanced by:
a fast detection
a large Rdump (but limited by Vmax)
a low inductance (HTS cables)

## Slide 14: HTS Quench protection criteria: Fast detection
Simulation (SCS4050-AP with 2x20 µm Cu)
SCS4050-AP, 4.2 K, 14 T (// ab), 150 µm Cu added, 20 µm Mylar insulation, 340 A/mm²
t250K, pancake = 0 ms
tdetection, 20mV = 100 ms
tdetection, 50mV = 250 ms
tdump/2 ~620-770 ms (pancake 50 mV-20 mV)
tdelay= 10 ms ; tswitch= 30 ms
Improve the turn to turn thermal contact *  increase the voltage
Develop fast detection system
Be careful: Simulation is a very simple case (same // field, same Ic, adiabatic, …)
250 K is an high Thot-spot for protection
T. Lécrevisse et al., IEEE Trans. Appl. Supercond., vol. 23, no. 3, June 2013
* H. Bai et al., IEEE Trans. Appl. Supercond., vol. 23, no. 3, June 2013

## Slide 15: HTS Quench protection criteria: Accelerate the dump
Active Protection Heaters (NHMFL)
32 T magnet : 52 disks
fheater~45 %
Pheater=50 kW
heating time : ~0.8 s
quench delay: ~0.1-0.6 s
H.W., Weijers et al., IEEE Trans. Appl. Supercond., vol. 24, no. 3, pp. 1-5, June 2014
Variable Rdump (EUCARD HTS insert study)
E. Haro et al., IEEE Trans. Appl. Supercond., vol. 23, no. 3,
pp. 4600104, June 2013

## Slide 16: HTS Quench protection criteria: Winding adaptation
No-Insulation Multi-Width: self-protection
When a quench occurs in DP9 (, all DPs quenched in ms.
All Energy (> 30 kJ) is discharged under constant voltage mode (PS limitation) in
NO protection, NO damage.
Y. Song et al., "Over-Current Quench Test and Self-Protecting Behavior of a 7-T / 78-mm Multi-Width No-Insulation REBCO Magnet at 4.2 K," to be published in Supercond. Sci. Technol., 2015.
T. Lécrevisse, Y. Iwasa, “A(RE)BCO Pancake Winding With Metal-as-Insulation”, presented at EUCAS2015
Metal tape co-wound with REBCO tape during a quench at 77 K, PS constant voltage mode.
Metal-as-Insulation

## Slide 17: Conclusion
HTS magnet can be protected BUT it is not so easy:
  Key issue remains the detection : What is the most efficient method to detect a quench? How to increase the voltage/NPZV * ?
  Once detected, energy dump ( can be done.
  Low inductance is for a better protection.
  What protection scheme suitable ? Dump ; heaters ; subdivision …
Winding might be optimized for the protection:
  Stabilizer ratio and properties
  Insulation
  New winding with No, Partial, or Metal-as-Insulation: allows the current to bypass the hot-spot  lower Thot-spot and higher quench capital (higher tquench).
    See S. Hahn presentation on NI technique tomorrow
* C. Lacroix and F. Sirois, “concept of a current flow diverter for accelerating the normal zone propagation velocity in 2G HTS coated conductors,” vol. 27, 035003 (10pp), 2014

## Slide 19
Thank You

## Slide 20
Back-up slides

## Slide 21
NI-MW
Constant voltage mode
Protection by :
Bypassing current
PS constant voltage mode
BUT : low resistance and still high current
 need to shut down the PS (not an issue)

## Slide 22
NI-MI
Over-current behavior
Below Ic :
low (NI) and almost no (MI) IR.
beginning of Field saturation (NI)
NI near and over Ic:
IR increase (over 0.5·Icoil at 2.2·Ic)
“Low” voltage
MI quench at “low” over current:
Quench at about 1.06·Ic
No Field saturation up to the quench.
almost no (MI) IR

## Slide 23
Metal-as-Insulation

## Slide 24
Metal-as-Insulation

## Slide 25
Metal-as-Insulation
Voltage name | Turns number | Conductor length [cm]
Radm8 (inner part) | 40 | 709
Radm7 | 40 | 863
Radm6 | 30 | 748
Radm5 | 20 | 547
Radm4 | 5 | 143
Radm3 | 5 | 145
Radm2 | 5 | 147
Radm1 | 4 | 120
Heated Turn | 1 | 30
RadP1 | 10 | 307
RadP2 | 30 | 978
RadP3 (outer part) | 16.5 | 575
Coil | 206.5 | 5312

## Slide 26
Metal-as-Insulation
T. Lécrevisse, Y. Iwasa, “A(RE)BCO Pancake Winding With Metal-as-Insulation”, presented at EUCAS2015