## Slide 1: MQXF Coil Fabrication: Observations and Summary
E.F. Holik
Acknowledgements: G. Ambrosio, M. Anerella, R. Bossert, N. Bourcey, E. Cavanna, D. Cheng, D. R. Dietderich, P. Ferracin, A. K. Ghosh, S. Izquierdo Bermudez, S. Krave, A. Nobrega, J. C. Perez, I. Pong, E. Rochepault, G. L. Sabbi, C. Santini, J. Schmalzle, and M. Yu

## Slide 2: Outline
Coil Fabrication Summary & Overview
Coil size and asymmetry
Cable Expansion / Gap Closure
Cross Section Analysis
Conclusion

## Slide 3: MQXF Coil Overview
6 short coils with 108/127 RRP
  Coil 01 – R&I @ BNL, leaky valve impregnation, was cut
  Coil 02 – R&I @FNAL, Mirror, 91% SSL @4.2K, Ta ternary
  Coil 03 – R&I @ BNL, coil in MQXFS01-AS
  Coil 04 – R @ LBNL, Reversed end parts, Not impregnated…
  Coil 05 – R&I @ BNL, coil in MQXFS01-AS
  Coil 06 – R&I @ FNAL, Spare, Slight epoxy voids near LE
LARP is beginning MQXF 2nd gen
  Coil 07 – Winding beginning this week, (108/127 RRP)
  Coils 09 & 10 in queue – 144/169 RRP
3 long coils in fabrication
  Long Coil 01 – Reacted @ BNL, prep for Impreg, For long mirror.
  Long Coil 01p – R&I @ FNAL, Test for 2nd gen radial insulation.
  Long Coil 02 – L1 cured, Spare for mirror and first long magnet.

## Slide 4: Coil DRs
Bubbles in Practice Coil 1
Reversed End Parts in Coil #4
Parts mislabeled by Plasma coating company. Coil Electrically sound.
Epoxy line valve leaked under vacuum.
Image from Keyence Laser Confocal Microscope

## Slide 5: Coil DRs
Weak Impregnation in Coils #2 and #6 near LE
Epoxy Overflow
Epoxy inlet
Channel will be filled in subsequent coils.
No adverse effects from Mirror Test
‘Racetracking’… Epoxy goes through side channel and fills overflow before filling coil, trapping some air in the process

## Slide 6: Impregnation
 | LBNL | FNAL | BNL
CTD-101k density = 1.03 g/cc | CTD-101k | CTD-101k | CTD-101k
SETUP |  |  | 
Backout temperature | 110°C | 55°C (80°C possible) (110°C with strip heaters) | 110°C
Bakeout pressure | 10 - 100 mT | 25 mT | 200 - 500 mT
Bakeout time | 6 hrs | 45 hrs | 8 hrs
Dryout Gas flow | none | none | none
Cool down temperature | 60°C | 55°C | 55°C
Coil Orientation | ~30° wrt horiz. | ~13° wrt horiz. | Vertical
Lead Orientation | Leads up | Leads up | Leads up
EPOXY DEGAS |  |  | 
Epoxy Volume mixed (1.7 l needed) |  | 22 liters (6 gal.) | 
Epoxy degas temperature | 50°C - 60°C | ? | 55°C
Epoxy degas time | ? | 45 min (2h tot mix/heat) | 2 h
Epoxy agitation while degassing | Y | Y | Y
Epoxy Vacuum while agitating | 300 mTorr | 800 mT | 500 mT
Epoxy container depth | ? | 18" | 3.25"
IMPREGNATION |  |  | 
Initial magnet temperature | 60°C | 55°C | 55°C
VPI coil vessel pressure | 1000 mT | 2000 mT | 500 mT
VPI epoxy vessel pressure | 760 Torr | 760 Torr | 760 Torr
Feed method | pressure diff. | pressure diff. | Peristaltic pump/ΔP
Flow measure method | none | visual (1 cm/s) | pump output
Epoxy flow rate | n/a | 7 cc/min | 25 cc/min
Fill time (short coil) | 1.5 h | 1.5 h - 3 h | 2 h
Gel / Soak |  |  | 
Additional Epoxy Through Flow | 30 min (line reservoir) | 30 min (line resevoir) | none
Backfill (re-absorption) | 1"-2" of large tube (~1/10 l [QXF equivalent]) | 2'-4' of tube (~1/3 liter) | n/a
Epoxy Inlet Valve | Closed | Closed | Open
Epoxy Outlet Valve | Open | Open | Closed
Press/Vac cycles (milking) | 2 | 0 | 0
VPI Vessel Pressure | 760 Torr | 760 Torr | 500 mTorr
Coil Back pressure | 760 Torr | 760 Torr | 760 Torr
Soak/Gel time @ 50°C - 60°C | 15 h | 18 h | 16 h
CURE |  |  | 
VPI Vessel Pressure | 760 Torr | 760 Torr | 500 mTorr
Coil Back pressure | 760 Torr | 760 Torr | 760 Torr
Ramp | 60°C - 110°C (4 h) | 60°C - 110°C (1.5 h) | 55°C - 110°C (6 h)
Soak | 110°C (4 h) | 110°C (5 h) | 110°C (5 h)
Ramp | 110°C - 125°C (4 h) | 110°C - 125°C (1 h) | 110°C - 125°C (1.5 h)
Soak | 125°C (17 h) | 125°C (16 h) | 125°C (16 h)
How does the CERN process differ from the LARP labs?

## Slide 7: 1st Gen Long Coil Fab
Roped Cable in MQXFP 01 (mirror coil).
Additional Insulation in MQXFP 01b practice coil
RXN complete
Additional Radial Insulation to mimic 2nd Gen QXF
Insulation was removed and the cable was placed back in registration.
Insulation repaired with 75 µm E-glass half wrap

## Slide 8: Coil Heat Treatment
47 hr
51.6 hr
50 hr target
48 hr target
47.8 hr
41.6 hr Equivalent
48 hr target
72 hr target
66.3 hr
50.4 hr Equivalent
Position of the thermocouple in block 5, 16 and 28.
Equivalent duration takes into account the estimated lag time.
Multiple TCs locations were tested recently by N. Bourcey for precise measurement of lag time.
CERN TC LARP TC

## Slide 9: Outline
Coil Fabrication Summary & Overview
Coil size and asymmetry
Cable Expansion / Gap Closure
Cross Section Analysis
Conclusion

## Slide 10: Coil Asymmetry and Size
Coils Best fit on the OD and coil Keyway.
Coil Size = L + R = -237 µm
Coil Asymmetry = L – R = +71 µm
10/30/2015 – E. Holik – FNAL
-154 µm
-83 µm
Left Side
Right Side
MQXFS Coil 2 816 mm from LE

## Slide 11: Coil Asymmetry and Size
L – R < 100 µm for < 1 unit a4, a3
L + R < 50 µm for < 1 unit a3, a6
How might coil size and asymmetry create undesired preload??? To be explored…
L – R
L + R
CERN
LARP

## Slide 12: Improving Coil Asymmetry
Size and Asymmetry is Tooling Dominated.
Add shim between form and mandrel blocks to account for tolerance buildup and create intimate contact between tooling components
Fabricate additional modified form blocks and select blocks that are ~15 µm within center.

## Slide 13: Outline
Coil Fabrication Summary & Overview
Coil size and asymmetry
Cable Expansion / Gap Closure
Cross Section Analysis
Conclusion

## Slide 14: Accommodating Expansion
Chart: CERN coils LARP coils
| 000 (Cu) | 101 (low gr.) | 102 (RRP) | 103 (RRP) | 104 (RRP) | 201 (PIT) | 202 (PIT) | 1 (RRP) | 2 (RRP) | 3 (RRP) | 4 (RRP) | 5 (RRP) | 6 (RRP)
Tension released | -0.03 | -0.12 | -0.09 | -0.11 | -0.125 | -0.075 | -0.11 | -0.105 | -0.075 | -0.008 | -0.061 | -0.035 | -0.052
Curing | -0.03 | -0.03 | -0.03 | -0.029 | -0.035 | -0.02 | 0.005 | -0.024 | -8.8818e-17 | -0.049 | -0.008 | -0.053 | -0.016
Heat treatment | -0.23 | -0.04 | -0.043 | -0.047 | 0 | -0.08 | -0.167 | -0.2615 | -0.139 | -0.188 | -0.168 | -0.171
10/30/2015 – E. Holik – FNAL
Nb3Sn Cable expands laterally when heat treated.
Nb3Sn Cable contracts axially when heat treated.
Room is left in coil cavity for cable to expand during heat treatment.
Gaps are left in the pole to allow cable/coil to contract
Azimuthal:
4.5% expansion allowed
Measured: 3.0 ± 0.3%
Radial:
2% → 1.2% allowed expansion
Free Cable 1.4%
LARP Cable 0.3%
CERN Cable 0.1%
Figure courtesy of E. Rochepault
0.03%
0.17%
L-01
L-01b
L-02
0.06%
0.13%

## Slide 15: Releasing the Tension
Chart: CERN coils LARP coils
| 000 (Cu) | 101 (low gr.) | 102 (RRP) | 103 (RRP) | 104 (RRP) | 201 (PIT) | 202 (PIT) | 1 (RRP) | 2 (RRP) | 3 (RRP) | 4 (RRP) | 5 (RRP) | 6 (RRP)
Tension released | -0.03 | -0.12 | -0.09 | -0.11 | -0.125 | -0.075 | -0.11 | -0.105 | -0.075 | -0.008 | -0.061 | -0.035 | -0.052
Curing | -0.03 | -0.03 | -0.03 | -0.029 | -0.035 | -0.02 | 0.005 | -0.024 | -8.8818e-17 | -0.049 | -0.008 | -0.053 | -0.016
Heat treatment | -0.23 | -0.04 | -0.043 | -0.047 | 0 | -0.08 | -0.167 | -0.2615 | -0.139 | -0.188 | -0.168 | -0.171
LARP Coils Contract Less than CERN when 25 kg of tension is released
For mechanical stability LARP braided insulation is tighter and initially constricts growth more
Width Expansion:
Unconfined Cable 1.4%
LARP Cable 0.3%
CERN Cable 0.1%
Figure courtesy of E. Rochepault
0.03%
0.17%
L-01
L-01b
L-02
0.07%
0.13%

## Slide 16: Altering Expansion
Chart: CERN coils LARP coils
| 000 (Cu) | 101 (low gr.) | 102 (RRP) | 103 (RRP) | 104 (RRP) | 201 (PIT) | 202 (PIT) | 1 (RRP) | 2 (RRP) | 3 (RRP) | 4 (RRP) | 5 (RRP) | 6 (RRP)
Tension released | -0.03 | -0.12 | -0.09 | -0.11 | -0.125 | -0.075 | -0.11 | -0.105 | -0.075 | -0.008 | -0.061 | -0.035 | -0.052
Curing | -0.03 | -0.03 | -0.03 | -0.029 | -0.035 | -0.02 | 0.005 | -0.024 | -8.8818e-17 | -0.049 | -0.008 | -0.053 | -0.016
Heat treatment | -0.23 | -0.04 | -0.043 | -0.047 | 0 | -0.08 | -0.167 | -0.2615 | -0.139 | -0.188 | -0.168 | -0.171
Both conductors expand similarly when unconfined.
CERN insulation preferably constricts width growth
Width Expansion:
Unconfined Cable 1.4%
LARP Cable 0.3%
CERN Cable 0.1%
Figure courtesy of E. Rochepault
0.03%
0.17%
L-01
L-01b
L-02
0.07%
0.13%
Friction between coil and tooling also effects pole gap closure (# layers of mica, pressure between components…, E. Cavanna)

## Slide 17: Outline
Coil Fabrication Summary & Overview
Coil size and asymmetry
Cable Expansion / Gap Closure
Cross Section Analysis
Conclusion

## Slide 18: Coil Cross Section Analysis
CERN coil 101, Turn location from Image analysis and edge detection
LARP coil 1, Turn location from Optical Coordinate Measurement Machine
270°

## Slide 19
Azimuthal Free Space
  Layer 1: 690 µm → 470 µm in 2nd Gen QXF
  Layer 2: 880 µm → 600 µm in 2nd Gen QXF
Strong similarities between CERN and LARP
Minor edge tends to shift toward midplane
Major edge tends to shift toward pole
Reduced Expansion → Turn Displacements
+
_
Peak Layer 2 difference is at middle turn and is 995 µm for both coils
Peak Layer 1 difference is at middle turn for both coils
645 µm
845 µm
LARP Coil 1
CERN Coil 101

## Slide 20: Free space mostly @ ID
Chart: QXFS_NT Radial Insulation Thickness Deviation from Nominal
| 3 | 4 | 5 | L1 Wedge | L2 Wedge | 9 | 19 | 20 | 21 | 22
Inner Radius | 49.9588 | 105.7564 | 146.3036 | 419.6481 | 468.4067 | 508.5767 | 601.6718 | 541.4625 | 464.235 | 810.6748
Interlayer | 534.9858 | 347.7026 | 364.4119 | -2.6022 | 115.3842 | 454.1815 | -5.307 | 140.5117 | 302.5587 | 32.0965
Outer Layer | 218.1708 | 86.1971 | 59.6698 | -24.7695 | -6.7584 | -26.8191 | 37.7828 | -57.6362 | -45.2279 | -117.5179
Total | 803.1154 | 539.6561 | 570.3854 | 392.2764 | 577.0325 | 935.9391 | 634.1476 | 624.338 | 721.5659 | 725.2535
Radial Free Space
  CERN 680 µm → 360 µm in 2nd Gen QXF
  LARP 600 µm → 280 µm in 2nd Gen QXF
ID heater is nominally 200 µm from Cable
Average distance is ~ 300 µm @ high field and ~700 µm in low field
New Input parameters for Quench Models
800 µm

## Slide 21: 2nd Gen MQXF S2-Glass
100 µm (4 mil )
Polyimide trace
Impreg Design: 310 µm
2 layers JPS 26781 933 HTS finish (314 um)
250 µm G-10
Thk: 240 – 265 um by micrometer
Reaction Design: 410 µm
2 layers BGF 6576 497A finish
(394 µm, 428 µm reacted)
100 µm (4 mil )
Polyimide trace
Interlayer Design: 660 µm
2 layers Binder BGF 6576 497A finish
(655 um, 642 µm reacted)
Impreg Design: 150 µm
1 layers JPS 26781, 933 HTS finish
(measured 150 um single layer)
Pole Design: 125 µm
Measures: 119 µm, 161 µm with binder
Wedge Sock Design: 125 µm
104 µm, 199 µm with binder
Cable Insulation
143 ± 3 µm (LARP) 146 ± 3 µm (CERN)
10/30/2015 – E. Holik & E. Cavanna
10-stack measurements of all insulation → Tighter Material Control
1st gen was undersized by 5 µm
1st gen was undersized by 75 µm
1st gen was undersized by 5 µm
1st gen was Oversized by 15 µm
1st gen was undersized by 90 µm total
2nd Gen design
150 → 145 µm

## Slide 22: Conclusion
LARP/CERN has fabricated 13 coils short MQXF coils with arguably the highest success rate of any new high-field Nb3Sn design.
LARP/CERN is preparing for the first full assembly test at FNAL.
Coil Size and Asymmetry should improve with slight tooling and fabrication adjustments.
Cable insulation Reduces Transverse Growth causing large turn displacement and free space.
The Inner layer heater is ~300 µm (~700 µm) in the High (low) field region rather than the designed 200 µm.
Increased thickness and tighter measurement in 2nd Gen MQXF insulation should improve turn displacement and may improve inner PH delay times.

## Slide 23: Spare Slides

## Slide 24: Coil Heat Treatment

## Slide 25: Max Tolerance
0.015 mm from hole size
-> Maximum L/R asymmetry is 578 um or nearly 23 mils!!!
0.050 mm from hole location
0.015 mm from pin size
0.050 mm from form block radius
0.019 mm from form and mandrel block radius centers
(0.110 mm if rigid assembly -> Assembly wouldn’t close.)
0.020 mm from pole keyway size
(0.050 mm) from pole edges (only effects turn asymmetry)
0.030 mm from SS outer shim
0.050 mm from mandrel block radius
0.289 mm total
0.030 mm from mandrel block coil midplane
0.010 mm from intrinsic design
Pin
Pin hole
Form block
Pole
Mandrel block
Base plate

## Slide 26: HQ02 Coil 17 and 20
10/30/2015 – Andrea Carbonara – FNAL
Pole Gap Closure = 0.01%
Pole Gap Closure = 0.15%

## Slide 27: Scans of HQ02

## Slide 28: Effect of L – R on Field?
These estimates suggest that we need at least ~100 µm of L-R accuracy to be within ±1 unit
Effect of several perturbations to QXF Field quality: https://indico.fnal.gov/getFile.py/access?contribId=2&resId=0&materialId=slides&confId=10554
10/30/2015 – E. Holik – FNAL
Chart: Rotate One MidPlane (Normal)
| 0 | 50 | 200
b3 | 0 | -0.00065084 | -0.010493
b4 | 0 | -0.00057302 | -0.0091778
b5 | 0 | -0.00043652 | -0.0069894
b6 | 0 | -0.00030357 | -0.0048253
b7 | 0 | -0.000192 | -0.0030739
b8 | 0 | -0.00011435 | -0.0018294
b9 | 0 | -6.3954e-05 | -0.0010238
b10 | 0 | -3.3826e-05 | -0.00054135
Chart: Rotate One MidPlane (Skew)
| 0 | 50 | 200
a3 | 0 | -1.1085 | -4.4341
a4 | 0 | -0.66348 | -2.6539
a5 | 0 | -0.36907 | -1.4763
a6 | 0 | -0.18711 | -0.74844
a7 | 0 | -0.086397 | -0.34558
a8 | 0 | -0.035749 | -0.14299
a9 | 0 | -0.012733 | -0.050923
a10 | 0 | -0.0032851 | -0.013135
Chart: All MP Shift (Normal)
| 0 | 25 | 50 | 100 | 200
b3 | 0 | -0.00015194 | -1.3505e-05 | -1.0366e-05 | -0.00014365
b4 | 0 | 3.2964e-05 | -8.8695e-06 | 2.1859e-05 | 2.4008e-05
b5 | 0 | -4.564e-05 | -7.6953e-06 | -2.1051e-05 | -4.6326e-05
b6 | 0 | -0.00065138 | -0.0015879 | -0.0060256 | -0.023308
b7 | 0 | -3.5563e-06 | -3.566e-07 | 2.81e-07 | -3.4109e-06
b8 | 0 | 9.7534e-07 | 3.5916e-09 | 6.6735e-07 | 1.0591e-06
b9 | 0 | -8.8014e-07 | -1.2699e-08 | -2.2712e-07 | -9.2779e-07
b10 | 0 | -4.5331e-05 | -0.00017975 | -0.00070556 | -0.0027863
Chart: All MP Shift (Skew)
| 0 | 25 | 50 | 100 | 200
a3 | 0 | 1.3942e-06 | 1.2112e-05 | 5.0771e-05 | -6.0351e-06
a4 | 0 | 7.9654e-05 | -9.9653e-06 | -2.3715e-05 | 8.146e-05
a5 | 0 | 4.584e-05 | -3.2673e-06 | 3.0351e-05 | 4.3718e-05
a6 | 0 | -0.40686 | -0.81368 | -1.6274 | -3.2548
a7 | 0 | 3.4008e-07 | 1.9398e-06 | 2.6249e-06 | 8e-08
a8 | 0 | 3.4374e-07 | -2.8585e-07 | -4.4392e-07 | 4.2042e-07
a9 | 0 | 8.5338e-07 | 1.5385e-07 | 6.9317e-07 | 8.9542e-07
a10 | 0 | -0.0074825 | -0.014965 | -0.029927 | -0.059833
0 100 200 300 400
L-R
0 100 200 300 400
L-R
L-R
L-R
0 100 200 300 400
0 100 200 300 400
Originally oversize by 100 µm
Rotate by 50 µm
Nominal
Nominal
Nominal
Compressed by 50 µm
Oversize by 50 µm
Undersize by -50 µm
Compressed by 50 µm

## Slide 29: Effect of L + R on Field?
These estimates suggest that we need at least ~50 µm of L+R accuracy to be within ±1 unit
10/30/2015 – E. Holik – FNAL
Chart: Shift Opposite MidPlanes (Normal)
| 0 | 50 | 200
b3 | 0 | 6.2667e-05 | 7.3751e-06
b4 | 0 | -6.4985e-06 | 1.1872e-07
b5 | 0 | -3.9198e-06 | -4.7281e-08
b6 | 0 | -0.0014677 | -0.022957
b7 | 0 | 1.2039e-06 | 1.1797e-07
b8 | 0 | -1.2601e-07 | 4.2179e-08
b9 | 0 | -5.6203e-08 | 6.2895e-08
b10 | 0 | -0.00017379 | -0.0027833
Chart: Shift Opposite MidPlanes (Skew)
| 0 | 50 | 200
a3 | 0 | -1.0592e-05 | -5.237e-06
a4 | 0 | -2.8111 | -11.2442
a5 | 0 | 1.6074e-06 | 1.0585e-07
a6 | 0 | 5.0509e-06 | -1.5697e-07
a7 | 0 | 3.2786e-08 | -5.0891e-08
a8 | 0 | -0.15923 | -0.63687
a9 | 0 | 6.1973e-08 | 5.8474e-08
a10 | 0 | 8.0954e-08 | -6.864e-08
Chart: Radial Shift One Coil (Normal)
| 0 | 50 | 200
b3 | 0 | -1.5885 | -6.3369
b4 | 0 | -3.9227e-07 | -2.5364e-06
b5 | 0 | 0.34361 | 1.3683
b6 | 0 | 0.0031192 | 0.012445
b7 | 0 | -0.10567 | -0.42001
b8 | 0 | -1.3148e-08 | -1.1728e-07
b9 | 0 | 0.037303 | 0.148
b10 | 0 | 0.0001482 | 0.0005983
Chart: Radial Shift One Coil (Skew)
| 0 | 50 | 200
a3 | 0 | 1.5885 | 6.337
a4 | 0 | 1.3317 | 5.308
a5 | 0 | 0.34361 | 1.3683
a6 | 0 | 1.7475e-07 | 6.1599e-06
a7 | 0 | 0.10567 | 0.42001
a8 | 0 | 0.12437 | 0.49388
a9 | 0 | 0.037303 | 0.148
a10 | 0 | -1.4401e-08 | 9.52e-08
0 100 200 300 400
L+R
0 100 200 300 400
L+R
0 80 160 240 320
L+R
0 80 160 240 320
L+R
Oversize by 50 µm
Undersizeby -50 µm
Oversize by 50 µm
Undersize by -50 µm
Oversize by 40 µm
Oversize by 40 µm
Radial shift by 50 µm

## Slide 30: MQXFS-AS, Estimated FQ
Chart: Normal Multipoles
| 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Nominal | 0.00022974 | -1.9917e-06 | 2.8869e-05 | 0.2879 | 5.0302e-06 | -1.0139e-07 | 5.3084e-07 | -0.39757
Adjust Coils According to Shims | -1.8438 | 9.7044e-07 | 0.77634 | -0.05064 | -0.044967 | -5.3091e-07 | 0.086787 | -0.44768
Adjust Coils According to Coil Size | -2.6375 | -1.2952e-05 | 0.94814 | -0.043155 | -0.097625 | -5.8466e-07 | 0.1054 | -0.44735
Chart: Skew Multipoles
| 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
Nominal | -9.2819e-06 | -3.3814e-05 | -2.4029e-05 | 5.4587e-05 | 1.4107e-06 | 5.6391e-08 | -5.661e-07 | 1.3395e-06
Adjust Coils According to Shims | -1.8439 | 4.7119 | -0.77632 | 1.6329e-05 | -0.044972 | 0.41536 | -0.086787 | 8.4078e-07
Adjust Coils According to Coil Size | -1.0525 | 8.0416 | -0.60553 | 3.7358e-05 | 0.0076322 | 0.7262 | -0.068279 | 9.4158e-07

## Slide 31: Goals of Next 2 Weeks…
HT, TC placement with N. Bourcey
Cross Section analysis with E. Rochepault
CMM / FARO with J. Ferradas Troitino
Coil fab (impreg, materials) with E. Cavanna
Splice equipment
Curing setup
Long coil fab
11 tesla
(ROXIE with S. Izquierdo Bermudez)