## Slide 2: SRF thin films @ CERN
Alban Sublet
on behalf of TE/VSC
08.07.2015

## Slide 3: Thin films activities @ CERN
3 main applications:
RF accelerating cavities  superconductive layer
Pumping in vacuum  NEG layer
Against electron cloud  low SEY layer
6.5 meter
3. SPS dipoles (~ 200 m)
a-C layer
2. LHC LSS (~7 km)
Ti Zr V layer
1. HIE-ISOLDE cavities
Nb layer

## Slide 4
Past:
288 Nb/Cu cavities installed in LEP
16 Nb/Cu cavities installed in LHC
(+ Soleil prototypes, 3HC, 200 MHz Cornell...)
Current:
20 Nb/Cu for HIE-ISOLDE
Spare LHC cavities
SRF thin films production activities I/III

## Slide 5: SRF thin films production activities II/III
HIE-ISOLDE QWR 100 MHz
  1 test cavity with sample holder + QPR sample
  20 “high-b” cavities (phase 1 + 2)  on going
  12 “low-b” cavities (phase 3)  to be approved
First cryomodule under commissioning
Coating of cavities for second cryomodule on the way
R&D continuing

## Slide 6: SRF thin films production activities III/III
LHC single cell 400 MHz spare cavities
  Test tube to asses coating setup
  2 prototypes  fabrication on going
  1 full cryomodule + spares

## Slide 7: SRF thin films R&D: projects
HIE-ISOLDE high/low-b (100 MHz)
HL-LHC Crab Nb/Cu (400 MHz)
LHC upgrade/ERL/FCC (800 MHz)
FCC (400/800 MHz)

## Slide 8: SRF thin films R&D: cavities shapes
QWR (HIE-ISOLDE)
WOW Crab Nb/Cu (HL-LHC)
elliptical x-cell(s) (FCC)
0.9 m
1.2 m
R. Calaga

## Slide 9: SRF thin films R&D: test substrates
Upper anode bias connection
Upper anode
Lower anode
Lower anode bias connection
Q4 sample cavity (HIE-ISOLDE)
elliptical 1.3 GHz cavity
Si-wafer/quartz/Cu coupons
126 mm
75 mm
400 mm
35 mm
Orsay Cu-disk
QPR-sample

## Slide 10: SRF thin films R&D: functionality characterization
Basic studies:
RRR on quartz sample  CERN
Point Contact Tunneling (PCT)  ANL
Muon Spin Rotation (m-SR)  PSI/TRIUMF
Third harmonic magnetometer  Saclay
RF characterization:
TE011 test cavity for Cu-disk  Orsay
RF Quadrupole Resonator for QPR-sample CERN
RF test on 1.3 GHz cavity (cryolab)  CERN
RF test on cavities (SM18)  CERN

## Slide 11: SRF thin films R&D: topics
Thin film R&D approach focused on 4 main topics:
Coating technics
SC Material
Material/thin film analysis
Plasma diagnostics and plasma simulation

## Slide 12: SRF thin films R&D: coating technics
DC bias diode sputtering, production level
DC magnetron Sputtering, production level
HiPIMS (+bias), development level
Cathode design/shape
Biasing, grid design
Heat treatment
Substrate temperature
Nitrogen treatments

## Slide 13: SRF thin films R&D: SC material
Niobium
A15 compounds: Nb3Sn and V3Si
BCS surface resistance at 4.2 K
and 500 MHz for films ( Nb ~ 45 n)
Planar magnetron Nb3Sn target sputtering

## Slide 14: SRF thin films R&D: material/thin film analysis
XRF, XPS, XRD (CERN), SIMS, …
SEM/EDS – FIB/SEM, STEM/TEM (CERN/EPFL)
HIE-ISOLDE
Q4 sample from middle antenna
Nb/Cu, 14 runs coating
Courtesy B. Bartova and EPFL-CIME

## Slide 15: SRF thin films R&D: plasma diagnostics
Plasma test bench
  current/voltage probes
  Retarding Field Energy Analyzer
  Fast intensified camera
  Quartz balance
  OES
  Langmuir probe
Bottom view of plasma
anode tube (+bias)
Nb cathode
DC bias diode
DCMS
HIPIMS
UHV vacuum chamber
diagnostic port:
RFA, Qz-balance
Cu strip for thickness profile
400 mm height

## Slide 16: SRF thin films R&D: plasma simulation
DSMC/PIC-MC code
p = 0.32 mbar (diode discharge)
Constant wall temperature (200°C)
Initial charged particles density = 1013 m-3
Power = 10 W
Maximum voltage = 1000 V
benchmarking with plasma test bench
Courtesy A. Pflug – Fraunhofer IST

## Slide 17
Thank you for your attention
TE-VSC group

## Slide 19
Possibility to coat substrates up to 1.2 m length, substrate rotation for complex shapes
Up to 3 independent targets for alloy deposition with tunable composition
Typical materials:
Cu, Au
Ti
NEG (TiZrV)
Nb, Nb3Sn
B4C
Foreseen developments:
- insulators, reactive sputtering, RF magnetron…..
Thin films activities @ CERN

## Slide 20
SRF cavity
S = superconducting
  Lower power losses through surface resistance reduction
  Increased quality factor
RF = radiofrequency excitation to provide accelerating gradient in the resonant cavity
Cavity = resonator for an electromagnetic wave
Resonator characterized by f0, Q0
U is the energy stored in the cavity volume and Pc/0 is the energy lost per RF period by the induced surface currents
 Cavity characterized by its Q0 vs accelerating gradient (Eacc) curve

## Slide 21: SRF cavities bulk Nb vs thin film
Nb bulk
Expensive (900$/Kg)
Low thermal conductivity
High accelerating gradients
Well known technology
Thin film
Q disease (early quench)
Behaviour not fully understood/explained
Cheaper bulk material (Cu)
High thermal conductivity
Well known technique used since LEP generation
Future accelerators needs:
Low power consumption  high efficiency cryogenics
Low cost  limit the use of bulk Nb as much as possible, superconductive thin film prefered
Approach:
Improve Nb coatings properties: substrate treatment / post coating treatment / coating technic
Look for new materials: higher Tc and lower Rs

## Slide 22: SRF thin films R&D topics
Plasma simulation: DSMC/PIC-MC code
Courtesy A. Pflug – Fraunhofer IST