## Slide 2: Status of the damage test on insulation of sc. cable
V. Raginel, D. Kleiven, D. Wollmann

## Slide 3: OUTLINE
Pre-experiment up to 900°C
Reminder of the experimental setup
Dummy High Voltage test
Experimental Plan

## Slide 4: Pre-experiment to measure variation of thickness of an insulated cable from 20°C up to 900 °C in Helium atmosphere.
Disintegration of insulation
Softening Copper
Unknown
~ 150 µm
1h
2h
3h
4h
5h
3 degrees/min
Courtesy O. Sacristan De Frutos
~ 2h
up to 400°C
up to 900°C

## Slide 5: Experimental setup: Stack of 6 cable under stress

## Slide 6
Each finger is instrumented with 4 strain gauges (bridge setup to take into account Poisson ratio and to cancel thermal strain)
6 cables per finger to compensate cable length.

## Slide 7: Experimental setup: Heating in argon atmosphere
L = ~ 700 mm, ø = 160 mm
Vacuum or Argon atmosphere
Actual tube in Quartz to be clean after experiment and spare flanges

## Slide 8: Experimental setup: High Voltage test

## Slide 9: Experimental setup: High Voltage test

## Slide 10: Dummy High Voltage Test: Cable 2 to 3

## Slide 11: Dummy High Voltage Test: Cable 4 to 5 (first test)

## Slide 12: Dummy High Voltage tests : Cable to cable

## Slide 13: Dummy High Voltage tests : Cable to Mould
- Cable 4 up to 16 kV
- Cable 5 up to 15 kV (not shown here)

## Slide 14
V
III
bottom

## Slide 15: Side of the mould in contact with the cable after HV test

## Slide 16: Experimental Plan
Stress measurement on a cable stack at room temperature with mould – week 50
  Adapt cavity height to get 100/120/150 MPa with stainless strip.
Trial Run up to 500 C with one mould (2 thermal sensors - one in nominal position and one in between the cable) – week 50
First Experimental runs with two moulds. 4 tests with different peak temperature – week 51/week 2
  200 C
  300 C
  400 C
  500 C
Second Experimental run with two moulds– refine temperature according to results of first run up to 4 tests - week 2/week 3
Total of up to 9 tests (including trial run – 25 m of insulated cable)

## Slide 19
Mould dimension 84 x 62 x 100
Material Stainless Steel 304L
Cavity for Six Cable Stack (~ 12 mm)
Fine setting of stress on the cable stack with stainless strip (40 um up to 500 um) insert between the side and top part of the mold
Strain Gauge Bar
Mould - Bottom Part
Mould – Top Part
Mould – Side Parts
Hole for Thermal Sensor
100
62
84
105
M10 screw