## Slide 1: Results of microscopic analysis II
V. Raginel, A. Gerardin

## Slide 3
T3 – Cylinder 1

## Slide 5: Base material: Average grain size ~100 um

## Slide 6
Non-molten
Molten
Columnar grains

## Slide 7
T3 – Cylinder 9

## Slide 9
First ~5 mm - T3-9/1

## Slide 10
Non-molten Grains ~ 100 um
Molten
Small Grains ~ 30 um
T3-9/1

## Slide 11
Non-molten
Partially molten
Non-molten
T3-9/2 - After last visible micro-cavity

## Slide 12
Crack following join of grains
T3-9/2 - After last visible micro-cavity

## Slide 13
T2 – Cylinder 8

## Slide 15
Zoom of the splash coming from cylinder 7 T2-8/1

## Slide 16
Non-molten
Between the two lines formed by the micro-cavities - T2-8/1
Molten
Small Grains ~ 30 um

## Slide 17
Single line crack in T2-8/2

## Slide 18
T1 – Cylinder 6

## Slide 20
Example of a crack in T1-6

## Slide 21: Conclusions
Damage Depth confirmed. (T1/58 cm, T2/79.5cm, T3/85cm)
Copper that has been molten shows smaller grains structure than the original material, or columnar grains (e.g. T3 cylinder 1)
It is confirmed that in the last damage cylinders of each target, the copper between the two lines of micro-cavities has be molten.