## Slide 1: Results of microscopic analysis II
V. Raginel, A. Gerardin, M. Thiebert

## Slide 3: Electropolishing of the Cylinder
Current passes from anode to cathode. Electrolyte bath is phosphoric acid (H3PO4)
Anode (Cylinder): Copper is oxidized and dissolved in the electrolyte
Cu -> Cu2+ + 2 e-
Cathode: Reduction of the copper
  Cu2+ + 2 e- -> Cu
Cu

## Slide 4
T3 – Cylinder 1
400 GeV/c
144b with 1.5E11p
σ = 0.2 mm

## Slide 6: Base material: Average grain size ~100 um

## Slide 7
Non-molten
Molten
Columnar grains

## Slide 8
T3 – Cylinder 9
400 GeV/c
144b with 1.5E11p
σ = 0.2 mm

## Slide 10
First ~5 mm - T3-9/1

## Slide 11
Non-molten Grains ~ 100 um
Molten
Small Grains ~ 30 um
T3-9/1

## Slide 12
Non-molten
Partially molten
Non-molten
T3-9/2 - After last visible micro-cavity

## Slide 13
Crack following join of grains
T3-9/2 - After last visible micro-cavity

## Slide 14
T2 – Cylinder 8
400 GeV/c
108b with 1.5E11p
σ = 0.2 mm

## Slide 16
Zoom of the splash coming from cylinder 7 T2-8/1

## Slide 17
Non-molten
Between the two lines formed by the micro-cavities - T2-8/1
Molten
Small Grains ~ 30 um

## Slide 18
Single line crack in T2-8/2

## Slide 19
T1 – Cylinder 6
400 GeV/c
144b with 1.5E11p
σ = 2 mm

## Slide 21
Example of a crack in T1-6

## Slide 22: Conclusions
Damage Depth confirmed. (T1/58 cm, T2/79.5cm, T3/85cm)
Copper that has been molten shows smaller grains structure than the original material, or columnar grains (e.g. T3 cylinder 1)
It is confirmed that in the last damage cylinders of each target, the copper between the two lines of micro-cavities has be molten.

## Slide 23: Spare Slides

## Slide 24: Electropolishing of the Cylinder