## Slide 1: SRF Activities at CERN – Overview
SM18 in the 1990’s

## Slide 2
The LHC SRF
First module swap last year
Spare module needs refurbishing
Spare cavity programme underway

## Slide 3: Bldg. 252: Cavity Production and Reception Area

## Slide 4: Clean Room Upgrade and Extension

## Slide 5
The SM18 Share of Activities

## Slide 6: SM18 SRF New Infrastructure

## Slide 7: The SRF SM18 Cryogenics Ugrade
M7
V3
SM18 RF Area
V4

## Slide 8: SRF Research in the Cryolab
Sample Testing with the
Quadrupole Resonator
RRR does not seem to be the cause of the Q-Slope of Nb Films.
1.3 GHz HIPIMS Cavities
Surface Resistance [nΩ]
RF Magnetic Field [mT]
Thermal cycling has a strong impact on the RS.
20
140
0
40
Chart: Surface Resistance [nΩ]
| 221 | 391 | 143 | 1 | 66 | 282
no trapped field | 61.5975 | 45.4614 | 70.888 | 84.271 | 77.927 | 57.9634
Cooling Rate [mK/s]
High precision tests of HIPIMS cavities
Understanding, controlling and minimizing field dependent losses of Nb/Cu cavities
Effects studied:
  Low temperature baking
  Thermal cycling
  Thermal boundary resistance
Simultaneous measurement of RS and pressure of helium gas introduced in the cavity as a function of Eacc show that global warming is not the cause for the field dependent surface resistance of Nb/Cu cavities
Measurement of the cavity’s
inner surface temperature

## Slide 9
The HIE-ISOLDE Project

## Slide 10
SPL 704 MHz half-module

## Slide 11
High Gradient Programme: The SPL cavity testing

## Slide 12
HL-LHC: SRF Crab cavities

## Slide 13
Cryomodule with DQW cavities
Cryomodule
Vacuum vessel
Warm magnetic shielding
Thermal shielding
Fundamental Power Coupler
High Order Modes Suppressor
Tuning system
Helium vessel
Cavity
Alignment monitoring system

## Slide 14
Cryomodule with RFD cavities
Cryomodule

## Slide 15: Ancillaries and Diagnostics

## Slide 16: Horizontal bunker M7
New long term decision
As M9 will be used for :
  LHC cryomodule
  HIE-ISOLDE cryomodule
  And later FCC 400 MHz project
M7 will be used for :
  SPL half cryomodule
  CRAB cryomodules
  And later new LHC 800 MHz project
  -------> Need to redesign a multipurpose cryo box !!

## Slide 17
Programme | Frequency (MHz) | Cavities | Units | Modules
LHC | 400 | 2 + 8 | 2 + 4 | 1 + 1
HIE-ISOLDE | 101 | 25 | 0 | 4
CRAB | 400 | ? | ? | 16 + 2 + 2
SPL | 704 | 5 + ? | 4 | 1
FCC | 800 (400) | ? | ? | ?
Summary: Cold Testing

## Slide 18
Conclusion
CERN SRF infrastructure and personnel today not sufficient for the medium term plan.
Material Budget available for partly compensation of needs.
Student and fellow requests underway for ramp-up of activities. Exchange with collaborations encouraged.
Some projects rely on In-Kind contributions from collaborations – follow-up essential.