## Slide 1
TASK 5.5 - Conductor Studies
First Proposal
CERN – 09th July 2015
EuroCirCol Meeting – WP5

## Slide 2: Wire Diameter & Layout Starting Point
In order to better use synergies with the HiLumi project, the 0.85 mm wire seems to be the best starting point
A 1 mm wire might be an alternative option in the case it would be necessary to reduce the inductance of the magnet
RRP 108/127 (55 μm in a 0.85 mm wire with Cu/Non-Cu=1.2)
  Alternative 132/169 (50 μm in a 0.85 mm wire with Cu/Non-Cu=1.2)
PIT with 192 Sub-Elements (41 μm in a 0.85 mm wire with Cu/Non-Cu=1.2)

## Slide 3: Relevant Wire Studies
Ic versus transversal pressure - Unige
Ic versus longitudinal strain – Twente, Unige
Ic Temperature Dependence – Twente, UniGe
Magnetization Temperature Dependence, Deff – CERN
Magneto Thermal Stability – CERN
Specific Heat, Thermal Conductivity – Unige, Twente

## Slide 4: Relevant Cable Studies
Ic versus transversal pressure – Twente, CERN
Inter-strand Resistance – Twente
Effect of large heat capacity compounds in the impregnation: training, MQE, quench propagation velocity - CERN

## Slide 5: Key Studies
Correlate the wire measurements under transversal pressure carried out at UniGe with cable measurements
  Sub-cable (18 wires  about 8 mm width ?) measured at CERN and Twente for benchmarking
  Full size cable (most likely 40 wire ) measured at Twente
Verify the compatibility of high Je with large transversal pressure on the conductor
  With the present wire design, can we go for relatively large sub-elements and large Sn content?

## Slide 6: Possible Initial Activity at Unige
Ic versus transversal pressure
  0.85 RRP 108/127 Regular-Sn, Ti-doped
    Goal: Study the impact of reduced-Sn on electromechanical behavior
    Reduced-Sn Ti-doped already measured by UniGe (HiLumi wire)
  The effect of the layout has been already assessed by UniGe
    132/169 more tolerant to transversal pressure than the 108/127 (at least for the reduced tin)
Ic versus longitudinal strain
    0.85 RRP 108/127 Regular-Sn, Ti-doped
    0.85 RRP 132/169 Regular-Sn, Ti-doped

## Slide 7: Possible Initial Activity at Twente
Ic versus longitudinal strain
    0.85 RRP 108/127 Regular-Sn, Ti-doped
    0.85 RRP 132/169 Regular-Sn, Ti-doped
Ic versus temperature
  0.85 RRP 108/127 Regular-Sn, Ti-doped
  0.85 RRP 108/127 Reduced-Sn, Ti-doped

## Slide 8: Possible Initial Activity at CERN
Magnetization versus temperature
  0.85 RRP 108/127 Regular-Sn, Ti-doped
  0.85 RRP 108/127 Reduced-Sn, Ti-doped
Manufacture and characterization of a sub-cable
  Cable Design and wire procurement
  Ic degradation
  RRR degradation