## Slide 1: The LHC ACS RF power couplers for testing magnetic SEY suppression F.Caspers, E.Montesinos ECM 08 Nov 08
Large Hadron Colider
Accelerating Cavities Superconducting
400 MHz 300 kW cw coupler

## Slide 2: LHC couplers (layout)
The LHC power coupler is a 400 MHz mobile RF power coupler with very high power requirements :
Continuous : 250 kW
Pulsed : 300 kW fwd + 670 kW rev, including beam loading, i.e. 1.85 MW local peak power.
Challenge
To design a mobile RF power coupler without sliding contacts for these very high power levels.
Main design features
A Cylindrical ceramic window with solid copper rings brazed to the ceramic ends, placed in the waveguide-to-coaxial transformer, provides vacuum integrity.
To suppress multipactor during operation two DC bias levels are applied:
  2.6 kV, to the low impedance 7 Ω λ/4 line transformer, isolated from ground by a coaxial capacitor in the waveguide.
  2.6 kV + 400 V, to the antenna, isolated from the λ/4 line transformer by a disk ceramic capacitor between λ/4 line transformer and bellows.
Air cooling is provided on the window and other critical elements of the coupler, such as the antenna.
A Vacuum gauge is located close to the window and is used for coupler conditioning and interlock.
Air inlets
Disk ceramic capacitor for second polarization
Main cylindrical ceramic window
Open ended 75 Ω coaxial line under vacuum:
Outer conductor double walled
Inner conductor copper antenna
Displacement mechanism
Main coaxial capacitor for polarization
Reduced height waveguide
Bellows λ/4 line
Low impedance 7 Ω λ/4 line

## Slide 3: LHC couplers (layout detail)
Copper antenna with inner air cooling cane
Note, that this coupler is like an anti-cryostat.. warm… and with air inside

## Slide 4: LHC couplers - where to install a double coil
Copper antenna :
external diameter = 41 mm
internal diameter = 38 mm
Inner air cooling cane
external diameter = 32 mm
Space for winding = 3 mm
First idea was to apply a nickel layer on the
outer surface of this coupler, coated with 10 micron
copper…but we need multipacting during the “running
in phase“ thus we require a „switchable“ SEY..
we need the double coil inside

## Slide 5: LHC couplers
Inner copper antenna with inner air cooling cane