## Slide 1: Radioactive ion beam production at other facilities
P. Delahaye, GANIL
And M. Hass, Weizmann Institute/SOREQ

## Slide 2: GANIL – SPIRAL 1
Most intense beams of 6He and 18Ne
6He
  2.108/s at low energy, 3.107 post-accelerated
  13C beam 75AMeV on a graphite target (1.5 - 3kW)
18Ne
  107/s at low energy (2+), 3.106 post-accelerated
  20Ne beam 95AMeV on a graphite target (1.5 - 3kW)
Graphite target, very efficient ionization with an ECR source

## Slide 3: GANIL – SPIRAL 1
Experimental areas
Ion sources
CSS1
CSS2
Production cave
CIME
Acceleration
Stable ions
Post-acceleration
Of radioactive ions

## Slide 4: Gaseous elements with Nanogan 3 and cold transfer tube
Cold transfer tube
=
Gazeous elements

## Slide 5: Graphite targets
1,5 kW
Ne, Ar, Kr, N, O, F
3 kW
He
Projectile fragmentation!

## Slide 6: Projects at SOREQ and GANIL
GANIL - SPIRAL 1: new target materials for target fragmentation and fusion – evaporation
GANIL – SPIRAL 2:
  UCx targets with 5mA 40 MeV d hitting a neutron converter in 12C
  Fusion – evaporation and transfer reactions with light - or medium heavy - intense beams
SOREQ - SARAF:
  Phase 1: 2mA 5 MeV d on neutron converter (Li)
  Phase 2: 2mA 40 MeV d on neutron converter (Li)

## Slide 7
/A

## Slide 8: SARAF - Soreq
RFQ
6 SMs
βo=0.09
βo=0.15
deuterons / protons
linear accelerator
5 MeV at Phase 1
with only 1 SM (2008)
40 MeV at Phase 2
with 6 SMs (2013)
2 mA current
2008
Nagler, LINAC2008
Piel, EPAC2008
Pekeler, LINAC2006
40 MeV , 2 mA Lithium Converter

## Slide 9: What interests for beta-beams?
Development of light RIBs for nuclear physics
  Joint (SOREQ+GANIL) development and tests of BeO targets with ISOLDE for high intensity 6He beams
  SOREQ: tests of a BN target for 8Li production
  GANIL: possibilities for testing (production) diffusion, effusion and ionization of 8B and 8Li beams at SPIRAL 1

## Slide 10: BeO and 6He: EURISOL
Converter technology: (J. Nolen, NPA 701 (2002) 312c)
9Be(n,a)
T. Stora et al, EURISOL-TN03-25-2006-0003
CEA Saclay Optimized Geometry
N Thollieres et al. EURISOL-TN03-25-2006-0004
Preferred to direct irradiation (heat transfer and efficient cooling allows higher power)
6He in target yield is ~2x1013 ions/s (dc) for ~200 kW on target
Use of a 4MW target is a priori possible

## Slide 11
SARAF and GANIL
Optimization Calculations (SOREQ/WI)
MCNPTM Monte Carlo N-Particle transport code
Hass et al., J. Phys. G: Nucl. Part. Phys., 35, 014042 (2008).
Expected in target yields for BeO:
SARAF (40 MeV, 2 mA): 8∙1012 [6He/sec]
SPIRAL2 (40 MeV, 5 mA): 2∙1012 -2∙1013 [6He/sec]
Expected in target Yields for a BN target:
SARAF (40 MeV, 2 mA): 2∙1012 [8Li/sec]

## Slide 12
SOREQ/WI: neutron flux simulation
2D slice inside the secondary target

## Slide 13: SOREQ/WI: target geometry
Cone shaped target
* RT stands for the distance between the two targets
2D slice of the target

## Slide 14: Plans SOREQ
NG
27Al(n,α)24Na
Production
γ
NG /
Phase 1
11BN(n,α)8Li
Production
extraction
β
Phase 1 /
Ganil /
ISOLDE
9BeO(n,α)6He
Production
extraction
β
27Al(n,α)24Na
Monte Carlo
Simulations
11BN(n,α)8Li
Monte Carlo
Simulations
9BeO(n,α)6He
Monte Carlo
Simulations
6He production
and extraction
numbers
15.2.2008 Aluminum cubes irradiation experiment number 1. Preliminary experiment for verification of target geometry in compare to Monte Carlo simulations.
28.4.2008 Aluminum cubes irradiation experiment number 2. Preliminary experiment for verification of target + reflector geometries in compare to Monte Carlo simulations and previous experiment.

## Slide 15
Aluminum Cubes Experiment
T.Y.Hirsh et al. PoS(NUFACT08)090, 2008.
1.4∙109 n/s

## Slide 16
8Li Production Experiment
measurement
irradiation
3 sec
3 sec
0.1 sec
time
movement
8Li production measurement.
11BN(n,)8Li by fast neutrons.
Automatic measurement system using a fast air-pressure rabbit.
Detection of betas from 8Li decay.
A benchmark for simulations.
6He production is also possible by replacing the target by BeO.

## Slide 17: Joint efforts BeO
SEM BeO SOREQ/WI
Heating tests with Ta or Mo container at ISOLDE
Diffusion and effusion test of 6He produced by SPIRAL 1 in a BeO pellet
Target is becoming a catcher – experiment at SIRA for mid 2010
Safety issues are being addressed
On line experiment foreseen mid of April with Ta converter
R. Hodak PhD Thesis
T. Stora
oven
BeO catcher pellet

## Slide 18: Future possibilities GANIL SPIRAL 1
1+ N+ 8Li ions in “Nanonake”
13C on 12C target
Primary beam
1+ Beam
deceleration
N+ RIB
Experiment scheduled in May
C. Eleon et al. NIMB206 (2008) 4362-4367 (EMIS2007) C. Eleon et al RSI 79, 02A904 (2008)

## Slide 19: Testing a difficult beam: 8B
Production using fragmentation of 13C on 12C
Flushing CF4 in the target surrounding to produce BF3
Ionization in Nanogan (0 to N+)
  Was already tested with 32S and 36Ar on graphite target but high background of 24Na

## Slide 20: Summary
In the frame of EUROnu
  Production tests of 8Li from a BN target irradiated by fast neutrons at SOREQ with neutron generator and SARAF phase 1 (2009)
  Production tests of 6He from a BeO target irradiated by fast neutrons at SOREQ from SARAF phase 1
  Diffusion of 6He in BeO at GANIL (2010)
  8Li (production) diffusion in graphite and ECR-ionization tests possible at GANIL (May – June 2009)
  Possibility of testing diffusion and ECR-ionization of 8B in a parasitic beam time at GANIL (?)

## Slide 21: People and institutes
Dan Berkovits
Leo Weissman
Yoram Nir-El
Michael Hass
Tsviki Hirsh
Vivek Kumar
Kuljeet Singh
F. De Oliveira
M.G. St Laurent
P. Delahaye
H. Franberg
R. Leroy
Pichard
G. Lhersonneau
Thanks a lot for your attention!

## Slide 22: What about 18Ne?..