## Slide 1: FCM: Concept and test results

## Slide 2: Specifications:
iron Dominated, Pulsed, Superconducting dipole magnet
Bnom = 1.8 T at dB/dtnom = 1.5 T/s triangular cycle
QAC < 2 W/mmagnet average over the reference cycle
Good field region (≈ 10-4 homogeneity):
Stable performance over a large number of cycles

## Slide 3: FCM magnet:
Cryostat
Warm Yoke
Thermal shield
Coil support
Superconducting coil

## Slide 4: The FCM magnet:
Short prototype model:
Yoke length: 0.76 m
Yoke width: 1.17 m
Magnet overall length: 1.69 m
Magnet weight: 4 tons
Aperture 70 mm

## Slide 5: Magnet Design (1/4):
Coil support structure
The coil support is attached to the cryostat by means of 8 rods.

## Slide 6: Mechanical support
Rods are made of invar:
Heat input per rode between 0.4 and 0.9 W (computed).

## Slide 7: Magnet Design (2/4):
Superconducting Coils

## Slide 8: Coil pre-stress:
G10 spacers between the coil and the structure:

## Slide 9: Magnet Design (3/4):
50 K thermal screen
Stainless-steel thermal screen

## Slide 10: Magnet Design (4/4):
Top and bottom cover for the cryostat + iron yoke

## Slide 11: Cable and coil:
Cable-around-conduit conductor made of Nb-Ti strands
Coils cross-section
5 mm
Co-wound quench detection wire
20 mm
45 mm
Cable cross-section

## Slide 12: Magnet Design:
Peak field on the conductor within 1 T

## Slide 13: Magnet Design:

## Slide 14: Field lines in the coil

## Slide 15: Electrical joints:
Demountable connection:
Cable
Copper
Indium
Sn-Ag solder
Measured between 2.4 nΩ and 4nΩ

## Slide 16: Instrumentation
Magnet equipped with 12 temperature sensors (At 4.5 K measurement error is 12 mK)
The mechanical structure and the rods are equipped with strain gauges

## Slide 17: Magnet testing
The magnet was tested in 2012

## Slide 18: Test results
One training quench at 4.5 K to reach 6 kA
20000 cycles to 6 kA without quench
Current pushed to 7.5 kA (magnetic forces 50% higher)  mechanical design is robust.

## Slide 19: Test results
Coils protected by a 5 mΩ dump resistor.
The quench detection with the co-wound wire was proven effective.
AC loss < 2W (1.2 W from computation).

## Slide 20: Spare slides:

## Slide 21: Electrical and cooling circuits: