## Slide 1
Sergey Belomestnykh
ICHEP 2016
4 August 2016
SC technology for future HEP particle accelerators

## Slide 2: Outline
Introduction: Future HEP particle accelerators and superconducting (SC) technology
Superconducting RF (SRF) technology challenges for future lepton colliders: ILC; FCC-ee/CEPC
High-field SC magnet technology needs for future hadron colliders: FCC-hh/SppC
Summary
TESLA SRF cavity
Short model of a SC magnet

## Slide 3: Introduction
Superconducting radio frequency accelerating cavities and High-field superconducting magnets and are a cornerstone technologies of future high-energy particle accelerators.
Due to short time allotted for the talk, I will address only future HEP colliders, which present most challenging demands.
Future generation of lepton colliders will require RF systems to be “affordable” and able to support high luminosity.
The former necessitates cavities operating at high accelerating gradients (acceleration system length) with low cryogenic losses (high quality factor). The latter means supporting very high beam currents (higher order mode damping) and delivering very high power to the beams (RF power couplers).
Next hadron colliders require a step up from the state-of-the-art accelerator-grade SC magnet technology: from 11 T (HL-LHC) to 16 T or even 20 T.
In this talk I will briefly discuss state of the art of these two technologies, outline how they enable future generation of HEP colliders and discuss challenges.

## Slide 4: Future colliders: scale of the problem
SRF: 800 cavities at 23.6 MV/m for EXFEL vs. 16,000 cavities at 31.5 MV/m for ILC
SRF: 22 MW SR power for LEP2 vs. 100 MW SR power for FCC-ee
SC magnets: 27 km LHC vs. 80 to 100 km FCC
SC magnets: 11 T Nb3Sn for HL-LHC vs. 16 T Nb3Sn / 20T hybrid for FCC-hh/SppC

## Slide 5: SRF technology for ILC: state of the art
The ILC TDR specs, 31.5 MV/m with Q > 1010 and 90% yield, have been demonstrated on a small scale.
Average gradient of XFEL cryomodules is 27.9 MV/m* with only 5 of 98 tested CM modules below spec (23.6 MV/m).
Field emission (FE) is still an issue at high gradients.
ILC cost is still a big concern for funding agencies.
*) Administratively limited to 31 MV/m

## Slide 6: SRF technology for ILC: path to cost reduction
From the ILC TDR: “[the cost] is dominated by the SRF components and related systems, together with the conventional facilities. These two elements account for 73% of the total. The main linac itself corresponds to 67% of the total project.”
Reducing the main linac cost is the most efficient way to bring the ILC cost down.
Possible directions for short-term R&D: improve accelerating gradient and cavity Quality factor (Q); reduce cost of cavity and component fabrication; simplify cavity treatment. Long-term R&D would concentrate on alternative materials, e.g. Nb3Sn.
Main Linac Cost Breakdown from ILC TDR

## Slide 7: Recent R&D progress on high Q / high gradient: “standard” vs “N infused” cavity surface treatment
FNAL recently demonstrated (on single-cell cavities) a new treatment, which utilizes “nitrogen infusion”.
Achieved so far:
  45.6 MV/m  194 mT
  with Q ~ 2∙1010!
Systematic effect observed on several cavities.
R&D to focus on :
  Optimize the recipe;
  Implement and demonstrate improvement with statistics on nine cells cavities;
  Better understanding and mitigation of FE;
  Demonstrate preservation of performance in cryomodule;
  Transfer technology to industry.
Increase in Q by a factor of two
Increase in gradient ~15%
Courtesy A. Grassellino (FNAL)

## Slide 8: Potential ILC cost reduction
A cost model based on the ILC TDR and new progress in the SRF technology on cavity achievable efficiency (Q) and acceleration (Eacc), showing potential cost reduction up to 20%.

## Slide 9: Future circular lepton colliders
Future e+e- colliders, FCC-ee and CEPC, are considered as a potential first step toward hadron colliders FCC-hh and SppC, a la LEP before LHC.

## Slide 10: Parameters of the circular lepton colliders
SRF systems for these machines will have to deal with very high RF power, high beam currents and strong HOM damping.
“high gradient” machines
“Ampere-class” machine
short bunches
Courtesy E. Jensen (CERN)

## Slide 11: SRF technology for FCC-ee
Parameters of the FCC-ee options cover very wide range and cannot be satisfied with one SRF system design.
At the “high current” end, where the total voltage is relatively small, the design will be determined by strong HOM damping requirements and RF power couplers. Hence, single-cell cavity design. The gradients will be moderate (4-5 MV/m). Nb/Cu at 4 K is OK.
At the “high gradient” end, the total voltage is large and the design will be driven by optimization of the accelerating gradient in CW mode of operation. The number of cells per cavity will be limited to 4-5 to ensure adequate HOM damping. Nb/Cu or other alternatives (Nb3Sn?) are under consideration, but require R&D.
400MHz, 1 cell, Nb/Cu
400MHz, multi-cells, Nb/Cu
800MHz, multi-cells, Nb/Cu - bulk Nb
Higher gradient
Higher currents
Courtesy E. Jensen (CERN)

## Slide 12: SRF technology for CEPC
CEPC’s main physics goal is operation at 240 GeV center-mass energy as a Higgs factory.
The collider RF system will consist of 384 650-MHz 5-cell SRF cavities operating at 19.3 MV/m with Q of 4∙1010.
Nitrogen doping and magnetic flux expulsion technologies will be used to support high Q.
Thin film SRF technology, e.g. Nb3Sn is under consideration as possible alternative.
CEPC layout from J. Y. Zhai, et al., SRF2015

## Slide 13: Nitrogen doping for 650 MHz
Applying nitrogen doping to 650 MHz (b = 0.9) leads to doubling Q compared to 120°C bake (standard surface treatment ILC/XFEL), ~7∙1010 at 2 K – world record at this frequency.
Courtesy A. Grassellino (FNAL)
CEPC spec

## Slide 14: Nb3Sn SRF cavity R&D
R&D on 1.3 GHz single-cell cavities at Cornell: Recent test results consistently demonstrate gradients >16 MV/m with Q > 1010 at 4.2 K.
Very promising for future colliders. Next steps: extend this technology to multi-cell cavities and lower frequencies.
Courtesy D. Hall and M. Liepe (Cornell)
Nb3Sn cavity surface
Courtesy Cornell University

## Slide 15: High-field SC magnet technology for future hadron colliders
Proposed future hadron colliders – HE-LHC, FCC-hh, SppC – require developing SC magnet technology beyond state-of-the-art.
State-of-the-art accelerator magnet technology will be utilized in HL-LHC and is based on 11-T class Nb3Sn magnets.
HE-LHC and FCC-hh plan to use 16 T magnets while SppC would need 20 T magnets.
The former can be developed using Nb3Sn technology while the latter would need to use HTS, most likely in a hybrid magnet configuration.
In both cases cost reduction for Nb3Sn and HTS superconductor is mandatory to make the projects affordable.
U.S. DOE is establishing a national Magnet Development Program (MDP) to develop SC magnet technology suitable for future energy-frontier colliders.

## Slide 16: 11-T class magnets for HL-LHC
Nb3Sn dipole for LHC collimation system upgrade
  60 mm aperture
  Bnom = 11.2 T at I = 11.85 kA
  cold mass cross-section is compatible with the LHC MB
STAINLESS STEEL
SKIN
NB3SN COIL
STAINLESS STEEL
COLLAR
IRON YOKE
Nb3Sn IR quadrupole for LHC luminosity upgrade
  150 mm aperture
  Gnom = 140 T/m at 17.5 kA
Courtesy A. Zlobin (FNAL)

## Slide 17: Timeline for high-field accelerator magnet R&D
VLHC
HL-LHC
LARP
FCC
Record field 13.8 T
HFDA HFDM-LM 43.5 mm Dipole mirror
10 T dipole
TQC TQM-LQM
90 mm 200 T/m Quadrupole quadrupole mirror
HFDC (R&W)
40 mm 10 T dipole
MBHDP
60 mm 11 T dipole
MBHSP MBHSM
60 mm 11 T dipole Dipole mirror
D20 (LBNL)
50 mm dipole
13.5 T (1997)
HD2 (LBNL)
35 mm dipole
13.8 T (2008)
Courtesy A. Zlobin (FNAL)

## Slide 18: Magnet Development Program
This is a generic R&D program designed to achieve 4 goals and address the driving questions.
Baseline cos-theta design
Canted cos-theta concept

## Slide 19: Magnet cost reduction strategy
Reduce magnet cross-section
Increase magnet length
Reduce component cost
Reduce labor
Improve performance - margin, Bop, Top
B. Palmer (BNL), 2014

## Slide 20: Conductor R&D program
Nb3Sn strand and cable
  Internal Tin, Powder-In-Tube wires → Rutherford cable
HTS conductor and cable
  Bi-2212 wire → Rutherford cable
  ReBCO tape → ROEBEL cable or CORC
Objective: improve Je and reduce cost
Chart: Year
| 1975.0 | 1980.0 | 1985.0 | 1990.0 | 2007.0
NbTi at 5T, 4.2 K | 720 | 1140 | 1200 | 1300
Nb3Sn at 12T, 4.2K | 630.45 | 990 | 1170 | 1350
Bi2212 at 20T, 4.2K | 448.28 | 600 | 800
Nb3Sn RRP strand, OST
Bi2212 PIT strand, OST
ROEBEL cable
Cable On Round Core (CORC)
40-strand Nb3Sn Rutherford cable
24-strand HTS Rutherford cable

## Slide 21: A new generation of Nb3Sn conductors
The key factor of Nb3Sn conductors for 16 T Nb3Sn magnets: critical current density, Jc
  What we have: Jc (15 T) = 1300-1500 A/mm2 for present state-of-the-art.
  What we need: Jc (15 T) = 2000-3000 A/mm2 for fabricating 16 T magnets economically.
We need 50-100% improvement of 15 T Jc over present Nb3Sn conductors.
How can we achieve such an improvement when Jc of Nb3Sn have plateaued for nearly two decades?
A new technique:
by generating ZrO2 artificial pinning centers (APC), Jc was doubled.
X. Xu et al., Adv. Mater. 27, 1346-50, 2015.
15 T Jc can be improved by a factor of 3.
More improvement by further optimization: add titanium dopant.
This new Nb3Sn has sufficient Jc for fabricating 16 to18 T magnets.
Its Jc at 20 T matches HTS.
Next steps:
Extend this technology to practical conductors.
Further optimization.

## Slide 22: Summary
Future energy-frontier colliders require advances in SC technology beyond state-of-the-art.
Cost reduction is very important aspect of R&D aimed at developing this technology
Electron-positron colliders will require large-scale SRF installations, e.g. 16,000 cavities for ILC.
Recent advances – nitrogen doping and nitrogen infusion, magnetic flux expulsion – demonstrate that there is still room for improvement using bulk Nb.
Further progress can be achieved with thin film techniques, especially Nb3Sn cavities.
High-field SC magnet technology is a cornerstone for future hadron colliders, which require fields of 16 to 20 T, beyond state-of-the-art.
R&D goals here include exploring performance limits of Nb3Sn; developing 16-T class accelerator quality magnets; pursuing Nb3Sn and HTS conductor development to increase performance and reduce cost.