## Slide 1: Collaboration Meeting on DS 11T Dipole Grounds
Current baseline design, project status and plan
F. Savary, on behalf of WP 11
23 September 2015

## Slide 2: OUTLOOK
Terminology and HL-LHC time line
Part I: Current baseline design
  Cable
  Cross section
  Cold mass assembly
  Integration, powering, trim
  Quench heaters and protection
Part II: Project status and plan
  Overall plan
  Model program
  Prototype
Conclusions

## Slide 3: Reminder on terminology – CRYO-ASSEMBLY
Create space in the dispersion suppressor regions of LHC, i.e. a room temperature beam vacuum sector, to install additional collimators (TCLD), which are needed to cope with beam intensities that are larger than nominal, such as in the High Luminosity LHC (HL-LHC)
Replace a standard MB by a pair of 11T dipoles (the 11T dipole is also called MBH)
Interconnect
Space for Collimator
11 T dipole cold mass
By-pass cryostat
15660 mm

## Slide 4: The DS 11T dipole on the HL-LHC timeline
Will start 6 months later
Will start a year later
First-of-a-kind shall be made before starting LS2
2nd unit immediately after
Possibly for IP2, however, installation during LS2 NOT ANYMORE in the baseline
6 additional units, of which:
  4 for installation in IP7
  2 spare units
In total up to 8 units
4 to 6 units to be installed
+ 2 spare units

## Slide 5: Another solution under study for IP2 – Heavy ions
Following 2013 Collimation Review:
  First installation (2 TCLD units) foreseen for ALICE Pb-Pb in LS2, subject to confirmation after 2015 Pb-Pb run and tests of bump mitigation techniques
Because of the form of the dispersion function in IR2, there is a possibility that we can combine bumps and an alternative location of the TCLD in the connection cryostat (missing MB)
  No 11 T magnets required
  Different but apparently simpler integration
  Significant orbit bump during luminosity operation!
  Option to include an additional horizontal corrector beside it
J.M. Jowett, Collimation Upgrade Meeting, 20/3/2015

## Slide 6: OUTLOOK
Terminology and HL-LHC time line
Part I: Current baseline design
  Cable
  Cross section
  Cold mass assembly
  Integration, powering, trim
  Quench heaters and protection
Part II: Project status and plan
  Overall plan
  Model program
  Prototype
Conclusions

## Slide 7: Conductor, cable and insulation scheme
  Type
  Diameter
  RRR
  Cu/non-Cu ratio
  Minimum strand critical current, IC (12T, 4.222 K)
  RRP 108/127
  0.700 ± 0.003 mm
  > 150
  1.15 ± 0.1
  438 A
Conductor (batch of 500 km)
  Number of strands
  Width before reaction
  Mid-thickness before reaction
  Keystone angle
  Cable unit length
  40
  14.7 mm
  1.25 mm
  0.79 degree
  ~ 600 m
Cable
Insulation scheme
  Mica tape, COGEBI FIROX®, thickness 80μ
  S2 glass gleeve
  Resin impregnation, CTD-101K
B. Bordini
D. Smekens

## Slide 8: Cross-section
Collared coils
Single aperture model
Two-in-one original
Two-in-one baseline
534 mm
6 block Nb3Sn coils of Ø 60 mm aperture
56 turns, 22 in inner layer, 34 in outer layer, no interlayer splice
Removable poles made of Ti
Separate stainless steel collars for each aperture
Vertically split iron yoke
Stainless steel shell of 15 mm thickness (2-in-1)
60 mm
182 mm
580 mm
Model MBHDP101
Models
570 mm
Model MBHDP102 – Proto P1
+ first 2 cryo-assemblies + …
Shim added between central yoke and laminations to allow adjustment

## Slide 9: Structural assessment
Yoke Outer Radius: 275 mm
Shell thickness: 15 mm
1 rod hole
Yoke Outer Radius: 270 mm
Shell Thickness: 15 mm
2 rod holes
F. Lackner, T. Lyon

## Slide 10: Structural assessment, 2
Chart: Coil Inner Mid-plane
| 0 | 0.75234999999999996 | 1.5046999999999999 | 2.2570000000000001 | 3.0093999999999999 | 3.7616999999999998 | 4.5141 | 5.2664 | 6.0187999999999997 | 6.7710999999999997 | 7.5235000000000003 | 8.2758000000000003 | 9.0282 | 9.7805 | 10.532999999999999 | 11.285 | 12.038 | 12.79 | 13.542 | 14.295 | 15.047000000000001
2-in-1 Yoke Ro 270 - Shell Weld | -23.66 | -26.672 | -29.684 | -32.488 | -35.291 | -37.86 | -40.429 | -42.762 | -45.096 | -47.203 | -49.311 | -51.208 | -53.105 | -54.812 | -56.519 | -58.055 | -59.591 | -60.973 | -62.356 | -63.608 | -64.86
2-in-1 Yoke Ro 275 - Shell Weld | -20.286 | -24.372 | -28.459 | -32.288 | -36.116 | -39.649 | -43.182 | -46.414 | -49.646 | -52.587 | -55.527 | -58.195 | -60.864 | -63.282 | -65.7 | -67.892 | -70.084 | -72.069 | -74.055 | -75.861 | -77.668
2-in-1 Yoke Ro 270 - Cool Down | -35.439 | -39.286 | -43.133 | -46.767 | -50.4 | -53.766 | -57.131 | -60.215 | -63.299 | -66.104 | -68.909 | -71.449 | -73.99 | -76.284 | -78.578 | -80.646 | -82.715 | -84.575 | -86.435 | -88.113 | -89.79
2-in-1 Yoke Ro 275 - Cool Down | -24.192 | -29.544 | -34.896 | -39.92 | -44.945 | -49.584 | -54.224 | -58.474 | -62.724 | -66.598 | -70.472 | -73.995 | -77.517 | -80.716 | -83.915 | -86.818 | -89.72 | -92.352 | -94.983 | -97.377 | -99.77
2-in-1 Yoke Ro 270 - 11T | -140.05 | -139.65 | -139.25 | -138.94 | -138.62 | -138.41 | -138.2 | -138.21 | -138.22 | -138.23 | -138.23 | -138.26 | -138.3 | -138.46 | -138.62 | -138.72 | -138.82 | -138.75 | -138.68 | -138.71 | -138.74
2-in-1 Yoke Ro 275 - 11T | -160.59 | -159.58 | -158.57 | -156.96 | -155.35 | -154.01 | -152.68 | -151.55 | -150.42 | -149.48 | -148.53 | -147.72 | -146.91 | -146.2 | -145.49 | -144.84 | -144.19 | -143.59 | -143 | -142.42 | -141.84
Chart: Coil Outer Mid-plane
| 0 | 0.75234999999999996 | 1.5046999999999999 | 2.2570000000000001 | 3.0093999999999999 | 3.7616999999999998 | 4.5141 | 5.2664 | 6.0187999999999997 | 6.7710999999999997 | 7.5235000000000003 | 8.2758000000000003 | 9.0282 | 9.7805 | 10.532999999999999 | 11.285 | 12.038 | 12.79 | 13.542 | 14.295 | 15.047000000000001
2-in-1 Yoke Ro 270 - Shell Weld | -64.477 | -65.616 | -66.755 | -67.794 | -68.833 | -69.796 | -70.759 | -71.676 | -72.593 | -73.498 | -74.404 | -75.341 | -76.277 | -77.307 | -78.337 | -79.559 | -80.78 | -82.363 | -83.946 | -86.764 | -89.583
2-in-1 Yoke Ro 275 - Shell Weld | -77.566 | -79.197 | -80.827 | -82.318 | -83.808 | -85.178 | -86.548 | -87.823 | -89.098 | -90.306 | -91.513 | -92.682 | -93.85 | -95.019 | -96.189 | -97.415 | -98.641 | -100.02 | -101.39 | -103.45 | -105.52
2-in-1 Yoke Ro 270 - Cool Down | -90.089 | -91.578 | -93.067 | -94.407 | -95.747 | -96.952 | -98.157 | -99.24 | -100.32 | -101.29 | -102.27 | -103.13 | -103.99 | -104.75 | -105.51 | -106.17 | -106.82 | -107.35 | -107.88 | -108.36 | -108.83
2-in-1 Yoke Ro 275 - Cool Down | -100.37 | -102.52 | -104.66 | -106.6 | -108.55 | -110.32 | -112.09 | -113.69 | -115.3 | -116.75 | -118.21 | -119.51 | -120.82 | -121.97 | -123.11 | -124.07 | -125.03 | -125.74 | -126.44 | -126.81 | -127.18
2-in-1 Yoke Ro 270 - 11T | -138.66 | -138.57 | -138.47 | -138.35 | -138.23 | -137.95 | -137.66 | -137.39 | -137.12 | -136.78 | -136.45 | -135.88 | -135.32 | -134.67 | -134.03 | -133.24 | -132.45 | -131.62 | -130.79 | -130.23 | -129.67
2-in-1 Yoke Ro 275 - 11T | -141.36 | -141 | -140.63 | -140.17 | -139.7 | -139.18 | -138.66 | -138.07 | -137.49 | -136.85 | -136.21 | -135.51 | -134.81 | -134.07 | -133.33 | -132.59 | -131.84 | -131.14 | -130.43 | -130.05 | -129.66
Chart: Coil Inner Pole
| 0 | 0.75234999999999996 | 1.5046999999999999 | 2.2570000000000001 | 3.0093999999999999 | 3.7616999999999998 | 4.5141 | 5.2664 | 6.0187999999999997 | 6.7710999999999997 | 7.5235000000000003 | 8.2758000000000003 | 9.0282 | 9.7805 | 10.532999999999999 | 11.285 | 12.038 | 12.79 | 13.542 | 14.295 | 15.047000000000001
2-in-1 Yoke Ro 270 - Shell Weld | -71.058 | -75.435 | -79.844 | -82.997 | -86.16 | -89.279 | -92.397 | -94.505 | -96.607 | -96.736 | -96.861 | -96.352 | -95.834 | -92.892 | -89.949 | -87.138 | -84.32 | -79.405 | -74.484 | -64.342 | -51.127
2-in-1 Yoke Ro 275 - Shell Weld | -89.456 | -94.786 | -100.15 | -103.85 | -107.56 | -111.21 | -114.87 | -117.24 | -119.61 | -119.52 | -119.43 | -118.53 | -117.61 | -113.73 | -109.85 | -106.13 | -102.41 | -96.179 | -89.944 | -77.457 | -61.353
2-in-1 Yoke Ro 270 - Cool Down | -99.697 | -106.76 | -113.93 | -117.01 | -120.09 | -123.37 | -126.64 | -129.56 | -132.47 | -133.13 | -133.79 | -133.54 | -133.27 | -129.7 | -126.13 | -122.37 | -118.59 | -112.74 | -106.88 | -94.261 | -85.465
2-in-1 Yoke Ro 275 - Cool Down | -117.49 | -125.69 | -134 | -137.63 | -141.26 | -145 | -148.74 | -151.83 | -154.9 | -155.26 | -155.6 | -154.82 | -154.01 | -149.41 | -144.79 | -140 | -135.19 | -128 | -120.8 | -106.02 | -94.809
2-in-1 Yoke Ro 270 - 11T | -51.132 | -53.834 | -56.611 | -57.384 | -58.15 | -59.335 | -60.514 | -62.363 | -64.201 | -65.228 | -66.246 | -66.97 | -67.683 | -66.615 | -65.541 | -64.28 | -63.01 | -60.507 | -57.999 | -52.18 | -52.253
2-in-1 Yoke Ro 275 - 11T | -35.785 | -36.42 | -37.115 | -37.59 | -38.055 | -38.944 | -39.827 | -41.537 | -43.237 | -44.566 | -45.886 | -47.075 | -48.253 | -48.081 | -47.904 | -47.467 | -47.022 | -45.638 | -44.25 | -40.847 | -46.588
Chart: Coil Outer Pole
| 0 | 0.75234999999999996 | 1.5046999999999999 | 2.2570000000000001 | 3.0093999999999999 | 3.7616999999999998 | 4.5141 | 5.2664 | 6.0187999999999997 | 6.7710999999999997 | 7.5235000000000003 | 8.2758000000000003 | 9.0282 | 9.7805 | 10.532999999999999 | 11.285 | 12.038 | 12.79 | 13.542 | 14.295 | 15.047000000000001
2-in-1 Yoke Ro 270 - Shell Weld | -69.432 | -64.76 | -60.02 | -59.123 | -58.194 | -57.85 | -57.492 | -57.211 | -56.922 | -56.581 | -56.24 | -55.745 | -55.252 | -54.505 | -53.763 | -53.07 | -52.373 | -51.661 | -50.954 | -39.317 | -27.705
2-in-1 Yoke Ro 275 - Shell Weld | -82.929 | -77.016 | -71.023 | -69.966 | -68.872 | -68.426 | -67.966 | -67.505 | -67.037 | -66.436 | -65.834 | -64.967 | -64.103 | -62.842 | -61.587 | -60.233 | -58.877 | -57.251 | -55.634 | -40.935 | -26.269
2-in-1 Yoke Ro 270 - Cool Down | -86.926 | -79.855 | -72.711 | -72.768 | -72.793 | -73.193 | -73.59 | -73.668 | -73.746 | -73.705 | -73.672 | -73.386 | -73.111 | -72.508 | -71.916 | -71.058 | -70.207 | -68.835 | -67.473 | -58.723 | -49.991
2-in-1 Yoke Ro 275 - Cool Down | -97.696 | -89.474 | -81.168 | -81.088 | -80.97 | -81.263 | -81.551 | -81.399 | -81.249 | -80.882 | -80.525 | -79.786 | -79.061 | -77.853 | -76.661 | -74.999 | -73.348 | -70.859 | -68.386 | -56.767 | -45.174
2-in-1 Yoke Ro 270 - 11T | -53.029 | -48.401 | -43.718 | -42.52 | -41.292 | -41.05 | -40.791 | -41.158 | -41.514 | -42.266 | -43.015 | -43.922 | -44.826 | -45.729 | -46.631 | -47.692 | -48.747 | -50.174 | -51.599 | -47.539 | -43.489
2-in-1 Yoke Ro 275 - 11T | -46.094 | -40.559 | -34.964 | -33.669 | -32.344 | -32.213 | -32.06 | -32.74 | -33.407 | -34.564 | -35.713 | -37.18 | -38.64 | -40.255 | -41.865 | -43.9 | -45.924 | -48.327 | -50.724 | -50.347 | -49.97
F. Lackner, T. Lyon

## Slide 11: Cold mass assembly – LMBH_001
H. Prin, D. Smekens, A. Temporal

## Slide 12: Cold mass assembly – LMBH_002
H. Prin, D. Smekens, A. Temporal

## Slide 13
Chart: z [mm]
magnetic length starts | -200 | 200
magnetic length ends | -200 | 200
Yoke starts | -200 | 200
Yoke ends | -200 | 200
Pad starts | -200 | 200
Pad ends | -200 | 200
Conductors starts | -200 | 200
Conductor ends | -200 | 200
Magnetic Yoke
Magnetic Length
Coil Length
Total Yoke Length
250 mm non magnetic
150 mm non magnetic
S. Izquierdo Bermudez

## Slide 14: Longitudinal section of the coil
The length of the coil is not finalized yet, as there are still uncertainties, and there are key parameters that need to be determined:
  The variations of length during/after binder curing and reaction need to be determined on long coils
  The introduction of the cut-back (non-magnetic laminations in the ends) to avoid peak field in the transition region between the straight part and the ends, means that the coils shall be ~ 20 mm longer
  Also, the reduction of the yoke OD shall be compensated by an increase of the coil length of  5 mm
  A stacking factor of 98.5 % ± 0.25 % will be implemented (coils will have to be slightly longer)
  The transfer function shall be checked
Final length will be determined when the magnetic measurements are done on the prototype P1

## Slide 15: Transfer function
  Possible sources of errors:
  Iron properties (the main source of errors)
        When using data measured during the LHC production, discrepancy decreases by 20 units (from ~70 to ~50 units)
  Stacking factor of the yoke laminations
      Can explain up to ~15 units
  Geometric
      Rather big displacements are needed to explain other 35 units (350 µm smaller coil gives ~15 units)
Modification on the BH data based on Wlodarski empirical relation.
Nom. Correspond to the parameters reported in S. Russenschuck book
Critical region!
MBHSP102
L. Fiscarelli, S. Izquierdo Bermudez

## Slide 16: Integration
Same 15660 mm length between the interconnect planes as an in the LHC Main Dipole
By-pass cryostat between two 11 T magnets to integrate the collimator (600 mm jaws)
LHC MB cryostat replaced by 3 cryostats + collimator, all independently supported and aligned
Same interfaces at the extremities: no change to nearby magnets, standard interconnection procedures & tooling
D. D. Ramos

## Slide 17: Integration 2
Cold mass enlarged to Ø750 on the collimator side
Constant LHC arc outer flange diameter: Ø1055
Flexible interconnects for alignment independency and thermal contraction
  Busbar routing is now in the shadow of the beam screens and CWT!
D. D. Ramos

## Slide 18: Integration 3
Interconnects become longer because of the beam screens
Very compact cold line because of the sector valve RF shielding
Transitions avoided because there are no sector valve on the other beam lines
Cold drift vacuum chamber
Vacuum group opts for cold line: “simpler” system, no failure prone sector valves
D. D. Ramos

## Slide 19: Electrical circuit – Powering
One protection diode for the 2 MBH Resistance to radiations need t.b.c. (peak dose value of up to ~1 MGy at the inner edge of the coils [in the horizontal plane])
Only 2 types of cold masses
IIN
IOUT
M3 line
L. Grand-Clement, H. Prin

## Slide 20: Electrical circuit – Trim
The integrated field of a pair of MBH’s is 119 Tm at 11.85 kA
The MBH is stronger than the MB below nominal current with a peak difference in integrated field around 6.5 kA
A trim current is used to correct for this and avoid deformation of the beam closed orbit
Conduction cooled leads: about 3.6 W/kA to 1.9 K
RT copper cables  towards power converter
  Main characteristics of the trim power converter:
  Current rating: 0 – 250 A
  Voltage rating: ± 1.5 V + V_cable (< ± 40 V)
  Accuracy: 40 ppm (12 mA)

## Slide 21: Quench heaters
Baseline after review of the analysis and test results
  QH located on the outer surface of the outer layer, and impregnated with the coil
Inter-layer QH are under development
  Will not be tested/available before we start the fabrication of the coils for the prototype P1. However, will be hopefully available for the first series magnets
Quench heater circuit(s) redundancy needs to be defined, e.g.
  Protection still effective when one (or two) of the QH is (are) lost
    OR
  Additional circuit is available and may be connected in case there is a failure in the already connected/used circuit
S. Izquierdo Bermudez

## Slide 22: Electrical circuit – Quench heaters and protection
L. Grand-Clement

## Slide 23: OUTLOOK
Terminology and HL-LHC time line
Part I: Current baseline design
  Cable
  Cross section
  Cold mass assembly
  Integration, powering, trim
  Quench heaters and protection
Part II: Project status and plan
  Overall plan
  Model program
  Prototype
Conclusions

## Slide 24: Model programme RRP cable
Coil
106
107
108
109
111
112
113
114
115
116
117
Single Aperture
SP101
SP102
SP103
SP104
SP105
SP106 (test 3rd Q 16)
Two-in-One
DP101
  Test Dec.15-Jan.16
DP102
  New yoke design
  Reduced OD
QH/Traces glued on outside surface of OL
QH/Traces impregnated on OL
QH/Traces impregnated on OL + interlayer QH
1
2
3

## Slide 25: The DS 11T dipole on the HL-LHC timeline
PROTOTYPE P1 - RRP
Q4-2016 / Q2-2019
Q2-2020 / Q2-2024
Production for LS2
Production for LS3
Models PIT cable
On-going / Q4-2016
Models RRP cable
Q1-15 / Q1-17
Q3-2016 / Q2 -2018
PROTOTYPE P2 - PIT
Q1-19 / Q4-20
PIT and/or RRP
Cold tests in first quarter of 2017
Start after cold tests of SP106 are done (inter-layer QH)
Start after coils for LS2 are done

## Slide 26: Production of first long coils in B180
2nd coil with braided Cu cable during winding
Detail of the 2nd Cu cable coil after curing
3rd coil, with braided Sc cable during winding
New clutch / PCS for better control of the tension on cable during winding
1st
Sc coil
Wound & cured

## Slide 27: Tooling for the production of the long coils
6.5 m long reaction furnace – fully operational
6 m long reaction fixture
10.5 m long impregnation chamber
6 m long impregnation fixture

## Slide 28: Other illustrations of tooling

## Slide 29
Terminology and HL-LHC time line
Part I: Current baseline design
  Cable
  Cross section
  Cold mass assembly
  Integration, powering, trim
  Quench heaters and protection
Part II: Project status and plan
  Overall plan
  Model program
  Prototype
Conclusions

## Slide 30: Conclusions
The DS 11T dipole plan was updated after the cost and schedule review of March 2015
The installation in LHC during LS2 is not anymore in the baseline but we are asked to be ready to install 2 cryo-assemblies during LS2 upon request
The baseline design was further developed with some adjustments. However, no major modifications
Some items need particular attention:
  Finalization and construction of the quench heaters
  Coil length
The engineering design of the full-length magnet, including the cryostat, is now well advanced
The major tooling is available in the Large Magnet Facility @ CERN