## Slide 1
Model Magnets Assembly at FNAL
Igor Novitski
September 21, 2015
Collaboration meeting on DS 11T Dipole grounds
FNAL, Sep. 21-23, 2015

## Slide 2
MBHSP02
Model Magnets
MBHSP01
Coil 2
Coil 3
Coil 5
Coil 7
MBHSP03
Coil 9
Coil 10
MBHSM01
Coil 8
MBHDP01
Coil 7
Coil 5
Coil 9
Coil 10

## Slide 3: Mechanical Models
Define “warm” magnet shim sizes
Check parts and tooling
Finalize collaring and yoke clamping procedures
“Study of Mechanical Models of a Single-Aperture 11 T Nb3Sn Dipole” presented at ASC 2012 (Portland, USA)

## Slide 4
FEA simplifies coil properties by using the cold elastic modulus
Coil warm and cold properties are different
Coil has an anisotropy in the azimuthal and radial directions
Warm magnet shims are different from calculated ones and need to be optimized with real parts to achieve the desired warm coil pre-stress.
Azimuthal stress distribution in Nb3Sn coil after collaring (top) and clamping (bottom).
Position in coil | Azimuthal Coil Stress, MPa |  | 
 | Collared coil | Clamped yoke | Cold mass
Inner pole | -44 | -60 | -120
Outer pole | -64 | -55 | -87
Inner midplane | -97 | -58 | -79
Outer midplane | -51 | -55 | -108
FEA results of the dipole mechanical structure
Coil Shims
Radial Shim
Middle Plane
Shim
Yoke Shim

## Slide 5
The coil outer diameter (OD) and midplane were measured in the coil free state using a coordinate measuring machine.
A collar lamination profile after laser cutting performed on the optical table
The deviations of the collar inner surface from the design value are < 50 µm
The inner diameter of the assembled and keyed collar packs was also measured with a micrometer
Based on the coil and collar pack sizes the coil-collar interface was shimmed to compensate for collar fabrication errors.
The accuracy of wire-cut 25 mm thick yoke laminations is within ± 25µm on all working surfaces.
Coils become smaller radially and azimuthally by 50-100µm after been used in the MMs.
  Coil Cavity Size Control
1 box =125 mm

## Slide 6
2 m long Nb3Sn practice coil was cut into six pieces
Resistive strain gauges glued on the coil inner surface, on the stainless steel wedges and on the titanium poles
Fuji film measures stress gradients
Six collared models were built with different shimming (0-0.12mm)
One collared model was clamped twice
Magnet shim plan was finalized
Mechanical Models

## Slide 7: MBHSP01 2m Long Magnet
RRP 108/127 conductor
No Core
Original ends
Laser cut collars
Collaring after MM
Shims after MM
Welded skin
Welded end plates
“Development and Test of a Single-Aperture 11 T Nb3Sn Demonstrator Dipole for LHC Upgrades” presented at ASC 2012 (Portland, USA)

## Slide 8: Collar Pack
Parameter | Value
Collar material | Nirosta high-Manganese SS
Collar width, mm | 17.75
Lamination thickness, mm | 1.5
Collar pack length, mm | 38
  Use 0.127 mm shim between laminations.
  Welded longitudinally along the pole
  and on the O.D. above the pole.
  Have 2 pins each welded at the ends.

## Slide 9
MBH02
445 mm from RE
MBH03
435 mm from RE
MBHSP01
Size Control
1 Box = 25.4 mm
1 box =125 mm
Laser Cut Collar lams
Wire EDM Iron lams

## Slide 10
220m Middle Plane Shim
175m Radial Shim
190 m Shim
215 m Shim
240 m Shim
215 m Shim
190 m Shim
325 m Shim
325 m Shim
Taper Yoke Shim
MBHSP01 Shim Plan
8.8mil Kapton
7mil Kapton
7.5mil Shim
8.5mil Shim
9.5mil Shim
8.5mil Shim
7.5mil Shim
13mil Shim
13mil Shim
Taper Yoke Shim

## Slide 11
Coil assembly process developed with mechanical model
Upper and lower collar packs are shifted to interlock all collar packs together
A layer of 0.112mm (4.4mil) thick pre-preg Kapton ironed to the coil
The two coils, surrounded by ground insulation (5x0.127mm Kapton) and 0.5mm protection shoes
Coils assembly

## Slide 12: Collaring
Parameter | Value
Protection shoe thickness, mm | 0.5
Protection shoe material | 304
Collar material | 316LN
Collar width, mm | 17.75
Lamination thickness, mm | 1.5
Collar pack length, mm | 38
Number of keys | 4
Key height, mm | 6
Key thickness, mm | 5
Key material | Bronze
Press gradually increase vertical pressure on a contact tooling to open collar keyways.
Tapered keys are hydraulically pressed into the collars
Press released with coil spring-back
12

## Slide 13
Splice block size even with magnet SS
Collared Coil Mechanical Measurements

## Slide 14: Yoking and Clamping
Collar-Yoke Shim

## Slide 15
Clamped Iron Mechanical Measurements

## Slide 16
Skin Welding
Gaps
Chart: Shell Stress at ±30°, Lead & Return End
| in press | fusion-skip 100 mm | final fusion-skip 100 mm | 1 filler | next day | 2 filler | 3 filler | next day | 4 filler | 5 filler | 6 filler | next day
30ALE | 0 | 46.8164 | 72.0209 | 71.8751 | 74.1999 | 65.7764 | 143.7273 | 143.5775 | 185.7197 | 217.9851 | 231.8955 | 235.608
30ARE | 0 | 34.638 | 62.746 | 35.2971 | 36.9128 | -4.3779 | 245.8676 | 251.1244 | 330.8232 | 406.9422 | 470.1097 | 473.8056
30BLE | 0 | 49.1594 | 88.645 | 128.8093 | 135.3926 | 193.3867 | 275.4283 | 277.9331 | 352.9487 | 420.6889 | 479.1629 | 479.4638
30BRE | 0 | 41.3804 | 87.0968 | 119.1534 | 128.4953 | 122.7881 | 278.1472 | 282.174 | 383.453 | 446.4268 | 514.0751 | 517.9311
30CLE | 0 | 66.3382 | 100.4671 | 121.8876 | 129.1493 | 163.5835 | 303.4664 | 304.3855 | 352.6783 | 381.4232 | 410.0571 | 410.7959
30CRE | 0 | 63.1936 | 94.3861 | 111.0436 | 115.0568 | 121.7794 | 281.3963 | 282.8224 | 360.9963 | 456.4805 | 534.3689 | 539.9592
30DLE | 0 | 27.253 | 88.5399 | 170.7949 | 177.0807 | 244.5532 | 328.2624 | 331.4674 | 401.864 | 462.8922 | 524.7011 | 527.4053
30DRE | 0 | 2.3015 | 71.1087 | 137.0749 | 153.7658 | 155.5826 | 276.6995 | 278.5094 | 350.2821 | 398.7851 | 451.5214 | 453.2847
Chart: Shell Stress at ±60°, Lead & Return End
| in press | fusion-skip 100 mm | final fusion-skip 100 mm | 1 filler | next day | 2 filler | 3 filler | next day | 4 filler | 5 filler | 6 filler | next day
60ALE | 0 | 132.4652 | 184.5079 | 200.6835 | 204.7982 | 260.454 | 330.5738 | 339.1588 | 378.3033 | 406.7642 | 433.625 | 443.3731
60ARE | 0 | 143.8035 | 198.3023 | 219.0072 | 221.3304 | 239.0749 | 342.0159 | 347.3569 | 399.9892 | 445.2166 | 482.2591 | 488.2023
60BLE | 0 | 116.8728 | 155.9539 | 175.0465 | 184.4299 | 224.5186 | 279.2319 | 283.6164 | 330.25 | 363.1608 | 389.9929 | 393.7005
60BRE | 0 | 81.3522 | 125.7253 | 156.5483 | 163.5269 | 174.4045 | 267.4211 | 272.7027 | 322.6947 | 359.2341 | 389.0284 | 394.7546
60CLE | 0 | 115.305 | 152.6564 | 171.3303 | 178.2914 | 206.1985 | 279.6104 | 284.324 | 318.3545 | 338.2272 | 362.0663 | 367.7897
60CRE | 0 | 40.3091 | 76.0835 | 97.3358 | 104.4444 | 116.1055 | 202.1208 | 203.845 | 247.9781 | 292.271 | 333.5115 | 338.3103
60DLE | 0 | 105.5512 | 139.5312 | 167.3468 | 175.8876 | 213.1472 | 265.9842 | 270.2099 | 310.0871 | 337.2329 | 366.8678 | 368.8545
60DRE | 0 | 30.4632 | 68.8091 | 99.8052 | 109.6153 | 122.567 | 194.7902 | 200.3885 | 242.9087 | 278.1919 | 313.1065 | 318.571
Actual gap ~3 mm (design=0.7mm)

## Slide 17
MBHSP01 SG Data

## Slide 18: Skin Cutting and End Plate Welding

## Slide 19: End Design
Parameter | Value
Yoke lam thickness, mm | 25
Yoke material | Hot rolled steel SAE 1045
Clamp material | Al 7075-T6
Skin material | 304L
Skin thickness, mm | 12.7
End plate material | 304L
End plate thickness, mm | 50
Bullets load, kN per end | 17.6
Return end cross section: 1 – end plate; 2 – strain gauge bullets; 3 – bullet pressure plate; 4 – skin
4
2
3
1
NbTi leads splicing
Instrumentation wiring and connectors soldering
Final electrical and hi-pot test

## Slide 20: MBHSP01 Test Results
Magnet reached 10.4 T or 78 % of SSL at 1.9 K showing limited quench performance. Most quenches at low ramp rates, all holding quenches and quenches at intermediate temperatures initiated in the mid-plane block of the outer coil layer. Only few training quenches occurred in the high field area at the very beginning of test at 4.5 K and 1.9 K. Quench location, ramp rate and temperature dependence studies, and additional tests point out on the problems with coil outer-layer lead in both coils. Possible conductor damage in the mid-plane area during fabrication could cause the observed degradation.

## Slide 21
Collared Coil Size “B”
Magnet Autopsy
LE Marks on the Collar-Yoke Interface – high pressure at the magnet LE
Collar-Yoke Shim
Yoke lamination

## Slide 22
Imprint on the GI and Protection shoe
LC Collar Pack Inner Surface at Middle Plane
Marks on the Protection Shoe

## Slide 23
Reduce skin load at the LE => reduce cold splice stress by ~40MPa
Change material for LE saddle and splice block cylinder from SS to AlBr => better match coil radial motion
Reduce radial yoke-collar shim at MP area
Bigger Collar ID
Thicker Retainer
Stamped Collars
Bolted Skin
Recommendation

## Slide 24: MBHSP02
RRP 150/169 conductor
Core cable
Modified ends
Laser cut lams and modified collar packs
Two Collaring Iterations
Thicker radial shim
Smaller bending shim
Horizontally bolted skin
Bolted end plates
“FABRICATION AND TEST OF A 1 M LONG SINGLE-APERTURE 11 T NB3SN DIPOLE FOR LHC UPGRADES ”
presented at IPAC 2014 (Dresden, Germany)

## Slide 25: Reworked Collar Packs
1 Box = 25.4 mm
Reworked
Reworked Collar Packs
for MBHSP02

## Slide 26
MBH02
445 mm from RE
MBH03
435 mm from RE
MBH05
479 mm from RE
MBH07
467 mm from RE
MBHSP01
MBHSP02
Coil Sizes

## Slide 27
MBHSP01 and MBHSP02 Shimming
8.8mil Kapton
7mil Kapton
7.5mil Shim
8.5mil Shim
9.5mil Shim
8.5mil Shim
7.5mil Shim
13mil Shim
13mil Shim
Taper Yoke Shim
Radial Shim
Middle Plane
Shim
8.8mil Kapton
10mil Kapton
8.5mil Shim
5mil SS+3.5 Kapton
5mil SS Shim
5mil SS Shim
Uniform Yoke Shim
Radial Shim
Middle Plane
Shim

## Slide 28
  MBHSP02 demonstrated better performance than MBHSP01 and reached 11.7 T or 97.5% of its design field at 1.9 K
  Still significant quench current degradation observed
  Both magnets showed so called “holding quenches”, when magnet is quenching at a fixed current after holding it for a certain time (resistive conductor)
MBHSP02 Test Results

## Slide 29
MBHSM01
RRP 109/127 conductor w core
Ordinal end parts
New coil sizing
Mirror structure
No collars
Reduced coil prestress and bending
Horizontally bolted skin
Bolted end plates
“TESTING OF A SINGLE 11 T Nb3Sn DIPOLE COIL USING A DIPOLE MIRROR STRUCTURE” presented at IPAC 2014 (Dresden, Germany)

## Slide 30
MBH02
445 mm from RE
MBH03
435 mm from RE
MBH05
479 mm from RE
MBH07
467 mm from RE
(1 box = 101.6 mm)
MBHSP01
MBHSP02
MBH08
447 mm from RE
MBHSM01
Mirror Block
Coil Sizes

## Slide 31
Design
contour
QC
contour
Real
contour
QC data
Coil #8
Coil #8 by 4mil smaller on OR and by 3mil bigger at MP wrt design Coil #2 by 5mil smaller on OR and by 1mil bigger at MP wrt design
Coil Sizes

## Slide 32
Coil #8 Instrumentation
Quench Antenna
SG at RE

## Slide 33
25+10mil–Shell+3K
2.446 – Yoke IRm
2.421:5x4-GIKapton
2.391 - Coil ORd
3.18mm(0.125mi)
shim
shim
5K+50G10+3.5aK+60G10+5K=123.5mil
MBHSM01 Shimming

## Slide 34: MBHSM01 Test Results
MBHSM01 reached ~ 13 kA or (92-100)% of SSL at 4.5 K, and 14.1 kA or 89-97 % of SSL at 1.9 K
The stainless steel core, successfully implemented in this model, significantly reduced the magnet ramp rate sensitivity at the high current ramp rates
The magnet exhibited stable performance, no spontaneous quenches observed when “holding” 12 kA at 4.5 K and 13 kA at 1.9 K for ~ 25 minutes

## Slide 35
MBHSP03
RRP 108/127 conductor w core
Modified ends
New coil sizing
New stamped collar with larger ID
Thicker shoe
Conservative coil prestress
Mirror as target
Less bending
Vertically bolted skin
Bolted end plates
“STATUS OF 11 T 2-IN-1 Nb3Sn DIPOLE DEVELOPMENT FOR LHC” presented at IPAC 2014 (Dresden, Germany)

## Slide 36: Coil Sizes
MBHSP02
MBHSP03
MBH05
MBH 07
262 mm from RE
Modified
Coil Bigger at MP

## Slide 37: Collar Packs
1 Box = 25.4 mm
Reworked
MBHSP02
MBHSP03
Laser Cut
Stamped
Larger ID (+0.48mm) for Bigger Shoe

## Slide 38
MBHSP02
MBHSP03
Shim Plans
17mil Shoe
10mil Radial Shim
8.8mil MP Shim
32mil Shoe
7 and 10 mil Radial Shim
0 MP Shim
7mil
10mil

## Slide 39
MBHSP03
MBHSP02
Magnet Assembly
Rotated 90°
MBHSP02
MBHSP03

## Slide 40: MBHSP03 Test Results
MBHSP03 was trained to 11.2 T or 93.3% of the magnet design field.
All the training quenches at 1.9 K occurred in the inner-layer high-field blocks.
Quench current fluctuations, seen at the field level of 11 T, are likely due to epoxy cracking between the inner-layer pole blocks and coil pole turns caused by the conservative coil pre-stress in this model.
To avoid possible conductor degradation the magnet training was interrupted.

## Slide 41: MBHDP01
First Nb3Sn twin aperture dipole magnet
Tested collared blocks
Symmetry of collar-yoke shimming
Welded skin
Welded end plates
“STATUS OF 11 T 2-IN-1 Nb3Sn DIPOLE DEVELOPMENT FOR LHC” presented at IPAC 2014 (Dresden, Germany)
“11 T Twin-Aperture Nb3Sn Dipole Development for LHC Upgrades” presented at ASC 2014 (Charlotte, USA)

## Slide 42
+75mm
Kapton
Coil 10
Coil 9
Coil 7
Coil 5
Coil 7
Coil 5
Coil 9
Coil 10
MBHSP02
MBHSP03
MBHDP01
Load symmetry
Load asymmetry
Re-collaring
after test
Twin-aperture Dipole: Coil History
After test

## Slide 43
Iron Geometry

## Slide 44: Geometry Check
Shim=40mil
Gap=40 at 2000
Red=contact
Shim=40mil
Gap=14 at 2000
4mil+2mil Kapton
4mil+2mil Kapton
4mil+2mil Kapton

## Slide 45
Magnet Yoking and Skinning

## Slide 46
Main
pressure
=1500psi
Contacts
Side bars
added for
stability
Skin Welding

## Slide 47
End Plates

## Slide 48
Coil 5
Coil 7
Coil 10
Coil 9
Leads Connection

## Slide 49
“QUENCH PERFORMANCE OF THE FIRST TWIN-APERTURE 11 T DIPOLE FOR LHC UPGRADES” presented at IPAC2015,( Richmond, USA)
MBHDP01 Test Results
The magnet reached a bore field of 11.5 T at 1.9 K, which is 97% of its design field, which is less than 1% lower than the maximum bore field obtained in the single-aperture models.
The magnet demonstrated similar quench performance which was limited by large conductor degradation in the collared coil used in MBHSP02. No additional coil degradation was introduced during re-assembly of one of the collared coils and twin-aperture dipole assembly process.
Magnetic measurements in one of the two apertures will be performed in the next test run.

## Slide 51: Back Up Slides

## Slide 52
MBHSP01

## Slide 53: Coil Ground Insulation
112um(4.4mil) thick pre-preg Kapton ironed to the coil

## Slide 54: Coil placement on the rotation station

## Slide 55: Ground Insulation Final Wrap

## Slide 56
-132
-329
Coil Straight section
-80
-264
Splice with SS cylinder
-102
-315
Splice with AlBr cylinder
197
184
213
FEA Result
300K
4K
dR in mic at coil MP OR before and after CD

## Slide 57
Splice
LE saddle
SS
Outer lead
Inner lead
Cable position
After CD
Radial Load at the Magnet Lead End
NbTi
Nb3Sn
G10
FEA Model of the
Magnet Splice Block

## Slide 58
MBHSP02

## Slide 59
4.846
4.838
4.849
4.850
4.854
4.8575
4.859
4.856
4.856
4.854
4.853
Unused Pack
Used and Modified Pack #12
Reworked Collar Packs

## Slide 60
Used and Modified Pack #21
Reworked Collar Packs

## Slide 61
MBHSP02 SG Data

## Slide 62
D
G
Coil #5
Coil #7
B
MBHSP01
MBHSP02
Collared Coil Size

## Slide 63
MBHSP01 after test
Clamped Iron Mechanical Measurements

## Slide 64
Skin Stress
MBHSP01

## Slide 65
MBHSM01

## Slide 66
Iron Laminations

## Slide 67
Skin Stress
MBHSP02

## Slide 68
MBHSM01 SG Data after Skin Bolting

## Slide 69
MBHSP03

## Slide 70
MBH02
445 mm from RE
MBH03
435 mm from RE
MBH05
479 mm from RE
MBH07
467 mm from RE
(1 box = 101.6 mm)
MBHSP01
MBHSP02
MBH08
447 mm from RE
MBHSM01
Mirror Block
Coil Sizes
MBHSP03

## Slide 71
After Skin Bolting

## Slide 72
MBHSP02
MBHSP03
Collared twice
with radial shim increase
by 3mil=75um
Main pressure 6000psi
Key pressure 8000psi
Main pressure 4000psi
Key pressure 10000psi
OD after Collaring
Design

## Slide 73
After Yoke Clamping
Main pressure 3000psi
Key pressure 3500psi
Main pressure 2500psi
Key pressure 3500psi
MBHSP02
MBHSP03

## Slide 74: Bullets
MBHSP02
MBHSP03

## Slide 75: MBHDP01

## Slide 76
MBHSP02
MBHSP03a
Collared Coil Shims
17mil Shoe
10mil Radial Shim
8.8mil MP Shim
32mil Shoe
10 and 13 mil Radial Shim
0 MP Shim
10mil
13mil

## Slide 77
Collared Coil Geometry
design

## Slide 78: Iron Geometry Check
“0” gap on Bars
1.503-1.505
Measured gap 10-15mils (design~40 mils)
At the ends ~0, locally at ss ~20
Witness marks on opposite sides

## Slide 79
Skin SG Readings
Stress, MPa
Massaging
Welding

## Slide 80
MBHDP01 SG Data

## Slide 81
MBHDP01 SG Data

## Slide 82
Bullets Loading