## Slide 3
SMC-11T: C1, C2
RRP 108/127
[B. Bordinini, 2014]
MBHSP: C105, C106, C108
[P. Wanderer 2009]
RRP 54/61 and 108/127
HQ01e: C5, C7, C8, C9
HQ02: C15, C16, C17, C20
[A. Godeke, 2014]
RRP 108/127 (jc >2800)

## Slide 4
7 voltage signals can triggered the protection scheme (redundancy)
Typical time windows and threshold:
V_sum and Dif : Vmax = 100 mV for 10 ms
Splices Vmax = 10 mV for 8 ms
Leads Vmax = 80 mV for 500 ms

## Slide 5
RRP 54/61 and 108/127
HQ01e: C5, C7, C8, C9
On the direct signal

## Slide 6
RRP 54/61 and 108/127
HQ01e: C5, C7, C8, C9
On the direct signal
Amplitude up to 2 V and duration between 5 to 60 ms: Trip of the protection

## Slide 7
FJ amplitudes higher @ 4.2 K than @ 1.9 K
FJ frequency lower @ 4.2 K than @ 1.9K
Amplitude up to 2 V at 4.2 K and 750 mV at 1.9 K.
Need to adapt threshold to pass flux jump occurrence current range
On the differential signal
HQ01e: C5, C7, C8, C9

## Slide 8
Voltage
10 A/s
50 A/s
The higher ramp rate, the lower the flux jump frequency.
Voltage
Effect of the Ramp Rate
@ 4.2 A/s

## Slide 9
HQ02: C15, C16, C17, C20
RRP 108/127 (jc >2800)
MBHSP: C105, C106, C108
Flux Jumps amplitude  at the limit of the detection (100 mV / 10 ms)
1.9 K measurement
Very similar behavior between
RRP (HQ vs.11T)

## Slide 10
100 mV
7 ms
HQ02: C15, C16, C17, C20
RRP 108/127 (jc >2800)
MBHSP: C105, C106, C108
Flux Jumps amplitude  at the limit of the detection (100 mV / 10 ms)  200 mV / 5ms

## Slide 11
The occurrence of the spike depends on the cable RRP filament size.
The amplitudes of the spike is higher at 4.2 K.
The frequency of the spike is higher at 1.9 K.
The frequency of the spikes is lower at higher ramp rate.
First HQ generation: issue with regard to voltage spikes with amplitude and duration within our «reference» quench detection setting (100 mV, 10 ms).
Second HQ generation: voltage spikes below our criteria if (200 mV, 5ms). No trip of the detection system

## Slide 12
RRP 108/127 1.9 K