## Slide 1: MQXFSM1 results
Guram Chlachidze
Stoyan Stoynev

## Slide 2: Status
The magnet was cooled down on May 3
RRR measurements and
warm up completed on
June 1st
Number of testing days: 15
Highlights
  30+ training quenches at 1.9 K,
  maximum current 19239 A
  (91.3% of SSL at 1.9 K)
  Reached 82% of SSL in 5 quenches
  but hit a limit (~90% of SSL) after 18 quenches
May 3

## Slide 3: Quench detection instrumentation
Voltage taps and
quench antennas
positions
IL
OL
QA:

## Slide 4: Quench location
Chart: Quench #
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 43 | 44
a3_a4 | 17810 | 18418 | 18711 | 18893 | 19000 | 18766 | 19239 | 19052 | 18668 | 18857
a4_a5 | 15948 | 17312 | 18254 | 19106 | 18726 | 18984 | 18984 | 18989 | 18937 | 18809 | 18905 | 18874
a6_a8 | 14814 | 16489 | 17424 | 17802 | 17992 | 18765 | 18847
b7_b6 | 16824 | 17444
b5_b4 | 18030 | 18430
Few days difference
All the a3_a4 and a4_a5 (after hitting the plateau) points are very similar with hard to
distinguish time difference between a3_a4 and a4_a5 (that is – it is likely a single location
quenching all the time); quench antennas support this as well – always LE ones active
retraining
(ramp rate studies;
quench protection
studies)
1
1
4
4
2
4
2
1
4
1
-
4
1
-
1
3
2
1
4
1
1
1
1
1
1
1
1
1
1
1
1
1
1
Quench antennas: 1 (LE) to 5 (RE)

## Slide 5: Training in terms of SSL fraction
In addition to the quenches shown there were also quenches related to other studies
(like ramp rate dependence) and also few re-training ones. No improvement was observed.
HQM04 is another magnet we can
tentatively compare to
(it is a quadrupole mirror)

## Slide 6: Temperature dependence
In terms of SSL fraction of the quench current there are no large variation
with temperature for MQXFSM1.

## Slide 7: Ramp rate dependence
The magnet did not quench at ramping down (from 18 kA) at 300 A/s
Quench current

## Slide 8: RRR
RRR values of 150 are typically obtained, no outliers.
IL
OL

## Slide 9: Holding current time
The magnet was at 16.5 kA flat top for two hours at 4.5 K
The magnet was at 17.8 kA flat top for two hours at 1.9 K
However at 1.9 K it quenched during ramp down at 20 A/s (Iq = 17.6 kA)

## Slide 10: Inductance measurement
The measured inductance
at 300 K and 20 Hz is 5.2 mH
4.5 K
200 A/s
1.9 K
Measurements at 200 vs 300 A/s
(4.5 K) are consistent
(despite some technical issues)

## Slide 11: Splice resistance
IL (A)
OL (B)

## Slide 12: Spike analysis
Spikes depend on the length and quality of cable,
there is typically a peak (magnitude, frequency of occurrence) at relatively low current
(long mirror)
(quadrupole)

## Slide 13: Quench protection studies

## Slide 14
Two inner layer PH strips, as well as 2 pole and 2 mid-plane outer layer strips were connected in series internally, during the magnet assembly.
The 2 OL heaters are connected in parallel or
tested/fired individually
IL
OL
IL – copper cladded SS
OL
(LQ style)

## Slide 15: Minimum power density
PH power density:
= 0.5 Ohm . m
stainless steel (heater) thickness and width :
IL (OL)
Minimum heater power density
inducing a quench
Time const
 ≈ 40 ms

## Slide 16: Minimum power density (2)
ZOOMED version of the previous slide’s plot

## Slide 17: Heater delay vs current
Reproducibility test – there are three
repeated measurements (points) here
Reproducibility test – there are three
repeated measurements (points) here
These are the time differences between
heater firing and
the start of quench development
For OL pole and middle plane tests
 ≈ 94 ms,
for IL -  ≈ 40 ms

## Slide 18: Heater delay vs current (2)
ZOOMED version of the previous
slide’s plots
Both plots here are in the same scale(s)

## Slide 19: Heater delay vs peak power density
For OL pole and middle plane tests  ≈ 94 ms ,
for IL -  ≈ 40 ms

## Slide 20: Heater delay vs decay time constant
The time constant was changed by changing the HFUs capacitance – 19.2/14.4/9.6 mF
The power density was ~ 108-113 W/cm2 (same for a given set)

## Slide 21: Quench propagation schematics
tHFU1 t’q t0(≡0) t’’q tdump time
IL
OL
Magnet current
Quench
development
(for a given segment)
tHFU1 : heater fired
tq : start quench development
t0(≡0) : quench detected
tdump : dump resistors engaged
tata : layer-to-layer
propagation time
FOR ILLUSTRATIVE PURPOSES
Example configuration:
- IL heater to unit HFU1
- OL heater off-line
- Dump delay of 1000 ms
tata

## Slide 22: Quench propagation
Quench propagation time between layers
{ t=0 < tq (layer1; heater induced) < tq (layer2; propagated) }
Dump delay is large (1000 ms).

## Slide 23: Quench integral
t = 0 ms here refers to the manual trip initiation time
tq is the start of (heater induced) quench development

## Slide 24: Summary
Quench training of MQXFSM1 reached 90 % of SSL
Behavior remains similar at higher temperature
Very good performance vs ramp rate
(eddy current losses well controlled by SS cored cable)
Holding current tests – stable performance
Good RRR and splice resistances
Consistent inductance measurements
Rich quench protection related data
(reproducibility checked)