## Slide 1: Surface Brillouin scattering of transitional metal nitrides, composite oxides
Daniel Wamwangi
School of Physics

## Slide 2: Projects overview:
Photovoltaic and opto-electronic properties
Light amplification approaches
Charge carrier transport and life stability
Inelastic light scattering on thin films
Thin film growth dynamics of Hard coatings
Stress evolution and relaxation in thin films
Elastic properties versus electronic/ dielectric properties
Thermal conductivity of phase change materials

## Slide 3: Outline
Introduction: Dynamics of thin films growth and hard coatings
Nucleation and growth Structure Zone model (SZM)
Methods of thin film growth: instrument and conditions
Characterizations of thin films:
Surface acoustic wave propagation: Rayleigh surface acoustic
waves, phonon velocity dispersion curves, elastic constants
Case studies or examples: Nitrides, complex oxides, carbides

## Slide 4: Introduction: thin films/ coatings
Unique properties, (TM>1500C), superior hardness, chemical inertness, high corrosion resistance
Protective coatings and diffusion barrier layers, magnetoelectric sensors, storage
Stress evolution and relaxation fundamental to intrinsic stress
Film microstructure versus mechanical properties of hard coatings
Epitaxial layers: strain mismatch, Reciprocal Space Mapping

## Slide 5: Introduction: Thornton (SZM) model

## Slide 6: Diversity of thin film growth
Etching/ plasma cleaning: SiO2:
P= 40W, UB = - 300V te= 5 min
Film growth conditions
Sputter Power: Variable
Inert or reactive gas (Ar2) : Pressure
Substrate bias 0 V and – 60V
DC reactive sputtering
RF magnetron sputtering
HiPIMS

## Slide 7: Characterization: X-ray reflectometry
kin
n = 1
c
Incident plane
Limit of refraction:
cos c = 1- 
2c = (2) = (re / ) 2 e
e = electron density
total external reflection of X-rays from surface and interfaces

## Slide 8: Surface Brillouin scattering:
Film probed with 514.nm
Ar+ line, laser
Back scattered light guided to
multi-pass FPR interferometer
Backscattered light frequency
shifted
Surface waves dynamics:
Rayleigh Surface Acoustic waves
Sezawas modes

## Slide 9: Microstructure, morphology and composition
ad atom energy effects on microstructure
ad atom energy effects on composition
Dual effects on elastic constants

## Slide 10: nitrides: ad atom energy variations

## Slide 11: BiFeO3: microstructure and morphology
Columnar growth
Increase in roughness

## Slide 12: BiFeO3: ad atom energy vs composition
Constant composition
Varied microstructure
Parameter Bi Fe O (At.  1.4%) (At.  1.4%) (At.  1.4%)
30W 25.5 10.6 63.8 40W 25.5 10.6 63.8 50W 24.4 10.8 64.8 75W 22.9 13.5 63.6

## Slide 13: BiFeO3: stress evolution
Substrate Bi Fe O Ar bias (At.  1.4%)
-25 24.4 14.3 61.2 0.1 -50 24.9 13.0 60.1 2.0 -75 26.5 12.4 57.3 3.8 -100 27.4 12.0 55.2 5.5
Coulombic effects on biasing, O2- reduction
Ar+ incorporation
RO2- < R Ar+ stress evolution

## Slide 14: Elastic constants: microstructure
ad atom energy variation at const. thickness phonon dispersion curves

## Slide 15: Elastic constants: stress evolution
Growth cond. | C11 (Gpa) | C12 (GPa) | C44(GPa
30 W | 188  22 | 108.0  2.0 | 39.0  4.0
50 W | 133  14 | 59.0  1.0 | 37.0  2.0
50 W & -50V | 171  25 | 79.0  10 | 63.0  5.0
75 W | 90  10 | 33.0  1.1 | 28.0  3.0

## Slide 16: Carbides: evolution of stress

## Slide 17: Carbides: evolution of stress
Elastic constants on iso- Hexagonal structure
c11 = 260.8  9.0 GPa
c33= 267.0  5.0 GPa
c13 = 83.5  4.0 GPa
c55 = 88.6  6.0 Gpa
c11/c33 < 1 : columnar growth
38% increase in stiffness normal to film

## Slide 18: Conclusions:
Growth of diverse thin films possible: Thornton model
X-ray reflectivity techniques spectroscopy in Å dimensions
density of single and multi-layers
Phase transition not shown here
Role of microstructure and composition on elastic constants to be decoupled
Stress evolution in thin films

## Slide 19: Acknowledgements

## Slide 20: Density, thickness, roughness
Density: X-ray Reflectometry
Snell‘s law: n1cos1 = n2cost
X-rays: nair = 1, t = 0°,
n= cosc, nmedia = 1-  - i,
Kiessig fringes:
2 - 2c= m2 (/2tf)2
Reflectivity (background)
R(Q)  q-4z

## Slide 21: Volume change

## Slide 22: T dependence:

## Slide 23: Volume change: X-ray reflectivity
Amorphous:
5.72 gcm-3
NaCl like:
6.23 gcm-3
Amorphous:
5.84 gcm-3
NaCl like:
6.48 gcm-3
NaCl like:
6.33 gcm-3
Amorphous:
5.92 gcm-3
Alloy | Volume change (/)
Ge2Sb1Te4 | 8.9%
Ge3Sb4Te8 | 7.1%
Ge2Sb2Te4 | 11%