## Slide 1: 16 T Dipole Design Options: Input Parameters and Evaluation Criteria
F. Toral - CIEMAT
CIEMAT-VC, Sept. 4th, 2015

## Slide 2
Input parameters
Evaluation criteria
Next steps
Summary

## Slide 3: Input parameters
3
The comparison will be performed for double aperture magnet models, which is the final aim of FCC study. However, the detailed analysis (tasks 5.4 and 5.7) will be done for a single aperture magnet, if cos-theta or block layouts are the preferred configuration, because in that case, the prototype will have a single aperture.

## Slide 4: General remarks (I)
4
Considering the given target cost of Nb3Sn for FCC program, in the exploration of the design options we will not consider grading with NbTi unless an evident advantage in terms of complexity can be justified for a specific design. However, grading may be done by changing the copper to superconductor ratio or using different cable sizes as proposed in next paragraph.
Aperture diameter provides the radial position of the insulated cables of the inner layer.
Reference radius is established using the classical criterion taking 2/3 of the aperture. This value is a bit high, since the physical aperture for the maximum particle excursion is 14 mm off-center.
Working temperature is 4.5 K, which is more advantageous from the cryogenics point of view, but implies some challenges for the beam pipe design. If final decision is 1.9 K, the impact on the magnet design will be moderate: operating margin will increase, but stability issues will be more significant.

## Slide 5: General remarks (II)
5
Only field multipoles created by the coil geometry and the iron saturation will be considered at this design stage. The allowable values with geometric origin are the following:
  b3geo < 3 units (means demonstrating that we can keep it under control and that we can very likely introduce, at the level of conceptual study, a possible compensation)
  b5geo < 5 units (it scales rapidly with the radius, and can be compensated with correctors)
  b7geo < 3 units (it scales even more rapidly, but we do not want b7 correctors)
Concerning saturation effects, set a “soft target” in the range of b3sat < 10 units.

## Slide 6: Cable properties
6
The maximum number of strands is kept as 40, according the existing cabling experience.
Critical surface is given by:
Where: with Bp as peak field on the conductor.
Tc0, Bc20, α, C0 are fitting parameters computed from the analysis of measurements on the conductor.
For a reasonable estimate of the critical current density of a round wire, magnet designers can assume the following parameters: Tc0 = 16 K, Bc20 = 28.8 T, α = 0.96, C0 = 255230 A/mm2 T.
For the cable degradation, we assume 5%.

## Slide 7: Reference conductor (I)
7
The magnet will be wound with two different types of Nb3Sn Rutherford cable: a “high-field” one and a “low field” one. Both types will be based on high Jc wires; the Cu-to-non-Cu ratio is expected to be around 1 for the “high field” cable and larger than 1.5 for the other one.
We consider here three baseline cables:
  1) a “high-field” cable constituted of 40 wires that have a relatively large diameter (1-1.1 mm); the precise dimensions of the wire and consequently of the cable are left as a free parameter for the magnet designers (in the case of a 1 mm wire the following reference cable dimensions can be taken: 1.82 mm for the mid-thickness; 21.0 mm for the width);
  2) a “low field” cable constituted of 20 wires that have the same diameter as the wire used for the “high-field” cable (this cable will have approximately the same thickness of the high-field cable and half of its width);
  3) a “low field” cable constituted of 40 wires that have relatively small diameter (0.7 mm); the following reference dimensions can be taken: 1.25 mm for the mid-thickness; 14.7 mm for the width.

## Slide 8: Reference conductor (II)
8
We assume that the cable can be produced either in rectangular shape or with a keystone angle. The keystone angle have to be sufficiently small to prevent a compaction c of the cable thin-edge larger than 0.14 (c =1-h/2d; where h is the cable thin edge thickness and d the wire diameter). As a reference, the keystone angle should not exceed 0.5°.
The specific characteristics of these cables and wires (in particular the Cu to non Cu ratio) can be later trimmed depending on the advancement and requirements of the study of the different design options.

## Slide 9: Structural analysis remarks
9
We assume that all materials are limited by the yield strength, or by the material degradation (coil).
Concerning the ferromagnetic material (low carbon steel), a limit of tensile stress of 200 MPa shall be considered at cold.
The stress on the coil can vary considerably depending on the coil spot, in particular the interface conditions between coil and surrounding structure. We assume that the “reference coil pre-stress” in the 2D section is the one at the middle of the cable. The coil is modelled as a sector, with smeared-out mechanical properties as shown in next slide.
Concerning this last point, we set a baseline design such that the coil is loaded until the nominal magnetic field in the aperture of 16T.
At the stage of exploring and comparing design options, we will consider that the pole tip is glued to the coil. If finite-element modelling is easier, pole and coil can be considered as independent parts, but not losing contact between them. At a later stage a decision about separate or glued coil will have to be taken: an independent coil can possibly allow the exploration of low pre-stress conditions.
The same criterion is followed for friction, which will be neglected at the level of the exploration of design options. At a later stage the use of a friction coefficient of 0.2 for most surfaces may be considered.

## Slide 10: Structural data
10
In accordance to the experience of the LARP program, we use the same coil elastic modulus at warm and at cold conditions.
This may evolve when performing the final design if new data will be available.
X cable side direction (radial in cos-theta), Y cable face direction (azimutal in cos-theta).

## Slide 11: Evaluation criteria
11

## Slide 12: Next steps
12
The analysis of the different magnet design options will be shared as agreed:
  CEA: block design
  CERN: review of the state of the art
  CIEMAT: common coil design
  INFN: cos-theta design
Mechanical issues must be kept in mind while performing the electromagnetic design: insulation thickness, support structure layout.
The electromagnetic design must be finished by the end of October. Next meeting is scheduled by Oct. 2nd , where the preliminary results will be presented.

## Slide 13: Timeline
13
End of August: design parameters, constraints and evaluation criteria.
End of October: first electromagnetic design.
End of December: first mechanical design. Identification of problems for further analysis.
End of March: Design report, including first considerations for coil-ends and fabrication feasibility.
Within end of April: internal review and choice.