## Slide 1
Numerical and Experimental Evaluation on
the Quench Detection Performance of NbTi/YBCO Hybrid Tape
S. Hasegawa*, S. Ito, H. Hashizume (Tohoku Univ.)
Thu-Af-Po4.09-15 [152]
Difficulty in Quench Detection for the RECBO tape
Quench detection by voltage measurement is difficult
1. Background
Proposal of LTS/REBCO Hybrid Tape
Low critical temperature
＋
Fig. Conceptual diagram of hybrid tape
REBCO
LTS
Quench detectable
LTS/REBCO hybrid tape
Slow quench propagation in a REBCO tape at very low temperature
Several methods have been proposed
(0.1 V < is needed while temperature of the YBCO tape is < 50 K)[1]
High Jc at very low temperature
(e.g. Magnetic coupling[2], using optical-fiber sensor[3])
2. Objective
Verification of the quench detection performance
of a LTS/REBCO hybrid tape used for 4.2 K
Research Issues
① Numerical simulation for the experiment
② Experiment with a prototype of the hybrid tape
To determine the suitable type of the NbTi wire
for the hybrid tape
To demonstrate the possibility of the hybrid tape
Especially for a NbTi/YBCO hybrid tape
To verify the result of the numerical simulation
5. Conclusion
・Quench in the YBCO tape can be detected using
the NbTi wire with high normal resistance was demonstrated
Future tasks
・Quench detection performance of the hybrid tape was sensitive to
the thermal resistance between the NbTi wire and the YBCO tape
Dependence of the external field
Dependence of the LTS materials
on the quench detectability of the hybrid tape will
be investigated
The suitable LTS materials for the hybrid tape
under high field will be determined
3. Numerical Simulation
Simulation Model
Fig. Three-dimensional model of the hybrid tape
Electrostatic Potential distribution
NbTi wire
YBCO tape
・Calculation of electrostatic potential
・Governing equation
・Current distribution in YBCO [4]
2-D Poisson equation on electrostatic field
1. ssc = ssc0 (ssc0 is sufficiently large)
2.
Iteration is continued until
ssc converges
Temperature Distribution
・Governing equation
3-D heat transfer equation
・Joule heat
Simulation Conditions
Results of the Simulation
・Electrical insulation over surfaces (x-y, y-z plane)
・Heat flux = h(T-To) over surfaces (x-y plane)
Fig. Simulation conditions
(f is assumed to be uniform in z-direction)
・0.1 V < can be detected
by the NbTi wire before
temperature of the YBCO
tape reaches 50 K
in Cases iii and iv
Case | Stabilizer | Cross sectional area
i | No NbTi wire | 
ii | Copper | 0.374 mm×0.374 mm
iii | Cupro Nickel | 0.374 mm×0.374 mm
iv | No stabilizer | 25×10-3 mm×1.35 mm
Table. Four cases for the numerical simulation
j is stabilizer
in Cases A and B
and NbTi in Case C
‘normal’ means
the normal conducting
state of NbTi
・Transition to normal conducting state in NbTi
・Detectable voltage in the
YBCO tape was < 0.1 V
Fig. Thermal resistance model
Fig. Dependence of thermal resistance
Thermal resistance
between the YBCO tape
and the NbTi wire is
important for the quench detection sensitivity
of the hybrid tape
Fig. Result of Case i
(no NbTi wire)
Fig. Result of Case ii
(with copper stabilizer)
Fig. Result of Case iii
(with CuNi stabilizer)
Fig. Result of Case iv
(pure NbTi wire)
・Detectable voltage in the NbTi wire was smaller
than that in the YBCO tape in Case ii (0.1 mV~)
・1 V scale voltage was measured in the NbTi wire
before the YBCO tape burned out in Case iv
・Quench in the YBCO tape can be detected
by using the pure NbTi wire
Fig. YBCO tape(Superpower® SC4050)
Fig. NbTi wire(Supercon® 54S43)
Overview of the Experiment
4. Experiment
Fig. Test section and the prototype hybrid tape
Experiment was conducted for two conditions of the NbTi wire
(Case ii: with copper stabilizer, Case iv: pure NbTi wire)
Fig. Experimental result of Case ii
(the NbTi wire was with copper stabilizer)[5]
Fig. Experimental result of Case iv
(the NbTi wire was pure NbTi wire)
・Quench detection sensitivity would be
influenced by 1.6 ~ 2.0 m2K/W
thermal resistance in Case iv
General threshold
for the quench detection
VYBCO: Voltage in the YBCO tape VNbTi: Voltage in the NbTi wire
[2] M. Mentink, et al., IEEE Trans. Appl. Supercond., 2015
[4] H. Hashizume, et al., Int. j. Appl. Electromag. Mater., 1992
Acknowledgements We would like to give gratitude to Axis Co. provided us NbTi wires.
[1] O. Tsukamoto, et al., Cryogenics, 2014
[3] F. Scurti, et al., Supercond. Sci. Technol., 2016
[5] S. Hasegawa, et al., Presented at 1st Asian ICMC-CSSJ 50th Anniv. Conf., Kanazawa, Japan, 2016
Corresponding author: shase@karma.qse.tohoku.ac.jp
Experimental results