## Slide 2: TE-VSC reporting to: Superconducting RF R&D coordination meeting 01 on Nb3Sn magnetron sputtering

## Slide 3: Current status
AS-DEPOSITED FILMS @ RT
As deposited films composition can be easily tuned by acting on coating pressure
Films are highly disordered with very small crystallites sizes (<10nm)
No superconductivity observed

## Slide 4: Current Status
ANNEALED FILMS
Annealing temperatures: 700 / 750 / 800 °C
Atmosphere: Vacuum (~1.10-6 mbar)
Duration: 24H
Goal: Obtain A15 superconducting cubic phase
Up to now: 1 film deposited at 1.10-3 mbar annealed.
A15 phase obtained (XRD)
Superconducting properties to be characterized
700°C
750°C
800°C

## Slide 5: Next steps: transition from EUCARD2 to FCC
Task | 2015 |  | 2016 |  |  | 
 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4
Nb3Sn – RT + annealing characterization |  |  |  |  |  | 
Nb3Sn high temperature coatings |  |  |  |  |  | 
V3Si coatings |  |  |  |  |  | 
Fellow contract |  |  |  |  |  | 
Scale-up cathode design |  |  |  |  |  | 
Eucard2 milestone
RF properties
EUCARD 2 milestone: March 2016 = RF characterization of Nb3Sn coating
Nov 2015 : High temperature coatings + V3Si ramp up