## Slide 1: Feedback from the SRF conference 2015
1st SRF R&D coordination meeting for FCC
14.10.2015
Sarah Aull

## Slide 2: SRF2015: 5 days, 332 participants, 385 contributions
Chart: 
| Fundamental SRF R&D - Bulk Nb | Fundamentals SRF R&D - Other Materials | New Proposals | Projects/Facilities - progress | SRF Technology - Ancillaries | SRF Technology - Cavity | SRF Technology - Cryomodule | SRF Technology - Processing
Fundamental SRF R&D - Bulk Nb Fundamentals SRF R&D - Other Materials New Proposals Projects/Facilities - progress SRF Technology - Ancillaries SRF Technology - Cavity SRF Technology - Cryomodule SRF Technology - Processing | 0.17662 | 0.12208 | 0.028571 | 0.090909 | 0.13766 | 0.26753 | 0.098701 | 0.077922
http://srf2015proc.triumf.ca/prepress/

## Slide 3: Key theoretical contributions
Non-equilibrium BCS theory describes anti-Q-slope in nitrogen and titanium doped cavities
Description on how an ambient magnetic field is trapped depending on a temperature gradient
T. Kubo, MOPB009
Description of the Q-slope in Nb/Cu cavities by thermal boundary resistance due to locally bad adhesion
A. Gurevich, WEA1A01
V. Palmieri, TUBA02

## Slide 4: Bulk Niobium: Losses due to trapped flux
Efficiency of trapping the ambient magnetic field depends on the cooling dynamics.
Temperature gradients along the cavity can induce thermo-electric currents which create additional magnetic fields that can be trapped. Stronger effect for dressed cavities and asymmetric cooling.
A. Romanenko, et al. J. App. Phys. 115, 184903 (2014)
Flux expulsion
Flux trapping
J.-M. Vogt, et al. Phys. Rev. ST-AB 18, 042001 (2015)
Thermally induced magnetic fields
Next generation of cryomodules must allow thermal cycling and defined cooling schemes.

## Slide 5: Progress on N doping
Suppression of nanohydrides was ruled out as origin of anti-Q-slope
High Q is explained by BCS optimum.
Doping recipe not 1:1 transferrable to lower frequencies
There seems to be a correlation between mean free path and quench field
650 MHz
A. Grasselino et al., MOBA06
A. Grasselino et al., MOBA06
If anti-Q-slope is a BCS effect, the same performance should be expected from a perfect Nb/Cu film

## Slide 6: Thin films: Nb/Cu
Energetic condensation gives first promising results on curing the Q-slope.
Thermo-electric seem to have strong effect on Nb films.
S. Aull, et al., TUBA03.
P. Zhang, et al., TUPB077.
Further development of high quality Nb/Cu coating is needed.
Dedicated studies on the cooling dynamics of Nb/Cu are needed

## Slide 7: Thin films: Nb3Sn based on diffusion recipe
D. Hall, et al., TUBA04.
Improved quench field on single cells
(Eacc = 13 MV/m in 2013)
Main issue: tin depleted areas
Coating 2-cell cavities started:
Limited to low gradients
G. Eremeev, et al., TUBA05.
Nb3Sn/Cu started at CERN

## Slide 8: Cavity fabrication
First 3.8 GHz single cell cavity from additive manufacturing (Arcam EBM)
First hydro-electro formed half cells show conservation of surface roughness and low wall thickness variation
Rres = 170 nΩ
Rres = 2.5 μΩ
P. Frigola, et al., THPB042.
Hydro-formed cavity reaches 36 MV/m (after CBP + 15 um EP)
M. Yamanaka, et al., THPB041.
S. Atieh, et al., THAA05.

## Slide 9: General take home messages for CERN
CERNs current SRF activities cover many different shapes and frequencies:
Continue development of geometry independent diagnostic tools
Benefit from synergies between different projects
Sample test cavities:
Quadrupole Resonator (QPR) is still the best setup on the market
Strong interest in QPR around the world: Upgrade of CERN’s QPR is essential