## Slide 1: Block design
CEA
C. Lorin & M. Durante
19 Nov. 2015
Acknowledgements:
To anybody who contributed via email interaction!

## Slide 2: Contents
Magnetic design
  3 old fit designs
    4 blocks + no-grading
    3 blocks + no-grading + low Cu/NonCu
    4 blocks + internal-grading
  1 new fit design
    3 blocks + no-grading
Margins discussion

## Slide 3: Part 1
Magnetic design

## Slide 4: Critical current density – v1
Top = 4.2 K
Bernardo Bordini CERN

## Slide 5: Design no-grading 4 blocks (v14)
Quantity | Unit | Value
W_bare | mm | 23.1
T_bare | mm | 2.0
Insul. | mm | 0.2
Cu/nonCu | . | 1.0
N strands | . | 40
Ф | mm | 1.1
Quantity | Unit | Value
Iop | kA | 12.0
N turns | . | 154
Bpeak | T | 16.33
Margin LL | % | 10.0
Cu/nonCu | . | 1.0
Outer dia | mm | 800
Fx per ½ coil | kN/m | 11,840
Ld 2 ap. | mH/m | 79
Energy 2 ap. | kJ/m | 5852
Strand area 2 ap. | m² | 0.0468

## Slide 6: Design no-grading 3 blocks (v17)
Quantity | Unit | Value
W_bare | mm | 23.1
T_bare | mm | 2.0
Insul. | mm | 0.2
Cu/nonCu | . | 0.8
N strands | . | 40
Ф | mm | 1.1
Quantity | Unit | Value
Iop | kA | 12.78
N turns | . | 122
Bpeak | T | 16.53
Margin LL | % | 9.7
Cu/nonCu | . | 0.8
Outer dia | mm | 800
Fx per ½ coil | kN/m | 9,660
Ld 2 ap. | mH/m | 56.4
Energy 2 ap. | kJ/m | 4862
Strand area 2 ap. | m² | 0.0371
can be protected

## Slide 7: No-grading protection (v17)
Quantity | Unit | Value
Iop | kA | 12.78
Cu/nonCu | . | 0.8
W_bare | mm | 23.1
T_bare | mm | 2.0
Insul. | mm | 0.2
Cu/nonCu | . | 0.8
N strands | . | 40
Ф | mm | 1.1
N turns |  | 122
Ld 2 ap. | mH/m | 56
Energy 2 ap. | kJ/m | 4764
Rdump | mΩ | 50
Validation time | ms | 10
Vthreshold | mV | 200
QH delay | ms | 100

## Slide 8: Design internal grading (v16)
Quantity | Unit | Value
W_bare | mm | 18.15
T_bare | mm | 2.0 / 1.525
Insul. | mm | 0.2
Cu/nonCu | . | 1.0 / 2.0
N strands | . | 31 / 40
Ф | mm | 1.1 / 0.85
Quantity | Unit | Value
Iop | kA | 9.2
N turns | . | 26 + 154
Bpeak | T | 16.39
Margin LL | % | 9.8
Cu/nonCu | . | 1.0 / 2.0
Outer dia | mm | 800
Fx per ½ coil | kN/m | 10,600
Ld 2 ap. | mH/m | 118
Energy 2 ap. | kJ/m | 5155
Strand area 2 ap. | m² | 0.0341

## Slide 9: Critical current density v2
Top = 4.2 K
Bernardo Bordini CERN
29.38
267845
0 %
1.9 K
4.2 K

## Slide 10: Design no-grading 3 blocks (v18)
Quantity | Unit | Value
W_bare | mm | 23.1
T_bare | mm | 2.0
Insul. | mm | 0.15
Cu/nonCu | . | 1.0
N strands | . | 40
Ф | mm | 1.1
Quantity | Unit | Value
Iop | kA | 13210
N turns | . | 119
Bpeak | T | 16.55
Margin LL | % | 10.25
Cu/nonCu | . | 1.0
Outer dia | mm | 800
Fx per ½ coil | kN/m | 9,520
Ld 2 ap. | mH/m | 52.3
Energy 2 ap. | kJ/m | 4,738
Strand area 2 ap. | m² | 0.0362
Quantity | Unit | Value
LL margin | % | 10.2
Iop/Ic@Top,Bpeak | . | 0.52
ΔT | K | 1.80
ΔH (adiabatic) | mJ/cm3 | 4.26

## Slide 11: Inner wall thickness
3 pancakes design:
Forces per ½ coil similar to Fresca2 @ 15 T
~10 MN/m (Fresca2 wall: 8 mm not optimized)
Inner wall thickness = 4.4 mm -> 5.4 mm
by margin reduction (10.25% -> 10 %)
Inner wall thickness 4.4 mm -> 7 mm
by increase of turns (119 – >127)
Mechanical analysis needed
(v18)
(v19 not shown)

## Slide 12: Conclusion
Possibility for a 3 pancakes design
Mechanical analysis to be done
b3 at low field 1 T (> 10 units)
Fringe field: r = 450 mm -> 375 mT
(1 m -> 28 mT)
ryoke = 400 mm
(v18)

## Slide 13: Part 2
Margins
discussions

## Slide 14: Margin 4.2 K vs 1.9 K (v1)
Basic relation
  Bpeak in conductor from 12 T to 18 T
  M4.2K from 5% to 15%
  To get 20% @ 1.9 K
  10% @ 4.2 K is optimistic

## Slide 15: Physical Margins
What can be used during magnet preliminary design phase? [suggestions from Luca Bottura]
  I/Ic [adim]: « how many strands can be broken » (current margin)
  ΔT [K] : bearable temperature excursion (temperature margin)
  ΔH [mJ cm-3]: required energy to increase by ΔT the cable temperature in adiabatic conditions (enthalpy margin)
  MQE (t,v) [mJ cm-3], same as before but taking into account temporal and spatial distribution of the energy deposition.
  (MQE requires time to be properly analyzed, see: Enrico Felcini, Analysis of the stability margin of the High Luminosity LHC superconducting cables with multi-strand model, Cern report in progress 18 nov 2015)

## Slide 16: Enthalpy margin
Relevance of ΔH compared to MQE
To fairly compare magnet based on ΔH we need the same:
1) specific heat capacity Cp for cable materials [J kg-1 K-1]
2) ‘density’ d for cable material [kg m-3]
3) definition of the Nb3Sn fraction
[courtesy of Enrico Felcini]
ΔH is obviously conservative
(adiabatic conditions)
but not too conservative.
-> Interesting
Mid-plane cable of QXF

## Slide 17: Proposition of Cp fit (Cu&G10)
Cable made of Cu, Nb3Sn and epoxy (G10)
  G10 [1.9 K to 300 K]:
  Copper [1.9 K to 10 K]:
to get the proper reference for both fits go to:
Giulio Manfreda, Review of Roxie’s material properties database for quench simulation,
cern internal note: 2011-24 (2011)

## Slide 18: Propositions of Cp fit (Nb3Sn)
  Option 1 [T < Tcs]:
  Option 2 [T < Tcs, Bpeak2 > 10 T]
to get the proper reference go to:
Giulio Manfreda, Review of Roxie’s material properties database for quench simulation, cern internal note: 2011-24 (2011)
Bernardo Bordini, Thermo-magnetic instabilities in Nb3Sn superconductin accelerator magnets, PhD Thesis, p156-159, (2006)
Bpeak2 = 16.55 T

## Slide 19
Fraction of Nb3Sn in the non-Cu
C. Tarantini et al., Composition and connectivity variability of the A15 phase in PIT Nb3Sn wires, SuST, (2015)
C. Tarantani et al., Corrigendum: Examination of the trade-off intrinsic properties in the optimization of a modern internal tin Nb3Sn conductor, SuST, (2105)
PIT:
~45% Nb3Sn within
the non-Cu fraction
RRP:
~ 60% Nb3Sn within
the non-Cu fraction
Arbitrary proposal: 50 %

## Slide 20: Enthalpy margin conclusion
Calculation proposal (open to discussion!)
with
with
with option 2 for CpNb3SN (BB fit)
Keep in mind that we just need to be consistent in the way we do the calculation for fair comparison and that MQE analysis will certainly be performed in the future.

## Slide 21: Thank you

## Slide 22
L. Bottura, « Cable stability », arxiv.org/pdf/1412.5373
Bonus