## Slide 1
Wound Conductor Test Facilities (TASK 2)
Status of visits performed at labs
Friedrich Lackner, November 18th, 2015
FuturE circular collider MAGNETS TECHNOLOGIES
Bernhard Auchmann, Amalia Ballarino, Emanuala Barzi, Johannes Bernardi, Thomas Baumgartner, Luca Bottura, Bernardo Bordini, Pierluigi Bruzzone, Shlomo Caspi, Michael Eisterer, Jerome Fleiter, Carmine Senatore, Christian Scheuerlein, Davide Tomassini, Davide Uglietti, Arjan Verweij, Gerard Willering,
Acknowledgements:

## Slide 2
Task 2.1
Description
Review of existing instrumentation and tools presently in use at CERN and at partner institutes to characterize the electromechanical performance of Nb3Sn cables
September 2015: FNAL, UNIGE, TU-Wien – Atominstitut;
2015 - 2016: TWENTE, PSI, NHMFL;
Design and set-up of a tool to characterize the cable wind-ability;
Design and set-up a tool to test splices under different mechanical constraints.
Deliverables
D1: Critical review of existing tools including internal review, 6 months;
D3: Procurement/fabrication, instrumentation and splicing methods, 3 months;
D2: Proposal tools and test program n, commissioning, 6 months;
D4: Test campaigns, 36 months.
Characterization of Cable Processing and Splicing

## Slide 3
Task 2.2
Description
Review of existing instrumentation and tools presently in use at CERN and at partner institutes to characterize the electromechanical performance of Nb3Sn superconductors;
Enhancement of an existing tool or design and manufacture of a new tool capable of exploring the electromechanical behavior of impregnated wound conductors as a function of different parameters, in particular the superconductor itself, the insulation schemes, the heat treatment, the impregnation, the role and possible transformation of the binder. It is important that the tool allows to explore different configurations (different samples and different testing conditions, load, magnetic field, current) with a short lead time;
Organize an internal review of the selected proposal as well as of the relevant test program;
The work also includes, where needed, the setting up of tailored instrumentation tools in particular to provide an accurate characterization of the structural conditions of the sample;
Perform the tests and analyze the relevant results.
Deliverables
D1: Critical review of existing tools, 6 months;
D2: Proposal of tools and test program, including internal review, 6 months;
D3: Procurement/fabrication, commissioning, 18 months;
D4: Test campaigns, 24 months;
Impregnated wound conductor insert

## Slide 4
CERN contributors to task 2
Person/Section | Task
TE-MSC-LMF | 
F. Lackner | Coordination
S. Triquet | Tooling
E. Grospelier | Tooling & design (will leave LMF in 2016)
N. Dalexandro | Splicing
D. Pulikowski | PhD student, windability + instrumentation aspects
P. Ebermann | PhD student (November 1st), complementary test setup
Fellow 1 + 2 | To be hired, testing + instrumentation + splicing
TE-MSC-SCD | 
EN-MME | Contributions to test campaigns

## Slide 5
Visits | Date | Persons
163 | Aug. 2015 | J. Fleiter
UNIGE | Sept.2015 | C. Senatore
FNAL | Sept.2015 | 11T collaboration
MT24 | Oct.2015 | 
PSI | Oct.2015 | P. Bruzzone
AIT | Oct.2015 | M. Eisterer
USTEM | Oct.2015 | J. Bernardi
AuM | Oct.2015 | N. Durakbasa
TWENTE | Contacted | M. Dhalle
NHMFL | ? | 
Overview on visits:

## Slide 6
Wire tests and facilities

## Slide 7
Uniaxial tensile and compression
1) Samples are soldered onto a sample holder:
So-called Walters spring, e.g. used at
NIST, University of Geneva.
Bending spring (so-called Pacman), e.g. used at University of Twente.
A device to investigate the axial strain dependence of the critical current density in superconductors
A. Godeke,a) M. Dhalle, A. Morelli, L. Stobbelaar, H. van Weeren, H. J. N. van Eck,
W. Abbas, A. Nijhuis, A. den Ouden, and B. ten Haken
Low Temperature Division, Faculty of Science and Technology, University of Twente, P.O. Box 217,
7500 AE, Enschede, The Netherlands
Finite element simulations on the practical planar shape of the Pacman (a) and on a U spring (b)

## Slide 8
Uniaxial tensile and compression
Walters Spring Probe. Courtesy of the Applied Superconductivity Group of the University of Geneva.
Long sample high sensitivity critical current measurements under strain,
C. R. Walters, I. M. Davidson, and G. E. Tuck
Cryogenics, vol. 26, pp. 406–412, Jul. 1986.
Spring materials:
Ti–6Al–4V with an upper elastic strain limit at 4.2 K of 1.3%.
Cu–2Be (UNS C17200) with 1.0% upper elastic strain limit at 4.2 K.
The magnetic field is applied in parallel to the spring axis.
Rotation angle and elastic strain is computed by FEA and compared with the
readings of the strain measurement.
Toward a standard for critical current
versus axial strain measurements of
Nb3Sn
B. Seeber, G. Mondonico and C. Senatore
Supercond. Sci. Technol. 25 (2012)

## Slide 9
Strain and Magnetic-Field Characterization of a Bronze-Route ITER Wire: Benchmarking of Strain Measurement Facilities at NIST and University of Twente”, IEEE Trans. Appl. Supercond. 22(3), (2012)
N. Cheggour, A. Nijhuis, H. J. G. Krooshoop, X. F. Lu, J. Splett, T. C. Stauffer, L. F. Goodrich, M. C. Jewell, A. Devred, Y. Nabara,
Strain Dependence of Critical Current in Bi2212
W & R Wires Under Magnetic Field Up to 30 T
M. Sugano, K. Itoh, and T. Kiyoshi, IEEE Trans. Appl. Supercond. 16(2), (2006)
Uniaxial tensile and compression
Comparison of the εmax values measured with Walters spring and Pacman:
Thermal contraction from 456 to 4.2 K is ΔL/L=-0.30 and
ΔL/L=-0.61 for Ti-6Al-4V and Cu-2wt.%Be, respectively.

## Slide 10
2) Samples can freely contract during cool down for irreversible damage characterisation. Developed for strand measurements but potential to be used for cables.
Measurement in self field at 77 K. Adding cryocooler would allow to measure below Tcrit of Nb3Sn.
Irreversible damage characterization
Simultaneous measurement of critical current, stress, strain and lattice distortions in high temperature superconductors
C. Scheuerlein et al. EUCAS 2015, invited talk
Reversible degradation of Nb3Sn must be studied under operating temperature and field;
Irreversible degradation of conductor could be performed without applied field and below Tcrit (but above 4.2 K).
Potential for measurments under transversal pressure would need development.

## Slide 11
Load case in accelerator magnet coils
Dominant load case: transversal stress
Typical stresses up to 200 MPa
2-in-1 structure, 11T dipole

## Slide 12
Transversal compression wire
Developed by University Geneva with the aim to o compare wire degradation under transversal compressive stress.
Electro-mechanical properties of PIT Nb3Sn
wires under transverse stress: experimental
results and FEM analysis
C. Calzolaio, G. Mondonico, A. Ballarino, B. Bordini, L. Bottura,
L. Oberli and C. Senatore.
Constrained in a U-shaped groove and is pressed by an upper anvil that fits the groove. Confinement within four walls, measuring effects of compressive stress on impregnated wires.

## Slide 13
Cable tests and facilities

## Slide 14
 |  | CERN FRESCA | EPFL-CRPP SULTAN | EPFL-CRPP EDIPO | TWENTE
Current supply |  | RT-PS or cold transformer | SC transformer | SC transformer | SC transformer
Max. field | (T) | 10 (dipole) | 11 (solenoid) | 12.35 (dipole) | 15 (solenoid)
Max. DC current (kA) | kA | ~40, being upgraded | 100 | 100 | 45
Operating Temperature (K) | K | 1.8 or 4.3 | 4.5 – 10 | 4.5 - 50 | 4.3
Insert | mm | Ø 70 | 94 x 142 | 89 x 138 | U & helical
Max. field region length | mm | 800 (600 – 1% homogeneity, 10T) |  | 900 (680 - 0.5% homogeneity, 12.3T) | 
Mechanical constraints (MPa) | MPa | YES at RT | YES at RT | YES at RT | 
Current distr. measurement |  | YES | YES | YES | NO
Specific functions |  |  | AC field 0.43T ≤10 Hz, 80 channels DAQ | AC field 0.312 T f ≤ 0.8 Hz, | 
Sample mounting |  | Vertical insert | Vertical insert | Vertical insert | 
Preparation |  | Careful preparation, demanding |  |  | 
Preliminary status, to be updated…

## Slide 15
Critical Current Measurements of High-Jc Nb3Sn
Rutherford Cables under Transverse Compression
B. Bordini, P. Alknes, A. Ballarino, L. Bottura, L. Oberli, MT23, 2013.
Transversal force: 2 MN/m
Cable length: 1.8 m
Transversal load εth: 90 MPa to 155 MPa
10 mm wide Rutherford cable
Fits into the Ø70 mm bore of FRESCA
CERN - FRESCA

## Slide 16
EPFL - PSI
Electromagnetic cycling
Thermal cycling of large CICC conductors
100% in use for testing of ITER CICC foreseen reduction in 2016 to 70%
Up to 10000 cycles to investigate cable degradation at the nominal operating conditions
Demanding sample preparation
ITER Conductors from Design, through Specification, Qualification, Production and Test
Pierluigi Bruzzone EPFL-CRPP, Villigen, Switzerland

## Slide 17
FBI (F force, B magnetic field, I current)
Measurement Facility for High Temperature
Superconducting Cable Designs
Imax =10 kA
Bmax =12 T
Fmax =100 kN.
FBI Measurement Facility for High Temperature
Superconducting Cable Designs
C. Bayer, C. Barth, P. V. Gade, K.-P. Weiss, and R. Heller
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 24, NO. 3, JUNE 2014
KIT - FBI
Critical current of a cable up to 10 kA
With an LTS split coil magnet of 12 T and a sample gap of 80 × 40 mm2
Different HTS cable types can be measured
Mechanical forces can be applied up to 100 kN in axial direction of a cable based on a electromechanical tensile machine

## Slide 18
FNAL
Sensitivity of Nb3Sn Rutherford-type cables to transverse pressure
E. Barzi , T. Wokas, and A. V. Zlobin
Fermi National Accelerator Laboratory
Batavia, Illinois 60510, USA
Transverse pressure: Hydraulic cylinder 20 t
Current up to 2000 A
Operating temperature 4.2 K
Transverse magnetic field up to 12 T
Tests were carried out at pressures up to 200 MPa
14 mm wide Rutherford-type cables, 28 Nb3Sn strands 1 mm in diameter
The cable sample (1)
Inconel plates (2)
Inconel rod assembly (3)
Top plate welded to Inconel tube (4)
Inconel tube (5) welded to the top flange
Copper leads (6) including a pair of Nb3Sn strand splices.
Sample after impregnation
Test setup

## Slide 19
TWENTE
Master Thesis A. Verweij
Alternative concept for electromechanical cable characterization:
Magnetic press for cable testing, still operational…

## Slide 20
Cable windability

## Slide 21
Task 2.1
Mechanical characterization for winding process “wind-ability”:
Tensile test conducted with EN-MME
New clamping tool, specific for 11T cable geometry
Preparation of test samples
Chart: Time [s]
-X Applied Force | 0 | -76.5367 | -141.4214 | -184.7759 | -200 | -184.7759 | -141.4214 | -76.5367 | -2.4503e-14
-Y Applied Force | -200 | -184.7759 | -141.4214 | -76.5367 | -1.2251e-14 | 76.5367 | 141.4214 | 184.7759 | 200
X-axis
Y-axis
Z-axis
Work ongoing by Dariusz Pulikowski (PhD student Poland - CERN)
Presentation on status on Friday, Nov. 20th, meeting room bldg. 180.