## Slide 1: UFSD update
Test beam results
Sensor design
Board design
Timeline
INFN and Università di Torino, Università Piemonte Orientale

## Slide 2: Testbeam Set-up
pions
Testbeam part of the July CMS HGC
UFSD

## Slide 3: Testbeam: signal and noise
pions
- Testbeam, very clean shape:
- 120 GeV muons
- Two UFSD, gain 10 and gain 20.
- Read-out with a CSA amplifier with a 4 ns integration time.
Noise ~ 1 mV,
Signal ~ 150-200 mV
Rise time 20-80% ~ 5 ns
online
offline
500 MHz FFT
cleaning

## Slide 4: Testbeam Results
300 micron thick, ~ 4 pF sensor
Gain 10  resolution ~ 145 ps
Gain 20  resolution ~ 85 ps
Previous testbeam
New testbeam

## Slide 5: New productions: winter 2015
FBK: 300 micron, UFSD new production.
Gain foreseen ~ 10-20
CNM: 50 and 100 micron thick silicon,
with final PPS geometry  next pages

## Slide 6: Possible Coverage
Use as reference the Quartic coverage
Beam
Detector occupancy per mm2 at pile-up = 50
How large each pad can be?
1 mm2 = 2 pF for 50 micron thick sensors
1 mm2 = 1 pF for 100 micron thick sensors
Need to evaluate
dV/dt vs area.
How long each bond wire can be
Electronic noise
Set as goal 1 mV noise  dV/dt ~ 50 mV/ns to obtain 20 ps resolution

## Slide 7
dV/dt vs Signal fraction for C = 4, 6 pF and gain = 8, 10, 12, 14, 16
dV/dt = 50 mV/ns
BB amplifier, 40 db,
R input = 50 Ohm,
Gain = 8 - 16
4 pF, G = 8
4 pF, G = 10
4 pF, G = 10
4 pF, G = 12
4 pF, G = 14
4 pF, G = 16
6 pF, G = 8
4 pF, G = 10
6 pF, G = 10
6 pF, G = 12
6 pF, G = 14
6 pF, G = 16
Fraction of the rising edge
dV/dt> 50 mV/ns
Gain = 14-16
C = 4-6 pF
60
50
40
30
20
10
0.2 0.4 0.6 0.8 1

## Slide 8: Bond wire
The geometry of the sensor has to take into account the bond-wire length
A bond wire act as an inductor of 0.8 nH/mm placed in between the detector capacitance C and the amplifier input resistance R
Simulation by
Marco Ferrero
Good

## Slide 9
CT-PPS proposed sensor geometry
16 Pixel ~ 3 mm2
Cap. Pixel ~ 6 pF
Asymmetric designed
Area = 12mmX6mm;
Thickness = 50 um;
# of pixels = 32
16 Pixel ~ 2 mm2
Cap. Pixel ~ 4 pF
6 mm
Beam
spot
4 mm
8 mm
3.1 mm
2.9 mm
Beam
180o turn
No cracks aligned: 2 (3) planes facing the beam, and 2 (3) turned by 180o
0.45 mm
0.5 mm
1.0 mm
0.95 mm
50 micron inactive gap

## Slide 10
CT-PPS proposed sensor geometry
16 Pixel ~ 3 mm2
Cap. Pixel ~ 6 pF
Asymmetric designed
Area = 12mmX6mm;
Thickness = 50 um;
# of pixels = 32
16 Pixel ~ 2 mm2
Cap. Pixel ~ 4 pF
6 mm
Beam
spot
4 mm
8 mm
3.1 mm
2.9 mm
Beam
180o turn
No cracks aligned: 2 (3) planes facing the beam, and 2 (3) turned by 180o
0.45 mm
0.5 mm
1.0 mm
0.95 mm
50 micron inactive gap

## Slide 11: UFSD expected time resolution
What resolution per plane can we expect?
There are 2 known main contributions:
Noise  jitter (from current electronics and testbeam)
Landau fluctuations  additional time spread (from simulation)
For gain >~15  s < 40 ps
Note we remain below 40 ps even assuming an un-accounted for additional time spread of 20 ps.

## Slide 12: Comparison with Quartic
Beam
Detector occupancy per mm2 at pile-up = 50
6 x 12 mm coverage,
to have 32 ch per plane

## Slide 13
Lateral collector ring and sensor fill factor
Very important: need n-deep well at the end of each pad to prevent particles hitting in between pads from reaching the gain region.
Dead region: ~ 50 micron along each internal pad border = 5 mm2
Active area: 67/72 = 93% per sensor.
No multiplication for particles hitting in between pads
Gain region
n-deep
Gain region
current
TCAD simulation
F. Cenna
p-stop
~ 50 micron

## Slide 14: Sensor thickness and slim edge
Rule: when the depletion volume reaches the edge, you have electrical breakdown.
It’s customary to assume that the field extends on the side by ~ 1/3 of the thickness.
edge = k* thickness
k = 1 very safe
k = 0.5 quite safe
K = 0.3 limit
depleted
~ 0.3 d
non depleted
By construction, thin detectors (~ 50 micron) have therefore slim edge

## Slide 15
Extra
PPS proposed read-out card
NINO 32
16 channels
16 channels
Bond wire: 0.8 nH/mm.
Rule: <~ 2 nH
Max. length: 2-3 mm
Low noise BB amplifier to match NINO inputs
Signal from
50 um thick UFSD,
Q = 5fC
Differential NINO
Input, ~ 100 fC
~ 1.5 ns
High Voltage
Low Voltage
Extra sensor for alignment

## Slide 16
Next steps
Done:
Testbeam in July with 300 micron thick UFSD sensors. Preliminary analysis indicates a time resolution of ~85 ps for a gain~20, and ~145 ps for a gain~10.
We finalized the 50 and 100 micron thick sensor design, and submit the production at CNM. Turn around time ~ 3-4 months.
 Foreseen time resolution ~ 40 ps
To be done:
Develop the pre-amplifier chain, to be compatible with the NINO inputs. Need to be rad-hard. Torino, Pilsen, Santa Cruz…?? ~ 6 month
Evaluate the heating requirements
Study the NINO behavior for very short pulses (Jose might help in this topic). Hopefully it works….
Define the services needed in the tunnel: Low voltage, High voltage, cooling

## Slide 17
Conclusions
Simulation shows a time resolution of ~ 40 ps for 4-6 pF sensors with gain ~ 15.
We have developed a sensor design with minima dead area, short bond-wires and the possibility of 100% coverage. Ready by ~ winter 2015.
We are working towards a pre-amplifier design compatible with the NINO+HPTDC read-out chain.
 Need to evaluate the NINO chip with UFSD sensors. Does it work?