## Slide 2: Superconducting Radio Frequency (SRF) Thin Film & Surface Treatment 2015 status
Leonel Ferreira, Guillaume Rosaz, Alban Sublet
VSC Seminar - 27.11.2015

## Slide 3: Outline
Introduction and HIE-ISOLDE production results
  A. Sublet
Surface treatment activities
  L. Ferreira
LHC cavities and alternative materials/coating
  G. Rosaz
Nb film R&D, simulations and collaborations
  A. Sublet

## Slide 4: Outline
Introduction and HIE-ISOLDE production results
Surface treatment activities
LHC cavities and alternative materials/coating
Nb film R&D, simulations and collaborations

## Slide 5: Technology Department objectives (from SRF mini workshop, 14.11.2014, CERN)
Fulfill LHC and HIE-ISOLDE cavities production specification
Increase Thin Film & Surface Treatment R&D activities
Be at the forefront of Thin Film SRF technology
Short term goal  4 cavities/month:
  1 LHC  2 cavities prototypes under production, moke-up tube coated
  1 HIE-ISOLDE  1 coating/month
  1 SPL/Crab  2 SPL + 1 Crab in 2015, 2 SPL + 1 Crab + 1.3 GHz for 2016
  1 R&D (1.3GHz/QPR…)  completely refurbished HiPIMS setup
   THIN FILM technology must be mature for 2018 (ESU)

## Slide 6: TE - Thin Film & Surface Treatment SRF plan 2015

## Slide 7: HIE-ISOLDE production 2015 (I)
First cryomodule installed and commissioned, physics started
…but coupler issue  switch with second cryomodule by spring 2016

## Slide 8: HIE-ISOLDE production 2015 (II)
courtesy of A. Miyazaki
5 cavities + 1 spare ready for second cryomodule
15 cavities to be coated till mid 2017: 2x 5 cavities for Phase 2 + 5 spares
…but issue with substrates (cracks), 4 rejected, 2 used for investigation (QS6 at RI + QS9 at CERN)
Production stopped at RI, lack of substrates, “recycling” of rejected substrate (ex. QS10)
Large troubleshooting campaign (MME/RF/VSC) on going
However difficult to correlate with cavities low performances
QS10
Before subu
QS9
QS11

## Slide 9: Outline
Introduction and HIE-ISOLDE production results
Surface treatment activities
LHC cavities and alternative materials/coating
Nb film R&D, simulations and collaborations

## Slide 10
OUTLINE
Present installations
Latest developments
Foreseen activities and developments

## Slide 11
Present installations in b.118
Copper chemical polishing (SUBU)
LHC
HIE-ISOLDE
1.3 GHz

## Slide 12
Copper electrochemical polishing
LHC
1.3 GHz
Present installations in b.118

## Slide 13
Niobium chemical polishing
BCP
CRAB
SCRF subcomponents
Present installations in b.118

## Slide 14
Niobium electrochemical polishing
Present installations in b.118

## Slide 15
HPWR
Present installations in b.118

## Slide 16
Niobium stripping
Niobium stripping
Present installations in b.118

## Slide 17
Latest developments
SPL >>> High gradient
HIE-ISOLDE
CRAB - DQW
1.3 GHz

## Slide 18
Foreseen activities and developments
LHC spare cavities (Nb/Cu):
- Define and build tool to improve bath agitation (SUBU):
- Homogeneous etching;
- Avoid pinholes.
- Evaluate electropolishing feasibility:
        Simulation work;
        Define facilities needs.
CRAB cavities (Nb):
- define and build setup for heavy BCP (200 microns);
- evaluate bath speed impact on polishing rate:
        Experimental + simulation work;
1x Eng + 2xTech
Possible impact on available space and services

## Slide 19
Foreseen activities and developments
FCC 800 MHz cavities (Nb/Cu):
- define and build tools for improved bath agitation SUBU;
- define v+h setup for electropolishing;
High gradient (5 cell and 1.3 GHz monocell: Nb/Nb):
- define v+h setup for electropolishing
Possible impact on available space and services
Possible impact on available space and services
1x Eng + 2xTech

## Slide 20
Foreseen activities and developments
Thin film CRAB (Nb/Cu):
- define and produce tools for improved bath agitation SUBU;
- define tools for electropolishing;
HIE-ISOLDE (Nb/Cu):
- define and produce tools for improved bath agitation (SUBU);
Possible impact on available space and services
1x Eng + 2xTech

## Slide 21
General R&D
New chemistries for niobium and copper:
- Different formulations;
- Ionic liquids (plating/polishing);
- pulse polishing;
Alternative cavity assembly process:
- Inverse Nb / electroforming
1x Eng + 1x Fellx + 1x PhD
External collaboration
New power supply

## Slide 22
Possible bottlenecks
HPWR availability for large (LHC) and small cavities (1.3 GHz)
Manpower & coactivity in B118
Space and/or services

## Slide 23: Outline
Introduction and HIE-ISOLDE production results
Surface treatment activities
LHC cavities and alternative materials/coating
Nb film R&D, simulations and collaborations

## Slide 24: Outline
LHC spares program
New materials for SRF cavities
New coating techniques for SRF cavities

## Slide 25: LHC SPARES PROGRAM

## Slide 26: Production
Short term : 2 prototypes to be built by end 2015
  Half cells to be welded in the next two weeks
  Dedicated to coatings/RF tests only
Long Term
  4 + 1 cavities for spare cryomodule
  Tuning bench to be manufactured/refurbished

## Slide 27: Coating of LHC spares
Setup installation @ 252
Electrical installation
Water supply
New BO system
Similar pumping group as HIE-ISOLDE benches

## Slide 28: Pre-coating rinsing /Cathode assembly
MOCK-UP
Rinsing
OK TO GO
Vertical assembly vs horizontal OK to GO
Safety
Efficiency
Cleanliness

## Slide 29: Vacuum / Bake out test
Cathode assembly (no clean room, no Nb sleeves)
Good behaviour of the tent
200C easily reached
OK TO GO

## Slide 30: 1st coating tests
Process point perfectly matches previous coatings i.e. I(V)
Infrared imaging showing the plasma discharge location through cavity temperature raise.
coil

## Slide 31: Next steps
High pressure water rinsing validation b118.
  Post coating step
  In case of Field Emission in the cavity
  All parts available
  Mock-up on its way to b118 for test.
  Mock-up modifications
      Plasma diagnostics
      Sample holders

## Slide 32: New Materials for SRF cavities

## Slide 33: SRF cavities
Accelerating component for particle accelerators
Use high power RF waves to provide accelerating gradient
S = superconducting
  Lower power losses through surface resistance reduction
  Increase quality factor
Quality Factor
Needs:
  High Tc
    High Q0
    Less cryo power required
  Low RS
  Low resistivity in NC state
Nb3Sn and V3Si are very promising candidates

## Slide 34: Current status
AS-DEPOSITED FILMS @ RT
As deposited films composition can be easily tuned by acting on coating pressure
Films are highly disordered with very small crystallites sizes (<10nm)
No superconductivity observed

## Slide 35: Current Status
ANNEALED FILMS
Annealing temperatures: 700 / 750 / 800 °C
Atmosphere: Vacuum (~1.10-6 mbar)
Duration: 24H
Goal: Obtain A15 superconducting cubic phase
Up to now: 1 film elaborated at 1.10-3 mbar annealed.
A15 phase obtained (XRD)
Superconducting properties to be characterized
700°C
750°C
800°C

## Slide 36: Current status
Effect of surface preparation for Cu
Degreasing only
Chemical polishing (SUBU)
PAr = 1.10-3 mbar
PAr = 5.10-2 mbar
Chemical Polishing:
Bigger crystallites ONLY at low pressure

## Slide 37: Next steps
Task | 2015 |  | 2016 |  |  | 
 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4
Nb3Sn – RT + annealing characterization |  |  |  |  |  | 
Nb3Sn high temperature coatings |  |  |  |  |  | 
V3Si coatings |  |  |  |  |  | 
Fellow contract |  |  |  |  |  | 
Scale-up cathode design |  |  |  |  |  | 
Eucard2 milestone
RF properties
EUCARD 2 milestone: March 2016 = RF characterization of Nb3Sn coating
Nov 2015 : V3Si ramp up
New fellow: K. Ilyina

## Slide 38: New Coating techniques for SRF cavities

## Slide 39: How to improve current Nb films?
Improve
  Density
  Grain size
  Roughness
  Conformity
Control of ion production in the plasma
Energetic condensation (HiPIMS)
Control ion flux at the substrate
Ionize species to be deposited – sensitive to bias

## Slide 40: Setup
Fully refurbished
  New holding frame
  Data acquisition
  Remotely controlled BO
  New Nb cathodes
  New ceramic spacers

## Slide 41: Unbalanced magnetron
Use magnetic field to bring electrons close to the substrate to create ions in its vincinity
P.J.Kelly et al, Magnetron sputtering: a review of recent developments and applications, Vacuum 56 (2000), 159-172
Cathode Power supply
Cavity Bias (grounded)
Cavity
Pumping
SmCo magnet
Ceramic insulator
Ceramic insulator
Magnet holder
Nb cathode
Cylindrical cathode makes things a bit more complicated
S
N
N
S
N
N

## Slide 42: magnetic configuration
Standard
Strongly unbalanced
e-
e-
e-
RFEA
RFEA

## Slide 43: Preliminary study
Ion flux vs magnetic configuration
350W
5.10-3 mbar
RFEA
MAGNET

## Slide 44: Next steps
Extend ion flux analysis to bias and HiPIMS cases.
Investigate film morphology depending on magnetic configuration and bias
Identify a potential working point for 1.3 GHz cavity test  few RF characterization slots
Plasma simulation
A standard DCMS 1.3 GHz in characterization as baseline (WW48)

## Slide 45: Outline
Introduction and HIE-ISOLDE production results
Surface treatment activities
LHC cavities and alternative materials/coating
Nb film R&D, simulations and collaborations

## Slide 46: Nb film: if cavity is not the vacuum chamber
Crab Nb/Cu
Substrate biasing and process pressure investigation (2 tests done in 2015)
HIE-ISOLDE double cathode to decouple inner/outer conductor coating
and allow magnetron sputtering larger process window (ready Jan. 2016)
High temperature coating study and comparison on 1.3 GHz cavity (spring 2016)
Crab Nb/Cu Wide Open Waveguide WOW cavity preliminary study (started mid-2015), Cu brazing study, as an alternative to weld, started (evaluate compatibility with chemistry)
1.3 GHz high temperature
0.4 m
Double cathode
0.9 m

## Slide 47: Plasma simulations
Benchmarking
anode
cathode
3D drawing
geometry mesh
Ar+ flux on the cathode
sputtered Nb distribution
Experimental reality
Numerical simulation
Ar plasma
courtesy of A. Sapountzis T. Richard and A. Pflug
Case study finished summer 2015
Fraunhofer simulation code installed since fall 2015
Experiment/simulation benchmarking on going
Simulations of 1.3 GHz/HIE-ISOLDE/WOW/hollow cathode started, but need much more server stability
Plasma diagnostics: OES, Langmuir probe and RFEA

## Slide 48: HIE-ISOLDE 2D, very preliminary plasma and Nb transport simulation © Thibaut Richard
2D slice of HIE-ISOLDE cavity with periodic boundary conditions
Encouraging start, but… we are still in the learning phase
Limitation with server access stability (crashes), 3D model not yet realizable
Need better understanding/optimization of code and parameters

## Slide 49: Collaborations
FCC (on going)
EPFL (Jan. 2015)  plasma simulations and diagnostics
LNL/STFC/CERN (Jun. 2015)  FCC 5 cells cavity, thin film R&D and characterization
Eucard3 (start 2017)  Thin film R&D (multilayers, Nb3Sn) and RF characterization
Fraunhofer (2016?):  simulation code

## Slide 50: Summary
2014 objectives partially fulfilled
2015 production activities limited by the availability of the substrates
2016 multi-activities in parallel (LHC/HIE-ISOLDE/SPL/Crab…)
Surface treatment of SPL and Crab cavities on going
b.118 infrastructure/manpower limitations with growing activities
Launch of alternative treatments studies
LHC coating system ready and process requalified
HiPIMS/DCMS refurbished, plasma diagnostic study
Nb3Sn/V3Si activity launched, fellow started in Nov. 2015
Plasma simulations launched and PhD started in Jan. 2015
Double cathode for HIE-ISOLDE and high temperature coating R&D
New collaborations on the way

## Slide 51
Thank you for your attention!
Acknowledgement to:
chemistry team, TTEs, HIE-ISOLDE coating team
RF and MME groups

## Slide 53: TE - Thin Film & Surface Treatment SRF plan 2014

## Slide 54: Materials
Nb3Sn
  A15 type
  Tc ~ 18K
V3Si
  A15 type
  Tc ~ 16K
Both materials exhibit very low surface resistance combined to high Tc

## Slide 55
Cathode Power supply
Cavity Bias (grounded)
Cavity)
Pumping
SmCo magnet
Ceramic insulator
Ceramic insulator
Magnet holder
Nb cathode
Upper anode bias
Upper anode
Lower anode
Lower anode bias

## Slide 56: RFEA

## Slide 57
Q4.13: -120V bias + wide ring top cathode
FIB cross section – e9 sample (weld outer conductor)
Q4.13 e9, bias -120V, 4.28 um
DC-bias diode sputtering (no pores)
Q4.8 e9, bias -80V, 2.53 um
 Baseline recipe
DC-bias diode sputtering
(1.0 % of volume porosity)
+70%
Dense and smooth layer (effect of larger bias)
Larger thickness (effect of top Nb ring)
BUT delamination on the antenna/ext. conductor middle samples
Bias optimum probably in between -120V and -80V

## Slide 58
Q4.8 / -80V bias
Q4.13 / -120V bias + top ring
Q4.13: -120V bias + wide ring top cathode
SEM surface imaging – sample e9 (weld outer conductor)

## Slide 59: Q4.14: 30% lower pressure DC-bias diode
Goal = lower process pressure (allowable with new power supply, HV up to 1.2 kV) to increase coating rate and get a more balanced in/out thickness
Hardware:
long cathode + 4 mm width/5 cm height ring at top (as already mounted for QS9)
Process compared to Q4.8 (baseline):
30% lower pressure  0.14 mbar instead of 0.2 mbar
~ 50% shorter coating time  176’ instead of 345’
Only 5 runs instead of 14
50% energy  21.5 kWh instead of 43 kWh
Same power = 8 kW

## Slide 60
As expected, ~ 25 to 50% larger deposition rate  to be tested for RF
Q4.14 vs Q4.8: deposition rate profile

## Slide 61: Q4 weld issue after 14 coatings…
before
after re-weld
EB facility at main workshop
(T. Tardy/M. REDONDAS MONTESERIN)
Optical inspection
(USB microscope)
Cavity probably re-usable, presence of cracks somewhere else?  Chemistry test

## Slide 62: HIE-ISOLDE 2D, very preliminary plasma and Nb transport simulation © Thibaut Richard
2D slice of HIE-ISOLDE cavity with periodic boundary conditions
Server connection lost after 72% of simulation, steady state not yet reached

## Slide 63: HIE-ISOLDE 2D, parameter file

## Slide 64: HIE-ISOLDE 2D, parameter file