## Slide 1: Breakdown experiments
CLIC09 workshop
15.10.2009
Jan Kovermann

## Slide 2
Outline
1. The quantitative approach to high gradients, an introduction
2. Which diagnostic methods are used?
3. Overview of measurable parameters
4. Results from comparative RF and DC breakdown studies
5. Details from optical breakdown spectroscopy
6. A proposal for RF breakdown detection
7. The DC breakdown movie
8. Summary

## Slide 3
The quantitative approach to high gradients
High-power scaling laws
(RF and materials)
Breakdown simulation
Breakdown diagnostics
RF
measurements
DC
measurements
Comprehensive
RF design

## Slide 4
The quantitative approach to high gradients
BREAKDOWN
DIAGNOSTICS
Spectroscopy
Plasma parameters simulation input
Plasma size/position  simulation and design input
Plasma composition simulation and mat.sci. input
OTR in nominal pulses  simulation and machine parameter input
RF measurements, FC, XRAY  simulation and design input
SEM 
simulation and design input
Missing energy ?
Machine protection
Conditioning
Breakdown source identification

## Slide 5
The connection between simulation and experiment
Emitted currents
Dark current spectrum
OTR
X-rays
Trigger mechanism
Missing energy
Breakdown rate
Ion currents
Fowler-Nordheim distribution
Plasma characteristics
-Time structure
-Physical dimension (imaging)
-Ion species (opt. spectroscopy)
-Ion currents
-Vacuum behaviour
Surfaces
-Crater morphology
-Material diagnostics
-Fatigue process

## Slide 6
RF and DC diagnostics: some results
RF
DC
OTR (Cu), no BD
Opt. BD spectroscopy
Cu I (7.7eV), Cu II (20eV), Cu III (36eV ) ions
Cu interband transition (@2.1eV) spectrum
Notes: This absorption edge, which is due to the d-band to Fermi level transition

## Slide 7
OTR (Cu), no BD
Opt. BD spectroscopy
Spectrum typical for OTR in Cu (interband transition @ 2.1eV)
Beta measurements possible close to the breakdown limit (~105)
OTR sometimes seems to rise before a breakdown
Oxide layers suppress OTR
An estimation of the energy absorbed by electrons in 30GHz structures: 0.1MW @ 14MW RF input power
found very little traces of O,H,C,S probably no contribution to breakdown physics in this sample
Estimated temperature from two-line-method: 1-5eV, but Cu III (T>36eV) seen, plasma is a non-LTE plasma!
Intensity waveform for different lines highly non-reproducible (clusters? Different plasma? just geometry?)
RF and DC diagnostics: some results

## Slide 8
RF
DC
RF (I,Q), Xray, FC @30GHz
Current, voltage and delay
?
SEM of single breakdowns
RF and DC additional diagnostics
SEM of single breakdowns

## Slide 9
BDs are very fast (~ns) transient phenomena
BD parameters change over orders of magnitude (e.g. dark current vs. BD current)
BDs are never the same (in RF!)
BDs affect S-parameters (RF) / current and voltage (DC)
random BD current emission (RF)
working on BD-plane formalism for position dependent missing E calculation
optimization of DC setup for fast transients ongoing
development of high dynamic range diagnostic tools (LogAmps etc.)
fast single-shot multi-channel equipment necessary
RF and DC diagnostics: BDs are never the same
30GHz speedbump structure

## Slide 10
Optical spectroscopy in RF and DC
RF
DC
SLAC C10 (vg 1.35) structure in ASTA, running at 100MV/m (@48MW), 200ns pulse length
CERN DC test stand, 6kV DC, OFE Cu sample, 300MV/m surface field

## Slide 11
RF and DC BD spectroscopy in detail
Typical Cu-plasma spectrum for RF and DC, but there is a problem in the RF spectrum…
CuII ???

## Slide 12
RF and DC BD spectroscopy in detail
… stainless steel! Looks like a BD between copper gasket and flange (confirmed recently by SLAC).

## Slide 13
RF and DC BD spectroscopy in detail
Unfortunately this is not a pure Cu-BD spectrum anymore (there is literature on StSt arc welding diagnostics, to be checked)…
Cu I temperature is ~1-3eV depending on line pairs

## Slide 14
RF and DC BD spectroscopy in detail
I you can‘t beat it, use it!
RF structures are getting more and more complex, not only in terms of geometry, they might contain one day:
New and alternative structure materials (e.g. CuZr)
Surface treatment and coatings (e.g. oxide layers, NEG)
Brazing alloys (e.g. Ag)
Joints and flanges (e.g. StSt, Al)
Damping material (e.g. SiC)
Impurities from production and handling (e.g. dust & dirt)

## Slide 15
RF and DC BD spectroscopy in detail
Proposal: (Simplified) spectroscopy system as standard diagnostic tool for future structure tests to save time of trembling uncertanty before you cut the structure…
Surprisingly the intensity ratio of Cu lines does not change from BD to BD, still looking for power or pulse length dependency…

## Slide 16
RF and DC BD spectroscopy in detail
Time resolved spectroscopy of selected lines in RF (SLAC C10@100MV/m, 200ns)
T [ns]
T [ns]
T [ns]
T [ns]
Initial peak similar for all Cu species
Hight density and/or Stark/Zeeman effects
White background in spectra
200ns RF pulse

## Slide 17
RF faraday cup measurements
High currents (5V in 50Ohms, 100mA, 50ns) of electrons hit the FC in each BD event, X-rays are produced by these electrons (30GHz CERN speedbump structure)
FC covers 1/200 of solid angle
approx. 10E13 electrons per BD
X-rays pass vacuum window and Al-foils
at least 10keV to be detectable,
for 10E13 electrons dissipated energy
is around 20mJ
X-rays pass 14mm Cu and 5mm Fe
 at least 100keV to be detectable,
for 10E13 electrons dissipated energy
is around 180mJ
In total:
~200mJ
Very similar to measured missing Energy in RF, but no direct correlation!
Electrons from BD
X-rays

## Slide 18
RF diagnostics spin-off
Breakdown current
Main
beam
DiffAmp
volts
time
volts
time
volts
time
Breakdown detection for CLIC accelerating structures
Breakdown detection using pairs of Rogowski-coils:
+ easy suppression of main beam signal
+ simple electronics
+ no reference needed
+ can resolve dark current and breakdown current
+ radiation hard
+ cheap feed-throughs
needs space between structures
beam impedance matching necessary
First test with one coil in 30GHz test stand

## Slide 19
RF diagnostics spin-off
And how (cheap) it looks like doing the first tests…
But now coming back to DC again!

## Slide 20
DC breakdown
The motion picture
Featuring: DC breakdown, 12kV, OFE Copper, 20um gap (500MV/m).
Storyline: Capacitor is discharged through the sparc, but the PSU stays connected with high impedance for seconds...
SAMPLE
TIP

## Slide 21
Summary
Breakdown diagnostics offer a new way of approaching the understanding of the breakdown mechanism and its possible feedback to high gradient designs
The experiments give input to breakdown simulation (plasma and transient behavior)
Breakdown detection methods besides RF signals and faraday cup were developed (which are under consideration for CLIC now)
Fast diagnostics for abnormal structure BD behavior have been presented and will be implemented in structure test stands
THANK YOU!